Supporting Information

Surfactant-Free Cellulose Filaments Stabilized Oil in Water Emulsions

Amir Varamesh1, Ragesh Prathapan1, Ali Telmadarreie1, Jia Li1, Keith Gourlay2, Gurminder Minhas2, Qingye Lu1, Steven L. Bryant1,*, Jinguang Hu1,

1. Department of Chemical and Petroleum Engineering, University of Calgary, Calgary T2N 1N4, Canada

2. Performance BioFilaments, 700 West Pender Street, Vancouver V6C 1G8, Canada

Table S1.  Span index of the emulsion immediately after their preparation

| CFs concentration (wt%) | d10 (µm) | d50 (µm) | d90 (µm) | Span Index |
| --- | --- | --- | --- | --- |
| 0.05 | 7.458 | 23.152 | 57.968 | 2.182 |
| 0.10 | 19.945 | 35.218 | 43.187 | 0.660 |
| 0.25 | 15.124 | 24.360 | 34.328 | 0.788 |
| 0.50 | 12.966 | 19.932 | 27.490 | 0.729 |

Figure S1. SEM image of the CFs sample

Figure S2. Size distribution of the emulsions at 0.05 wt% CFs concentration

Figure S3. Size distribution of the emulsions at 0.1 wt% CFs concentration

Figure S4. Size distribution of the emulsions at 0.25 wt% CFs concentration

Figure S5. Size distribution of the emulsions at 0.5 wt% CFs concentration

Corresponding authors: Steven L. Bryant (steven.bryant@ucalgary.ca), Jinguang Hu (jinguang.hu@ucalgary.ca)