Table 1. Screening of reaction conditions for direct arylation of benzene.

| Entry | Variation from the standard condition | Yield (%) |
| --- | --- | --- |
| 1 | None | 93 |
| 2 | Without irradiation | 0.1 |
| 3 | Without AgI/Mg2Al1LDH | 1.2 |
| 4 | Without iodobenzene | 0 |
| 5 | Hexane instead of benzene | 1.5 |
| 6 | Mg2Al1LDH | 2.3 |
| 7 | AgI/ZrO2 | 10.5 |
| 8 | AgI/ZrO2, with Na2CO3 added (50 mg) | 11.1 |
| 9 | Air instead of argon | 56.4 |

Standard reaction conditions: iodobenzene (0.1 mmol), benzene (1 mL), catalyst (50 mg), Ar atmosphere, irradiated under a 400 nm wavelength LED light with 0.1 W cm-2 of intensity, the reaction was conducted at 60℃ for 20 h. Yields are determined by GC analysis.

Table 2. Reaction scope of (hetero) aryl iodides and arenes.

| 1a 87% (<0.1%) | 2b 91% (<0.1%) | 3b 99% (1%) | 4c 99% (<0.1%) |
| --- | --- | --- | --- |
| 5c 98% (0.1%) | 6d 94% (0.1%) | 7d 91% (0.1%) | 8e 63% (<0.1%), o/m/p = 62/24/14 |
| 9f 94% (<0.1%) o/m/p = 61/24/15 | 10f 98% (<0.1%) o/m/p = 56/28/16 | 11f 74% (<0.1%) o/m/p = 53/33/14 | 12f 97% (<0.1%) 3,4-/2,3-dichlorobiphenyl = 69/31 |
| 13f 54% (<0.1%) | 14f 52% (<0.1%) 2,4-/3,5-/2,6- dimethylbiphenyl= 50/43/7 | 15f 46% (<0.1%) | 16f 27% (<0.1%) o/m/p = 52/31/17 |

Reaction conditions: aryl iodide (0.1 mmol), arene (1 mL), AgI/Mg2Al1LDH catalyst (50 mg), Ar atmosphere, irradiated under a 400 nm wavelength LED light. Yields were determined by GC analysis. aReaction was conducted at 60℃ for 20 h, and the light intensity was 0.1 W cm-2. bReaction was conducted at 80℃ for 20 h, and the light intensity was 0.1 W cm-2. cReaction was conducted at 60℃ for 48 h, and the light intensity was 0.1 W cm-2. dReaction was conducted at 85℃ for 48 h, and the light intensity was 0.2 W cm-2. To enhance the yield of the products 1-7, the catalyst was filtered out at half of the reaction time during photocatalysis, followed by the addition of 50 mg of fresh catalyst to the liquid mixture. eReaction was conducted at 60℃ for 20 h, and the light intensity was 0.2 W cm-2. fReaction was conducted at 60℃ for 20 h, and the light intensity was 0.1 W cm-2. Iodobenzene was used in producing the products 8-16.