Supporting Information

Direct observation of unidirectional exciton-polariton in layered van der Waals semiconductors

Section S1: Plane wave expansion of the field of circularly polarized dipole

Section S2: Simulation of AFM apex induced circularly polarized dipoles

Section S3: Experimental setup

Section S4: Calibration by TE0 mode in ultra-thin MoS2 layer

Section S5: Real-space imaging of unidirectional waveguide modes in MoS2 layer

Section S6: Coupling efficiency of near-field waveguide modes with s-SNOM tip

Section S7: Characterization of TMD nanoflakes with Raman spectroscopy

Section S8: Strong coupling of unidirectional waveguide EP modes in WS2 layer

- Section S1: Plane wave expansion of the field of circularly polarized dipole

The wave equation of vector potential A(x,y,z) in a homogeneous non-magnetic medium is:

(S1.1)

where k is the wavevector of the free space. Considering the dipole and TMD nanoflakes are placed along z axis, we can expand the field distribution into plane waves propagate along xoy plane with in-plane wavevector (kx,ky) as:

(S1.2)

To ensure this plane wave solution satisfies the wave equation Eq. S(1.1), the spatial frequency distribution A(kx,ky,z) satisfies the restriction equation in z direction:

(S1.3)

where kz  = k2-kx2-ky2 and kz reveals free space wave as kx2 + ky2 ≤ k2, while it reveals evanesent wave as kx2 + ky2 > k2, i.e. the waveguide exciton-polariton mode in our work.

In this case, we expanded the vector potential of an electric dipole as followes (1):

(S1.4)

where r = x2 + y2 + z2, into plane wave by using the Weyl identity:

(S1.5)

where the + sign for field above the dipole (z > 0) and – sign for field below the dipole (z < 0), such that:

(S1.6)

With the definition of magnetic field and vector potential H(x,y,z) = ∇×A(x,y,z) / μ , we can further expand the magnetic field of the dipole into a set of plane wave as:

(S1.7)

Based on the Maxwell's equations in frequency domain that E(x,y,z) = ∇×H(x,y,z) / (iωε), the electric field of the dipole can be expanded as:

(S1.8)

where the spatial frequency distribution of dipole's electric field is shown as:

(S1.9)

Consider the plane wave components which propagate along x direction, i.e., the components with ky = 0, we can derived the spatial frequency distribution of TE modes excited by horizontal dipole components (px,py,0) and of TM modes induced by vertical dipole components (px,0,pz) after considering the position of dipole zdipole as followed:

(S1.10)

(S1.11)

As shown in Fig. S1, the elliptical polarization converts the positive correlation between unidirectionality R = |Ez(kx)/ Ez(-kx)| and the in-plane momentum kx of circularly polarized incidence into negative correlation, i.e. the unidirectionality of elliptically dipole is more significant when the coupled waveguide modes have smaller in-plane momentum.

- Fig. S1| Unidirectionality of a circularly polarized (orange line) dipole with (px, py, pz) = (1, 0, -i) and an elliptical polarized (cyan line) dipole with (px, py, pz) = (1, 0, -0.3i), where R = |Ez(kx)/ Ez(-kx)|. Inset: illustration of the elliptic circularly polarized dipole at the AFM tip via oblique illumination. The wavelength of incident light is 632.8 nm.

- Section S2: Simulation of AFM apex induced circularly polarized dipoles.

To model the atomic force microscope (AFM) apex induced transition from free-space chiral illumination to circularly polarized dipole, numerical simulations were performed with finite difference time domain method. As shown in Fig. S2, a circularly polarized plane wave is incident on the 3D simplified pyramid shaped tip. To estimate the polarization of the electric field near the AFM apex, we calculated the Stokes parameter S3 = - 2Im(EyEz*) at the yoz cross section at x = 0 μm. We marked the areas where |S3| > 0.98 which reveals significant circularly polarization in yoz plane. The results for LCP and RCP illuminations are shown in Fig. S1a and Fig. S1b, and these results illustrate that the AFM apex modulates the chiral illuminations into chiral electric field near it. More importantly, the calculations show that the chiral electric field localizes in a small area near the top of apex and forms a circularly polarized dipole.

- Fig. S2| Numerical simulation of the distribution of Stokes parameter S3 near the AFM apex. The illumination is circularly polarized planewave and the apex of AFM is a simplified pyramid shaped tip. With LCP (a) and RCP (b) incident lasers, the distribution of S3 shows the polarization states near the top of apex are consisted with the illumination.

- Section S3: Experimental setup

Figure S3 shows the experimetal setup utilized to probe the TMD sample in the near field. A helium-neon laser in the visible spectram (λ=632.8 nm) is used as the light source. And a polarizer ensures the incident light is linearly polarized and a 1/4 waveplate is used to convert the linear polarization to circular polarization, which is further controlled by a 1/2 waveplate. The circularly polarized laser is then used to excite and to probe the EP through a typical s-SNOM based on a Michelson interferometer configuration. The detected signal is collected by a detector and modulated by the tapping frequency of the AFM tip through a lock-in amplifier to excluding the scattering far-field noise and filtering the near-field signals.

- Fig. S3| Schematic illustration of the near-field measurement setup.

Figure S4 shows the formation of near-field EPs at the edge of TMD material. Under left circularly polarized illumination, unidirectional EPs are excited due to the asymmetric high-spatial-frequency components of the circularly polarized dipole radiation coupled into waveguide modes. As illustrated in Fig. S4, the amplitude of exponential-decay blue curve propagating to the left is larger than that of orange curve which propagates to the right. Tip-launched waveguide modes propagate and get scattered to the free space as edge scattering signal. With tip moving away from the edge, the amplitude of inference pattern between edge and tip scattering signals gradually decreases, leading to darker inteference fringes shown as Fig. 4S(d).

Fig. S4| Formation of the near-field EPs at the edge.

- Section S4: Calibration by TE0 mode in ultra-thin MoS2 layer

In order to further verify our probing method, another van der Waals material, 12 nm-thick MoS2, was used to first obtain the calibration value and normalized factor. Here, we used scattering-type scanning near-field optical microscopy (s-SNOM), which is bulit based on an AFM in tapping mode. The AFM tip used in experiments are PR-EX-SNM-A with the tapping frequency of 277 kHz.

- Fig. S5| Experimental observation of TE0 mode on the MoS2 flake. a, Topography image of a 12 nm-thick MoS2 on the SiO2 substrate. The inset white line denotes the height of MoS2. Measured amplitude images of the TE0 mode by illuminating right (b) and left (c) circularly polarized light at wavelength of 632.8 nm, respectively. d, Amplitude line profiles extracted from near-field images (b and c). e, Fourier transform of the experimental near-field signals after calibration.

- Section S5: Real-space imaging of unidirectional waveguide modes in MoS2 layer

- Fig. S6| Real-space imaging of unidirectional waveguide modes by s-SNOM. a, Optical microscope images of the 85 nm-thick MoS2 flake. The measured areas are marked by white dashed circles. Profiles taken from the scanning regions are shown as white lines. (b and c) Polarization-dependent amplitudes of TM0 mode. d, Dispersion colormap of an Air/MoS2/SiO2 waveguide calculated by transform matrix method. The experimental data points (red pentagrams) show good agreement with the calculated dispersion of TM0 mode (red line). e, FT of the near-field images shown in (b and c). The frequency peak corresponds to TM0 mode equals to 2.03k0.

- Section S6: Coupling efficiency of near-field waveguide modes and s-SNOM tip.

The propagating waveguide modes in the WS2 flakes interfere with tip scattering of the illuminating laser, forming the interferometric patterns as shown in Fig. 3. It is worth mentioning that the Fourier transform of the near-field signals exhibits two peaks, one around 1.56k0 is associated with TM1 mode, while the other one (2.26k0) denotes the TM0 mode. The calculated coupling efficiency of the tip-induced hotspot and the former waveguide mode (0.045), Ceff=0ztipEzdz-∞∞Ezdz, is predominant than that of TM0 mode (0.021). The interval 0 nm < z < ztip denotes the efficient coupling region (green region), where ztip equals to 100 nm. The tip-sample coupling efficiency is shown in Fig. S7.

- Fig. S7| Coupling efficiency of s-SNOM tip with (a) TM0 and (b) TM1 modes in 125 nm-thick WS2 at incident wavelength of 632.8 nm. The blue dashed lines denote the region of the WS2 layer (125 nm). The green region is the efficient coupling region. The coupling factor for TM1 (0.045) mode is higher than that for TM0 (0.021) mode, denoting the predominant position of TM1 mode in the measured signal in Fig. 3k.

- Section S7: Characterization of TMD nanoflakes with Raman spectroscopy

To confirm that the exfoliated nanoflakes we used to support the unidirectional waveguide EP modes are indeed MoS2 and WS2, we perform Raman spectroscopy of these flakes. Figure S8 shows Raman spectra signals, obtained with a homemade Raman microscope, of the MoS2 and WS2 sample illustrated in the insets, as well as in Fig. S6 and Fig. 3d. The typical first order in-plane phonon mode E2g1(Γ) (at 382 cm-1) peak and out-plane phonon mode A1g(Γ) (at 407 cm-1) peak for MoS2 flake are obtained as shown in Fig. S8a, while the first-order modes LA(M) (at 176 cm-1), E2g1(Γ) (at 356 cm-1) and A1g(Γ) (at 418 cm-1) Raman peaks and the significant second-order mode 2LA(M) (at 352 cm-1) of WS2 sample are revealed in Fig. S8b. The Raman spectra obtained from the samples we used to reveal the unidirectional EP modes are greatly consisted with previous works (2, 3).

Fig. S8| Raman spectra of MoS2 sample (a) and WS2 sample (b). Insets: the corresponding optical microscope images.

- Section S8: Strong coupling of unidirectional waveguide EP modes in WS2 slab

Moreover, these self-hybridized EPs also work in the strong coupling regime, with Rabi splitting energies (ħΩ) of 100.7 meV at room temperature. For instance, Fig. S9 shows the dispersion color map of an Air/125 nm WS2/SiO2 waveguide, where energy-momentum relation of the waveguide modes is constructed. The obtained experimental data (pentagram points) coincide with the energy of exciton polaritons in the split position of calculated dispersion relation. In the dispersion color map, we plot the imaginary part of the p-polarized reflection coefficient, which illustrates the TM photonic density of states. The solid lines denote the theoretical dispersion relations revealed by pure modes analysis.

Fig. S9| Dispersion colormap of an Air/WS2/SiO2 waveguide calculated by transform matrix method. Dispersion of TM0 mode (yellow line) and TM1 mode (red line) are calculated by pure modes analysis. Experimental data points (yellow pentagrams) show good agreement with the calculated dispersion.

References

1.	J. D. Jackson, Classical Electrodynamics. (ed. 3rd, 1925).

2.	A. Berkdemir et al., Identification of individual and few layers of WS2 using Raman Spectroscopy. Scientific Reports 3, 1755 (2013).

3.	H. Li et al., From Bulk to Monolayer MoS2: Evolution of Raman Scattering. Advanced Functional Materials 22, 1385-1390 (2012).