Supplementary Materials

Influence of the reaction conditions on the degree of substitution of carboxymethyl seriguela gum for application as a flocculant aid

Henety Nascimento Pinheiro1* (ORCID:0000-0002-4039-5401), João Lucas Isídio de Oliveira Almeida2 (ORCID:0000-0002-5073-3072), Flavia Freitas Veloso3 (ORCID:0000-0002-6740-921X) and Flavia Oliveira Monteiro da Silva Abreu1 (ORCID:0000-0003-4759-2739)

1 Natural Polymers Laboratory, State University of Ceará, Natural Sciences Graduate Program, 60714903, Fortaleza, CE, Brazil

2 Laboratory of Chemistry, Federal Institute of Piauí, 64980000, Corrente, PI, Brazil

3 Natural Polymers Laboratory, State University of Ceará, Chemistry Degree Course, 60714903, Fortaleza, CE, Brazil

*henety.pinheiro@aluno.uece.br

Table S1. ANOVA Results for the Effect of NaOH concentration, Chloroacetic acid (CA) and interaction effect on the absolute substitution degree (p < 0.05)

| Factors | Sum Square | Degrees of Freedom | Mean Square | F0 | Fcritical |
| --- | --- | --- | --- | --- | --- |
| NaOH | 2088 | 1 | 2088 | 194.00 | 4.00 |
| CA | 537 | 3 | 179 | 16.60 | 3.30 |
| NaOH x Acid | 323 | 3 | 108 | 9.99 | 3.27 |
| Error | 86 | 8 | 10.8 |  |  |
| Total | 3034 |  |  |  |  |

Fig S1.1H NMR spectrum of carboxymethylated samples with different substitution degree CMSG3A, CMSG7A and CMSG9A.

Fig. S2. 13C NMR spectrum of carboxymethylated samples with different substitution degree, SG and CMSG3A.