Supplementary Materials for

“Intertwined charge-density-wave order in vanadium-based kagome superconductors”

Kuanglv Sun1‡, Linpeng Nie1‡, Hongyu Li1, Jiyin Zhao1, Huachen Rao1, Fanghang Yu1, Mengzhu Shi1, Ziji Xiang1, Jianjun Ying2,3, Zhenyu Wang2,3, Tao Wu1,2,3,4,5* and Xianhui Chen1,2,3,4,5*

1. Hefei National Research Center for Physical Sciences at the Microscale, University of Science and Technology of China, Hefei, Anhui 230026, China

2. CAS Key Laboratory of Strongly coupled Quantum Matter Physics, Department of Physics, University of Science and Technology of China, Hefei, Anhui 230026, China

3. CAS Center for Excellence in Superconducting Electronics (CENSE), Shanghai 200050, China

4. Collaborative Innovation Center of Advanced Microstructures, Nanjing University, Nanjing 210093, China

5. Hefei National Laboratory, University of Science and Technology of China, Hefei 230088, China

‡These authors contributed equally to this work

*Correspondence to: wutao@ustc.edu.cn, chenxh@ustc.edu.cn

This PDF file includes:

S1. Asymmetric (E2g) and symmetric (A1g) elastoresistance responses

S2. Geometry-dependent elastoresistance coefficientd(∆R/R)yy/dεxx

S3. Nonideal current path in the two-bar method

S4. Discussion of strain inhomogeneity

S5. Nonideal current path in the modified Montgomery method

S6. Finite value at high temperature and Scaling procedure

S1. Asymmetric (E2g) and symmetric (A1g) elastoresistance responses

The strain applied on a hexagonal lattice sample can be decomposed into three parts in the form of irreducible representations: A1g, E1g and E2g. According to the strain classification, we can obtain corresponding elastoresistance responses. Specifically, the A1g strain represents isotropic deformation, such as volume expansion or contraction, and it can be divided into an in-plane term (εxx +εyy)/2 and an out-of-plane term εzz. The E1g strain (εxz, εyz) indicates an out-of-plane deformation caused by out-of-plane shear distortions. The E2g strain ((εxx -εyy)/2, εxy) is the degenerate B1g and B2g strain described in the D4h point group, indicating that arbitrary in-plane strain is equivalent. Briefly, arbitrary in-plane strains can be composed of A1g and E2g strains. The formula of elastoresistance responses for E2g and A1g symmetry are given as [1]:

mE2g=11+vxydΔR/Rxxdεxx-dΔR/Ryydεxx=m11-m12,

mA1g=11-vxydΔR/Rxxdεxx+dΔR/Ryydεxx=m11+m12-2vxz1-vxym13,

where vxy = - εyy/εxx represents the Poisson's ratio of the PZT stack and vxz = - εzz/εxx represents the out-of-plane Poisson's ratio of a specific sample. By the combination of the elastoresistance coefficient in the x and y directions, we can obtain the elastoresistance responses for E2g and A1g symmetry. We notice that the relative magnitudes of mA1g and mE2g, which is inconsistent among different reports [2–4], seems to be dependent on the geometry of sample in practice. Next, we will show evidence that the sign of the elastoresistance coefficient dΔR/Ryydεxx is actually width dependent, which strongly affects the magnitude of both mA1g and mE2g. A nonideal current path is proposed to account for the width-dependent effect, which could also affect the results from the modified Montgomery method. A scaling of the raw data to the finite value at high temperature has been used to extract the intrinsic value for both mA1g and mE2g.

S2. Geometry-dependent elastoresistance coefficient d(∆R/R)yy/dεxx

In our elastoresistance measurement, we found that the relative magnitudes of mA1g and mE2g seems to be dependent on the geometry of sample phenomenally. In practice, we have repeated our elastoresistance measurement on different pristine CsV3Sb5 samples with different aspect ratio (Fig. S2a). Among these results, we noticed that the elastoresistance coefficient dΔR/Rxxdεxx is always a positive value, but the sign of the elastoresistance coefficient dΔR/Ryydεxx is changed from positive to negative with increasing the aspect ratio as shown in Fig. S2. The sign problem of dΔR/Ryydεxx is also shown in recent three preprints, in which the sign of dΔR/Ryydεxx is also inconsistent in these independent elastoresistance measurement [2-4]. The different value of dΔR/Ryydεxx can make a significant difference on the relative magnitudes of mA1g and mE2g.

Figure S2. Two-bar method for CsV3Sb5 single crystals of different widths. a, Detail information for all the samples is listed as a table, with sample width, length between two voltage measurement electrodes, residual resistivity ratio (RRR), Tc-zero, Tc-onset and the sign of the elastoresistance coefficient in the y direction, where #1 and #2 represent different sample batches. b, Renormalized resistance R(T)/R(5K) for different samples sticked on PZT stack. c, Elastoresistance coefficient in the y direction d(∆R/R)yy/dεxx for different samples. The error bars attached on each point are the standard deviation from the linear fitting. A clear sign change is observed in the samples with different aspect ratio. For S1, S2 and S3, the sign of elastoresistance coefficient is negative, while for S5, S6 and S7, the sign of elastoresistance coefficient is positive. An interesting case is S4, where the sign of elastoresistance coefficient changes from negative to positive with temperature decreasing. d, E2g and A1g elastoresistance coefficients for different samples, which is calculated with the same d(∆R/R)xx/dεxx presented in the main text. When the sign of d(∆R/R)yy/dεxx is negative (S1, S2 and S3), the values of E2g and A1g elastoresistance coefficients are comparable. When the sign is positive (S5, S6 and S7), the value of A1g elastoresistance coefficient is approximately 6 times larger than the value of E2g elastoresistance coefficient. The sixfold difference in magnitude for A1g and E2g elastoresistance coefficients was also found in the Montgomery method (see details in S5 section below). In the next section, we would further discuss the possible explanation on the geometry-dependent d(∆R/R)yy/dεxx.

S3. Nonideal current path in the two-bar method

To explain the geometry-dependent d(∆R/R)yy/dεxx, we propose that the nonideal current path could be responsible for the change of sign in different sample with different aspect ratios. As shown in Figure S3, we consider that the rectangle sample used to measure d(∆R/R)yy/dεxx is perfectly aligned along the y direction. Then, the electrodes for transport measurement are assumed to be misaligned with an angle θ. In practice, this misalignment could occur due to imperfect electrode contact or geometry, which is almost inevitable in practical operations. This misalignment will lead to a nonideal current path which picks up a partial elastoresistance response from the x direction in the measurement of d(∆R/R)yy/dεxx. It could be used to explain the observed change of sign in different measurements. Next, we try to make a quantitative analysis on the possible sign change in this situation. The resistance tensor can be expressed as Rxx,Ryy,Rzz,Ryz,Rzy,Rzx,Rxz,Rxy,Ryx. Applying the tensor transformation matrix [5] with a tilting angle θ, we obtain:

ΔR/Ryy'=ΔR/Rxxsin2θ+ΔR/Ryycos2θ-12ΔR/Rxy+ΔR/Ryxsin2θ.

Taking the derivative of εxx on both sides, the elastoresistance coefficient in yy´ direction can be expressed as the combination of elastoresistance coefficient in the xx, yy and xy directions. In our measurement setup, the diagonal term xy could be inconsequential under strain [5], which will be ignored in the following analysis. By now, the elastoresistance coefficient in the yy´ direction can be expressed as:

dΔR/Ryy'dεxx=dΔR/Rxxdεxxsin2θ+dΔR/Ryydεxxcos2θ.

Recalling the results in Fig. 1c, we roughly estimate the intrinsic value of dΔR/Rxxdεxx to be 12 and dΔR/Ryydεxx to be -3. By substituting these two values, we could consider the critical case where dΔR/Ryy'dεxx is equal to zero. Then, we obtain:

0=12sin2θ-31-sin2θ.

We obtain that the critical angle θ for sign change is approximately 26°. Using this critical angle, we could estimate the critical aspect ratio for sign change, in which the sample width is equal to half of the length between the two voltage electrodes (Fig. S3c). If the sample width is smaller, the current is more likely to flow along the ideal direction (θ ~ 0) and dΔR/Ryy'dεxx is negative. If the sample width becomes bigger than the critical value, the angle θ could be easily increased owing to the nonideal current path and dΔR/Ryy'dεxx will become positive.

Similarly, this sign change problem could also occur in the measurement of dΔR/Rxxdεxx, which would suppress the original positive elastoresistance coefficient in the x direction. To avoid this nonideal current path, it is better to use a bar-shaped sample etched by a focused ion beam, similar to Hall measurements. In our experiments, we cut the single crystal into bar-shaped samples and consider the positive responses in the x direction and negative responses in the y direction as intrinsic results.

Figure S3. The effect of nonideal current path in elastoresistance measurements. a, Schematic diagram of the two-bar configuration for the y direction, whose elastoresistance response is dependent on its width. Red arrows represent the strain in the x direction εxx, while blue arrows represent strain in the y direction εyy. The gray block represents the sample along the y direction, attached by four yellow probes that measure resistance. The frames of crystal, strain and transport measurements are denoted as x, x’ and x’’, respectively. In this setup, we assume that the sample is perfectly aligned along the y direction, but the transport frame could be misaligned with an angle θ, as shown in b. This transport misalignment could be caused by imperfect electrode contact or geometry, as shown in c. These nonideal current paths could pick up partial elastoresistance responses in the x direction when trying to detect the y direction response, which could lead to the sign change problem described in S2.

S4. Discussion of strain inhomogeneity

Another possible explanation for the sign change problem is the inhomogeneity of strain experienced on samples. The bar-shaped sample glued along the x(y) direction could experience dominantly uniaxial strain εxx(εyy) rather than nominal strain εxx-εyy [3]. Adopting the elastoresistance tensor formulation, this condition can be evaluated qualitatively. In principle, the elastoresistance coefficients in the y direction can be expressed as:

∆RRyy=m12εxxPZT+m11εyyPZT+m13εzz=m12-vxyPZTm11-voutsamplem13εxxPZT

where vxyPZT~0.45 represents the Poisson's ratio of the PZT stack and voutsample represents the out-of-plane sample Poisson's ratio. In the ideal case, the strain experienced by the sample perfectly follows the strain applied by the PZT stacks, i.e., εxxsample=εxxPZT and εyysample=εyyPZT.

Now, we consider the nonideal condition, where εyy is dominantly experienced according to PZT stacks, but εxx is not. The worst case is that the sample does not feel the strain applied by the PZT stacks in the x direction but follows the strain in the y direction according to the in-plane sample Poisson's ratio vinsample. In this condition, the sample experienced strain in the y direction εyysample still equal to the PZT applied strain in the y direction εyyPZT, i.e., εyysample=εyyPZT. However, the sample experienced strain in the x direction εxxsample depends on εyysample (which equals εyyPZT) and the in-plane sample Poisson's ratio vinsample, given as

εxxsample=-εyyPZTvinsample.

By now, the elastoresistance coefficients in the y direction can be expressed as:

∆RRyy=vxyPZTvinsamplem12-vxyPZTm11-voutsamplem13εxxPZT.

Compared with the ideal equation, we found that the only difference is an additional coefficient for m12, i.e., vp/vinsample. According to Ref [2], in-plane sample Poisson's ratio is 0.44, which is similar to Poisson's ratio of the PZT stack. Hence, this additional coefficient nearly equals 1, which will not largely modify the elastoresistance coefficients in the y direction. In a short summary, based on above analysis, the strain inhomogeneity could not explain the sign change problem in d(∆R/R)yy/dεxx.

S5. Nonideal current path in the modified Montgomery method

Furthermore, the modified Montgomery method could also suffer this nonideal current path. We cut a squared sample with length Lx = 1.25 mm, width Ly = 1.33 mm, and thickness Lz = 0.015 mm. Following the formula derivations in Ref [6], we obtain the A1g and E2g elastoresistance coefficients shown in Figure S5.

Both the E2g and A1g symmetries present similar temperature behavior: a jump at TCDW and a decrease at approximately 35 K. Selecting the temperature region from 60 K to 80 K, the value of A1g elastoresistance coefficient is 51.08 on average, and the value of E2g elastoresistance coefficient is 8.79 on average. This sixfold difference in magnitude of A1g and E2g elastoresistance coefficients is similar as that in two-bar measurement with a comparable sample geometry. We think that this is also related to the nonideal electrodes contact or geometry, which could rotate the transport frame, as shown in Fig. S5. The formulation derivation of the modified Montgomery method asks for the assumption of perfect electrodes at four corners of squared samples. However, the electrodes are not an ideal point at the corner but a partial circle because of the droplet of silver paste. In this condition, the current possibly follows a nonideal path, which can be regarded as the rotation of the transport frame, namely, the scenario of a mixture of x and y elastoresistance responses discussed above. Hence, the elastoresistance coefficient dΔR/Ryydεxx is positive, corresponding to the results of a wider sample.

In addition to the nonideal current path, the squared samples also lower the sample resistance, which makes it difficult to measure the relative resistance change at lower temperatures. We can roughly give an estimation. For example, the resistance of squared CsV3Sb5 is approximately 0.01 Ohm at 300 K. Considering that RRR is approximately 50, the strain is approximately 10-4, and the elastoresistance coefficient is approximately 10, we obtain that the absolute change in resistance at low temperature is 10-7 Ohm. If we apply a current of 1 mA, we obtain a voltage change of approximately 0.1 nV. This voltage change is beyond the resolution of the delta mode of Keithley 6221/2182. Hence, the resistance measurements of squared metals challenge the equipment limit. Overall, considering the possible nonideal current path and smaller resistance in the squared sample, we propose that it is better to use the two-bar method with careful scaling estimation.

Figure S5. Modified Montgomery method for CsV3Sb5. a, Schematic diagram of the modified Montgomery method. b, Picture of the piezoelectric stack with a square CsV3Sb5 single crystal glued on its surface. Sample length Lx = 1.25 mm, width Ly = 1.33 mm, and thickness Lz = 0.015 mm. c, E2g and A1g symmetry elastoresistance responses calculated by the Montgomery method. Both E2g and A1g symmetry present similar temperature behavior: a jump at TCDW and a decrease at approximately 35 K. Selecting the temperature region from 60 to 80, the A1g elastoresistance responses are 51.08 on average, and the E2g elastoresistance responses are 8.79 on average, which gives A1g responses that are larger than the E2g responses by approximately 5.8 times. This sixfold relation between A1g and E2g corresponded to the two-bar method when the width of sample y increased. d, Diagram of the ideal and nonideal current paths in the modified Montgomery method.

S6. Finite value at high temperature and Scaling procedure

Theoretically, we can obtain the finite value of the elastoresistance response at high temperature when using the two-bar method. This response comes from geometry change. The resistance for the sample along the x direction can be expressed as

Rxx=ρxxLxLyLz.

Taking the natural logarithm for both sides of the equation and then differentiating, we obtain

dRRxx=dρρxx+dLLx-dLLy-dLLz.

Dividing the strain εxx on both sides since these changes are due to the strain, we obtain

dRRxxεxx=dρρxxεxx+dLLxεxx-dLLyεxx-dLLzεxx=dρρxxεxx+1+vxy+vxz,

where εxx=(dL/L)x, εyy=-vxyεxx and εzz=-vxzεxx. Similarly, the same procedure can be performed for the sample in the y direction, which gives

dRRyyεxx=dρρyyεxx+dLLyεxx-dLLxεxx-dLLzεxx=dρρyyεxx-vxy-1+vxz.

By now, we can obtain E2g and A1g responses,

χE2g=11+vxydRRxx-dRRyyεxx=11+vxydρρxx-dρρyyεxx+2+2vxy,

χA1g=11-vxydRRxx+dRRyyεxx=11-vxydρρxx+dρρyyεxx+2vxz,

where vxy~0.45 is the Poisson's ratio for the PZT stack and vxz~0.3 is the sample out-of-plane Poisson's ratio. Hence, we find that the geometric effect contributes to a constant 2 for the E2g channel at high temperature and approximately 1.09 for the A1g channel. At high temperature, without approaching any phase transition or instability, we anticipate that χE2g and χA1g attributed to electronic resistivity are nearly zero. Hence, we suggest scaling the raw data at high temperature to this calculated finite value. By doing so, geometric effects are considered ideally, and the remaining temperature dependences at lower temperatures are attributed to pure elastoresistivity, which comes from the change in electronic states (see Fig. S5). To avoid possible uncertainty, we take the average when calculating the high temperature value of the raw data.

Fig S6. Elastoresistance responses for hole-doped CsV3Sb5. a-f, Temperature dependence of elastoresistance responses in the A1g (hollow circle) and E2g (hollow triangle) symmetry channels for CsV3Sb5-ySny (y = 0, 0.04 and 0.06) and CsV3-xTixSb5 (x = 0.03, 0.05 and 0.09), respectively. The A1g and E2g responses are scaled to finite values at high temperature, following the scaling procedure discussed above. All the samples present a clear peak or dip feature around the TCDW (marked as a light gray region). The black dashed line indicates the finite value at high temperature. Below the CDW transition (light gray region), a kink-like behavior can be clearly distinguished, depicted as the dark gray region. The error bars attached on each point in a-f are the standard deviation from the linear fitting. All the horizontal axes and vertical axes in a-f follow the same scale.

Reference

1.	Wiecki, P. et al. Emerging symmetric strain response and weakening nematic fluctuations in strongly hole-doped iron-based superconductors. Nat Commun 12, 4824 (2021).

2.	Frachet, M. et al. Colossal c-axis response and lack of rotational symmetry breaking within the kagome plane of the CsV3Sb5 superconductor. Preprint at: arXiv:2310.06102 (2023).

3.	Liu, Z. et al. Absence of nematic instability in the kagome metal CsV3Sb5. Preprint at: arXiv:2309.14574 (2023).

4.	Asaba, T. et al. Evidence for an odd-parity nematic phase above the charge density wave transition in kagome metal CsV3Sb5. Preprint at: arXiv:2309.16985 (2023).

5.	Shapiro, M. C., Hristov, A. T., Palmstrom, J. C., Chu, J.-H. & Fisher, I. R. Measurement of the B1g and B2g components of the elastoresistivity tensor for tetragonal materials via transverse resistivity configurations. Rev. Sci. Instrum. 87, 063902 (2016).

6.	Kuo, H.-H., Chu, J.-H., Palmstrom, J. C., Kivelson, S. A. & Fisher, I. R. Ubiquitous signatures of nematic quantum criticality in optimally doped Fe-based superconductors. Science 352, 958–962 (2016).