The table presents the viability results of cell suspensions obtained from different formulas designed for cell recovery in 3D cultures with medium stiffness. The reactions were conducted at 37 °C for 15 minutes. Notably, the formula comprising 0.9 U of dispase II and 100 U of collagenase type I in 1 ml of calcium chloride solution exhibited the highest cell viability. Additionally, this formulation demonstrated the capability to completely dissolve samples across three distinct groups of matrix stiffness.

Supplementary Table 1 Viability of Cell Suspension Derived from Various Formulas for Cell Recovery in 3D Cultures

| Trypsin (0.25%) | Dispase | Collagenase | Cell viability (%) |
| --- | --- | --- | --- |
| 1 ml |  |  | 80.1% |
| 1 ml | 100U |  | 88.5% |
| 1.2 ml | 50U |  | 93.0% |
|  | 1.8U |  | 76.5% |
|  | 0.9U |  | 89.0% |
|  |  | 100U | 83.5% |
|  |  | 150U | 86.0% |
|  | 0.9U | 100U | 90.5% |
|  | 0.9U | 50U | 86.5% |
|  | 1.8U | 50U | 83.5% |
| Cell suspension kit Minute™ (Invent Biotechnologies, USA) |  |  | 38.5% |

The depicted sequence illustrates the retrieval process of cell-laden gels from the agarose support (left column), subsequent dissolution using collagenase/dispase (middle column), and mechanical dissociation with a pipette (right picture). The resulting cell suspension is then centrifuged for subsequent flow cytometry analysis.

Supplementary Figure 1 Cell Retrieval and Analysis Process