Engineering motile aqueous phase-separated droplets

via liposome stabilisation

Shaobin Zhang1, Claudia Contini1, James W. Hindley1,2,3, Guido Bolognesi4, Yuval Elani2,5, Oscar Ces1,2,3*

- Department of Chemistry, Imperial College London, Molecular Sciences Research Hub, Shepherd’s Bush, London, W12 0BZ, UK

- Institute of Chemical Biology, Imperial College London, Molecular Sciences Research Hub, Shepherd’s Bush, London, W12 0BZ, UK

- fabriCELL, Imperial College London, Molecular Sciences Research Hub, Shepherd’s Bush, London, W12 0BZ, UK

- Department of Chemical Engineering, Loughborough University, Loughborough, LE11 3TU, UK

- Department of Chemical Engineering, Imperial College London, South Kensington, London, SW7 2AZ, UK.

* Correspondence: o.ces@imperial.ac.uk

1 ATPS composition

Table 1 Composition of two phases in ATPS

| Phase | PEG content (%w) | DEX content (%w) | water content (%w) |
| --- | --- | --- | --- |
| PEG-rich phase | 17.1 | 4.8 | 78.1 |
| DEX-rich phase | 0.8 | 30.5 | 68.7 |

2 Characterization of liposomes

Supplementary Fig. 1 liposome structure and size distribution. (a) TEM picture for prepared liposomes. The prepared liposomes are unilamellar. (b) Size distribution for prepared liposomes. The average diameter of liposomes is 150.5 nm, which is consistent with filter size used for extrusion.

3 Size exclusion chromatography

Supplementary Fig.2 Intensity for different elution batches in size chromatography experiment. Two peaks can be observed, and the first peak is corresponding to encapsulated calcein, while the second is for free calcein.

4 Droplet stability

Supplementary Fig.3 Droplet size at different time points. Liposome concentration is 0.10 mg/mL. From 0 min to 120 min, droplet size first gradually increases due to droplet merge, then limited change in droplet size occurs after liposome coverage is enough to stabilize emulsion droplets. Scale bar is 50 μm.

5 Fluorescence intensity change

Supplementary Fig.4 Intensity change during Janus transformation and droplet motion. Before droplet motion, the intensity of droplets keeps nearly constant (the plateau stage), which means no loss of liposome. When droplet starts moving, the intensity will gradually decrease due to the loss of liposomes caused by surface flow.

6 Effect of PEG-rich addition and DEX-rich addition

Supplementary Fig.5 Effect of PEG-rich addition and DEX-rich addition. PEG-rich addition simply causes limited droplet merging within the local vicinity, while adding more of the DEX-rich phase eliminates a great number of emulsion droplets within the chamber. Scale bar is 50 μm.

7 The relationship between Umax and D for chosen droplets

Supplementary Fig.6 The relationship between maximum velocity and droplet diameter. These 10 droplets were chosen from two different trials (with or without liposome). The correlation coefficient for Umax-D curve is 0.91, which means these 10 chosen droplets experienced roughly the same polymer gradient.

8 Liposome surface concentration

Emulsion droplets are produced via vortex, and the initial average droplet size is only dependent on vortex strength, i.e. initial average droplet size is approximately constant once vortex strength is fixed. Since the volume of DEX-rich phase is fixed at 6 μL, thus the initial number of emulsion droplets is approximately constant. At same liposome concentration, the initial number of liposomes in liposome coating (i.e. liposome coverage coefficient) then should be approximately the same. We can consider these droplets as unit droplets that create new droplets via droplet merge. The volume of a new droplet should be integer multiples to that of unit droplet.

For a unit droplet,

Nunit=σunitAunit

(8-1)

Where Nunit is the initial number of liposomes in a liposome coating, Aunit is the initial droplet surface area, and σunit is the initial surface concentration for liposomes on droplet’s surface.

Consider a droplet generated via the merge of n unit droplets,

N1=σ1A1

(8-2)

Where N1 is the number of liposomes in a liposome coating, A1 is droplet surface area, and σ1 is surface concentration.

The volume for this new droplet (V1) can be calculated as below,

V1=nVunit=πD136=nπDunit36

(8-3)

Where Dunit and D1 is the diameter for unit droplet and the new droplet                                                                                                                                                        respectively.

Thus, the surface area for this new droplet can be calculated as below,

A1=π6V1π23=n23πDunit2

(8-4)

Then σ1 can be calculated as below,

σ1=N1A1=nNunitA1=nσunitAunitA1=n13σunit

(8-5)

Combine Equation (8-3) and (8-5),

σ1=n13σunit=D1σunitDunit=kD1

(8-6)

Where k=σunitDunit is s constant for droplets. Equation (8-6) means that liposome surface concentration is proportional to droplet diameter.

9 Theoretical model for droplet motion

For a qualitative analysis of droplet motion, we can model the droplet surface as a sharp (not diffuse) interface with an IFT γ(cP,σ) that depends on the total polymer concentration cP and the surface concentration σ. A Cartesian (ex,ey,ez) and spherical (er,eθ,eϕ)  coordinate systems are defined with the origin at the droplet centre and z axis parallel to the total polymer concentration gradient, ∇cP=dcPdz ez. The IFT gradient at the droplet interface (i.e., at r=R with R the droplet radius) can be written as

∇γ=-sinϑdcPdz∂γ∂cP+1R∂γ∂σ∂σ∂ϑeθ

(9-1)

Such a gradient induces the droplet motion by Marangoni effect at speed U=U ez. To determine the expression of U, the Stokes equations must be solved

∇⋅u(o)=0

(9-2)

μo ∇2u(o)=∇ p(o)

(9-3)

∇⋅u(i)=0

(9-4)

μi ∇2u(i)=∇p(o)

(9-5)

with u(α), p(α), μα represent the velocity, pressure and viscosity, respectively, of the inner (α=i) and outer (α=o) liquid phase. Due to the symmetry of the problem [1], the velocity fields can be expressed in term of stream functions ψ(α), such that

uϑ(α)=-1rsin2ϑ ∂ψα∂ϑ  ,      ur(α)=1rsinϑ ∂ψ(α)∂r

(9-6)

with u(α)= ur(α)er+uϑ(α)eθ . For sake of simplicity, we neglect the effects of liposomes on the droplet interface, so that the IFT gradient can be re-written as

∇γ=-sinϑdcPdzdγdcPeθ

(9-7)

If we also assume that both dcPdz and ∂γ∂cP are constant,  the stream functions ψ(α) can be written as

ψα=sin2ϑA(α) r410-Bα r2+C(α)r2+D(α)r

(9-8)

The eight arbitrary constant A(α), Bα, C(α), D(α)  are determined by imposing the following boundary conditions

uro→ -Ucosϑ,    uϑo→ Usinϑ       for       r→ ∞,

uro=uri=0,  uϑo=uϑi     for       r→ R,

p(i)=p(o)+2γR,     τrϑ(i)-τrϑo=∇γ⋅eθ     for       r= R,

uϑi  ,   uri    finite  for       r→ 0

(9-9)

with the tangential stresses at the droplet interface given by

τrϑ(α)=μα∂uϑα∂rr=R-uϑα(r=R)R

(9-10)

From Eq. (9-9), one can obtain

A(o)=0,   B(o)=Rμo+μiU23μi+2μo+R3  dcPdz dγdcP ,

C(o)=0 ,   D(o)=R32(μi+μo)Uμi2+R3 dcPdz dγdcP

Ai=53 R μi+μo3Uμo2 R-dcPdz dγdcP,   Bi=0,

C(i)=-R6 μi+μo3Uμo2 R-dcPdz dγdcP,   Di=0

(9-11)

Due to the symmetry of the problem [1], the total force exerted by the fluid on the droplet can be expressed as

F=F ez=-4 π μo B(o) ez

(9-12)

By casting the expression of B(o) in Eq. (9-12), we get the expression for the force F

F=-4 π μo Rμo+μi U23μi+2μo+R3  dcPdz dγdcP

(9-13)

In absence of the IFT gradient, Eq. (9-13) reduces to the known expression [1] for the drag force on a droplet moving at constant speed U, and, by taking μ(i)→∞, it further reduces to the know expression for the drag force on a solid particle, namely F=6 π μ(o) R U. By imposing the force balance on the droplet (F=0), the following expression of  U can be obtained

U=-D3 2μo+3μi dcPdz dγdcP

(9-13)

with D=2 R, the droplet diameter. It is worth noting that this expression matches that one obtained by Young et al. [2] for a bubble moving along a temperature gradient, ∇T=dTdzez , by Marangoni effect when the term dcPdz dγdcP is replaced with dTdz dγdT , the gravity effect is neglected and the outer and inner media have the same thermal conductivity.

The proposed model has a number of limitations. First of all, the effect of liposomes adsorbed to the droplet interface is not accounted for. Furthermore, the dynamics of PEG and DEX polymers within the outer and inner phases is neglected and, for sake of simplicity, a constant total polymer concentration gradient dcPdz is considered. Time-dependent effects on droplet dynamics are also neglected and only droplet motion at steady-stated is considered. Finally, the water flow through the droplet interface was neglected and the boundary conditions of flow impenetrability was used instead. Despite these limitations, the proposed model still captures the basic physical mechanisms governing the droplet motion and the predicted droplet behaviour is consistent with our experimental observations.

Eq. (9-13) can be used to estimate the order of magnitude of the maximum droplet speed under our experimental conditions. The term dγdcP is estimated by using spinning droplet tensiometer measurements, reported in [3], for PEG and DEX solutions under varying total polymer concentration. According to [3], the relation between γ and cp can be written as

γ=γ cPcP, cr -1m

(9-14)

from which follows

dγdcP=m γcP, cr  cPcP, cr -1m-1

(9-14)

with cP, cr =0.05 g/mL, m=1.67 and γ=146 µN/m. For our experiments conditions (cP≃0.3 g/mL) , we can estimate dγdcP≃14×10-6 N m2 kg-1 and dcPdz≃0.3gmL1 cm≃0.3×106 kg m-4. If we assume a viscosity of 100 cSt for both PEG and DEX phases, Eq. (9-13) predicts a velocity of ca. 6 µm/s for a droplet of diameter D=20 μm.

References

      - Happel, J. and Brenner, H. (2012). Low Reynolds number hydrodynamics: with special applications to particulate media (Vol. 1). Springer Science & Business Media.

      - Young, N.O., Goldstein, J.S. and Block, M.J. The motion of bubbles in a vertical temperature gradient. J Fluid Mech 6, 350-356 (1959). Note: The expression for the bubble velocity in this paper is not correct. The corrected expression can be found in Thompson, R.L., DeWitt, K.J. and Labus, T.L. Marangoni bubble motion phenomenon in zero gravity. Chem Eng Commun 5, 299-314 (1980).

      - Liu, Y., Lipowsky, R. and Dimova, R. Concentration dependence of the interfacial tension for aqueous two-phase polymer solutions of dextran and polyethylene glycol. Langmuir 28, 3831-3839 (2012).