Supplementary Material for The Effects of Chromium on the High Temperature Corrosion of Ni-Cr Alloys Exposed to Calcium Sulfate

Nicholas Ury1, Vilupanur Ravi1

1California State Polytechnic University, Pomona 3801 W. Temple Ave. Pomona, CA 91768

*Corresponding author: Vilupanur Ravi; Email: vravi@cpp.edu

Figure S1: EDS locations on Ni5Cr exposed to CaSO4 at 900 °C for 50 hours.

Table S1: Composition of corresponding EDS points shown in Figure S1

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 0.05 | 0.00 | 7.74 | 82.41 | 9.81 |
| B | 0.06 | 0.03 | 11.53 | 74.70 | 13.67 |
| C | 39.36 | 4.60 | 0.23 | 55.80 | 0.02 |
| D | 94.86 | 2.03 | 0.20 | 2.83 | 0.08 |
| E | 2.11 | 0.23 | 14.70 | 69.38 | 13.58 |
| F | 96.79 | 1.79 | 0.14 | 1.17 | 0.12 |
| G | 97.18 | 1.06 | 0.19 | 1.57 | 0.00 |
| H | 39.52 | 5.46 | 0.56 | 54.05 | 0.41 |
| I | 93.29 | 5.95 | 0.00 | 0.74 | 0.02 |

Figure S2: EDS locations on Ni10Cr exposed to CaSO4 at 900 °C for 50 hours.

Table S2: Composition of corresponding EDS points shown in Figure S2

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 45.83 | 0.68 | 0.22 | 53.20 | 0.07 |
| B | 24.55 | 16.59 | 4.16 | 54.55 | 0.15 |
| C | 92.92 | 5.91 | 0.17 | 0.96 | 0.04 |
| D | 37.05 | 1.35 | 0.60 | 60.96 | 0.04 |
| E | 11.53 | 26.51 | 1.15 | 60.77 | 0.04 |
| F | 93.19 | 5.50 | 0.19 | 1.08 | 0.04 |
| G | 47.47 | 0.44 | 0.24 | 51.79 | 0.06 |
| H | 50.95 | 15.06 | 0.74 | 33.12 | 0.13 |
| I | 88.72 | 10.38 | 0.00 | 0.88 | 0.02 |

Figure S3: EDS locations on Ni18Cr exposed to CaSO4 at 900 °C for 50 hours.

Table S3: Composition of corresponding EDS points shown in Figure S3

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 0.07 | 2.17 | 9.38 | 79.53 | 8.86 |
| B | 0.12 | 2.05 | 9.16 | 79.69 | 8.98 |
| C | 36.77 | 10.35 | 0.19 | 52.65 | 0.04 |
| D | 10.92 | 24.97 | 12.93 | 50.85 | 0.33 |
| E | 86.36 | 12.80 | 0.00 | 0.84 | 0.00 |
| F | 8.33 | 31.38 | 16.69 | 43.10 | 0.50 |
| G | 89.44 | 9.73 | 0.12 | 0.70 | 0.00 |
| H | 51.10 | 1.08 | 0.77 | 46.56 | 0.48 |
| I | 80.02 | 19.79 | 0.00 | 0.19 | 0.00 |

Figure S4: EDS locations on Ni5Cr exposed to CaSO4 at 1000 °C for 50 hours.

Table S4: Composition of corresponding EDS points shown in Figure S4

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 1.17 | 1.07 | 13.10 | 71.78 | 12.89 |
| B | 45.83 | 0.54 | 0.10 | 53.51 | 0.01 |
| C | 45.87 | 0.13 | 0.47 | 53.51 | 0.02 |
| D | 0.33 | 1.17 | 13.62 | 71.27 | 13.61 |
| E | 17.00 | 21.06 | 0.16 | 61.78 | 0.00 |
| F | 34.00 | 9.03 | 0.00 | 56.96 | 0.01 |
| G | 11.54 | 27.63 | 0.25 | 60.52 | 0.06 |
| H | 2.43 | 32.11 | 0.03 | 65.38 | 0.06 |
| I | 98.43 | 0.61 | 0.00 | 0.94 | 0.02 |
| J | 81.60 | 6.46 | 0.01 | 0.41 | 11.52 |
| K | 2.21 | 30.83 | 0.06 | 66.64 | 0.27 |
| L | 9.47 | 34.21 | 0.01 | 0.00 | 56.31 |
| M | 91.56 | 4.54 | 0.03 | 3.87 | 0.00 |
| N | 73.79 | 7.12 | 0.00 | 19.09 | 0.00 |
| O | 92.68 | 6.12 | 0.05 | 1.16 | 0.00 |

Figure S5: EDS locations on Ni10Cr exposed to CaSO4 at 1000 °C for 50 hours.

Table S5: Composition of corresponding EDS points shown in Figure S5

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 0.15 | 3.43 | 12.56 | 73.60 | 10.25 |
| B | 33.13 | 6.56 | 0.08 | 60.20 | 0.03 |
| C | 93.89 | 2.84 | 0.03 | 3.23 | 0.02 |
| D | 17.69 | 15.39 | 12.56 | 53.80 | 0.56 |
| E | 46.30 | 0.38 | 0.10 | 53.19 | 0.02 |
| F | 76.18 | 9.04 | 0.15 | 14.59 | 0.03 |
| G | 94.05 | 3.49 | 0.06 | 2.40 | 0.00 |
| H | 22.21 | 17.57 | 0.27 | 59.90 | 0.04 |
| I | 47.37 | 0.51 | 0.12 | 51.99 | 0.01 |
| J | 11.75 | 12.53 | 12.20 | 62.82 | 0.70 |
| K | 63.86 | 17.24 | 0.06 | 1.43 | 17.41 |
| L | 87.74 | 10.41 | 0.02 | 1.82 | 0.02 |

Figure S6: EDS locations on Ni18Cr exposed to CaSO4 at 1000 °C for 50 hours.

Table S6: Composition of corresponding EDS points shown in Figure S6

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 0.06 | 3.06 | 9.55 | 79.78 | 7.55 |
| B | 91.75 | 7.34 | 0.11 | 0.77 | 0.04 |
| C | 43.01 | 7.24 | 7.62 | 41.68 | 0.45 |
| D | 16.31 | 22.62 | 0.82 | 60.21 | 0.04 |
| E | 51.43 | 0.88 | 0.31 | 47.35 | 0.04 |
| F | 72.00 | 4.18 | 2.95 | 20.73 | 0.14 |
| G | 0.96 | 30.57 | 14.76 | 53.65 | 0.07 |
| H | 7.94 | 17.37 | 17.79 | 56.05 | 0.85 |
| I | 92.05 | 6.54 | 0.22 | 1.15 | 0.04 |
| J | 20.12 | 7.15 | 10.58 | 61.73 | 0.41 |
| K | 80.02 | 19.57 | 0.05 | 0.34 | 0.02 |

Figure S7: EDS locations on Ni5Cr exposed to CaSO4 at 1100 °C for 50 hours.

Table S7: Composition of corresponding EDS points shown in Figure S7

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 0.70 | 0.40 | 14.55 | 68.92 | 15.44 |
| B | 0.57 | 0.20 | 12.94 | 72.17 | 14.13 |
| C | 45.93 | 0.37 | 1.38 | 52.24 | 0.07 |
| D | 47.30 | 0.32 | 0.25 | 52.08 | 0.05 |
| E | 7.95 | 19.76 | 10.59 | 60.81 | 0.89 |
| F | 7.59 | 20.94 | 10.63 | 60.83 | 0.01 |
| G | 6.50 | 22.08 | 11.50 | 59.88 | 0.06 |
| H | 0.91 | 29.38 | 9.86 | 59.79 | 0.06 |
| I | 98.11 | 0.99 | 0.00 | 0.90 | 0.00 |
| J | 98.08 | 1.29 | 0.05 | 0.59 | 0.00 |
| K | 97.95 | 1.23 | 0.00 | 0.74 | 0.08 |
| L | 98.09 | 0.46 | 0.02 | 1.44 | 0.00 |

Figure S8: EDS locations on Ni10Cr exposed to CaSO4 at 1100 °C for 50 hours.

Table S8: Composition of corresponding EDS points shown in Figure S8

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 0.47 | 13.99 | 21.00 | 62.90 | 1.64 |
| B | 0.36 | 12.37 | 18.91 | 66.67 | 1.70 |
| C | 0.47 | 13.00 | 20.28 | 64.42 | 1.82 |
| D | 47.15 | 0.13 | 0.84 | 51.85 | 0.04 |
| E | 4.46 | 4.70 | 15.94 | 65.15 | 9.75 |
| F | 9.90 | 13.13 | 18.40 | 57.21 | 1.37 |
| G | 46.74 | 0.11 | 0.83 | 52.32 | 0.00 |
| H | 46.82 | 2.41 | 0.96 | 49.80 | 0.01 |
| I | 1.23 | 24.41 | 11.93 | 62.43 | 0.01 |
| J | 95.55 | 3.72 | 0.14 | 0.59 | 0.00 |
| K | 0.90 | 13.34 | 20.94 | 62.91 | 1.90 |
| L | 39.39 | 26.44 | 0.05 | 34.09 | 0.03 |
| M | 5.02 | 31.99 | 0.09 | 62.91 | 0.00 |
| N | 96.10 | 3.54 | 0.05 | 0.28 | 0.04 |
| O | 4.00 | 20.58 | 10.22 | 65.21 | 0.00 |
| P | 0.66 | 12.46 | 19.93 | 65.07 | 1.88 |
| Q | 0.70 | 33.37 | 0.76 | 65.16 | 0.00 |
| R | 89.85 | 9.33 | 0.00 | 0.78 | 0.04 |

Figure S9: EDS locations on Ni18Cr exposed to CaSO4 at 1100 °C for 50 hours.

Table S9: Composition of corresponding EDS points shown in Figure S9

| Element | Ni | Cr | Ca | O | S |
| --- | --- | --- | --- | --- | --- |
| A | 42.92 | 1.09 | 0.11 | 55.83 | 0.05 |
| B | 43.23 | 1.19 | 0.01 | 55.53 | 0.05 |
| C | 1.66 | 28.68 | 0.06 | 69.58 | 0.03 |
| D | 92.51 | 7.30 | 0.00 | 0.16 | 0.04 |
| E | 8.41 | 21.18 | 9.94 | 60.46 | 0.02 |
| F | 33.50 | 3.42 | 0.03 | 63.05 | 0.00 |
| G | 3.28 | 23.47 | 11.56 | 61.69 | 0.00 |
| H | 0.50 | 32.00 | 0.12 | 67.38 | 0.01 |
| I | 93.04 | 6.38 | 0.14 | 0.44 | 0.00 |
| J | 78.78 | 17.69 | 0.00 | 0.39 | 3.14 |
| K | 79.94 | 19.78 | 0.03 | 0.12 | 0.13 |