Extended Data Tables

Extended Data Table 1 | Initiator and inhibitor concentrations for spin and uniform modes of front propagation and the corresponding front velocity, maximum front temperature, and heat of reaction for a 5.29 g (6 mL) sample.

| Initiator | Mode of Front Propagation | Mass of initiator (mg) | Initiator Concentration (mmol) | Volume of Inhibitor (μL) | Inhibitor Concentration (mmol) | Molar equiv. of Inhibitor to Initiator | vf† (mm/sec) | Tmax (°C) | Hr‡ (J/g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ru-1 | Spin | 7.68 | 0.0090 | 5.0 | 0.018 | 2.0 | 0.45 ± 0.03 | 159 ± 4 | 298.2 ± 4.5 |
| Ru-1 | Uniform | 7.68 | 0.0090 | 2.5 | 0.0092 | 1.0 | 0.41 ± 0.01 | 158 ± 6 | 305.6 ± 6.3 |
| Ru-2 | Spin | 7.20 | 0.0087 | 4.0 | 0.015 | 1.7 | 0.28 ± 0.03 | 152 ± 3 | 290.8 ± 5.8 |
| Ru-2 | Uniform | 7.20 | 0.0087 | 2.0 | 0.0074 | 0.85 | 0.33 ± 0.02 | 158 ± 2 | 303.4 ± 7.1 |
| Ru-3 | Spin | 8.40 | 0.0089 | 2.4 | 0.0089 | 1.0 | 0.26 ± 0.02 | 153 ± 1 | 304.9 ± 5.9 |
| Ru-3 | Uniform | 8.40 | 0.0089 | 1.2 | 0.0044 | 0.50 | 0.23 ± 0.02 | 157 ± 2 | 306.3 ± 8.5 |
| Ru-3* | Spin | 16.80 | 0.018 | 1.2 | 0.0044 | 0.25 | 0.28 ± 0.03 | 156 ± 2 | 305.1 ± 7.6 |

# Vf: front speed; Tmax: maximum front temperature; Hr: heat of reaction

# Reported values and error bars represent the average and standard deviation, respectively for a n=3.

# * Represents the resin formulation for successful spin mode propagation of Ru-3 at ambient temperatures below 40 °C.

# † Front temperatures and velocities are highly dependent on the material and geometrical conditions used for manufacturing. The values reported here correspond to the experimental conditions described in the Methods section.

# ‡ The heat of reaction was measured from differential scanning calorimetry dynamic scans at a rate of 5 °C/min.

# Extended Data Table 2 | Physical and thermal properties of COD and silicone rubber used in numerical modeling.

|  | κ (W m-1 K-1) | ρ (kg m-3) | Hr (J g-1) | Cp (J kg-1 K-1) | A (s-1) | E (kJ mol-1) | n | m |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| COD (r) | 0.133 | 882 | 259 | 1,838 | 1.57 x 1017 | 117.45 | 2.60 | 0.83 |
| Silicone rubber (s) | 1.0 | 1,500 | - | 1,200 | - | - | - | - |

Extended Data Table 3 | Comparison of the percent distribution of polymer chains for specimens derived from the three ruthenium initiators and by different modes of front propagation.

| Initiator | Specimen Type | Ambient Temperature (°C) | Percent Distribution θ = 0° | Percent Distribution θ = ± 90° |
| --- | --- | --- | --- | --- |
| Ru-1 | Architected | 25 | 45.5 | 54.5 |
| Ru-2 | Architected | 25 | 41.6 | 58.4 |
| Ru-3 | Architected | 25 | 36.2 | 63.0 |
| Ru-1 | Uniform | 20 | 33.0 | 67.0 |
| Ru-2 | Uniform | 30 | 44.0 | 56.0 |
| Ru-3 | Uniform | 50 | 41.3 | 58.7 |

| Initiator | Specimen Type | Specimen Orientation | Ambient Temperature (°C) | Elastic Modulus (GPa) | Tensile Strength (MPa) | Strain Energy Density (MJ/m3) | Strain to Failure (mm/mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ru-1 | Architected | 1 | 20 | 0.1 ± 0.008 | 4.2 ± 0.2 | 1.4 ± 0.3 | 1.0 ± 0.2 |
| Ru-1 | Architected | 2 | 20 | 0.1 ± 0.008 | 4.0 ± 0.2 | 1.5 ± 0.2 | 1.1 ± 0.1 |
| Ru-2 | Architected | 1 | 30 | 0.2 ± 0.01 | 5.2 ± 0.4 | 0.2 ± 0.1 | 0.1 ± 0.02 |
| Ru-2 | Architected | 2 | 30 | 0.2 ± 0.01 | 5.8 ± 0.6 | 0.4 ± 0.1 | 0.1 ± 0.06 |
| Ru-3 | Architected | 1 | 40 | 0.3 ± 0.02 | 7.6 ± 0.5 | 0.4 ± 0.1 | 0.1 ± 0.005 |
| Ru-3 | Architected | 2 | 40 | 0.7 ± 0.05 | 11.1 ± 0.4 | 0.5 ± 0.1 | 0.1 ± 0.01 |
| Ru-1 | Uniform | 1 | 20 | 0.8 ± 0.08 | 12.2 ± 0.5 | 0.6 ± 0.3 | 0.1 ± 0.01 |
| Ru-1 | Uniform | 2 | 20 | 0.6 ± 0.03 | 10.1 ± 0.9 | 0.3 ± 0.1 | 0.04 ± 0.004 |
| Ru-2 | Uniform | 1 | 30 | 0.6 ± 0.02 | 9.8 ± 0.1 | 0.3 ± 0.1 | 0.04 ± 0.006 |
| Ru-2 | Uniform | 2 | 30 | 0.7 ± 0.05 | 10.0 ± 0.7 | 0.3 ± 0.1 | 0.04 ± 0.008 |
| Ru-3 | Uniform | 1 | 40 | 0.8 ± 0.08 | 11.4 ± 0.8 | 0.2 ± 0.02 | 0.03 ± 0.002 |
| Ru-3 | Uniform | 2 | 40 | 0.8 ± 0.08 | 10.2 ± 0.3 | 0.2 ± 0.02 | 0.03 ± 0.004 |

Extended Data Table 4 | Comparison of the mechanical properties for specimens derived from the three ruthenium initiators and by different modes of front propagation.

# Reported values and error bars represent the average and 95% confidence interval, respectively, for a n=5.