Methods

Materials. 1,5-cyclooctadiene (COD) and tributyl phosphite (TBP) were purchased from TCI America. COD was passed through a plug of basic alumina to remove the octadecyl 3-(3′,5′-di-tert-butyl-4′-hydroxylphenyl) propionate stabilizer. TBP was stored under an inert atmosphere. 5-ethylidene-2-norbornene (ENB), Grubbs Catalyst® M204 (Ru-1), Grubbs Catalyst® M207 (Ru-2), and Grubbs Catalyst® M202 (Ru-3) were purchased from Sigma-Aldrich and used as received. A 26-gauge Kanthal wire (D = 0.40 mm, resistivity = 1.4 × 10−4 Ω cm) was used to initiate FROMP. High temperature silicone rubber gaskets were purchased from McMaster-Carr. 1 mm thick glass slides were purchased from Ted Pella.

Frontal polymerization. In a typical experiment for the spin mode of front propagation with the Ru-1 initiator, 5.29 g (6 mL, 5400 mol equiv to Ru-1) of monomer resin composed of 97 wt% COD (5.13 g / 5.82 mL) and 3 wt% ENB (0.16 g / 0.18 mL) was measured out in a vial. Unless otherwise noted, all references to COD refer to the 97:3 COD/ENB mixture. The phosphite inhibitor (4.98 μL, 0.0184 mmol, 2 mol equiv to Ru-1) was then added to the vial with monomer using a microliter syringe. In a separate vial, 7.68 mg (0.00905 mmol) of the Ru-1 initiator was weighed out. The monomer / inhibitor solution was then added to the vial containing the initiator, and the resulting mixture was sonicated for 5 min to ensure complete dissolution of the initiator. The monomer resin was then added to a rectilinear geometry before initiation of the front. Please refer to Extended Data Table 1 for the other resin formulations that yielded uniform and spin modes of front propagation with Ru-1, Ru-2, and Ru-3 initiators. Rectilinear closed molds were fabricated by compressing a U-shaped high temperature silicone rubber gasket cut into the desired geometry between two 1 mm thick glass slides. For a typical experiment, the frontal polymerization process was carried out in a 1.5 cm x 6.0 cm (w x h) geometry with a 5 mm thick silicone rubber gasket. The polymerization was initiated by local heating with a 26-gauge resistive wire and an Agilent (U8031A) triple output programmable DC power supply (3.5 V, 3.0 A). The ambient temperature was maintained in a custom-built environmental chamber equipped with an AC-162 Peltier module, TC-720 temperature controller, and PS-2425 power supply from TE Technology, Inc. Target ambient temperature T0 was achieved by setting the environmental chamber to the desired temperature and monitoring with a thermocouple. A schematic of the mold and initiation scheme employed for experiments is summarized in Extended Data Fig. 1a.

Front velocity and temperature measurements. To a 13 x 100 mm test tube, 8 mL of freshly prepared monomer mixture was immediately transferred. FROMP was initiated from the top of the test tube using the tip of a soldering iron, set to the highest heat setting. The front propagation is tracked with a Canon EOS R5 DSLR camera. Frontal velocities were measured using Tracker®, an open-source physics (OSP) video analysis and modeling tool. Using the built-in tracking feature, position, time, and velocity were extracted from the videos. Each video was analyzed a total of three times, and the front velocity of the resin formulation was determined by the average of the three samples. To measure the maximum front temperature, a T-type thermocouple (TMQSS, Omega) was inserted at the center of the test tube before initiating FROMP and the temperature profiles were monitored by a custom Labview program. The average maximum front temperature was taken from a n=3.

Heat of reaction and heat of fusion analysis. Differential scanning calorimetry (DSC) measurements were carried out on a TA Instruments Discovery DSC 250 equipped with an RCS 90 cooling system and an autosampler. Samples were transferred into aluminum hermetic DSC pans at room temperature and sealed. The sample mass was determined using an analytical balance (XPE205, MettlerToledo). The mass of the liquid resin samples was carefully maintained to ensure the maximum heat flow of the exothermic reaction was between 6 – 10 mW. Dynamic curing profiles of liquid resins were determined at temperatures between -50 °C and 180 °C with constant ramp rates (Extended Data Figure 1b). The heat of reaction (Hr) was determined through the integration of heat flow over the exothermic peak after baseline correction for cure profiles1 with a ramp rate of 5 °C/min. The heat of fusion (Hf) was measured by cutting cured polymer specimens at various time points and transferring them into aluminum hermetic DSC pans at room temperature. The mass of the polymer specimens was carefully maintained between 5-10 mg. The melting profiles of polymer specimens were determined at temperatures between 20 °C and 150 °C with a constant ramp rate of 10 °C/min. The endothermic peak in the heat flow signal was integrated to extract the heat of fusion for each specimen.

Nanoindentation. Nanoindentation was performed with a Hysitron TI-950 TriboIndenter equipped with a Hysitron 3D Omniprobe high-load transducer and Berkovich tip from Bruker. Samples that were left to sit for 24 h post polymerization at room temperature were loaded at 0.2 mN/s up to a maximum load of 8 mN, which was held for 5 s, and subsequently unloaded at 0.2 mN/s. Reduced moduli were calculated from the unloading curves using the Hysitron software by fitting a slope to the unloading force-displacement curve.

Raman confocal imaging. Raman spectra were obtained with a Horiba LabRAM HR 3D Raman confocal imaging microscope equipped with an 830 nm laser, a 300 groove 1/mm grating (blazed at 600 nm), a long working distance 20x objective from Leica, and a Horiba Synapse back-illuminated deep depletion CCD camera2.

Nuclear magnetic resonance (NMR). 1H NMR and 13C spectra were obtained at room temperature in deuterated chloroform (CDCl3) on Bruker CB500 with cryoprobe (1H NMR at 500 MHz and 13C NMR at 126 MHz), using deuterium lock. Data for 1H NMR spectra are quoted relative to solvent as an internal standard (7.26 ppm), and data for 13C NMR spectra are quoted relative to dichloromethane as an internal standard (77.16 ppm). 1H NMR spectra were collected over 16 scans from 16 to -4 ppm. 13C NMR spectra were collected over 252 scans from 235 to -15 ppm. Heteronuclear Single Quantum Coherence (HSQC) NMR spectra were collected over the range used in the 1D NMR studies.

Computational modeling. Numerical analyses were conducted in a two-dimensional domain comprising two subdomains of the COD resin and the silicone rubber bands, as presented in Extended Data Fig. 1. The length (l= 50 mm) and width (Ws= 2.5 mm) of the silicone rubber band were kept as constant in all simulations while the width of the COD resin wr varied between 5 and 50 mm, consistent with the experimental setup. The polymerization front was numerically initiated at an inclined boundary (marked by the red dashed line) to mimic the asymmetric effect on frontal polymerization in experiment. The length of the boundaries l1= 2 mm and l2= 1 mm remained constant in all simulations. The glass mold was not explicitly considered in the numerical analyses.

Frontal polymerization of COD was modeled by the following reaction-diffusion partial differential equations:

&κr∇2T+ρrHr∂α∂t-H(T-T0)=ρrCp,r∂T∂t,&∂α∂t=Aexp-ERTgα.#1

The main variables are the temperature T (in K) and the degree of cure α (dimensionless), which takes values between 0 (monomer) and 1 (polymer) and describes the fractional conversion based on the enthalpy of the reaction. In the first equation, κr (in W/mK), ρr (in kg/m3), Hr (in J/kg), and Cp,r (in J/kg∙K) represent the thermal conductivity, density, enthalpy of reaction, and heat capacity of the resin, respectively, with the subscript ‘r’ denoting the resin. The term of -H(T-T0) was introduced to approximate the heat loss through the glass mold, where H= 140 kW/m3 is a heat loss coefficient. With this setting, a quenched front was observed with W= 5 mm at room temperature, consistent with experimental observation. The second equation models the cure kinetics of the resin, where A (in /s), E (in J/mol), R (=8.314 J/kg∙K) stand for the pre-exponential factor, activation energy, and the ideal gas constant, respectively. The Prout-Tompkins model3 was adopted to capture the dependence of cure kinetics on α, and gα=1-αnαm, where n (dimensionless) and m (dimensionless) are reaction orders. The thermal conduction in the silicone rubber (subscript ‘s’) was modeled by:

κs∇2T-HT-T0=ρsCp,s∂T∂t.#2

A Dirichlet boundary condition Tx,y,t= 160 ℃ was adopted at the inclined boundary for t≤ 5 s to trigger the polymerization front, and an adiabatic boundary condition was imposed to replace the Dirichlet boundary condition. Adiabatic boundary conditions were utilized at all other boundaries. The continuity of temperature and heat flux were imposed at all material interfaces between the COD resin and the silicone rubber bands. The initial degree of cure α0 was set as 0.04 and the initial temperature varied between 20 and 40 ℃.

The thermal properties of COD and silicone rubber are adopted from literature5,4 and given in Extended Data Table 2. DSC tests were performed under various temperature ramping rate to parametrize Hr, A, E, n and m. The cure kinetics parameters are presented in Extended Data Table 2, and the comparison between the DSC experiments and cure kinetics model is demonstrated in Extended Data Fig. 2. The cure kinetics model can be further validated by comparing the numerical front velocity of 0.44 mm/s and front temperature of 162.7 ℃ in unidirectional frontal polymerization with the experimental values of 0.45 mm/s and 159.2 ℃ measured in the FP experiments in a test tube.

All finite element simulations were conducted using the Multiphysics Object-Oriented Simulation Environment (MOOSE)6, an open-source C++ finite element solver with robust mesh and time-step adaptivity to capture the gradients in temperature and degree of cure in the vicinity of the unstable polymerization front. The average size of the mesh was ~ 0.4 mm, and the h-level of the mesh adaptivity was set as 6. The typical time step was 0.01 s and was reduced to ~ 0.00001 s when experiencing large gradients of T and α during instabilities.

Image Analysis. Optical images of the resulting polymer specimens 24 h post polymerization were captured using a digital microscope (VHX-5000, Keyence) with a 20x objective. The distance between the material domains was analyzed using FIJI (ImageJ 1.54b). The average distance was determined by measuring the spatial separation between the material domains at three positions (left, middle, and right) along the samples, covering roughly 50 mm.

Fabrication of specimens for X-ray diffraction. Various resin formulations were used to fabricate different polymer specimens derived with three different initiators (Ru-1, Ru-2, Ru-3) which can be found in Extended Data Table 1. For this fabrication method, 5.29 g (6 mL) of COD was used. We use a 15 mm x 60 mm x 3.3 mm U-shaped high temperature silicone rubber spacer between two 1 mm thick glass slides for X-ray diffraction specimens. The specimen thickness was specifically chosen such that about 70% penetration of the X-ray source could be achieved. FROMP is initiated immediately by applying an electric current to a resistive wire placed along one edge of the mold. The power supply is turned off a few seconds after frontal propagation is observed and remains off for the remainder of the propagation. Specimens sat for 24 h under N2 at 23.5 °C before removing the polymers from the glass mold. Samples were then cut to a 1 cm x 4 cm rectangular geometry and let to sit for another 48 h under N2 at 23.5 °C before being placed in the freezer (ca. -20 °C) to mitigate the evolution of the material domains prior to testing.

Small/wide angle X-ray scattering (S/WAXS). Simultaneous S/WAXS experiments were conducted at beamline 12-ID-B, Advanced Photon Source (APS), Argonne National Laboratory, using a Pilatus2M/Eiger9M detector (Dectris, Switzerland) for SAXS and a Pilatus300K detector (Dectris, Switzerland) for WAXS. X-ray beams with an average photon energy of 13.3 keV were used. The sample-to-detector distances (SDDs) for SAXS and WAXS were approximately 2 m and 0.46 m, respectively. All calibrations for SDDs were performed using a silver behenate powder standard. The obtained scattering patterns were radially and azimuthally integrated using an Igor-based package, NIKA7.

To determine the percent distribution of the polymer chain orientation, we performed the following steps. First, the 1D azimuthal plots acquired at each sample point were fitted using three Gaussian curves centering at -90, 0, and 90 degrees. We selected the higher height values from the Gaussian curves centered at -90 and 90 degrees. Using the selected height value, we calculated the percent height ratio by including the height of the curve centered at 0 degrees. The percent height ratio is equivalent to the percent distribution. In this data process, we fairly assumed that the 1D azimuthal plots give rise to peaks only at -90, 0, 90 degrees. To better illustrate the percent distribution of the polymer chain orientation, violin plots were overlaid with data points using the software OriginPro. The Kernel bandwidth was set to zero.

Fabrication of specimens for mechanical testing.  For this fabrication method, 22.94 g (26 mL) of COD was used and the initiator and inhibitor concentrations found in Extended Data Table 1 were scaled accordingly. Various resin formulations were used to fabricate different polymer specimens derived with the three initiators. The resin mixture was sonicated for 10 minutes until complete dissolution of the initiator and then transferred into the rectilinear mold. We used a 60 mm x 65 mm x 4.2 mm U-shaped high temperature silicone rubber spacer between two 1 mm thick glass slides for tensile specimens.  The ambient temperature was set to T0 = 20 °C for the Ru-1 derived specimens, T0 = 30 °C for the Ru-2 derived specimens, and T0 = 40 °C for the Ru-3 derived specimens. FROMP is initiated immediately by applying an electric current to a resistive wire placed along one edge of the mold. The power supply is turned off a few seconds after frontal propagation is observed and remains off for the remainder of the propagation. All specimens fabricated were left between glass for 24 h before removing specimen from the glass mold. We cut dog-bone specimens for tensile testing 48 h post polymerization from the manufactured polymer specimen using an ASTM D638 Type V dimension die from Qualitest. Dog-bone specimens were then stored under N2 at 23.5 °C for the remainder of their aging process prior to quasi-static tensile testing. Ru-1 uniform specimens were left under N2 for 48 h (72 h aged post polymerization) and Ru-1 architected specimens were left under N2 for 120 h (144 h aged post polymerization). Ru-2 and Ru-3 uniform specimens were left under N2 for 48 h (72 h aged post polymerization) and the respective architected specimens were left under N2 for 96 h (120 h post polymerization). The respective heat of fusion for each specimen type at the time of testing can be found in Supplementary Data Table S5.

Quasi-static tensile testing. Tensile tests were conducted using an Instron 5984 universal testing system equipped with a 5 kN load cell and a video extensometer under ambient conditions. Any compressive load introduced during the tightening of the frame’s grips was removed by loading the sample until the load read 0 N at 10% of the final testing rate. Tensile tests were performed under displacement control at a constant rate of 5 mm/min until the samples failed. Young’s modulus was calculated using the slope of the best-fit line for the stress-strain curve from 0.1-0.3% strain. The tensile strength of the sample was recorded as the maximum stress achieved during the test. Strain-to-failure was taken as the maximum strain the samples achieved at the point of failure. The strain energy density was calculated from the area under the curve of the stress-strain curve up to the point of failure. The error bars represent the 95% confidence interval for n=5 calculated using a Z-score of 1.96.

Thermomechanical Characterization. The thermomechanical properties of uniform and architected specimens derived from the three initiators were evaluated 24 h post polymerization using dynamic mechanical analysis (DMA). These tests were performed on a TA instruments Q800 equipped with a gas cooling accessory and tension clamps. Uniform and architected specimens were cut into rectangular samples 25 mm x 4 mm x 0.9 mm and the gauge length was maintained at 16 mm. DMA was performed in multi-frequency strain mode with an oscillation strain of 0.1 % and a static force of 0.001 N. The temperature was increased linearly from -130°C to 50 °C at 5 °C/min. Data were obtained for a minimum of three specimens.

Method References

- Kessler, M. R.; White, S. R. Cure Kinetics of the Ring-Opening Metathesis Polymerization of Dicyclopentadiene. J. Polym. Sci. Part A Polym. Chem. 2002. https://doi.org/10.1002/pola.10317.

- Cornell, S. W.; Koenig, J. L. The Raman Spectra of Polybutadiene Rubbers. Macromolecules 1969, 2 (5). https://doi.org/10.1021/ma60011a018.

- Hardis, R.; Jessop, J. L. P.; Peters, F. E.; Kessler, M. R. Cure Kinetics Characterization and Monitoring of an Epoxy Resin Using DSC, Raman Spectroscopy, and DEA. Compos. Part A Appl. Sci. Manuf. 2013, 49. https://doi.org/10.1016/j.compositesa.2013.01.021.

- Lloyd, E. M.; Feinberg, E. C.; Gao, Y.; Peterson, S. R.; Soman, B.; Hemmer, J.; Dean, L. M.; Wu, Q.; Geubelle, P. H.; Sottos, N. R.; Moore, J. S. Spontaneous Patterning during Frontal Polymerization. ACS Cent. Sci. 2021, 7 (4). https://doi.org/10.1021/acscentsci.1c00110.

- Silicone Rubber, <https://www.azom.com/properties.aspx?ArticleID=920>

- Gaston, D., Newman, C., Hansen, G. & Lebrun-Grandie, D. MOOSE: A Parallel Computational Framework for Coupled Systems of Nonlinear Equations. Nucl. Eng. Des. 2009, 239, 1768-1778. https://doi.org/10.1016/j.nucengdes.2009.05.021

- Ilavsky, J. Nika: Software for Two-Dimensional Data Reduction. J. Appl. Crystallogr. 2012, 45 (2). https://doi.org/10.1107/S0021889812004037.