Supplementary Information

for

Effect of Na2CO3 on production of NaHCO3

using desulfurized Na2SO4 waste

Chaehyun Lim*,‡, Youngchul Byun**,‡, Hwan Gi Kim**, Sang Sook Park*, Jung Gi Min**,†

*Dept. of Environmental Eng, Suncheon National University, Suncheon-si 57922, Korea

**Research Institute of Industrial Science and Tech(RIST), Gwangyang-si, 57801, Korea

‡These Authors contributed equally

Table S1. Simulation conditions of MINEQL+

| No. | Content |
| --- | --- |
| 1 | Conc. of Na+: 6.580075 mol/L |
| 2 | Conc. of Ca2+: 0.16592 mol/L |
| 3 | Conc. of K+: 0.87685 mol/L |
| 4 | Conc. of Cl-: 0.116316 mol/L |
| 5 | Conc. of Fe2+: 0.056632 mol/L |
| 6 | Conc. of SO42-: 2.134184 mol/L |
| 7 | Conc. of CO32-: 3.367035 mol/L |
| 8 | pH is set as “calculated by MINEQL+” |
| 9 | CO2 is selected as “closed to the atmosphere” |
| 10 | All solid are not considered |
| 11 | Ionic strength corrections: off |
| 12 | Temperature corrections: off |
| 13 | No surface model |

Table S2. 	Solubility table of possible impurities on Na2SO4 waste after the addition of Na2CO3

| No. | Chemical | Soluble & Insoluble | Solubility (g/100 mL) | Temperature (°C) |
| --- | --- | --- | --- | --- |
| 1 | Mg(OH)2 | insoluble | 0.00064 | 25 |
| 2 | MgCO3 | insoluble | 0.014 | 25 |
| 3 | MgSO4 | soluble | 26.91 | 20 |
| 4 | Al(OH)3 | insoluble | 0.00012 | 25 |
| 5 | Al2(CO3)2 | - | - | - |
| 6 | Al2(SO4)2 | soluble | 36.41 | 25 |
| 7 | Si(OH)4 | - | - | - |
| 8 | Si2(CO3)4 | - | - | - |
| 9 | Si2(SO4)4 | - | - | - |
| 10 | KOH | soluble | 121.12 | 25 |
| 11 | K2CO3 | soluble | 110.31 | 20 |
| 12 | K2SO4 | soluble | 11.12 | 20 |
| 13 | Ca(OH)2 | insoluble | 0.17 | 20 |
| 14 | CaCO3 | insoluble | 0.0013 | 25 |
| 15 | CaSO4 | insoluble | 0.26 | 25 |
| 16 | Fe(OH)2 | insoluble | 0.000052 | 20 |
| 17 | FeCO3 | insoluble | 0.00067 | 20 |
| 18 | FeSO4 | soluble | 29.51 | 25 |
| 19 | Fe(OH)3 | insoluble | - | - |
| 20 | Fe2(CO3)3 | insoluble | - | - |
| 21 | Fe2(SO4)3 | slowly soluble | 25.61 | 20 |
| 22 | Cu(OH)2 | insoluble | - | - |
| 23 | CuCO3 | insoluble | - | - |
| 24 | CuSO4 | soluble | 20.52 | 20 |
| 25 | Zn(OH)2 | insoluble | - | - |
| 26 | ZnCO3 | insoluble | 0.000091 | - |
| 27 | ZnSO4 | soluble | 57.71 | 20 |
| 28 | Se(OH)4 | insoluble | - | - |
| 29 | Se2(CO3)4 | - | - | - |
| 30 | Se2(SO4)4 | - | - | - |
| 31 | RbOH | soluble | 173.11 | 30 |
| 32 | Rb2CO3 | very soluble | - | - |
| 33 | Rb2SO4 | soluble | 5.08 | - |
| 34 | Pb(OH)2 | insoluble | 1.615 × 10-4 | 20 |
| 35 | PbCO3 | insoluble | 7.269 × 10-5 | 20 |
| 36 | PbSO4 | insoluble | 0.0044 | 20 |

Table S3. 	Chemical composition data of precipitated impurities measured by XRF after the addition of Na2CO3

| No. | Chemical formula | Value (wt%) |
| --- | --- | --- |
| 1 | C | 7.87 |
| 2 | Na2O | 6.35 |
| 3 | MgO | 2.73 |
| 4 | Al2O3 | 1.66 |
| 5 | SiO2 | 3.68 |
| 6 | P2O5 | 0.17 |
| 7 | SO3 | 4.35 |
| 8 | Cl | 0.19 |
| 9 | K2O | 0.32 |
| 10 | CaO | 33.4 |
| 11 | TiO2 | 0.43 |
| 12 | Cr2O3 | 0.024 |
| 13 | MnO | 0.18 |
| 14 | Fe2O3 | 35.41 |
| 15 | CuO | 0.088 |
| 16 | ZnO | 0.20 |
| 17 | SeO2 | 0.072 |
| 18 | Br | 0.0071 |
| 19 | SrO | 0.024 |
| 20 | Tl2O3 | 0.030 |
| 21 | PbO | 2.74 |
| 22 | Bi2O3 | 0.045 |

Fig. S1. Experimental schematic of SO2 removal.

Fig. S2. Solubility curves of Na2SO4 and NaHCO3 with different temperatures.

Fig. S3. Carbonate system with different pH.

Fig. S4. 	XRD patterns of solid product with different NH3:Na+ ratios of (a) 1.0, (b) 1.1, (c) 1.2, (d) 1.3, and (e) 1.5. The XRD pattern of pure NaHCO3 is shown on the bottom line for comparison.

Fig. S5. XRD pattern of precipitated impurities after the addition of Na2CO3.