Electronic Supplementary Information for

Computational screening of sodium solid electrolytes through unsupervised learning

Damdae Park1†, Wonsuk Chung1†, Byoung Koun Min1,3, Ung Lee1,3,4,
Seungho Yu2,4 * and Kyeongsu Kim1,4*

1 Clean Energy Research Center, Korea Institute of Science and Technology (KIST), Seoul 02792, Republic of Korea

2 Energy Storagte Research Center, Korea Institute of Science and Technology (KIST), Seoul 02792, Republic of Korea

3 Graduate School of Energy and Environment (Green School), Korea University, 145 Anam-ro, Seongbuk-gu, Seoul 02841, Republic of Korea

4 Division of Energy and Environmental Technology, KIST school, Korea University of Science and Technology (UST), Seoul 02792, Republic of Korea

† These authors contributed equally to this work.

* These authors contributed equally to this work.

Correspondence should be addressed to Kyeongsu Kim (kyeongsu@kist.re.kr).

Table S1. Descriptors constituting the feature vector. The numbers represent the valid dimensions. Invalid descriptors, namely Chemical ordering (CO), global instability index (GII), and structural variance (SV) descriptors, are omitted.

|  | A | A40 | AM | AM40 | CAMN | CAMN40 | CAN | CAN40 | Original | All |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| R |  |  |  |  |  |  |  |  | 1 | 1 |
| SOAP |  |  |  |  | 60 | 60 |  |  | 60 | 180 |
| V |  |  |  |  |  |  |  |  | 1 | 1 |
| APE |  |  | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 35 |
| BC |  |  | 1 | 1 | 1 | 1 | 1 | 1 |  | 6 |
| BF |  | 9 |  |  | 20 | 21 |  | 10 |  | 60 |
| Density | 3 | 3 | 3 | 3 | 3 | 3 | 3 | 3 |  | 24 |
| EE | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 9 |
| END |  |  | 3 | 3 | 5 | 5 | 4 | 4 | 5 | 29 |
| JCFID |  |  |  |  |  | 1529 |  | 1527 |  | 3056 |
| Lattice type |  |  |  |  |  |  |  |  | 1 | 1 |
| MD |  |  | 15 | 15 | 17 | 17 | 16 | 16 | 102 | 198 |
| MPE | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 9 |
| OFM | 9 | 9 | 16 |  | 25 | 25 | 16 | 16 | 1025 | 1141 |
| OS | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 4 | 36 |
| RDF | 92 | 93 | 92 | 94 | 94 | 94 | 94 | 94 | 94 | 841 |
| SC | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 18 |
| SCM |  | 9 |  |  | 20 | 21 |  | 10 |  | 60 |
| Space group |  |  |  |  |  |  |  |  | 1 | 1 |
| VO |  |  | 4 | 4 | 4 | 4 | 4 | 4 | 8 | 32 |
| mXRD | 451 | 451 | 451 | 451 | 451 | 451 | 451 | 451 | 451 | 4059 |
| YSS |  |  | 2 | 2 | 2 | 2 | 2 | 2 | 2 | 14 |
| All | 563 | 582 | 600 | 586 | 715 | 2246 | 604 | 2151 | 1764 | 9811 |

Table S2. Hyperparameter setups for HDBSCAN and PACMAP in clustering. Default values have been used unless otherwise unspecified.

|  |  | Group clustering | Subgroup clustering |
| --- | --- | --- | --- |
| HDBSCAN (sklearn v1.3.0) | min_cluster_size | 50 |  |
|  | min_samples | 50 | 5 |
| PACMAP (pacmap v0.7.0) | n_neighboirs | 30 |  |

Figure S1. Band gap and Ehull distributions over clustered groups.

Figure S2. Band gap and Ehull distributions over the subgroups within Group 5 and 7.

Figure S3. Average atomic fractions over the groups.

Table S3. Ionic conductivity of Na-ion solid-state conductors at room-temperature. aMaterials that can form different lattice structures.

| MP-ID | Formula | Space group | Conductivity [S cm-1] | Group | Reference |
| --- | --- | --- | --- | --- | --- |
| 648 | Na2S | Fm3̅m | 1.00×10-7 | 1 | Bertheville et al., 19971 |
| 1266 | Na2Se | Fm3̅m | 1.00×10-13 | 1 | Liu et al., 20202 |
| 22862 | NaCl | Fm3̅m | 1.00×10-13 | 1 | Hooton et al., 19883 |
| 23268 | NaI | Fm3̅m | 2.00×10-10 | 1 | Matsuo et al., 20124 |
| 677437 | aNa3Zr2Si2PO12 | P1 | 6.70×10-4 | 5A | Zhang et al., 20175 |
| 695119 |  | P1 |  | 5A |  |
| 695354 |  | P1 |  | 5A |  |
| 1133351 |  | P1 |  | 5A |  |
| 1221148 |  | C1c1 |  | 5A |  |
| 2713548 |  | C1c1 |  | 5A |  |
| 2713573 |  | C1c1 |  | 5B |  |
| 16956 | aNa3Sc2(PO4)3 | C1c1 | 3.04×10-4 | 5A | Rettenwander et al., 20186 |
| 1221287 |  | C1c1 |  | 5A |  |
| 2715413 |  | C1c1 |  | 5A |  |
| 1221280 |  | C12/c1 |  | 5A |  |
| 2715518 |  | C1c1 |  | 5B |  |
| 555608 |  | R3̅c |  | 5A |  |
| 2713249 | Na3Hf2Si2PO12 | C1c1 | 4.59×10-4 | 5A | Tial et al., 20217 |
| 2713308 |  | C1c1 |  | 5B |  |
| 23705 | Na3AlH6 | P12₁/c1 | 6.40×10-7 | 7B | Oguchi et al., 20128 |
| 23704 | NaAlH4 | I4₁/a | 2.00×10-10 | 7B | Oguchi et al., 20128 |
| 38725 | aNaBH4 | P4₂/nmc | 3.00×10-10 | 7B | Matsuo et al., 20124 |
| 1101862 |  | P4̅2₁c |  | 7B |  |
| 1190869 |  | Pnma |  | 7B |  |
| 1190586 |  | P4̅3m |  | 7B |  |
| 2646982 |  | Pnma |  | 7B |  |
| 976181 |  | F4̅3m |  | 7B |  |
| 24810 |  | Pnma |  | 7B |  |
| 23850 | NaNH2 | Fddd1 | 1.00×10-10 | 7H | Angelova et al., 20129 |
| 2646917 | NaCB9H10 | Pna2_1 | 8.00×10-5 | 7H | Tang et al., 201610 |
| 2646947 | NaCB11H12 | Pca2_1 | 4.00×10-6 | 7L | Tang et al., 201511 |
| 776332 | Na2B10H10 | P12₁/c1 | 2.00×10-7 | 7L | Udovic et al., 2014a12 |
| 978278 | Na2B12H12 | P12₁/c1 | 6.00×10-8 | 7L | Udovic et al., 2014b13 |
| 1020646 | Li2NaBP2O8 | P1̅ | 4.40×10-18 | 7M | Laskowski et al., 202314 |
| 16283 | KNa2Li3Fe2(Si2O5)6 | P6/mcc | 1.00×10-10 | 7N | Laskowski et al., 202314 |
| 6783 | NaLiSO4 | P31c | 8.80×10-10 | 7P | Laskowski et al., 202314 |
| 28542 | Na3ErCl6 | P12₁/c1 | 1.00×10-9 | 7S | Schlem et al., 202015 |
| 23363 | NaAlCl4 | P2_12̅_121̅ | 3.90×10-6 | 7S | Park et al., 202216 |
| 1078419 | Na3PSe4 | I4̅3m | 1.16×10-3 | 7U | Zhang et al., 201517 |
| 10167 | Na3SbS4 | I4̅3m | 1.10×10-3 | 7U | Xiong et al., 201818 |
| 8703 | Na3SbSe4 | I4̅3m | 8.50×10-4 | 7U | Xiong et al., 201818 |
| 29976 | Na3BS3 | C12/c1 | 3.70×10-10 | 7U | Tsuji et al., 202119 |
| 1193265 | Na3SbSe3 | P2_13̅ | 1.00×10-11 | 7U | Pompe and Pfitzner, 201220 |
| 4068 | Na2GeS3 | C12/c1 | 1.00×10-13 | 7U | Kassem et al., 202221 |
| 29143 | Na3VS4 | P4̅2₁c | 1.16×10-8 | 7U | He et al., 201922 |
| 29628 | Na4SnS4 | P4̅2₁c | 1.00×10-11 | 7U | Xiong et al., 202018 |
| 554395 | Na5Li4(TiS4)2 | C12/c1 | 8.80×10-6 | 7U | Laskowski et al., 202314 |
| 28782 | Na3PS4 | P4̅2₁c | 3.00×10-6 | 7V | Hayashi et al., 201223 |
| 985584 | Na3PS4 | I4̅3m | 4.60×10-4 | 7V | Hayashi et al., 201223 |
| 1193673 | Na3SbS3 | P2_13̅ | 3.00×10-9 | 7V | Pompe et al., 201324 |

Table S4. Summary on clustered groups.

| Group | Count | Average Ehull [meV/atom] | Average Eband gap [eV] | # of available data points | # of data points with conductivity > 10-5 S cm-1 |
| --- | --- | --- | --- | --- | --- |
| 1 | 56 | 11.1 | 2.32 | 4 | 0 |
| 2 | 226 | 68.9 | 2.02 |  |  |
| 3 | 101 | 61.2 | 3.36 |  |  |
| 4 | 211 | 45.0 | 2.96 |  |  |
| 5A | 166 | 30.9 | 3.19 | 3 | 3 |
| 5B | 1084 | 44.4 | 3.19 | 3 | 3 |
| 5C | 459 | 31.8 | 2.71 |  |  |
| 6 | 69 | 78.1 | 2.00 |  |  |
| 7A | 66 | 50.0 | 3.06 |  |  |
| 7B | 293 | 8.0 | 4.41 | 3* | 0 |
| 7C | 125 | 24.6 | 3.29 |  |  |
| 7D | 139 | 24.3 | 3.50 |  |  |
| 7E | 99 | 17.8 | 2.19 |  |  |
| 7F | 71 | 40.0 | 2.37 |  |  |
| 7G | 137 | 15.4 | 3.42 |  |  |
| 7H | 308 | 25.4 | 3.74 | 2 | 1 |
| 7I | 177 | 12.1 | 3.47 |  |  |
| 7J | 184 | 26.3 | 2.26 |  |  |
| 7K | 128 | 19.5 | 2.13 |  |  |
| 7L | 109 | 11.0 | 4.19 | 3 | 0 |
| 7M | 312 | 8.4 | 3.32 | 1 | 0 |
| 7N | 150 | 7.1 | 3.95 | 1 | 0 |
| 7O | 256 | 14.7 | 3.79 |  |  |
| 7P | 237 | 14.1 | 3.12 | 1 | 0 |
| 7Q | 272 | 13.5 | 2.80 |  |  |
| 7R | 282 | 26.3 | 1.94 |  |  |
| 7S | 84 | 7.5 | 3.16 | 1 | 0 |
| 7U | 71 | 14.7 | 2.39 | 9 | 3 |
| 7V | 203 | 8.6 | 1.68 | 3 | 1 |
| 8 | 112 | 10.3 | 1.33 |  |  |
| 9 | 310 | 26.9 | 2.64 |  |  |
| 10 | 410 | 53.8 | 2.73 |  |  |
| 11 | 133 | 65.8 | 2.56 |  |  |
| 12 | 73 | 68.8 | 2.98 |  |  |
| Noise | 90 | 35.7 | 2.01 |  |  |

Table S5. Representative materials of the clustered groups.

| Promising group |  | Materials |  |  |
| --- | --- | --- | --- | --- |
| 7B |  | NaBH4, NaAlH4, Na3AlH6, NaBF4, NaAlF4, Na3AlF6 |  |  |
| 7H |  | NaNH2, NaCB9H10, NaB3H4O7, Na3Ga7H12S13O6 |  |  |
| 7L |  | Na2B10H10, Na2B12H12, NaCB11H12*, Na3B5S9 |  |  |
| 7S |  | Na3ErCl6, NaGdCl4, Na2ZnBr4, NaSbCl6 |  |  |
| 7U |  | Na3PSe4, Na3SbS4, Na3SbSe4, Na3VS4, Na3BS3, Na6Ge2S7, Na4GeSe4, Na2PS3 |  |  |
| 7V |  | Na3PS4 (cubic), Na3PS4 (tetragonal), NaMgAs, NaLi2N, Na3SbS3, Na3BP2 |  |  |
| Group | Materials |  | Group | Materials |
| 1 | NaCl, Na2O, Na2S, Na3OCl, Na3OBr, Na4OI2 |  | 7J | Na2Mn3O7, Na4Ti5O12 |
| 2 | Na5FeP2(O4F)2, Na2Ti4O9 |  | 7K | NaErO2, Na2FeO3 |
| 3 | Na15Cr7N19, Na6GaP3, Na4CoO4 |  | 7M | NaGdH2S2O9, NaGe4(PO4)3 |
| 4 | Na6Mg7Zr(SO4)12, Na3Y(SiO3)3 |  | 7N | NaBePO4, Na4AlP2HO9 |
| 5A | Na3Zr2Si2PO12, NaZr2(PO4)3, Na3Sc2(PO4)3, Na3Hf2Si2PO12 |  | 7O | NaPO3, Na4Al3Si3NO14 |
| 5B | Na3Zr2Si2PO12, Na3Sc2(PO4)3, Na3Hf2Si2PO12, NaNbAl(PO4)3, |  | 7P | Na2SiO3, NaYGeO4 |
| 5C | NaMgSc(SO4)3, NaTa2Si2PO12 |  | 7Q | Na2TeO4, NaVO3 |
| 6 | Na2Y4Ti4Si3(S3O16)3 |  | 7R | Na5GaO4, Na6ZnO4 |
| 7A | NaGaH8(NF3)2, NaMg30MnO31* |  | 7T | NaHoS2, Na2ZrSe3, NaGdS2 |
| 7C | Na3TmCl6, NaCs2NdBr6 |  | 8 | Na2NiPCO7, Na3FePCO7 |
| 7D | NaCs2TlF6, NaRb2CoF6 |  | 9 | Na2Ca17V2(PO4)14, Na7Mg2Nb2Si3P3O24 |
| 7E | NaTaO3, NaBi2Sb3O11 |  | 10 | Na2Y3Nb5(PO4)12 |
| 7F | Na17(WO3)19, Na7(WO3)9 |  | 11 | Na14Sc4Si9Sn4S3O48 |
| 7G | NaBO2, Na3Sc(BO3)2 |  | 12 | Na2Zr3Zn5(SO4)12, Na2Ta5In3(PO4)12 |
| 7I | NaSc(SiO3)2, NaKZrSi3H4O11 |  | Noise | NaGe, Na3TiF8 |

Figure S4. MSD trajectories obtained from 1000K AIMD simulations.

Figure S5. MSD trajectories obtained from 800K AIMD simulations.

Figure S6. Dataset matrix after clustering. the entire descriptor matrix of which pixel is the relative descriptor value for corresponding material is visualized. In JarvisCFID, AC: average chemical, RCD: radial charge distribution, ADF1: angular distribution function up to 1st neighbor, ADF2: angular distribution function up to 2nd neighbor, DHA: dihedral angles, NN: nearest neighbors. (1) APF, BC, BF, LV, Na-ratio, LT, DF, EE, END, MPE, SG. (2) OS, SC, VO, YSS.

Table S6. Key descriptors of non-promising groups. ADF1: angular distribution function up to 1st neighbor, ADF2: angular distribution function up to 2nd neighbor.

| Descriptor | Gini importance |
| --- | --- |
| Group 1 |  |
| JarvisCFID-CAN40 Radial charge distribution | 1 |
| Group 2 |  |
| JarvisCFID-CAMN40 Dihedral angles | 0.768 |
| JarvisCFID-CAN40 ADF1 | 0.234 |
| Group 3 |  |
| JarvisCFID-CAN40/CAMN40 ADF1 | 0.997 |
| Group 4 |  |
| JarvisCFID-CAMN40 ADF1 | 0.486 |
| SC-original | 0.257 |
| SC-CAMN | 0.150 |
| SC-CAMN40 | 0.103 |
| Group 5C |  |
| Meredig-CAMN/CAMN40 #103 | 0.714 |
| JarvisCFID-CAN40/CAMN40 ADF1 | 0.286 |
| Group 6 |  |
| JarvisCFID-CAN40 ADF1 | 0.541 |
| JarvisCFID-CAN40 ADF2 | 0.458 |
| Group 7A |  |
| mXRD-A #257~261 | 0.692 |
| OFM-CAMN #84 | 0.297 |
| Group 7B |  |
| APE-original #4 | 0.218 |
| END-original #1 | 0.215 |
| APE-original #3 | 0.152 |
| mXRD (overall) | 0.142 |
| OFM-original #267 | 0.082 |
| OFM-original #1293 | 0.079 |
| Group 7C |  |
| SOAP-CAMN #10 | 0.906 |
| Group 7D |  |
| mXRD (overall) | 0.787 |
| Meredig-original #110 | 0.212 |
| Group 7E |  |
| mXRD (overall) | 0.883 |
| OFM-original #1292 | 0.117 |
| Group 7F |  |
| mXRD (overall) | 0.978 |
| Group 7G |  |
| Meredig-original #4~5 | 0.620 |
| JarvisCFID-CAMN40/CAN40 #1472 (Nearest neighbors) | 0.144 |
| OFM (overall) | 0.106 |
| Group 7HL |  |
| OFM-original #71 | 0.235 |
| OFM-original #1319 | 0.233 |
| OFM-original #227 | 0.162 |
| Meredig-original #105 | 0.153 |
| Meredig-original #4 | 0.053 |
| Group 7I |  |
| Meredig-original #13 | 0.534 |
| mXRD (overall) | 0.211 |
| OFM-CAMN/CAMN40 #1 | 0.119 |
| OFM-CAMN #34 | 0.098 |
| Group 7J |  |
| mXRD (overall) | 0.432 |
| OFM-original #1398 | 0.384 |
| OFM-original #1370 | 0.101 |
| Group 7K |  |
| mXRD (overall) | 0.817 |
| Density-CAMN #2 | 0.090 |
| Group 7M |  |
| mXRD-CAMN40 #78~83 | 0.404 |
| Meredig-original #14 | 0.325 |
| JarvisCFID-CAMN40 #839 | 0.175 |
| OFM-original #199 | 0.064 |
| Group 7N |  |
| RDF #40~43 | 0.512 |
| OFM-original #122 | 0.305 |
| JarvisCFID-CAN40/CAMN40 RDF | 0.101 |
| Group 7O |  |
| mXRD-A40/AM40 #241~246 | 0.574 |
| mXRD-CAN40/CAMN40 #60~74 | 0.365 |
| Group 7P |  |
| mXRD-CAN40/CAMN40 #257~266 | 0.604 |
| mXRD-A/AM #122~125 | 0.097 |
| Group 7Q |  |
| JarvisCFID-CAN40/CAMN40 #841 | 0.259 |
| OS-original #3 | 0.170 |
| OFM-original #696 | 0.167 |
| mXRD-A/AM #126~128 | 0.123 |
| Meredig-original #41 | 0.112 |
| Group 7R |  |
| SOAP-original #14 | 0.400 |
| SOAP-CAMN #14 | 0.239 |
| SOAP-original #8 | 0.087 |
| SOAP-CAMN #11 | 0.076 |
| Density-A #0,2 | 0.071 |
| Group 7S |  |
| Meredig-original #16,34 | 0.526 |
| OFM (overall) | 0.123 |
| JarvisCFID-CAN40 ADF | 0.077 |
| mXRD (overall) | 0.060 |
| Group 7T |  |
| mXRD (overall) | 0.801 |
| Density-CAMN #2 | 0.093 |
| OFM-A40 #1327 | 0.055 |
| OFM-A40 #40 | 0.052 |
| Group 8 |  |
| Meredig-original #5 | 0.376 |
| mXRD-original #32~33 | 0.351 |
| mXRD-A40 #68~87 | 0.242 |
| Group 9 |  |
| JarvisCFID-CAN40 ADF1 | 0.693 |
| RDF (overall) | 0.182 |
| SC (overall) | 0.125 |
| Group 10 |  |
| JarvisCFID-CAN40/CAMN40 ADF1 | 0.755 |
| JarvisCFID-CAN40/CAMN40 ADF2 | 0.244 |
| Group 11 |  |
| JarvisCFID-CAN40/CAMN40 ADF1 | 0.839 |
| RDF (overall) | 0.161 |
| Group 12 |  |
| RDF-A40 #82 | 0.632 |
| JarvisCFID-CAMN40 ADF1 | 0.124 |
| RDF-A40 #88 | 0.060 |

References

1.	Bertheville, B., Lovy, D., Bill, H. & Kubel, F. Ionic conductivity of Na2S single crystals between 295 and 1350 K experimental setup and first results. J. Phys. Chem. Solids 58, 1569–1577 (1997).

2.	Liu, Z., Hu, W. & Deng, H. Chemistry of Defects in Crystalline Na 2 Se: Implications for the Na–Se Battery. J. Phys. Chem. C 124, 27930–27936 (2020).

3.	Hooton, I. E. & Jacobs, P. W. M. Ionic conductivity of pure and doped sodium chloride crystals. Can. J. Chem. 66, 830–835 (1988).

4.	Matsuo, M. et al. Sodium ionic conduction in complex hydrides with [BH 4] - and [NH 2] - anions. Appl. Phys. Lett. 100, 2–6 (2012).

5.	Zhang, Z. et al. A Self‐Forming Composite Electrolyte for Solid‐State Sodium Battery with Ultralong Cycle Life. Adv. Energy Mater. 7, 1–11 (2017).

6.	Rettenwander, D. et al. Arrhenius Behavior of the Bulk Na-Ion Conductivity in Na 3 Sc 2 (PO 4 ) 3 Single Crystals Observed by Microcontact Impedance Spectroscopy. Chem. Mater. 30, 1776–1781 (2018).

7.	Zhu, Z., Chu, I. H. & Ong, S. P. Li3Y(PS4)2 and Li5PS4Cl2: New Lithium Superionic Conductors Predicted from Silver Thiophosphates using Efficiently Tiered Ab Initio Molecular Dynamics Simulations. Chem. Mater. 29, 2474–2484 (2017).

8.	Oguchi, H., Matsuo, M., Kuromoto, S., Kuwano, H. & Orimo, S. Sodium-ion conduction in complex hydrides NaAlH4 and Na3AlH6. J. Appl. Phys. 111, 4–7 (2012).

9.	Matsuo, M. et al. Sodium and magnesium ionic conduction in complex hydrides. J. Alloys Compd. 580, S98–S101 (2013).

10.	Tang, W. S. et al. Liquid-Like Ionic Conduction in Solid Lithium and Sodium Monocarba-closo-Decaborates Near or at Room Temperature. Adv. Energy Mater. 6, 1–6 (2016).

11.	Tang, W. S. et al. Unparalleled lithium and sodium superionic conduction in solid electrolytes with large monovalent cage-like anions. Energy Environ. Sci. 8, 3637–3645 (2015).

12.	Udovic, T. J. et al. Exceptional Superionic Conductivity in Disordered Sodium Decahydro- closo -decaborate. Adv. Mater. 26, 7622–7626 (2014).

13.	Udovic, T. J. et al. Sodium superionic conduction in Na 2 B 12 H 12. Chem. Commun. 50, 3750–3752 (2014).

14.	Laskowski, F. A. L., McHaffie, D. B. & See, K. A. Identification of potential solid-state Li-ion conductors with semi-supervised learning. Energy Environ. Sci. 16, 1264–1276 (2023).

15.	Schlem, R., Banik, A., Eckardt, M., Zobel, M. & Zeier, W. G. Na 3– x Er 1– x Zr x Cl 6 —A Halide-Based Fast Sodium-Ion Conductor with Vacancy-Driven Ionic Transport. ACS Appl. Energy Mater. 3, 10164–10173 (2020).

16.	Park, J. et al. NaAlCl 4 : New Halide Solid Electrolyte for 3 V Stable Cost-Effective All-Solid-State Na-Ion Batteries. ACS Energy Lett. 7, 3293–3301 (2022).

17.	Zhang, L. et al. Na3PSe4 : A Novel Chalcogenide Solid Electrolyte with High Ionic Conductivity. Adv. Energy Mater. 5, 1501294 (2015).

18.	Xiong, S. et al. Na3SbSe4−xS x as Sodium Superionic Conductors. Sci. Rep. 8, 9146 (2018).

19.	Tsuji, F. et al. Preparation and characterization of sodium-ion conductive Na 3 BS 3 glass and glass–ceramic electrolytes. Mater. Adv. 2, 1676–1682 (2021).

20.	Pompe, C. & Pfitzner, A. Na3SbSe3: Synthesis, crystal structure determination, raman spectroscopy, and ionic conductivity. Zeitschrift fur Anorg. und Allg. Chemie 638, 2158–2162 (2012).

21.	Kassem, M. et al. Deciphering Fast Ion Transport in Glasses: A Case Study of Sodium and Silver Vitreous Sulfides. Inorg. Chem. 61, 12870–12885 (2022).

22.	He, Y., Lu, F. & Kuang, X. Enhanced sodium ion conductivity in Na 3 VS 4 by P-doping. RSC Adv. 9, 39180–39186 (2019).

23.	Hayashi, A., Noi, K., Sakuda, A. & Tatsumisago, M. Superionic glass-ceramic electrolytes for room-temperature rechargeable sodium batteries. Nat. Commun. 3, 856 (2012).

24.	Pompe, C. & Pfitzner, A. Na 3 SbS 3 : Single Crystal X‐ray Diffraction, Raman Spectroscopy, and Impedance Measurements. Zeitschrift für Anorg. und Allg. Chemie 639, 296–300 (2013).