Supporting Information

Prediction of higher thermoelectric performance in BiOCuSe by weakening electron-polar optical phonon scattering

Tianqi Zhao*,1, Quinn D. Gibson2, Luke M. Daniels2, Ben Slater1, Furio Corà*,1

1Department of Chemistry, University College London, Gower Street, London, WC1E 6BT, United Kingdom

2Department of Chemistry, University of Liverpool, Crown Street, Liverpool, L69 7ZD, United Kingdom

*Corresponding author: E-mail address: tianqi.zhao@ucl.ac.uk (T. Zhao), f.cora@ucl.ac.uk (F. Corà)

Supplementary Figures

Supplementary Figure 1 | Lattice thermal conductivity of BiOCuSe as reproduced from literature,1 which is used to calculate thermoelectric figure of merit ZT of BiOCuSe in this work.

Supplementary Figure 2 | The variation of thermoelectric charge transport properties with carrier concentration. The calculated results as compared to that by excluding PF with frequency > 200 cm-1 of (a) Seebeck coefficient, (b) electrical conductivity, (c) electrical thermal conductivity. The calculated results as compared to that by excluding PF with frequency < 200 cm-1 of (d) Seebeck coefficient, (e) electrical conductivity, (f) electrical thermal conductivity.

Supplementary Figure 3 | The variation of (a) power factor and (b) ZT of BiOCuSe as a function of carrier concentration and temperature after excluding the scattering effects of PO phonon with frequency > 200 cm-1. The variation of (c) power factor and (d) ZT of BiOCuSe as a function of carrier concentration and temperature after excluding the scattering effects of PO phonon with frequency < 200 cm-1.

Supplementary Tables

| Supplementary Table 1 ¦ Longitudinal optic phonon frequencies of BiOCuSe in cm-1 |  |  |  |
| --- | --- | --- | --- |
| LO Modes | This work | Literature2 | Experiment3 |
| Eu | 56.2 | 61.2 |  |
| A2u | 91.4 | 89.4 | 92.0 |
| Eu | 135.9 | 142.7 |  |
| A2u | 175.2 | 178.6 |  |
| Eu | 341.9 | 347.7 |  |
| A2u | 472.9 | 473.7 | 475.0 |

| Supplementary Table 2 ¦ Born effective charge of BiOCuSe |  |  |  |
| --- | --- | --- | --- |
|  |  | This work | Literature2 |
| ZBi* | In plane | 6.50 | 6.46 |
|  | Out of plane | 5.94 | 5.93 |
| ZO* | In plane | -4.28 | -4.28 |
|  | Out of plane | -4.36 | -4.42 |
| ZCu* | In plane | 1.46 | 1.44 |
|  | Out of plane | 1.09 | 1.06 |
| ZSe* | In plane | -3.67 | -3.67 |
|  | Out of plane | -2.67 | -2.70 |
| k∞ | In plane | 17.61 | 18.01 |
|  | Out of plane | 13.25 | 13.79 |

Supplementary References

1.	Ren, G. K. et al. Enhanced thermoelectric properties in Pb-doped BiCuSeO oxyselenides prepared by ultrafast synthesis. RSC Adv. 5, 69878–69885 (2015).

2.	Saha, S. K. Exploring the origin of ultralow thermal conductivity in layered BiOCuSe. Phys. Rev. B 92, 041202 (2015).

3.	Berdonosov, P. S. Powder X-Ray and IR Studies of the New Oxyselenides MOCuSe (M = Bi, Gd, Dy). J. Solid State Chem. 118, 74 (1995).