Supplementary Information

Title: Toxicological inhalation studies in to substantiate grouping of zinc oxide nanoforms

Additional File 1

Additional file 1 includes the following information:

- Additional method description of test item characterization

  - Transmission Electron Microscopy (TEM)

  - Dissolution in Continuous Flow System (CFS)

- Table S1: Physicochemical properties of the test items

# Transmission Electron Microscopy (TEM)

A tip of a spatula of material was dispersed in 5 mL of ethanol. The dispersion was treated for 5 min in an ultrasonic bath. 5 drops of the dispersion were applied between two glass slides in order to create a thin liquid film. A carbon coated TEM grid was dipped onto the film to transfer the particles to the TEM substrate.

The TEM samples were analyzed using a Tecnai Osiris machine (Thermo-Fisher) operated at 200 keV under bright-field (BF) conditions (Spotsize; 100 µm condenser aperture; 20 µm objective aperture). ~10 images per sample were taken using a Gatan 1000XP 2K CCD camera with an acquisition time of 2s at magnifications of 13500x and 26500x.

The particle size was evaluated using the free ParticleSizer plugin for “imageJ” developed and validated within the EC FP7 project NanoDefine.(1, 2). Automated evaluation is faster, reproducible and limits operator bias to a minimum compared to manual image analysis. We carefully checked that the settings of the Particle Sizer Plugin (1) are robust for the ZnO materials.

# Dissolution in Continuous Flow System (CFS)

The flow-through setup was described in detail by several publications as an implementation of a CFS according to ISO TR 19057 (3-5). A ZnO mass of M0 = 1 mg was weighed onto a membrane (cellulose triacetate, Sartorius Stedim Biotech GmbH, Goettingen, Germany: 47 mm diameter, 5 kDa pore size), topped by another membrane, and enclosed in flowthrough cells. The flow through cells at 37 ± 0.5 °C were kept upright to ensure that emerging air bubbles can leave the system and do not accumulate within the cell. The flow rate (V) was 48 mL/d; this corresponds to a ratio, SA/V around 0.02 h/cm, which was independently found to lead to correct predictions (6). The PSF medium – previously validated by US-NIOSH for the purpose of particle dissolution (7) and recommended by the ISO 19057 (3) - was employed to simulate the lysosomal compartment at pH 4.5 (4). The programmable sampler drew 10 mL eluates twice per day. These were stabilized by 0.1N HNO3 and analyzed by ICP-MS (Perkin Elmer Nexion 2000b).

All ZnO materials dissolved in the lysosomal pH 4.5 conditions with half-times of less than 1 day. The dissolution kinetics were overall compatible with mono-exponential decays, but the hydrophobic coating resulted in a delayed onset of dissolution with a few hours delay against the uncoated nanoform. The fitted halftime can be converted to a dissolution rate kmin. To complement the evaluation, we also determined from the same data set the highest observed dissolution rate in a single sampling interval, kmax. Only for perfectly exponential kinetics the two evaluation approaches would match perfectly.

Table S1: Physicochemical properties of test items

|  | Size and shape measured by TEM |  |  | Shape (TEM) | Specific Surface Area (BET) | Surface modification | Dissolution measured by CFS |  |  | Crystallinity/ impurities/ purity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Diameter D50 | Aspect ratio AR50 | Aspect ratio AR90 |  |  |  | kmax | Fitted halftime from exponential decay | kmin calculated from halftime |  |
|  | nm | unitless | unitless | descriptive | m2/g |  |  | days | ng/cm²/h | % |
| uZnO | 18.2 | 1.3 | 1.7 | spheroidal | 10 | None | 323 | 0.19 | 378 | 98.2 (ZnO) Loss on drying 1.0 Loss on ignition 1.5 |
| cZnO | 18.3 | 1.3 | 1.7 | spheroidal | 10 | Coated | 246 | 0.74 | 97.5 | 93.8 (ZnO) Loss on drying 0.3 Loss on ignition 1.8 |
| µZnO | n.d. | n.d. | n.d. | n.d. | 4.48 | None | n.d. | n.d. | n.d. | 99.8 (ZnO) |
| ZnSO4 | 1080 | n.d. | n.d. | n.d. | n.d. | - | n.d. | n.d. | n.d. | 36.2 (Zn) |

n.d. = not determined

# REFERENCES

1.	Verleysen E, Wagner T, Lipinski H-G, Kägi R, Koeber R, Boix-Sanfeliu A, et al. Evaluation of a TEM based Approach for Size Measurement of Particulate (Nano) materials. Materials. 2019;12(14):2274.

2.	Mech A, Rauscher H, Rasmussen K, Babick F, Hodoroaba V-D, Ghanem A, et al. The NanoDefine Methods Manual. 2020.

3.	ISO/TR19057. Nanotechnologies — Use and application of acellular in vitro tests and methodologies to assess nanomaterial biodurability. ISO/TR. 2017;19057.

4.	Zanoni I, Keller J, Sauer UG, Mueller P, Ma-Hock L, Jensen K, et al. Dissolution Rate of Nanomaterials Determined by Ions and Particle Size under Lysosomal Conditions: Contributions to Standardization of Simulant Fluids and Analytical Methods. Chem Res Toxicol. 2022;35(6):963-80.

5.	Keller JG, Graham UM, Koltermann-Jülly J, Gelein R, Ma-Hock L, Landsiedel R, et al. Predicting dissolution and transformation of inhaled nanoparticles in the lung using abiotic flow cells: The case of barium sulfate. Scientific Reports. 2020;10(1):458.

6.	Keller JG, Peijnenburg W, Werle K, Landsiedel R, Wohlleben W. Understanding Dissolution Rates via Continuous Flow Systems with Physiologically Relevant Metal Ion Saturation in Lysosome. Nanomaterials. 2020;10(2):311.

7.	Stefaniak AB, Guilmette RA, Day GA, Hoover MD, Breysse PN, Scripsick RC. Characterization of phagolysosomal simulant fluid for study of beryllium aerosol particle dissolution. Toxicology in Vitro. 2005;19(1):123-34.