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Table S1. Silver concentration as measured by ICP-MS; error bars represent ± one standard deviation about the mean.

	Mask
	1
	2
	3
	4
	5
	6
	7
	8
	9
	10

	
	Silver detected in solution (mg metal/mL solution)

	1 hr DI water
	n.d
	5.81E-03
	±
	1.25E-04
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d

	1 Detergent Cycle
	n.d
	9.00E-03
	±
	4.30E-04
	n.d
	n.d
	n.d
	n.d
	n.d
	5.32E-03
	±
	1.64E-05
	n.d
	n.d

	10 Detergent Cycles
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	9.32E-04
	±
	8.83E-05
	n.d
	n.d

	Saliva F-1 hr
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d

	Saliva F-8 hr
	n.d
	8.91E-05
	±
	5.96E-05
	n.d
	n.d
	2.83E-04
	±
	4.08E-05
	n.d
	n.d
	3.16E-04
	±
	2.38E-05
	n.d
	n.d

	Saliva A-1 hr
	n.d
	1.55E-03
	±
	5.96E-05
	n.d
	n.d
	n.d
	n.d
	n.d
	7.58E-04
	±
	2.38E-05
	n.d
	n.d

	Saliva A-8 hr
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d
	n.d

	
	Silver detected in digested mask (mg/mask)

	As Received
	n.d
	0.236
	±
	0.00263133
	n.d
	1.905
	±
	0.010
	0.429
	±
	0.008
	n.d
	n.d
	105.4
	±
	0.5
	n.d
	n.d

	1 hr DI Water
	n.d
	n.d
	n.d
	1.796
	±
	0.010
	0.429
	±
	0.005
	n.d
	n.d
	103.3
	±
	1.6
	n.d
	n.d

	1 Detergent Cycle
	n.d
	n.d
	n.d
	1.761
	±
	0.02596
	0.353
	±
	0.006
	n.d
	n.d
	61.4
	±
	0.2
	n.d
	n.d

	10 Detergent Cycles
	n.d
	n.d
	n.d
	1.869
	±
	0.020
	0.286
	±
	0.003
	n.d
	n.d
	44.9
	±
	0.4
	n.d
	n.d

	Saliva A - 8 hr
	n.d
	n.d
	n.d
	2.090
	±
	0.0451
	0.414
	±
	0.004
	n.d
	n.d
	61.3
	±
	0.8
	n.d
	n.d

	Saliva F - 8 hr
	n.d
	0.156
	±
	0.00155029
	n.d
	1.880
	±
	0.02221
	0.347
	±
	0.003
	n.d
	n.d
	43.1
	±
	0.7
	n.d
	n.d
















Table S2: Copper concentration as measured by ICP-MS; error bars represent ± one standard deviation about the mean.

	Mask
	1
	2
	3
	4
	5
	6
	7
	8
	9
	10

	
	Copper detected in solution (mg Metal/mL solution)

	1 hr DI Water
	3.48E-03
	±
	1.98E-04
	3.53E-03
	±
	6.02E-05
	n.d
	3.13E-02
	±
	1.10E-03
	n.d
	n.d
	n.d
	n.d
	2.90E-03
	±
	1.97E-04
	n.d

	1 Det Cycle
	1.01E-02
	±
	2.64E-04
	7.26E-03
	±
	3.43E-04
	n.d
	5.74E-02
	±
	6.16E-04
	n.d
	n.d
	n.d
	n.d
	6.07E-02
	±
	3.41E-04
	n.d

	10 Det Cycles
	n.d
	n.d
	n.d
	2.97E-03
	±
	1.29E-04
	n.d
	n.d
	n.d
	n.d
	3.58E-03
	±
	2.79E-04
	n.d

	Saliva F - 1 hr
	4.48E-03
	±
	1.22E-04
	n.d
	n.d
	2.23E-02
	±
	4.73E-04
	n.d
	n.d
	n.d
	n.d
	
	n.d
	
	n.d

	Saliva F - 8 hr
	n.d
	n.d
	n.d
	3.10E-02
	±
	2.47E-03
	n.d
	n.d
	n.d
	n.d
	6.36E-03
	±
	2.16E-04
	n.d

	Saliva A - 1 hr
	n.d
	n.d
	n.d
	5.23E-03
	±
	1.01E-04
	n.d
	n.d
	n.d
	n.d
	9.22E-03
	±
	2.10E-04
	n.d

	Saliva A - 8 hr
	n.d
	n.d
	n.d
	1.54E-02
	±
	2.04E-04
	n.d
	n.d
	n.d
	n.d
	4.77E-02
	±
	2.63E-04
	n.d

	
	Copper detected in digested mask (mg/mask)

	As Received
	12.62
	±
	0.22
	1.29
	±
	0.04
	n.d
	13.31
	±
	0.07
	n.d
	1.44
	±
	0.04
	n.d
	n.d
	8.34
	±
	0.05
	n.d

	1 hr DI Water
	11.27
	±
	0.16
	0.62
	±
	0.01
	n.d
	7.89
	±
	0.05
	n.d
	1.23
	±
	0.02
	n.d
	n.d
	4.70
	±
	0.07
	n.d

	1 Det Cycle
	8.24
	±
	0.09
	n.d
	n.d
	9.13
	±
	0.03
	n.d
	1.33
	±
	0.03
	n.d
	n.d
	7.70
	±
	0.15
	n.d

	10 Det Cycles
	12.02
	±
	0.09
	n.d
	n.d
	5.68
	±
	0.05
	n.d
	1.42
	±
	0.01
	n.d
	n.d
	2.94
	±
	0.02
	n.d

	Saliva A - 8 hr
	12.48
	±
	0.38
	0.77
	±
	0.02
	n.d
	8.10
	±
	0.06
	n.d
	1.44
	±
	0.01
	n.d
	n.d
	6.80
	±
	0.08
	n.d

	Saliva F - 8 hr
	9.91
	±
	0.13
	1.30
	±
	0.04
	n.d
	11.25
	±
	0.41
	n.d
	1.35
	±
	0.03
	n.d
	n.d
	7.57
	±
	0.04
	n.d












[image: Chart

Description automatically generated with medium confidence]



Figure S1. UV-Vis spectra of as-used (pure) soak solutions including diluted detergent for wash cycles, DI water for rinse, and both artificial saliva solutions.
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a. DI water soak
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b. 1st Detergent cycle soak
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c. 10th Detergent cycles soak
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d. Artificial Saliva A soak before washing 
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e. Artificial Saliva F soak before washing 
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f. Artificial Saliva F soak after 1st wash cycle
        c
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g. Artificial Saliva F soak after 10th wash cycle 

Figure S2. UV-Vis spectra of solutions post mask-exposure sorted by treatment. 
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