Supplementary Information

Figure S1. Diffractograms of samples in group1-blue (see manuscript).

Figure S2. Diffractograms of samples in group2-red (see manuscript).

Figure S3. Diffractograms of samples in group3-green (see manuscript).

Figure S4. Diffractograms of samples in group4-grey (see manuscript).

Table S1. Terms used in the Elamite language to designate different bricks

| Period | Mudbrick terms | Baked brick terms | Glazed brick terms | Siliceous bricks |
| --- | --- | --- | --- | --- |
| Old Elam | - | erientumimma | - | - |
| Middle Elam-I (1400-1200 BCE) | - | upat hussipme | upqumimma, ubqumiya | akti |
| Middle Elam-II (1200-1100 BCE) | Halatimma, halatni | upatimma, erientum-ia, erientumma | upat aktiya kuramma karrah | upat aktini |

Table S2. Chemical composition of the samples (wt%) determined by EPMA. Values are averages of 5-10 single measurements (with standard deviation in parenthesis).

| sample number | sample name | Na2O | MgO | Al2O3 | Si2O | CaO | P2O5 | K2O | TiO2 | Fe2O3 | Petrographic fabric | MgO+CaO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | CZT-4012 | 1.32 (0.46) | 5.04 (1.13) | 9.93 (1.14) | 43.84 (3.9) | 14.70 (1.45) | 0.39 (0.08) | 0.81 (0.38) | 0.57 (0.2) | 1.77 (0.8) | NS | 12.88 |
| 2 | CZT-4011 | 0.92 (0.36) | 5.03 (1.07) | 8.84 (1.64) | 39.71 (4.64) | 20.61 (2.78) | 0.64 (0.32) | 1.03 (0.35) | 0.47 (0.12) | 1.58 (0.81) | Voids-Plant matter fabric | 25.64 |
| 3 | CZT-4005 | 3.01 (1.22) | 4.05 (1.03) | 11.83 (4.07) | 56.21 (11.5) | 8.83 (4.08) | 0.32 (0.14) | 1.87 (1.21) | 0.71 (0.91) | 1.89 (2.72) | NS | 12.88 |
| 4 | CZT-4013 | 1.29 (0.92 | 2.11 (0.73) | 2.44 (0.29) | 85.50 (6.83) | 4.74 (5.02) | 0.12 (0.20) | 0.68 (0.10) | 0.17 (0.01) | 0.68 (0.65) | Quartz-based fabric | 6.85 |
| 5 | CZT-4001 | 1.13 (0.81) | 5.06 (2.64) | 9.35 (3.85) | 53.14 (14.8) | 9.52 (4.54) | 0.37 (0.19) | 1.61 (1.06) | 0.61 (0.28) | 1.87 (3.15) | NS | 14.58 |
| 6 | CZT-4004 | 1.47 (0.58) | 5.12 (1.99) | 10.14 (1.97) | 41.19 (7.38) | 15.71 (4.61) | 0.48 (0.15) | 1.55 (0.78) | 0.53 (0.27) | 1.83 (1.42) | Voids-Plant matter fabric | 20.83 |
| 7 | CZT-4002 | 1.13 (0.75) | 5.22 (1.81) | 9.68 (1.46) | 42.44 (7.18) | 18.70 (6.44) | 0.50 (0.12) | 1.41 (1.16) | 0.65 (0.35) | 1.83 (1.28) | Voids-Plant matter fabric | 23.92 |
| 8 | CZT-4010 | 0.80 (0.31) | 5.54 (0.65) | 10.63 (1.75) | 39.02 (4.18) | 19.38 (3.35) | 0.56 (0.10) | 1.46 (0.85) | 0.52 (0.09) | 1.76 (0.90) | Voids-Plant matter fabric | 24.92 |
| 9 | CZT-4006 | 13.10 (1.37) | 2.92 (0.72) | 1.25 (1.53) | 66.87 (3.41) | 5.33 (0.72) | 0.28 (0.12) | 3.12 (0.11) | 0.054 (0.07) | 0.26 (1.02) | Quartz-based fabric | 8.25 |
| 10 | CZT-4009 | 1.94 (0.55) | 5.47 (0.61) | 9.90 (0.67) | 38.79 (3.94) | 18.96 (22.8) | 0.80 (0.22) | 0.85 (0.34) | 0.71 (0.22) | 1.70 (0.46) | NS | 24.43 |
| 11 | CZT-4014 | 1.45 (1.13) | 6.00 (1.61) | 9.60 (2.37) | 40.27 (6.86) | 17.23 (5.93) | 0.84 (0.34) | 1.14 (0.75) | 0.81 (0.82) | 1.64 (1.14) | NS | 23.23 |
| 12 | HT-1016 | 0.81 (0.25) | 3.18 (0.74) | 7.14 (0.63) | 33.31 (9.83) | 29.80 (6.71) | 0.75 (0.21) | 0.76 (0.25) | 0.59 (0.60) | 1.13 (1.04) | Calcareous fabric | 32.98 |
| 13 | HT-1001 | 1.73 (0.77) | 2.77 (0.30) | 8.97 (1.33) | 35.33 (4.97) | 21.39 (5.35) | 0.65 (0.23) | 1.95 (0.35) | 0.60 (0.43) | 1.44 (0.72) | Calcareous fabric | 24.16 |
| 14 | J-2505 | 2.97 (0.92) | 3.99 (1.28) | 9.85 (2.96) | 49.20 (9.19) | 12.92 (4.25) | 0.39 (0.10) | 1.75 (1.43) | 0.58 (0.29) | 1.82 (0.76) | NS | 16.91 |
| 15 | J-7009 | 1.13 (0.62) | 3.53 (0.57) | 10.18 (2.16) | 42.39 (9.85) | 17.22 (4.46) | 0.46 (0.16) | 2.02 (0.49) | 0.56 (0.19) | 1.62 (0.87) | Voids-Plant matter fabric | 20.75 |
| 16 | J-2001 | 1.24 (0.55) | 4.23 (0.90) | 11.37 (0.92) | 35.48 (4.15) | 21.14 (2.13) | 0.64 (0.17) | 2.39 (0.45) | 0.46 (0.06) | 1.68 (0.51) | NS | 25.37 |
| 17 | J-2005 | 3.22 (0.23) | 9.59 (0.87) | 9.90 (0.49) | 34.51 (1.91) | 11.24 (1.05) | 0.46 (0.14) | 1.24 (0.43) | 0.42 (0.02) | 1.58 (0.61) | NS | 20.83 |
| 18 | J-7008 | 1.52 (0.57) | 2.74 (2.42) | 11.94 (5.67) | 44.22 (16.0) | 16.93 (13.3) | 0.39 (0.23) | 4.65 (6.62) | 0.35 (0.31) | 1.13 (2.94) | NS | 19.67 |
| 19 | J-2607 | 1.91 (0.58) | 4.55 (1.84) | 10.37 (0.74) | 37.80 (2.83) | 17.75 (3.73) | 0.51 (0.14) | 1.76 (0.20) | 0.52 (0.15) | 1.86 (1.62) | NS | 22.30 |
| 20 | J-2501 | 3.60 (0.52) | 3.57 (0.63) | 10.34 (1.49) | 49.35 (6.16) | 10.61 (1.24) | 0.45 (0.08) | 1.46 (0.29) | 0.62 (0.18) | 1.63 (0.48) | NS | 14.18 |
| 21 | J-2004 | 0.80 (0.18) | 3.57 (0.81) | 10.37 (2.75) | 51.85 (11.2) | 11.06 (3.12) | 0.41 (0.22) | 2.76 (1.12) | 0.74 (0.50) | 1.67 (1.11) | NS | 14.63 |

Figure S5. SEM-AsB image of altered glass and calcium carbonate zones in sample J-2003, and the EDS result of each spectrum.

Table S3. Chemical composition of the points indicated in Figure S5 determined by EDX-SEM (wt%).

| Element |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | O | C | Si | Al | Na | K | Mg | Ca | S | Fe | Total |
| Point 1 (Ca carbonate) | 45.2 | 15.9 | 0.6 | - | - | - | 0.5 | 37.2 | 0.6 |  | 100 |
| Point 2 | 46.3 | - | 46.8 | 1.6 | - | 1.0 | 0.6 | 1.8 | - | 0.9 | 100 |
| Point 3 | 49.8 | - | 41.0 | 1.4 | 0.4 | 1.3 | 0.5 | 4.0 | - | 1.0 | 100 |
| Point 4 | 56.0 | - | 37.8 | 1.9 | - | 1.7 |  | 1.7 | - | 0.9 | 100 |

Not Studied