Supplementary Information

# One-pot microfluidic fabrication of micro ceramic particles

Chenchen Zhou1,2, Shuaishuai Liang3, Bin Qi3, Chenxu Liu2, Nam-Joon Cho1,*

1School of Materials Science and Engineering, Nanyang Technological University, 639798 Singapore, Singapore

2Department of Mechanical Engineering, Tsinghua University, Beijing 100084, P.R. China

3School of Mechanical Engineering, University of Science and Technology Beijing, Beijing 100083, P.R. China

# Table of Contents

S1 “Groove & tongue” assembling for gear-shaped MC fabrication	5

S2 Rheological test	9

S3 Sliding assembling for MCs fabrication	10

S4 Characterizations of MP green bodies	12

S5 Scratch tests	17

S6 Characterization of MP’s corner	20

S7 Assessment of our OPMF system	21

References	24

# S1 “Groove & tongue” assembling for gear-shaped MC fabrication

The standard parameters of micro gear are selected as follows: module m = 0.1, pitch diameter d = 1 mm, outer diameter Do = 1.2 mm, root diameter Dr = 0.75 mm. The cross-section area ag and length of the gear outer contour lg are calculated as 0.7557 mm2 and 6.1370 mm, respectively. The assembled MC is divided into ten pieces, according to which a convex metal mold is designed (Supplementary Fig. 1a). To ensure the precision of the MC fabrication, a reverse molding strategy (Supplementary Fig. 2) is presented. An additional concave PDMS reverse mold demolded from the metal mold serves as an intermediary MC features transferer (Supplementary Fig. 1b), which is to ensure the convex feature of the initial machined metal mold so as to get rid of influences from the non-negligible diameter of machining wires as much as possible, therefore avoiding the rounded features in PDMS substrate that will lead to wedge-shaped channel conners consequently. The obtained MC substrate is cut into ten pieces (Supplementary Figs. 1c,d,3a). The partially enlarged views of a single MC piece (Supplementary Fig. 1e) schematically show an intact contour of a gear tooth and intermediate groove and tongue. The separated MC pieces are assembled one by one and finally form an MC with a closed gear-shaped cross-section (Supplementary Figs. 1f−h). The outer contour of MC is a regular decagon, and the distance between MC’s inner surface and outer surface is too thick for efficient heat transfer. Thus, the peripheral part of MC is cut to form a square outer shape, and the scratches caused by the cutting process are eliminated by coating a thin layer of PDMS, therefore, the top view of the straight gear-shaped MC can be observed (Supplementary Fig. 3b).

## Supplementary Fig. 1 | Fabrication of gear-shaped MCs based on precise “groove & tongue” assembling. a, Liquid PDMS prepolymer was cast and fully cured over the metal mold with designed structures. b, PDMS reverse mold was peeled off and coated with the releasing agent, followed by casting and half-curing of the new batch of PDMS prepolymer. c, MC substrate was demolded and cut into pieces. d, The split MC piece each has an entire profile of e-i, one gear tooth on the tip and e-ii, groove & tongue structures at the side walls. f, The split MC pieces were assembled subsequently and fully cured to form g, a closed MC with h, a gear-shaped cross-section.

## Supplementary Fig. 2 | Comparison between traditional direct molding and novel reverse molding strategies for gear-shaped MCs fabrication. a, Traditional direct molding: The concave edge of the wire-cut metal mold is roundly shaped with a corner radius that equals the wire’s radius instead of being sharp, which causes wedge-shaped defects in the channel. b, Novel reverse molding: An additional PDMS reverse mold is introduced as an intermediary MC features transferer to remove the influences from the non-negligible thickness of the machining wire to the utmost extent. Once the cutting wire meets the convex edges, two spare moving distances are additionally incorporated into the processing path of the wire. The wire trace is denoted as the red dotted line with an arrow. The sharpness of the convex edge is well-defined, contributing to fabricating assembled MCs with high precision.

## Supplementary Fig. 3 | Structural characterizations of the gear-shaped MC. a, Optical image of the precisely assembled gear-shaped MC substrate after cutting the thin layer of PDMS joints between adjacent pieces. b, Optical image of the gear-shaped MC from the top view. The gear-shaped MCs were first peeled peripherally to form a square outer shape, and then the peeling scratches were smoothed by applying a thin layer of PDMS coating.

# S2 Rheological test

The modulus variation of the mixing precursor as temperature increases is imitated in a rheometer set-up with constant humidity (Supplementary Fig. 4). BS is initially filled in the gap between the spindle bottom and the substrate base. The temperature of this set-up is raised from 20 to 70 ℃ at a rate of 6.49 ℃/min. Proportionate CS is added into BS at room temperature (RT, 25 ℃).

## Supplementary Fig. 4 | Rheological measurement setup. Modulus change of the precursor is imitated and monitored  during the curing process inside MC.

# S3 Sliding assembling for MCs fabrication

## Supplementary Fig. 5 | Fabrication of triangular MCs based on sliding assembling. a, Liquid PDMS prepolymer was cast and fully cured over the metal mold with designed structures. b, PDMS reverse mold was peeled off and coated with the releasing agent, followed by casting and half-curing of the new batch of PDMS prepolymer. c, MC substrate was demolded and cut into pieces along the seams. d, The split MC pieces were assembled and fully cured to form g, a closed MC with f, a regular triangular cross-section.

## Supplementary Fig. 6 | Schematic illustrations of the intact map for square MC sliding assembling. The cross-sections of MC transform through tuning the sliding distance s1 and s2.

# S4 Characterizations of MP green bodies

The compositions and structures of the obtained MP green bodies and a pure polyacrylamide (PAM) control sample are characterized by Fourier transform infrared (FTIR) spectroscopy (Supplementary Fig. 7). The absorption peaks at 3348 and 3190 cm-1 are attributed to the asymmetric and symmetric stretching vibration of −NH2 groups, respectively. The absorption peak at 2924 cm-1 is associated with the stretching vibration of −CH2 groups included in macromolecular chains and crosslinking bridges, while 2853 cm-1 is assigned to −N−CH2− bonds from the crosslinking bridges. The absorption peak associated with the stretching vibration of C=O red shifts (from ~1700 to 1647 cm-1) due to the conjugation effect with −NH2 and −NH− groups1. Deformation vibrations corresponding to −NH− appear at 1536 cm-1 2. The absorption peak at 1448 cm-1 is for −CH2− bending vibration1. These FT-IR analysis results indicate the major functional groups of PAM are detected, while the intensity of the individual absorption peak varies with the sample species. The absorption peaks of SiO2+PAM samples at 1050 and 794 cm-1 are detected to be assigned to the asymmetric and symmetric stretching vibration of Si−O−Si, respectively3. For Al2O3+PAM samples, the absorption peak at 713 cm-1 is assigned to Al–O stretching mode in tetrahedron4. The absorption band of Si3N4+PAM samples, assigned to Si−N stretching vibration, centers at 852 cm-1 5.

XPS is further used to characterize the compositions of MP green bodies (Supplementary Fig. 8). The broad-spectrum scan reveals the elemental compositions of all the samples. Compared with pure PAM, SiO2+PAM and Al2O3+PAM have additional Si and Al elements, respectively, while the Si3N4+PAM sample not only has Si but also contains Al and Y elements, which come from the sintering aids. The peaks from high-resolution XPS spectra of each element at different binding energies correspond to the characteristic compositions of samples. The superimposed curve from three individual intensity peaks corresponding to C−C, C−N, and N−C=O aligns well with the signal spectrum curve. Similarly, the characteristic peaks of CONH2 and N−C−N can also be split from the spectrum of N 1s. Notably, another peak at 397.1 eV is detected in the Si3N4+PAM sample, which is assigned to compound Si3N4. In O 1s spectrum, the peaks at binding energy of 533.0, 531.3, and 531.1 eV are attributed to SiO2, Al2O3, and Al2O3, respectively in SiO2+PAM, Al2O3+PAM, and Si3N4+PAM samples, and Si 2p, Al 2p, Si 2p XPS tests show the characteristic peaks corresponding to SiO2, Al2O3, and Si3N4 in these samples. Peaks for sintering additive Y2O3 are detected in Y 3d and 3p spectra, while Al2O3 is testified in Al 2p spectrum.

The EDX mapping images of three MP green body samples show that the compositional elements of each sample are well-mixed and distributed uniformly (Supplementary Fig. 9), indicating the homogeneous mixing effect of our OPMF system.

## Supplementary Fig. 7 | FTIR spectra for composition identification of SiO2/Al2O3/Si3N4 MP green bodies. A pure PAM sample is compared here as a control sample.

## Supplementary Fig. 8 | XPS spectra for composition identification of SiO2/Al2O3/Si3N4 MP green bodies. a, full scan, b, C 1s, c, N 1s, d, O 1s, e, other typical elemental XPS spectra of different samples. A pure PAM sample is compared here as a control sample.

## Supplementary Fig. 9 | EDX mapping results showing the individual channels for specific elements distribution. a, SiO2, b, Al2O3 and c, Si3N4 MP green bodies’s surface.

# S5 Scratch tests

Scratches from the MPs of S-Al2O3, T/S-SiO2, and T/S-Si3N4 are characterized in a similar way as the Scratches caused by T-Al2O3 MPs (Supplementary Figs. 10−12).

## Supplementary Fig. 10 | Scratch test results of star-shaped Al2O3 MPs on substrates made of different materials, including Cu, Al, PS, PMMA, and wood.

## Supplementary Fig. 11 | Scratch test results of isosceles triangular and star-shaped SiO2 MPs on substrates made of different materials, including Cu, Al, PS, PMMA, and wood.

## Supplementary Fig. 12 | Scratch test results of isosceles triangular and star-shaped Si3N4 MPs on substrates made of different materials, including Cu, Al, PS, PMMA, and wood.

# S6 Characterization of MP’s corner

## Supplementary Fig. 13 | SEM images of a, triangular and b, star-shaped Al2O3 MPs’ corners. The edge radiuses are about 4.78 and 1.32 μm, respectively.

# S7 Assessment of our OPMF system

## Supplementary Table 1 | Literature investigations on various methods for microtools manufacture have been reported so far.

| Method | Dc (μm) | L (μm) | Cross-section shape | N | Processing rate (μm3/min) | Precision (μm) | Material | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| µWEDM | 100 | 100 | D shape | 2 | 8726.64626 | Ra 0.06, Rz 0.1, Rmax 0.3 | WC | 20046 |
| µWEDM | 50 | 500 | Circle | 1 | 15387.89505 | Ra 0.15 | Tungsten | 20047 |
| µWEDM | 50 | 500 | Circle | 1 | 14024.9672 | Ra 0.26 | Tungsten | 20047 |
| µWEDM | 50 | 500 | Circle | 1 | 4095.735103 | Ra 0.45 | Tungsten | 20047 |
| µWEDM | 50 | 135 | Circle | 1 | N.A. | Ra 0.06, 0.13, 0.53, 0.78 | PCD | 20048 |
| µWEDM | 80 | 525 | Circle | 1 | N.A. | Ra 0.12 | X38CrMoVS_1 steel | 20059 |
| µWEDM | 47.8 | 400 | Rectangle | 4 | N.A. | Ra 0.12 | X38CrMoVS_1 steel | 20059 |
| µWEDM | 1000 | 6000 | Gear | 32 | N.A. | Ra 0.12 | X38CrMoVS_1 steel | 20059 |
| µWEDM | 500 | 6000 | Gear | 32 | N.A. | Ra 0.12 | X38CrMoVS_1 steel | 20059 |
| µWEDM | 1000 | 10000 | Gear | 32 | N.A. | N.A. | SiSiC ceramic | 20059 |
| µWEDM | 110 | N.A. | Circle | 1 | N.A. | N.A. | WC | 200510 |
| µWEDM | 163 | N.A. | Triangle | 3 | N.A. | N.A. | WC | 200510 |
| µWEDM | 178 | N.A. | Square | 4 | N.A. | N.A. | WC | 200510 |
| µWEDM | 100 | 135 | Round square | 4 | N.A. | Dimensional error <1 | WC | 200711 |
| µWEDM | 1000 | 600 | Hex-polygon (3D, 2-flute cutter) | 6 | N.A. | N.A. | PCD | 200812 |
| µWEDM | 200 | 200 | Hex-polygon (3D, 6-flute cutter) | 6 | N.A. | N.A. | PCD | 200812 |
| µWEDM | 207.4 | 335 | Circle (3D, hemisphere) | 1 | N.A. | Radius variation ±2.0 | PCD | 200913 |
| µWEDM | 135 | 1445 | Circle | 1 | 172362.9901 | X, Y, Z motion resolutions 0.1 | Brass | 201014 |
| µWEDM | 135 | 1445 | Circle | 1 | 86181.49503 | X, Y, Z motion resolutions 0.1 | Steel | 201014 |
| µWEDM | 99 | 750 | Square | 4 | 30628.125 | X, Y, Z motion resolutions 0.1 | Brass | 201014 |
| µWEDM | 450 | 267 | Circle | 1 | N.A. | N.A. | PCD | 201115 |
| µWEDM | 800 | 300 | Square | 2 | N.A. | N.A. | PCD | 201115 |
| µWEDM | 350 | 200 | Triangle | 3 | N.A. | N.A. | PCD | 201115 |
| µWEDM | 400 | 400 | D shape | 4 | N.A. | N.A. | PCD | 201115 |
| µWEDM | 500 | 500 | Quadrilateral | 4 | N.A. | R 6.7, Ra ~ 0.265 | PCD | 201316 |
| µWEDM | 864.8 | ~800 | Circle (3D, hemisphere) | 1 | N.A. | N.A. | PCD | 201317 |
| µWEDM | 781.2 | ~800 | D shape (3D, quarter sphere) | 2 | N.A. | R 1.8, Ra 0.186, Rz 0.824 | PCD | 201317 |
| µWEDM | 282.9 | 67 | Square (3D, pyramid) | 4 | 15761820.9 | Ra 0.12 | PCD | 201618 |
| µWEDM | 346.4 | 200 | Square (3D, pyramid) | 4 | 8191204.86 | Ra 0.12 | PCD | 201618 |
| µWEDM | 1200 | 2200 | Gear | 40 | N.A. | Ra 0.9, X/Y resolution 0.1 | X153CrMoV12 | 201819 |
| µWEDM | 796.6 | 2085 | Round square (3D, helix) | 4 | N.A. | Position resolution 0.1 | Cemented carbide | 202220 |
| µWEDM | 713.6 | 2000 | Round square (3D, helix) | 4 | N.A. | Position resolution 0.1 | Cemented carbide | 202220 |
| µWEDM | 878.3 | 2000 | Round square (3D, helix) | 4 | N.A. | Position resolution 0.1 | Cemented carbide | 202220 |
| µIM | 1188 | 2460 | Rectangle | 4 | N.A. | Rz < 0.05 | ZrO2 | 200121 |
| µIM | 170 | 1700 | Cogwheel | 49 | N.A. | Rmax 2–3 | ZrO2 | 200121 |
| µIM | 1295 | 166 | Gearwheel | 41 | N.A. | N.A. | Al2O3 | 200222 |
| µIM | 1215 | 155 | Gearwheel | 41 | N.A. | N.A. | ZrO2 | 200222 |
| µIM | 8.36 | 24 | Circle | 1 | N.A. | Ra 0.25, Rmax 2 | Iron | 200223 |
| µIM | 81.3 | 160 | Circle | 1 | N.A. | Ra 0.25, Rmax 2 | Iron | 200223 |
| µIM | 413.9 | 600 | Circle | 1 | N.A. | Ra 0.25, Rmax 2 | Iron | 200223 |
| µIM | 834.8 | 700 | Circle | 1 | N.A. | Ra 0.25, Rmax 2 | Iron | 200223 |
| µIM | 300 | ~150 | Gear | 49 | N.A. | Ra 0.6, Rmax 4.5 | 316L stainless steel | 200223 |
| µIM | 200 | 8.06 | Circle (3D, Dome-like shape) | 1 | 3844858.901 | Absolute height deviation ~0.1, Ra 2.315 (PS), 1.606 (PMMA), 3.025 (PC) nm | PS, PMMA, PC | 200424 |
| µIM | 300 | 17.21 | Circle (3D, Dome-like shape) | 1 | 7360488.705 | Absolute height deviation ~0.1, Ra 2.315 (PS), 1.606 (PMMA), 3.025 (PC) nm | PS, PMMA, PC | 200424 |
| µIM | 500 | 20.81 | Circle (3D, Dome-like shape) | 1 | 62052593.67 | Absolute height deviation ~0.1, Ra 2.315 (PS), 1.606 (PMMA), 3.025 (PC) nm | PS, PMMA, PC | 200424 |
| µIM | 85 | 170 | Circle | 1 | N.A. | N.A. | 316 L stainless steel | 200425 |
| µIM | 50 | 50 | Circle | 1 | N.A. | N.A. | 316 L stainless steel | 200626 |
| µIM | 100 | 350 | Circle | 1 | N.A. | N.A. | PP, POM, ABS | 200727 |
| µIM | 150 | 400 | Circle | 1 | N.A. | N.A. | PP, POM, ABS | 200727 |
| µIM | 850 | 300 | Gear | 24 | N.A. | N.A. | PP, POM, ABS | 200727 |
| µIM | 60 | 250 | Circle | 1 | 14137166.94 | N.A. | PP | 200828 |
| µIM | 90 | 250 | Circle | 1 | 31808625.62 | N.A. | PP | 200828 |
| µIM | 110 | 250 | Circle | 1 | 47516588.89 | N.A. | PP | 200828 |
| µIM | 130 | 250 | Circle | 1 | 66366144.81 | N.A. | PP | 200828 |
| µIM | 60 | 191 | Circle | 1 | N.A. | N.A. | 316L stainless steel | 201129 |
| µIM | 100 | 200 | Circle | 1 | N.A. | N.A. | 316L stainless steel | 201129 |
| µIM | 28 | 100 | Square | 4 | N.A. | N.A. | Pb(Mg, Nb)O3–Pb(Zr, Ti)O3 | 201630 |
| µIM | 56.6 | 400 | Square | 4 | N.A. | N.A. | Pb(Mg, Nb)O3–Pb(Zr, Ti)O3 | 201630 |
| µIM | 205 | 80 | Circle | 1 | 1671207.991 | N.A. | PC, PP | 201831 |
| µIM | 0.407 | 5 | Circle | 1 | 0.411710191 | N.A. | PC, PP | 201831 |
| µIM | 608 | 57.12 | Gear | 36 | 47914467.1 | N.A. | PP | 201832 |
| Micro grinding | 500 | 2500 | Centrosymmetric irregular shape (3D, helix) | 8 | N.A. | N.A. | TiAIN-coated cemented carbide | 200533 |
| Micro grinding | 100 | 1000 | Centrosymmetric irregular shape (3D, helix) | 8 | N.A. | N.A. | TiAIN-coated cemented carbide | 200533 |
| Wire electrodischarge grinding | 20 | 25 | Circle | 1 | 5492.294849 | Ra 0.06–0.065 | WC | 200634 |
| Wire electrodischarge grinding | 20 | 50 | Circle | 1 | 10984.5897 | Ra 0.06–0.065 | WC | 200634 |
| Wire electrodischarge grinding | 20 | 90 | Circle | 1 | 19772.26146 | Ra 0.06–0.065 | WC | 200634 |
| Micro grinding | 20 | 30 | D shape | 2 | N.A. | N.A. | WC | 201235 |
| Micro grinding | 10 | 20 | D shape | 2 | 78.53981634 | N.A. | WC | 201235 |
| Micro grinding | 44 | 140 | Circle | 1 | N.A. | N.A. | WC & Co | 201736 |
| Laser-induced graphitization & micro grinding | 2040 | 2000 | Rectangle | 4 | 40000000 | R 2.3, Ra 0.053, Sa 0.177 | CVD diamond | 201937 |
| Micro grinding | 1000 | 4000 | Centrosymmetric irregular shape (3D, helix) | 10 | N.A. | R 3–3.5 | TiAlN-WC | 201938 |
| Micro grinding | 500 | N.A. | Centrosymmetric irregular shape (3D, helix) | 8 | N.A. | R 0.2 | AlTiN coated carbide | 201939 |
| Micro grinding | 777 | N.A. | Centrosymmetric irregular shape (3D, helix) | 6 | N.A. | R 1.64–2.45 | Ti(C7N3)-based cermet | 201940 |
| Micro grinding | 500 | 1000 | Centrosymmetric irregular shape (3D, helix) | 8 | N.A. | N.A. | WC | 202041 |
| Micro grinding | 469 | 1000 | Centrosymmetric irregular shape (3D, helix) | 6 | N.A. | N.A. | WC | 202041 |
| Micro grinding | 500 | N.A. | Centrosymmetric irregular shape (3D, helix) | 8 | N.A. | R 2.1 | Alloy | 202042 |
| Micro grinding | 993 | N.A. | Centrosymmetric irregular shape (3D, helix) | 6 | N.A. | R 3.57 | Ti(C7N3)-based cermet | 202043 |
| Focused ion beam | 20 | 25 | Two-flute circle variation | 4 | 38.75 | N.A. | WC | 200634 |
| Focused ion beam | 20 | 50 | Two-flute circle variation | 4 | 77.5 | N.A. | WC | 200634 |
| Focused ion beam | 20 | 90 | Two-flute circle variation | 4 | 139.5 | N.A. | WC | 200634 |
| Femtosecond pulsed laser | 1025 | 513 | D shape (3D, quarter sphere) | 2 | 7048232.659 | R 0.8; Ra 0.022 | PCD | 201644 |
| Microfludics | 835.9 | N.A. | Gear | 40 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 183.4 | N.A. | Regular triangle | 3 | 2038246156 | N.A. | SiO2 | This work |
| Microfludics | 270.5 | N.A. | Isosceles triangle | 3 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 290.4 | N.A. | Regular triangle | 3 | 6040446487 | N.A. | Si3N4 | This work |
| Microfludics | 262.5 | N.A. | Isosceles triangle | 3 | 2038246156 | Ra 0.391 | SiO2 | This work |
| Microfludics | 378 | N.A. | Regular triangle | 3 | 4056314840 | R 4.78; Ra 0.255 | Al2O3 | This work |
| Microfludics | 431.6 | N.A. | Isosceles triangle | 3 | 6040446487 | Ra 0.754 | Si3N4 | This work |
| Microfludics | 316.8 | N.A. | Trapezoid | 4 | 2038246156 | N.A. | SiO2 | This work |
| Microfludics | 462.9 | N.A. | Trapezoid | 4 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 538.9 | N.A. | Trapezoid | 4 | 6040446487 | N.A. | Si3N4 | This work |
| Microfludics | 481.7 | N.A. | Square_i | 4 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 168.8 | N.A. | Hexagon | 6 | 2038246156 | N.A. | SiO2 | This work |
| Microfludics | 257.6 | N.A. | Hexagon | 6 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 273.8 | N.A. | Hexagon | 6 | 6040446487 | N.A. | Si3N4 | This work |
| Microfludics | 384.7 | N.A. | Regular triangle_ii | 6 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 401.9 | N.A. | Regular triangle_iii | 6 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 423.5 | N.A. | Regular triangle_iv | 6 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 716.6 | N.A. | Square_ii | 8 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 706.5 | N.A. | Square_iii | 8 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 679 | N.A. | Square_iv | 8 | 4056314840 | N.A. | Al2O3 | This work |
| Microfludics | 893.8 | N.A. | Square_v | 8 | 4056314840 | R 1.32; Ra 0.255 | Al2O3 | This work |
| Microfludics | 632.11 | N.A. | Square_v | 8 | 2038246156 | Ra 0.391 | SiO2 | This work |
| Microfludics | 1039.3 | N.A. | Square_v | 8 | 6040446487 | Ra 0.754 | Si3N4 | This work |

## Abbreviation Explanation:

| µWEDM: Micro-wire electrical discharge machining |  | PCD: Polycrystalline diamond |
| --- | --- | --- |
| µIM: Micro injection molding |  | PMMA: Polymethyl methacrylate |
| ABS: Acrylonitrilebutadiene-styrene |  | POM: Polyoxymethylene |
| CVD: Chemical vapor deposited |  | PP: Polypropylene |
| Dc: Circumcircle diameter |  | PS: Polystyrene |
| L: Length |  | R: Edge radius |
| N: Edge number of the cross-section |  | Ra: Average roughness |
| N.A.: Not applicable |  | Rmax: Maximum roughness depth |
| PC: Polycarbonate |  | Rz: Average maximum surface height |

# References

1.	Liu, Y. et al. Synthesis of a cationic polyacrylamide by a photocatalytic surface-initiated method and evaluation of its flocculation and dewatering performance: nano-TiO2 as a photo initiator. RSC Adv. 8, 28329-28340 (2018).

2.	Dumitrescu, A. M. et al. Ni ferrite highly organized as humidity sensors. Mater. Chem. Phys. 156, 170-179 (2015).

3.	Guo, H. et al. Realization of high-percentage addition of fly ash in the materials for the preparation of geopolymer derived from acid-activated metakaolin. J. Clean Prod. 285, 125430 (2021).

4.	Du, X., Wang, Y., Su, X. & Li, J. Influences of pH value on the microstructure and phase transformation of aluminum hydroxide. Powder Technol. 192, 40-46 (2009).

5.	Liu, Y. C. et al. In-situ infrared reflective absorption spectroscopy characterization of SiN films deposited using sputtering-type ECR microwave plasma. Appl. Surf. Sci. 121-122, 233-236 (1997).

6.	Fleischer, J., Masuzawa, T., Schmidt, J. & Knoll, M. New applications for micro-EDM. J. Mater. Process. Technol. 149, 246-249 (2004).

7.	Vallance, R. R., Morgan, C. J., Shreve, S. M. & Marsh, E. R. Micro-tool characterization using scanning white light interferometry. J. Micromech. Microeng. 14, 1234-1243 (2004).

8.	Morgan, C. J., Vallance, R. R. & Marsh, E. R. Micro machining glass with polycrystalline diamond tools shaped by micro electro discharge machining. J. Micromech. Microeng. 14, 1687-1692 (2004).

9.	Schoth, A., Förster, R. & Menz, W. Micro wire EDM for high aspect ratio 3D microstructuring of ceramics and metals. Microsyst. Technol. 11, 250-253 (2005).

10.	Liu, H.-S., Yan, B.-H., Huang, F.-Y. & Qiu, K.-H. A study on the characterization of high nickel alloy micro-holes using micro-EDM and their applications. J. Mater. Process. Technol. 169, 418-426 (2005).

11.	Chern, G.-L., Wu, Y.-J. E., Cheng, J.-C. & Yao, J.-C. Study on burr formation in micro-machining using micro-tools fabricated by micro-EDM. Precis. Eng. 31, 122-129 (2007).

12.	Cheng, X. et al. Development of ultra-precision machining system with unique wire EDM tool fabrication system for micro/nano-machining. CIRP Ann. 57, 415-420 (2008).

13.	Cheng, X., Wang, Z. G., Nakamoto, K. & Yamazaki, K. Design and development of a micro polycrystalline diamond ball end mill for micro/nano freeform machining of hard and brittle materials. J. Micromech. Microeng. 19, 115022 (2009).

14.	Peng, Z., Wang, Z., Dong, Y. & Chen, H. Development of a reversible machining method for fabrication of microstructures by using micro-EDM. J. Mater. Process. Technol. 210, 129-136 (2010).

15.	Perveen, A., San, W. Y. & Rahman, M. Fabrication of different geometry cutting tools and their effect on the vertical micro-grinding of BK7 glass. Int. J. Adv. Manuf. Technol. 61, 101-115 (2011).

16.	Gao, C., Zhan, Z., Wang, S., He, N. & Li, L. Research on WEDM process optimization for PCD micro milling tool. Procedia CIRP 6, 209-214 (2013).

17.	Zhang, Z., Peng, H. & Yan, J. Micro-cutting characteristics of EDM fabricated high-precision polycrystalline diamond tools. Int. J. Mach. Tools Manuf. 65, 99-106 (2013).

18.	Oliaei, S. N. B. & Karpat, Y. Fabrication of PCD mechanical planarization tools by using μ-wire electrical discharge machining. Procedia CIRP 42, 311-316 (2016).

19.	Wang, Y., Chen, X., Wang, Z. & Dong, S. Fabrication of micro gear with intact tooth profile by micro wire electrical discharge machining. J. Mater. Process. Technol. 252, 137-147 (2018).

20.	Sun, Y. et al. Experimental evaluation of surface generation and force time-varying characteristics of curvilinear grooved micro end mills fabricated by EDM. J. Manuf. Process. 73, 799-814 (2022).

21.	Piotter, V., Bauer, W., Benzler, T. & Emde, A. Injection molding of components for microsystems. Microsyst. Technol. 7, 99-102 (2001).

22.	Merz, L. et al. Feedstock development for micro powder injection molding. Microsyst. Technol. 8, 129-132 (2002).

23.	Rota, A., Duong, T. V. & Hartwig, T. Micro powder metallurgy for the replicative production of metallic microstructures. Microsyst. Technol. 8, 323-325 (2002).

24.	Lee, B. K., Kim, D. S. & Kwon, T. H. Replication of microlens arrays by injection molding. Microsyst. Technol. 10, 531-535 (2004).

25.	Fu, G., Loh, N. H., Tor, S. B., Murakoshi, Y. & Maeda, R. Replication of metal microstructures by micro powder injection molding. Mater. Des. 25, 729-733 (2004).

26.	Zauner, R. Micro powder injection moulding. Microelectron. Eng. 83, 1442-1444 (2006).

27.	Sha, B., Dimov, S., Griffiths, C. & Packianather, M. S. Investigation of micro-injection moulding: factors affecting the replication quality. J. Mater. Process. Technol. 183, 284-296 (2007).

28.	Lu, Z. & Zhang, K. F. Morphology and mechanical properties of polypropylene micro-arrays by micro-injection molding. Int. J. Adv. Manuf. Technol. 40, 490-496 (2009).

29.	Liu, L. et al. Preparation and characterization of micro components fabricated by micro powder injection molding. Mater. Charact. 62, 615-620 (2011).

30.	Han, J. S., Gal, C. W., Kim, J. H. & Park, S. J. Fabrication of high-aspect-ratio micro piezoelectric array by powder injection molding. Ceram. Int. 42, 9475-9481 (2016).

31.	Zhou, M., Xiong, X., Jiang, B. & Weng, C. Fabrication of high aspect ratio nanopillars and micro/nano combined structures with hydrophobic surface characteristics by injection molding. Appl. Surf. Sci. 427, 854-860 (2018).

32.	Oshima, K. & Kunieda, M. Attempts to fabricate micro injection molding tools and assemble molded micro parts on same EDM machine. CIRP Ann. 67, 213-216 (2018).

33.	Uhlmann, E. & Schauer, K. Dynamic load and strain analysis for the optimization of micro end mills. CIRP Ann. 54, 75-78 (2005).

34.	Ali, M. Y. & Ong, A. S. Fabricating micromilling tool using wire electrodischarge grinding and focused ion beam sputtering. Int. J. Adv. Manuf. Technol. 31, 501-508 (2006).

35.	Aurich, J. C., Reichenbach, I. G. & Schüler, G. M. Manufacture and application of ultra-small micro end mills. CIRP Ann. 61, 83-86 (2012).

36.	Arrabiyeh, P. A. et al. Experimental analysis for the use of sodium dodecyl sulfate as a soluble metal cutting fluid for micromachining with electroless-plated micropencil grinding tools. Inventions 2, (2017).

37.	Zhao, G. et al. Fabrication and performance of CVD diamond cutting tool in micro milling of oxygen-free copper. Diam. Relat. Mat. 100, 107589 (2019).

38.	K, V. & Mathew, J. Wear behavior of TiAlN coated WC tool during micro end milling of Ti-6Al-4V and analysis of surface roughness. Wear 424-425, 165-182 (2019).

39.	Alhadeff, L. L., Marshall, M. B., Curtis, D. T. & Slatter, T. Protocol for tool wear measurement in micro-milling. Wear 420-421, 54-67 (2019).

40.	Wang, Y., Zou, B. & Huang, C. Tool wear mechanisms and micro-channels quality in micro-machining of Ti-6Al-4V alloy using the Ti(C7N3)-based cermet micro-mills. Tribol. Int. 134, 60-76 (2019).

41.	Khaliq, W., Zhang, C., Jamil, M. & Khan, A. M. Tool wear, surface quality, and residual stresses analysis of micro-machined additive manufactured Ti–6Al–4V under dry and MQL conditions. Tribol. Int. 151, 106408 (2020).

42.	Zhang, X., Yu, T., Dai, Y., Qu, S. & Zhao, J. Energy consumption considering tool wear and optimization of cutting parameters in micro milling process. Int. J. Mech. Sci. 178, 105628 (2020).

43.	Wang, Y., Zou, B., Wang, J., Wu, Y. & Huang, C. Effect of the progressive tool wear on surface topography and chip formation in micro-milling of Ti–6Al–4V using Ti(C7N3)-based cermet micro-mill. Tribol. Int. 141, 105900 (2020).

44.	Ogawa, Y. et al. A study on machining of binder-less polycrystalline diamond by femtosecond pulsed laser for fabrication of micro milling tools. CIRP Ann. 65, 245-248 (2016).