This supplementary information file includes:

Notes S1–8

Figures S1–22

References 1–17

# Supplementary Notes

Supplementary Note 1.  Our exploration on the O2 structure (Cmca) revealed that each rotation of the structure to a certain angle yields a unique combination of  and  stacking sequences (Fig. 1f). Specifically, when the rotation angle was set to 0 degrees or 180 degrees, the projected dumbbell structures were exclusively aligned with the  sequence, with no other stacking sequences observed. However, as the structure is rotated to different angles, a noticeable change occurs in the alignment of the dumbbell structures. At the rotation angles of 60, 120, 240, and 300 degrees, the projected structures exhibit alternating  and  sequences. For instance, at 60 and 120 degrees, the structures are stacked with alternating γ/β sequences from top to bottom in the figure. Similarly, at 240 and 300 degrees, the structures display alternating β/γ sequences. What is noteworthy here is that even with the same stacking sequences, different arrangements of honeycomb structures can be discerned because of the varying positions of superstructures between two adjacent TM layers, as discussed in Figs. 1c-e. Supplementary Figs. S1a and b provide top and front views, respectively, of the honeycomb structures for the middle of the three adjacent layers shown in Fig. 1f. In the 0-degree projection, the top and bottom layers have same position in the ab-plane, while the mid-layer is slightly misaligned along the a-axis (Supplementary Figs. S1a and b). This stacking order made the structure have the sequence of (I)and(II) simultaneously when viewed from front. These stacking combinations were switched in the 180-degree projection due to the change in the relative ab-plane position of the mid-layer, leading to the exchange of α(I) and α(II) sequences. Similarly, in the 60-degree projection, the relative positions of the top and mid-layers result in the (I) sequence, whereas the arrangements of the mid- and bottom layers correspond to the (II) sequence. This order is changed to (II) and (I) sequences in the 120-degree projection. The same stacking pattern is observed in the 240-degree and 300-degree projections, with the opposite sequences of γ(II)/β(I) and γ(I)/β(II) exhibited, respectively.

Supplementary Note 2. Rotational stacking faults, characterized by a sequence of multiply stacked layers with different rotational angles, can arise through two distinct slab movements. Fig. S2 illustrates the transformation of the O2 structure (Cmca) at 0 degrees to combined sequences of 0 degrees and 240 degrees along the same projection angles. To trace the formation of RSFs, an understanding of relative slab movements across three upper layers (denoted as layer 1-3 in the figure) is essential. Firstly, if the entire middle slab (layer 2) undergoes a 240-degree rotation concerning adjacent layers 1 and 3 during synthesis, the resulting configuration of layers 1-3 exhibits stacking sequences observed along a 240-degree rotation, giving rise to a rotationally faulted unit of 0°/240°. These multiple units can also be generated through the translational motion of layer 2 to another crystallographic lattice, as depicted in the figure, where the relative movement of the slab produces the same RSFs as those created with the rotational motion of layer 2. Consequently, we can infer that these two distinct pathways can yield identical rotational stacking faults. However, the detailed processes governing their different formation kinetics and energetics require further investigation in subsequent studies.

Supplementary Note 3. We assessed the displacements of different transition-metal slabs along the ab-plane to identify the varying gliding modes of adjacent transition-metal slabs at the RSFs interface after charging. In the absence of RSFs, interlayer oxygen dimerization was not observed in the DFT calculations (Supplementary Fig. S3a). In this case, the absolute displacement of the upper layer was found to be 0.70 Å with an angle of 13.0° along the ab-plane (Supplementary Figs. S4a and b). Notably, this relatively small change in the structure facilitates a homogeneous distribution of lithium ions in the lithium layers (Fig. 2a). The even distribution of lithium ions impedes interlayer oxygen dimerization by restraining the gliding of each transition-metal slab. Conversely, in the faulted structures (Figs. 2b and c), the transition-metal slabs were dynamically glided to mitigate the internal microstrain, eventually leading to the collapse of the lithium slab with interlayer oxygen dimerization (Supplementary Figs. S3b and c). At the interface between the α and β sequences (multiple units of 0°/120° in Fig. 2b), the upper transition metal slab was displaced by 1.51 Å with an angle of 53.8° along the ab-plane direction (Supplementary Figs. S4a and b). Similarly, between the α and γ sequences (multiple units of 0°/240° in Fig. 2c), the upper transition metal slab was displaced by 1.53 Å with an angle of -51.3° (Supplementary Figs. S4a and b). Considering that the two multiple units (Figs. 2b and c) are 120˚ rotated from each other, the translational motion of the two structures at 105.1° after charging confirms that the layers glide in different directions at the interface where the rotational stacking faults exist (Supplementary Fig. S4c).

Supplementary Note 4. The pristine electrode was composed of Li32Mn16O48, which can be characterized by alternating TM and Li layers. Based on experimental results, we defined SOC of 75% as the charged state, where the unit cell retained 8 Li atoms, corresponding to same number of Li vacancies in the TM layer. Upon the introduction of RSFs in the charged structure, the optimized configurations exhibited significant deviations from the pristine structure. In the pristine structure without RSFs, Li can be uniformly distributed across tetrahedral sites by same physical/chemical environment, allowing stable accommodation after relaxation. However, the integration of RSFs disrupted the stability of these Li sites due to the altered TM arrangement, leading to slab gliding as a necessary adjustment to find stable Li configurations. Moreover, during the relaxation of RSFs-involving system, interlayer oxygen dimerization was observed at the interface. We also revealed that TM migration predominantly took place after interlayer oxygen dimerization occurred at the RSFs interface (Supplementary Fig. S5). Remarkably, we discovered that TM migration in these systems is a thermodynamically downhill reaction. This suggests that as more TMs migrate within the structure, the overall thermodynamic stability of the system increases. Furthermore, the TM migration led to the formation of molecular oxygen, characterized by a shorter bond length of approximately ~1.2 Å, which signified a significant decoordination of the metal-oxygen bonds.

Supplementary Note 5. To gain further insights into the dynamic processes of RSFs, we performed ab initio molecular dynamics simulations on Li-rich layered oxides, considering scenarios with either one or two TM migrations. These simulations demonstrated a sequential occurrence of events, including oxygen dimerization, TM migration, and layer densification, as depicted in Fig. 2d and Supplementary Fig. S6. The simulation results revealed that in systems where only a single TM had migrated, structural degradation was observed after 7520 fs (Supplementary Fig. S6). Conversely, in systems where two TMs had migrated, the structural degradation, encompassing oxygen dimerization and TM migration, occurred significantly earlier, at approximately 400 fs (Fig. 2d). These findings emphasize the strong dependence of the observable time for structural evolutions on the extent of TM migration, attributed to the kinetics of the metal-oxygen decoordination process. Therefore, the degree of TM migration exerted a notable influence on the structural stability of the materials, with increased migration leading to accelerated structural degradation.

Supplementary Note 6. Electron energy-loss spectroscopy (EELS) analysis was performed on the tenth-cycled O2-Lix(Li0.25Ni0.05Mn0.7)O2 to investigate the chemical states of the bulk regions across the intragranular crack area (Supplementary Fig. S7a). The spectra obtained near the crack (dashed spectra) exhibited a reduced intensity of O K-edge (527 ~ 550 eV) compared to the intact bulk region (solid spectra), indicating a relatively lower oxygen content attributed to gas release during the formation of internal defects (Supplementary Figs. 7b and c).1,2 Additionally, the Mn L2,3-edges (635 ~ 660 eV) in the region near the crack shifted to the low energy region, and the L3/L2 edge intensity ratio notably decreased, which are characteristic signatures of Mn reduction to the 3+ state.1,3,4 Considering that the measured electrode is in a fully oxidized state (i.e., charged state), it can be confirmed that the reduction of Mn ions is associated with the electrochemically inactive phase transformation occurring around the crack region.1

Supplementary Note 7. Supplementary Figs. S16a-c present ex-situ XRD patterns collected for every quarter of the state-of-charges (SOCs) of the 750, 850, and 950 ℃ electrodes in the second cycle. In these figures, the main (002) diffraction peak representing the c-lattice parameter is highlighted, and we focused on two features: peak shift and intensity, both of which serve as critical indicators of structural changes in the material.1,5-7 Overall, the Bragg position of the (002) peak increases particularly in the high-voltage region where oxygen redox dominates the charge compensation,1,8-11 and it is reversibly restored back to the initial state upon discharging. Comparable peak position changes across all electrodes (Fig. S16d) indicate that the lattice expansion/contraction behavior during lithium (de)intercalation is similar among the differently synthesized electrodes. However, as shown in Fig. S16e, the peak intensity in the fully charged states differed obviously, with the layeredness being markedly suppressed as the synthesis temperature decreased. This observation suggests that the accumulation of microstrain within the structure can vary substantially, even though the structure experiences a similar degree of volumetric change. And we expect that the presence of rotational stacking faults in the pristine state triggers the distinct structural evolution among the electrodes during the charging process, as demonstrated by the computational results in Fig. 2. This signifies that how the entire structure changes synchronously is more critical to the mechanical degradation of the layered structure than the extent to which the lattice contracts and expands.

Supplementary Note 8. STEM analysis was performed to investigate the microstructural evolution even in the 950 ℃ electrode after long-term cycling (Fig. S21). As shown in Fig. S21a, the overall region could be divided into two groups, Region I and II, based on the Fast-Fourier transform (FFT) pattern. Compared to the FFT pattern in Region II, where clear diffraction spots of the layered structure were observed (Fig. S21c), only a few FFT patterns were observed in Region I (Fig. S21b), indicating that incipient cracking generated in Region I. Noteworthy is that these structural degradations occurred in the faulted areas where the rotational stacking sequence was altered, which is in line with our discussions in this study.

To further investigate the electronic states of Mn and O species in each region, EELS analysis was conducted (Fig. S21d). It was confirmed that the ratios of pre/main O K-edge and L3/L2 Mn L-edge decreased near the cracks in Region I, and the Mn L-edge shifted to lower energies, indicating oxygen release and manganese reduction. These observations were consistent with the evolution of the crack region in the cycled 850 ℃ electrode, as revealed in Supplementary Fig. S7 and Note 6. Our findings suggest that despite the low presence of rotational stacking faults in the pristine 950 ℃ electrode, repetitive charge and discharge processes can induce unintentional local stacking faults, which can gradually lead to intragranular crack nucleation and capacity fading.

Several factors can contribute to these observations: i) incomplete defect annihilation, ii) non-uniformity of lithium content within the structure during the (de)intercalation reaction, iii) gliding energetics change due to in-plane disorder. First, considering the thermodynamic defect equilibrium (particularly entropy aspects) and the additional ion-exchange process, it can be expected that it will be virtually challenging to completely eliminate all rotational stacking sequences even if the synthesis temperature continues to increase. Therefore, even in the 950 ℃-annealed electrode, a small amount of RSFs may unavoidably exist in the layered structure, which can potentially generate microcracks after sufficient electrochemical cycles. However, the presence of these defects is significantly reduced, leading to a suppressed degradation rate compared to electrodes synthesized at lower temperatures. Additionally, non-uniform lithium content within single particles upon (de)intercalation reactions, arising from limited Li ion diffusion kinetics, can compromise structural stability during repetitive electrochemical reactions. This non-uniformity induces inhomogeneous surface-to-bulk lattice breathing and local phase transformations, especially at high-voltage operations. These processes, in turn, impose severe mechanical strain and create various types of defects, such as domain boundaries, RSFs, or microcracks.12-14 Furthermore, although the out-of-plane TM migration is highly restricted in the O2-type layered cathodes, in-plane migration of TM species can occur under specific electrochemical conditions or compositions,15,16 leading to disordering within the TM layers and non-uniform atomic arrangements, such as the TM vacancy agglomerations or lattice oxygen evolution.11,15,16 The gradual accumulation of such local structural evolution can induce stacking rotations and the formation of additional RSFs and intragranular cracks after repeated electrochemical reactions. Considering that the bulk defect states significant influence the energetics of slab movement in layered materials,17 the gradual accumulation of such local environment can induce stacking rotations in a certain direction where the gliding energetics are most favorable. This then leads to the formation of additional RSFs and subsequent development of bulk intragranular cracks during repeated electrochemical reactions. Despite these speculations, it is noteworthy that electrochemical degradation observed in the 950 ˚C electrode is considerably suppressed compared to the 750 or 850 ˚C electrodes. These findings raise questions about whether electrochemically activated stacking faults exhibit a different degradation mechanism compared to RSFs formed during the synthesis process. To gain a comprehensive understanding of these differences and address the remaining challenges associated with slowly occurring electrochemo-mechanical degradation, further investigations are necessary to explore the underlying behaviors of RSFs.

Fig. S1. a, Top views of the honeycomb structures between the three adjacent transition metal layers specified in Fig. 1f, viewed from different angles. b, Front views of the honeycomb structures and their stacking sequences between the three adjacent transition metal layers, viewed from different angles.

Fig. S2. Two comparable pathways for generating rotational stacking faults: rotation (upper arrow) and translation (lower arrow).

Fig. S3. a-c, Comparison of honeycomb structures between two adjacent transition metal layers for (a) single unit (0˚), (b) multiple units (0˚/240˚), and (c) multiple units (0˚/120˚) in the pristine and charged states. The two adjacent transition metal layers here refer to the two transition metal layers in the boxed area of Figs. 2b and c.

Fig. S4. a, Relative displacement vectors of the honeycomb structure during the charging process in Fig. S3 projected onto the ab plane. Red, green, and blue arrows indicate the movements in the structures of single unit (0˚), multiple units (0˚/240˚), and multiple units (0˚/120˚), respectively. b, Components of the relative displacement vectors for each case in a. c, The angle between the two vectors of the two multiple units in a.

Fig. S5. Computed reaction energies associated with out-of-plane TM migration reactions at the RSFs interface. Mn, O, and Li atoms are represented by purple (and blue), red, and green spheres, respectively. Red and yellow oxygen dimers are classified according to whether the bond length of the oxygen is longer (red) or shorter (yellow) than that of superoxide (1.34 Å), respectively.

Fig. S6. AIMD simulation of intragranular crack formation near the dimerization region of the charged structure in which only one cation migrated (blue octahedron) in the initial model. Purple and grey polyhedrons depict the original and migrated sites of manganese, respectively, while lithium ions are represented by green sphere. Red and yellow oxygen dimers are classified according to whether the bond length of the oxygen is longer (red) or shorter (yellow) than that of superoxide (1.34 Å), respectively. Each snapshot shows intermediate structures within the dotted box of the leftmost structure at different times, with the average dimer length indicated below.

Fig. S7. a,b, ADF image (a) and EELS spectra (b) of the 10th charged electrode. The arrow in the figure indicates the direction in which the EELS measurement was scanned. c, Contour plot of the EELS results in b.

Fig. S8. a,b, Cross-sectional SEM (a) and nano-CT (b) images of the O2-Lix(Li0.25Ni0.05Mn0.7)O2 electrode after 50 cycles.

Fig. S9. Comparison of XRD patterns of Na5/6(Li0.25Ni0.05Mn0.7)O2 structures synthesized at different temperatures. Reference XRD patterns of P2- and P3-NaCoO2 are shown together. Phase transformation from P3 (R3m) to P2 (P63/mmc) structures in the targeted Na5/6(Li0.25Ni0.05Mn0.7)O2 composition was identified above 750 ˚C; below 750 ˚C, pure P3 and P2/P3 binary phases were observed at 650 ˚C and 700 ˚C, respectively.

Fig. S10. XRD pattern generations for P2-Na2/3(Li1/3Mn2/3)O2 structure with distinct rotational stacking sequences. Yellow, green, and purple spheres depict sodium, lithium, and manganese ions, respectively. The colored trapezoids in the atomic configurations represent the respective stacking sequence of the transition metal layers.

Fig. S11. XRD patterns of pristine O2-Lix(Li0.25Ni0.05Mn0.7)O2 electrodes synthesized at different temperatures.

Fig. S12. a,b, SEM images of P2-Na5/6(Li0.25Ni0.05Mn0.7)O2 series (a) and O2-Lix(Li0.25Ni0.05Mn0.7)O2 series (b) synthesized at different temperatures.

Fig. S13. a-c, Electron diffraction pattern simulations along the [100] zone axis for (a) single unit (0˚), (b) multiple units (0˚/240˚), and (c) multiple units (0˚/120˚). Consistent with the experimental results in Figs. 3e-g, the rotational stacking faults create additional diffraction planes along the (0 2 4n) and (0 4 4n) planes where n is an integer. These additional spots generate streak lines as in Figs. 3e-g.

Fig. S14. a-c, XAS spectra of the O K edge (a) and Ni (b) and Mn L edges (c) of pristine O2-Lix(Li0.25Ni0.05Mn0.7)O2 electrodes synthesized at different temperatures.

Fig. S15. Initial voltage profiles of O2-Lix(Li0.25Ni0.05Mn0.7)O2 electrodes synthesized at different temperatures.

Fig. S16. a-c, Ex-situ XRD patterns for each point in the 2nd electrochemical profiles (left panels) of O2-Lix(Li0.25Ni0.05Mn0.7)O2 electrodes synthesized at 750 ˚C (a), 850 ˚C (b), and 950 ˚C (c). A wavelength of λ=1.5406 Å was used for this measurement. d, Comparison of (002) peak position changes during the second cycle. e, Deconvolution results for the (002) peak of the electrodes charged to 4.6 V. The pink and gray shaded areas represent main XRD peaks of the O2 and impurity O3 phases, respectively.

Fig. S17. Five different 3D rendered particles at various voltages in the 10th cycle of the O2-Lix(Li0.25Ni0.05Mn0.7)O2 (850 ˚C).

Fig. S18. Five different 3D rendered particles at various voltages in the 10th cycle of the O2-Lix(Li0.25Ni0.05Mn0.7)O2 (950 ˚C).

Fig. S19. a,b, Five different 3D rendered particles at different electrochemical cycles of the O2-Lix(Li0.25Ni0.05Mn0.7)O2 electrodes synthesized at 850 ˚C (a) and 950 ˚C (b). All electrodes after electrochemical cycling are in the charged state.

Fig. S20. Electrochemical voltage profiles during long-term cycling of O2-Lix(Li0.25Ni0.05Mn0.7)O2 electrodes synthesized at 750, 850, and 950 ˚C.

Fig. S21. a, ADF image of the 10th charged O2-Lix(Li0.25Ni0.05Mn0.7)O2 (950 ˚C). The white dotted region in a indicates the incipient intragranular crack area, and the colored trapezoids in the STEM image represent the respective stacking sequence of the transition metal layers. And the arrow in the figure indicates the direction in which the EELS measurement was scanned. b,c, FFT patterns of Regions I (b) and II (c) in the STEM image in a. d, EELS spectra of the O K edge and Mn L edge for Regions I and II in the STEM image in a. Top and bottom panels are results for Regions I and II, respectively. Each spectrum was deconvoluted with the peaks specified in the figures.

# Fig. S22. a-c, HAADF-STEM images and GPA strain maps of pristine O3-Li(Li0.2Ni0.2Mn0.6)O2 electrodes synthesized at 750 ˚C (a), 850 ˚C (b), and 950 ˚C (c). The inset shows FFT patterns of the STEM images. The colored trapezoids in the STEM images represent the respective stacking sequence of the transition metal layers. The yellow circles in the strain maps indicate singularity points, and white boxes show areas where the singularities are linearly distributed

References

1	H. -Y. Jang et al. Structurally robust lithium-rich layered oxides for high-energy and long-lasting cathodes, Nat. Commun. In revision (2023).

2	Qiu, B. et al. Gas–solid interfacial modification of oxygen activity in layered oxide cathodes for lithium-ion batteries. Nat. Commun. 7, 12108 (2016).

3	Yan, P. et al. Injection of oxygen vacancies in the bulk lattice of layered cathodes. Nat. Nanotechnol. 14, 602-608 (2019).

4	Han, J.-G. et al. Unsymmetrical fluorinated malonatoborate as an amphoteric additive for high-energy-density lithium-ion batteries. Energy Environ. Sci. 11, 1552-1562 (2018).

5	Singer, A. et al. Nucleation of dislocations and their dynamics in layered oxide cathode materials during battery charging. Nat. Energy 3, 641-647 (2018).

6	Ryu, H.-H. et al. Capacity Fading Mechanisms in Ni-Rich Single-Crystal NCM Cathodes. ACS Energy Lett. 6, 2726-2734 (2021).

7	Li, J. et al. Structural origin of the high-voltage instability of lithium cobalt oxide. Nat. Nanotechnol. 16, 599-605 (2021).

8	Eum, D. et al. Voltage decay and redox asymmetry mitigation by reversible cation migration in lithium-rich layered oxide electrodes. Nat. Mater. 19, 419-427 (2020).

9	Eum, D. et al. Effects of cation superstructure ordering on oxygen redox stability in O2-type lithium-rich layered oxides. Energy Environ. Sci. 16, 673-686 (2023).

10	Song, J.-H. et al. Anionic Redox Activity Regulated by Transition Metal in Lithium-Rich Layered Oxides. Adv. Energy Mater. 10, 2001207 (2020).

11	Kim, B. et al. A theoretical framework for oxygen redox chemistry for sustainable batteries. Nat. Sustain. 5, 708-716 (2022).

12	Song, J.-H. et al. Slab gliding, a hidden factor that induces irreversibility and redox asymmetry of lithium-rich layered oxide cathodes. Nat. Commun. 14, 4149 (2023).

13	Merryweather, A. J., Schnedermann, C., Jacquet, Q., Grey, C. P. & Rao, A. Operando optical tracking of single-particle ion dynamics in batteries. Nature 594, 522-528 (2021).

14	Xu, C. et al. Operando visualization of kinetically induced lithium heterogeneities in single-particle layered Ni-rich cathodes. Joule 6, 2535-2546 (2022).

15	House, R. A. et al. Superstructure control of first-cycle voltage hysteresis in oxygen-redox cathodes. Nature 577, 502-508 (2020).

16	Boivin, E. et al. Bulk O2 formation and Mg displacement explain O-redox in Na0.67Mn0.72Mg0.28O2. Joule 5, 1267-1280 (2021).

17	Meng, X.-H. et al. Kinetic Origin of Planar Gliding in Single-Crystalline Ni-Rich Cathodes. J. Am. Chem. Soc. 144, 11338-11347 (2022).