| Table S1 Converter slag-added solutions |  |
| --- | --- |
| Solution (abbreviation) | Preparation method |
| Converter slag-added solution (CSS) | 0, 15, 75, and 750 mg of well-milled converter slag were mixed with 500 ml of sterilized distilled water, respectively, followed by filtration |
| Neutralized converter slag-added solution (NCSS) | CSS neutralized to pH 6.5 by 0.1 M HCl and 0.1 M NaOH |
| Soil extract (SE) | Solution extracted from a mixture of 500 g of dry soil and 300 ml of distilled water |
| Converter slag-added soil extract (CSSE) | Solution extracted from a mixture of 1.5 g of well-milled converter slag, 500 g of dry soil, and 300 ml of distilled water |

Table S2 Chemical composition of the converter slag

|  | T a-Ca | T-Mg | T-P2O5 | T-Fe | T-SiO2 | T-Mn | T-B | CaO | MgO | P2O5 | Fe2O3 | SiO2 | Mn | B |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mean b | 26000 | 4333 | 1600 | 23667 | 16667 | 196 | 4.07 | 12667 | 15.33 | 2.93 | 867 | 547 | 0.29 | 0.09 |
| SD c | 1000 | 153 | 100 | 577 | 577 | 306 | 0.90 | 1155 | 1.53 | 1.67 | 58 | 15.28 | 0.05 | 0.02 |

a Total

b Average of three replicates (mg/100 g)

c Standard deviation

Table S3 Analysis of soil compounds

|  |  | pH |  | CEC a |  | BS b |  | CaO | MgO | K2O | P2O5 | Fe2O3 | SiO2 | Mn | B |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | cmol/kg |  | (%) |  | mg/100 g |  |  |  |  |  |  |  |
| Mean c |  | 5.5 |  | 10.2 |  | 60.1 |  | 140 | 14.7 | 17.3 | 10 | 966.7 | 9.4 | 3.1 | 0.02 |
| SD d |  | 0.1 |  | 0.7 |  | 3.6 |  | 0 | 0.6 | 0.6 | 0 | 57.7 | 1.4 | 0 | 0 |

a Cation-exchange capacity

b Base saturation (%)

c Average of three replicates

d Standard deviation