Table.1 Nominal chemical composition of Al-12 powder (wt%).

| Elements | Si | Mg | Cu | Ni | Fe | Mn | Zn | Al |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Content | 12.0-12.5 | ≤ 1.0 | ≤ 0.8 | ≤ 1 | ≤ 0.2 | ≤ 0.04 | ≤ 0.01 | Balance |

Table.2 Nominal chemical composition of Fe Amorphous powder (wt%).

| Elements | Cr | Mo | B | C | Fe |
| --- | --- | --- | --- | --- | --- |
| Content | ≤ 5.0 | ≤ 2.0 | ≤ 2.5 | ≤ 7.5 | Balance |

Table. 3 Friction coefficients (f), wear scar parameters (d, w, A), and wear volume (Ws) of the samples.

| Sample | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Friction coefficient f | 0.200 | 0.164 | 0.154 | 0.178 | 0.181 | 0.186 | 0.127 | 0.138 |
| Wear scar depth d (mm×10-2) | 6.20 | 4.56 | 3.76 | 4.95 | 5.65 | 5.89 | 2.43 | 3.27 |
| Wear scar width w (mm) | 1.03 | 0.84 | 0.80 | 0.93 | 1.01 | 1.02 | 0.63 | 0.70 |
| Wear scar area A (mm2×10-2) | 4.27 | 2.50 | 2.00 | 3.04 | 3.73 | 3.96 | 1.00 | 1.58 |
| Wear rate Ws (×10-5 mm3·(N·m)-1) | 9.49 | 5.56 | 4.44 | 6.76 | 8.29 | 8.8 | 2.23 | 3.51 |