### Supplementary Information

### Figure Captions

Fig. S1 XRD plots of CF-biochar.

Fig. S2 Isotherm models (a) Langmuir model; (b) Freundlich model; (c) Tempkin model; (d) D-R model.

Fig. S3 Effect of temperature on the catalytic oxidation of CF-biochar, Biochar, and PMS.

Fig. S4 Biochar (a) and CF-biochar (b) contact angle plots.

Fig. S5 (a) IR spectra before and after modification of CF-biochar; (b) IR spectra before and after adsorption of CF-biochar.

Table Captions

Table S1 Physico-chemical properties of TZD.

Table S2 CF-biochar and Biochar isotherm model parameters

Table S1

| Parameter | Character |
| --- | --- |
| Molecular formula | C17H16FN6O6P |
| CAS number | 856867-55-5 |
| Molar mass | 450.32 |
| Density | 1.75±0.1 g cm-3 |
| pKa | 1.81±0.10 |
| Stability | hygroscopic |
| Solubility in water | slightly |
| Storage condition | under inert gas (nitrogen or Argon) at 2-8 °C |
| Molecular structural |  |

Table S2

| Isotherm model | Parameter | Parameters value |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | CF-biochar | CF-biochar+PMS | Biochar | Biochar+PMS |
| Langmuir | (mg g-1) | 3322.74 | 20548.21 | 742.47 | 1219.30 |
|  | (L mg-1) | 0.00030 | 0.00005 | 0.00144 | 0.00079 |
|  |  | 0.87491 | 0.85643 | 0.96939 | 0.97854 |
| Freundlich | (mg g-1) | 2.3627 | 2.0439 | 4.0453 | 2.7612 |
|  |  | 1.0551 | 1.0082 | 1.2525 | 1.1301 |
|  |  | 0.99919 | 0.99992 | 0.99894 | 0.99962 |
| Tempkin | (L mg-1) | 206.1456 | 205.0576 | 133.2138 | 148.5580 |
|  |  | -3.6272 | -3.5634 | -3.3159 | -3.3912 |
|  |  | 0.99118 | 0.99755 | 0.99758 | 0.99677 |
| D-R | (mg g-1) | 439.11 | 575.02 | 371.33 | 428.52 |
|  | (kJ mol-1) | 0.0221 | 0.0287 | 0.0221 | 0.0260 |
|  |  | 0.98607 | 0.99222 | 0.99302 | 0.98983 |

Text S1

Pseudo-first order model                 (4)

Pseudo-second order model                       (5)

Intra-particle diffusion model                       (6)

where  is the adsorption time; and  are the rate constants of pseudo-first-order and pseudo-second-order models, respectively;  is liquid film diffusion constants;  the constant to describe the thickness of the bounder layer.

Text S2

Langmuir isotherm                            (7)

Freundlich isotherm                       (8)

Temkin isotherm                           (9)

D-R isotherm                   (10)

Where (mg g-1) is the equilibrium adsorption capacity; (mg L-1 ) the concentration of equilibrium;  the monolayer saturation adsorption capacity;  the Langmuir adsorption equilibrium constant;  and  are the Freundlich constants, related to the adsorbent, adsorbate type and temperature;  is the Temkin constant reflecting the adsorption heat;  (L mg-1) is the Temkin binding constant reflecting the maximum combine energy.

Text S3

(11)

(12)

(13)

(14)

where  (mL g-1) is the thermodynamic equilibrium constan