Supplementary Material

Insight into catalytic effects of alkali metal salts addition on bamboo and cellulose pyrolysis

Wei Chena, b, Xuan Taoa, Xiaolei Shia, Wenjuan Guoa, Yurou Wanga, Biao Liub, c, Haiping Yangb, *

aCollege of Engineering, Nanjing Agricultural University, 40 Dianjiangtai Road, Nanjing 210031, China

bState Key Laboratory of Coal Combustion, School of Power and Energy Engineering, Huazhong University of Science and Technology, Wuhan 430074, China.

cState Grid Hunan Integrated Energy Service Company Limited, Changsha 410007, China

Correspondence information: Haiping Yang, yhping2002@163.com; 1037 Luoyu Road, Wuhan 430074, China; Tel: +086+027-87542417-8109; fax: +086+027-87545526.

List of contents

Table S1. Bio-oil compositions from cellulose catalytic pyrolysis.

Table S2. Bio-oil compositions from bamboo catalytic pyrolysis.

Table S3. A summary for FTIR bands of main gaseous products and functional groups.

Table S1. Bio-oil compositions from cellulose catalytic pyrolysis.

| Species | SiO2 | KCl | K2SO4 | K2CO3 | NaCl | NaSO4 | Na2CO3 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Linear aliphatic compound |  |  |  |  |  |  |  |
| Acetic acid | 1.2 | 2.2 | 1.7 | - | 3.3 | 1.9 | - |
| 2-Propanone, 1-hydroxy- | 0.9 | 1.9 | 2.9 | 14.6 | 3.9 | 2.4 | 12.0 |
| Acetoin | - | - | - | 3.2 | - | - | 3.5 |
| 1-Hydroxy-2-butanone | 0.3 | 0.6 | 0.9 | 1.7 | 1.0 | 0.7 | 2.0 |
| Butanoic acid, 4-hydroxy- | - | - | - | 5.1 | - | - | 3.5 |
| Furan compound |  |  |  |  |  |  |  |
| Furfural | 4.1 | 5.9 | 5.5 | - | 6.5 | 4.7 | - |
| 2-Furanmethanol | - | - | 0.9 | 5.1 | 2.3 | - | 5.5 |
| 2-Furancarboxaldehyde, 5-methyl- | 1.1 | 2.6 | 2.0 | 1.3 | 3.2 | 1.8 | 1.5 |
| 5-Hydroxymethylfurfural | 1.6 | 4.5 | 2.2 | - | 5.3 | 2.5 | - |
| Cyclopentanone compound |  |  |  |  |  |  |  |
| Cyclopentanone | - | - | - | 2.7 | - | - | 3.7 |
| 2-Cyclopenten-1-one | - | - | - | 8.2 | - | - | 8.3 |
| Cyclopentanone, 2-methyl- | - | - | - | 2.1 | - | - | 2.3 |
| Cyclopentanone, 3-methyl- | - | - | - | 1.3 | - | - | 1.5 |
| 2-Cyclopenten-1-one, 2-methyl- | - | 1.2 | 0.9 | 5.7 | 0.9 | 0.6 | 6.9 |
| 1,2-Cyclopentanedione | 1.7 | 2.5 | 1.3 | - | 2.2 | 1.4 | - |
| 2-Cyclopenten-1-one, 3-methyl- | 0.4 | 0.5 | 0.8 | 4.5 | 0.6 | 0.5 | 5.1 |
| 2-Cyclopenten-1-one, 3,4-dimethyl- | - | - | 0.6 | 1.8 | - | - | 2.1 |
| 2-Cyclopenten-1-one, 2,3-dimethyl- | - | - | - | 2.2 | - | - | 2.6 |
| 1,2-Cyclopentanedione, 3-methyl- | 1.1 | 1.9 | 3.2 | 4.1 | 3.0 | 2.3 | 4.4 |
| 2-Cyclopenten-1-one, 2,3-dimethyl- | - | - | 0.3 | 3.4 | - | - | 4.5 |
| 2-Cyclopenten-1-one, 2-hydroxy-3,4-dimethyl- | - | - | 1.1 | 5.5 | - | - | 6.3 |
| 2-Cyclopenten-1-one, 3,4,4-trimethyl- | - | - | - | 1.5 | - | - | 2.0 |
| 2-Cyclopenten-1-one, 3-ethyl- | - | - | - | 1.8 | - | - | - |
| 2-Cyclopenten-1-one, 3-ethyl-2-hydroxy- | - | - | 0.4 | 2.8 | 0.4 | - | 2.4 |
| Phenyl compound |  |  |  |  |  |  |  |
| Phenol | - | - | - | 1.4 | 0.9 | 0.7 | 1.0 |
| p-Cresol | - | - | - | 2.7 | - | - | 4.4 |
| 1,2-Benzenediol, 3-methoxy- | - | - | - | 1.8 | - | - | 1.8 |
| Phenol, 3,5-dimethyl- | - | - | - | 2.7 | - | - | - |
| Anhydrosugar and pyrone |  |  |  |  |  |  |  |
| 2H-Pyran-2-one, 4-methoxy-6-methyl | - | - | - | 2.3 | - | - | 2.2 |
| 4H-Pyran-4-one, 3,5-dihydroxy-2-methyl- | 3.4 | 3.5 | - | - | - | - | - |
| 1,4:3,6-Dianhydro-α-D-glucopyranose | 4.9 | 2.4 | 3.0 | - | 1.8 | 2.8 | - |
| 1,6-Anhydro-β-D-glucopyranose | 59.2 | 53.2 | 57.7 | - | 48.6 | 60.9 | - |
| 1,6-Anhydro-α-D-galactofuranose | 6.8 | 2.6 | 5.3 | - | 1.3 | 4.4 | - |

Table S2. Bio-oil compositions from bamboo catalytic pyrolysis.

| Species | SiO2 | KCl | K2SO4 | K2CO3 | NaCl | NaSO4 | Na2CO3 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Linear aliphatic compound |  |  |  |  |  |  |  |
| 2,3-Butanedione | 1.5 | 1.1 | 1.2 | - | 0.9 | 0.9 | 0.3 |
| 2-Butanone | 1.0 | 0.8 | 0.6 | 1.2 | 0.4 | 0.5 | 0.8 |
| Acetic acid | 18.6 | 16.7 | 17.9 | - | 18.5 | 17.7 | - |
| 2-Propanone, 1-hydroxy- | 4.1 | 3.9 | 3.5 | 1.7 | 3.9 | 3.5 | 2.1 |
| 1-Hydroxy-2-butanone | 2.4 | 2.3 | 2.2 | 1.1 | 2.1 | 1.9 | 1.3 |
| Succindialdehyde | 1.0 | 1.1 | 1.1 | - | 1.1 | 1.0 | - |
| 1,2-Ethanediol, diacetate | 1.0 | 0.9 | 1.0 | - | 1.0 | 0.9 | - |
| Furan compound |  |  |  |  |  |  |  |
| Furfural | 5.9 | 5.4 | 5.3 | 4.2 | 4.9 | 4.9 | 5.5 |
| 2-Furanmethanol | 2.7 | 2.8 | 2.6 | 1.3 | 2.6 | 2.5 | 1.0 |
| Cyclopentanone compound |  |  |  |  |  |  |  |
| Cyclopentanone | - | - | - | 1.2 | - | - | 1.2 |
| 2-Cyclopenten-1-one, 2-methyl- | 1.2 | 1.2 | 1.0 | 2.8 | 0.9 | 0.9 | 3.2 |
| 1,2-Cyclopentanedione | 1.6 | 1.7 | 2.0 | - | 1.8 | 1.5 | - |
| 2-Cyclopenten-1-one, 3-methyl- | 0.9 | 0.9 | 0.5 | 2.6 | 0.6 | 0.7 | 2.8 |
| 1,2-Cyclopentanedione, 3-methyl- | 3.1 | 3.3 | 2.7 | 2.0 | 2.8 | 2.9 | - |
| Phenols |  |  |  |  |  |  |  |
| Phenol | 2.8 | 2.9 | 2.2 | 6.5 | 2.5 | 2.4 | 6.9 |
| Phenol, 2-methyl- | 1.8 | 2.0 | 1.2 | 5.1 | 1.6 | 1.7 | 4.9 |
| p-Cresol | 2.8 | 2.8 | 2.3 | 6.4 | 2.5 | 2.6 | 6.4 |
| Phenol, 2-methoxy- | 1.9 | 2.5 | 1.7 | 5.0 | 1.8 | 1.6 | 4.5 |
| Phenol, 2,3-dimethyl- | - | - | - | 2.6 | 0.4 | 0.5 | 2.3 |
| Phenol, 2,4-dimethyl- | - | - | - | 2.7 | - | - | 1.9 |
| Phenol, 2,5-dimethyl- | - | - | - | 2.1 | - | - | 1.4 |
| Phenol, 4-ethyl- | 3.4 | 2.8 | 2.7 | 11.7 | - | 3.5 | 11.4 |
| Phenol, 3,5-dimethyl- | - | - | - | 2.4 | - | - | 2.1 |
| Creosol | 1.3 | 1.6 | 1.2 | 1.3 | 1.1 | 1.2 | 1.0 |
| Phenol, 3,4-dimethyl- | - | - | - | 1.5 | - | - | 1.3 |
| Catechol | 2.5 | 2.4 | 3.2 | - | 3.5 | 3.6 | - |
| 4-Vinylphenol | 9.7 | 10.5 | 9.3 | 4.2 | 9.7 | 9.3 | 8.6 |
| Benzene, 1-ethyl-4-methoxy- | - | - | - | 4.0 | - | - | 2.6 |
| Phenol, 3-ethyl-5-methyl- | - | - | - | 2.9 | - | - | 2.8 |
| 1,2-Benzenediol, 3-methoxy- | 1.9 | 2.9 | 4.2 | - | 4.2 | 4.3 | - |
| Phenol, 2,3,5-trimethyl- | - | - | - | 1.6 | - | - | 1.2 |
| Phenol, 4-ethyl-2-methoxy- | 1.3 | 1.6 | 1.8 | 3.6 | 1.8 | 1.5 | 3.0 |
| 1,2-Benzenediol, 4-methyl- | 1.6 | - | 1.6 | - | 1.8 | 2.1 | - |
| 2-Methoxy-4-vinylphenol | 2.4 | 3.0 | 2.3 | - | 2.3 | 2.0 | 1.8 |
| Phenol, 2,6-dimethoxy- | 3.9 | 5.2 | 3.7 | 6.7 | 3.9 | 1.4 | 6.7 |
| Phenol, 3,4-dimethoxy- | 1.5 | 1.3 | 1.5 | - | 1.5 | 1.6 | - |
| 3,5-Dimethoxy-4-hydroxytoluene | 1.5 | 1.9 | 1.6 | 1.9 | 1.5 | 1.3 | 0.8 |
| trans-Isoeugenol | 1.4 | 1.6 | 1.3 | 1.5 | 1.3 | 1.2 | 1.7 |
| 4-Ethylbiphenyl | 1.1 | 1.5 | 1.9 | 3.1 | 1.2 | 3.4 | 2.4 |
| (E)-2,6-Dimethoxy-4- (prop-1-en-1-yl)-phenol | 1.7 | 2.3 | 1.7 | 1.2 | 1.6 | 1.4 | 1.2 |
| Anhydrosugar |  |  |  |  |  |  |  |
| 1,6-Anhydro-β-D-glucopyranose | 4.8 | 2.8 | 5.0 | - | 4.9 | 4.6 | - |

Table S3. A summary for FTIR bands of main gaseous products and functional groups.

| Wave number (cm-1) | Functional groups and structures |
| --- | --- |
| 3400-3650 | -OH stretching vibration from phenols and alcohols |
| 3010-3100 | Aromatic C-H stretching vibration |
| 2860-2960 | Alkyl and aliphatic C-H stretching vibration |
| 1720-1750 | C=O stretching vibration from ketone and aldehyde |
| 1708 | C=O stretching vibration from esters |
| 1610-1700 | C=O stretching vibration conjugated to the aromatic ring, aromatic ring vibration |
| 1500,1600 1460-1600 | Aromatic skeletal vibration combined with C-H in plane deformation |
| 1420-1460 | O-CH3 stretching vibration |
| 1370-1400 | O-H bending of Acid |
| 1240-1320 | Esters, epoxides and acyclic C-O-C groups conjunction with C=C in olefinic or aromatic structures |
| 1230-1250 | C-O-C stretching vibration from aryl-alkyl ether linkage |
| 1110-1215 | aromatic C-O stretching vibration |
| 1000-1150 | C-O stretching vibration from alcohols |
| 730-900 | Aromatic C-H out of plane deformation |