Molecular Biology Reports

Supplementary Data

Optimization of the Redox-Sensitive Doxorubicin Loaded Chitosan-based Nanoparticles by Box–Behnken Experimental Design

Mahsa Babaei 1, Soheila Kashanian 2,3*, Zahra Salemi 4

1 Department of Biology, Faculty of Science, Razi University, Kermanshah, Iran

2 Faculty of Chemistry, Sensor and Biosensor Research Center (SBRC), Razi University, Kermanshah, Iran

3 Nanobiotechnology Department, Faculty of Innovative Science and Technology, Razi University, Kermanshah, Iran

4 Department of Biochemistry, Arak University of Medical Sciences, Arak, Iran

Corresponding Author: Kashanian_s@yahoo.com

Table A. The levels of dependent and independent variables employed in BBD

| Levels |  |  | Variables |
| --- | --- | --- | --- |
| High | Middle | Low |  |
| 2 1.5 3 | 1.25 1 2 Maximize | 0.5 0.5 1 | Independent variables A-Cs-Cys Con.(mg/ml) B-TPP Con. (mg/ml) C-Cs-Cys/TPP Dependent variables Y: %EE |

Table B. Different optimum conditions and predicted and observed EE% values

| Optimum /No. | Cs-Cys Con. (mg/ml) | TPP Con. (mg/ml) | Cs-Cys/TPP ratio | Predicted %EE | Observed EE% | Error% |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.257 | 1.075 | 2.092 | 81.28% | 78.82% | 4.25% |
| 2 | 1.255 | 1.189 | 2.052 | 82.406% | 78.63% | 4.58% |
| 3 | 1.194 | 1.197 | 2.260 | 81.396% | 78.56% | 3.48% |

Table C. Optimized NPs size, PDI, and zeta potential analysis by DLS and zeta sizer

| Optimized Formulation | Size (nm) | PDI | Zeta Potential (mv) |
| --- | --- | --- | --- |
| Cs-CysNPs-DOX | 144.55 | 0.262 | +35.2 |

Figure A. Size distribution of NPs by DLS