Supporting Information

A nanofluidic chemoelectrical generator with enhanced energy harvesting by ion-electron Coulomb drag

Yisha Jiang1,2,#, Tao Wang1,#, Wenchao Liu1, Yitian Wu1, Tingting Mei1, Li Wang1, Guoheng Xu1, Nannan Liu2,*, Yude Wang3,* and Kai Xiao1,*

1Department of Biomedical Engineering, Guangdong Provincial Key Laboratory of Advanced Biomaterials, Institute of Innovative Materials, Southern University of Science and Technology, Shenzhen, 518055, P.R. China.

2Key Laboratory of Carbon Materials of Zhejiang Province, College of Chemistry & Materials Engineering, Wenzhou University, Wenzhou, 325027, P.R. China.

3School of Materials and Energy, Yunnan University, Kunming, 650091, P.R. China.

# Yisha Jiang and Tao Wang contributed equally

*co-corresponding author

E-mail: liunannan@wzu.edu.cn;

E-mail: ydwang@ynu.edu.cn;

E-mail: xiaok3@sustech.edu.cn; xiaokai@iccas.ac.cn;

Supplementary Fig. 1 | The structure of the NCEG and the fabrication process of nitrogen-doped CNTM and the SEM images of the AAO substrate and CNTM.

Supplementary Fig. 2 | The XPS spectra of AAO substrate and CNTM.

Supplementary Fig. 3 | Optical image of bubbles generated on the surface of the electrode when the electrolyte was replaced by strong acid or alkaline solution.

Supplementary Fig. 4 | Top surface energy dispersive spectroscopy (EDS) mapping for the CNTM without contact to the electrolyte solution after 1 h testing.

Supplementary Fig. 5 | The deviation of current density values between (ΔJSC1) with and without electrolyte solution under a range of external voltage from -2 to 2 V.

Supplementary Fig. 6 | The current density difference (ΔJSC2) between theoretical value and measured value when different resistances were loaded in the circuit. U = 0.8 V is the average voltage output of the NCEG device, RS = 10000 Ω is the internal resistance of the device, determined by the maximum power output when the external resistance is equal to the internal resistance (Fig. 4a), and the RL is the load resistance, including 100, 500, 1000, 3000, 5000, and 10000 Ω.

Supplementary Fig. 7 | The influences of air flow (a) and light (b) on the output of the device.

Supplementary Fig. 8 | The voltage of fourteen NCEG devices that are connected in series. The inset is the optical photograph of the fourteen NCEG devices connected in series.

Supplementary Table 1 | Performance parameter comparison of hydroelectric devices in different working environments.

| Work environment | VOC (V) | JSC (μA·cm-2) | Power density (μw·cm-2) | Reference |
| --- | --- | --- | --- | --- |
| Moisture (50%RH) | 0.5 | 1 | 5 | 1 |
| Moisture (85%RH) | 1.38 | 4 | 5.52 | 2 |
| Moisture (93%RH) | 0.76 | 11.3 | 8.58 | 3 |
| Drop (30 μL) | 0.24 | 34.29 | 8.23 | 4 |
| Drop (0.1 mL) | 1.5 | 0.6 | 0.9 | 5 |
| Bulk water | 0.66 | 5.25 | 3.465 | 6 |
| Bulk water | 0.55 | 22 | 11 | 7 |
| 2 M NaCl | 1.04 | 2.36 | 2.45 | 8 |
| 2 M NaCl | 0.72 | 360 | 259.2 | 9 |
| 0.1 M NaCl | 0.8 | 800 | 74 | This work |

References

1.	Liu, X. et al. Power generation from ambient humidity using protein nanowires. Nature 578, 550-554 (2020).

2.	Wang, H. et al. Bilayer of polyelectrolyte films for spontaneous power generation in air up to an integrated 1,000 V output. Nat. Nanotechnol. 16, 811-819 (2021).

3.	Zhang, Y. et al. Sustainable power generation for at least one month from ambient humidity using unique nanofluidic diode. Nat. Commun. 13, 3484-3494 (2022).

4.	Bae, J. et al. Towards watt-scale hydroelectric energy harvesting by Ti3C2Tx-based transpiration-driven electrokinetic power generators. Energy Environ. Sci. 15, 123-135 (2022).

5.	Shao, B. et al. Freestanding silicon nanowires mesh for efficient electricity generation from evaporation-induced water capillary flow. Nano Energy 94, 106917-106929 (2022).

6.	Li, L. et al. Sustainable and flexible hydrovoltaic power generator for wearable sensing electronics. Nano Energy 72, 104663-104672 (2020).

7.	Shao, B. et al. Bioinspired hierarchical nanofabric electrode for silicon hydrovoltaic device with record power output. ACS Nano 15, 7472-7481 (2021).

8.	Li, L. et al. A novel, flexible dual-mode power generator adapted for wide dynamic range of the aqueous salinity. Nano Energy 85, 105970-105980 (2021).

9.	Jiang, Z. et al. Simultaneous electricity generation and steam production from a wide range of salinity by using unique nanofluidic diode. Nano Energy 108, 108220-108231 (2023).