# Electric-field-induced crystallization of Hf0.5Zr0.5O2 thin film based on phase-field modeling

Zhaobo Liua,b,  Xiaoming Shia,b,c, Jing Wanga,b, and Houbing Huanga,b*

aAdvanced Research Institute of Multidisciplinary Science, Beijing Institute of Technology, Beijing, 100081, China

bSchool of Materials Science and Engineering, Beijing Institute of Technology, Beijing, 100081, China

cDepartment of Physics, University of Science and Technology Beijing, Beijing, 100083, China

Supplementary Note 1: The crystallization of HZO film under different electric field.

We further applied varying electric field for 4000 times cycling. As it is considered that the critical electric field is 2MV/cm, the crystallization does not occur under applying electric field at 1MV/cm, which is shown in figure. S1. However, as the electric field magnitude increasing, the drive force intensified, which is manifested by the potential well at ηi,j,k=1 becoming deeper in double-well model, resulting in a faster transition to the crystalline phase. Hence, the degree of crystallinity will reach 1 with fewer cycles of the electric field.

Fig. S1. Simualted crystalline volume fraction under different electric field for 4000 cycles.

Supplementary Note 2: The polarization response of different states under readout electric field signals.

To analyze the stability of the four storage states, we applied electric fields of 1MV/cm as readout signals separately for 100 cycles. And the result is depicted in figure. S2, which illustrates that at varying degrees of crystallinity, applying a readout signal smaller than the critical field can maintain the polarization in a stable state, meeting the performance requirements for artificial synapses as information storage devices.

Fig. S2. The polarization response of different states under 1MV/cm electric field pulses as readout signals.