Supplementary material

Synergetic treatment of dihydroartemisinin and perillyl alcohol by liposomal nanoplatform for enhanced therapy of cerebral malaria and neurological injury alleviation in C57BL/6J mice

Guolian Ren1,*, †, Geng Wang1,†, Qiuyue Jin1, Xiaomin Niu1, Rongrong Wang1, Canqi Ping1, Jihong Qiang1, Qingxia Li1, Jingjing Han1, Ruili Wang1, Guoshun Zhang1, Shuqiu Zhang1,*

†Guolian Ren and Geng Wang contributed equally to this work.

*Correspondence: glren2007@126.com; shuqiu.zhang@126.com

1School of Pharmacy, Shanxi Medical University, Shanxi Provincial Key Laboratory of Medicine Synthesis and Advanced Pharmaceutics, 55 Wenhua Street, Jinzhong, 030619, China.

- The hydrogen spectrum of TPGS-Tyr.

- The hemolysis results of DP@Tyr-Lips incubated with erythrocytes under naked eye observation.

- The absorbance values of Evans Blue in the brain tissue homogenate supernatant after intravenously treated with different formulations via the tail vein (A). The quantitative analysis of Evans Blue content in the brain tissue of mice in each group (B) (P < 0.05，n=3).

- The predicted and experimental values of DP@Tyr-Lips prepared by the optimized prescription.

| Value | Predicted values | Experimental values | RE (%) |
| --- | --- | --- | --- |
| Size (nm) | 84.40 | 83.08 ± 0.927 | 1.5 |
| PDI | 0.295 | 0.324 ± 0.009 | 7.0 |
| EEDHA (%) | 99.48 | 87.53 ± 1.11 | 12.0 |
| EEPOH (%) | 85.51 | 81.44 ± 0.25 | 4.7 |

- The Size, PDI, Zeta potential, EE, and DL of DP@Tyr-Lips.

| Value | Size (nm) | PDI | EEDHA (%) | EEPOH (%) | DLDHA (%) | DLPOH (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Average | 91.99 | 0.32 | 88.60 | 82.89 | 14.70 | 12.00 |
| SD | 2.67 | 0.019 | 3.23 | 3.76 | 1.06 | 2.00 |

- In vitro hemolysis rate of DP@Tyr-Lips.

| Number |  | Concentration (mg/ml) | Visual observation | Absorbance | Hemolysis rate (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.600 |  | - | 0.0620 | 4.8 |
| 2 | 0.719 |  | - | 0.0620 | 4.8 |
| 3 | 0.839 |  | - | 0.0616 | 4.7 |
| 4 | 0.959 |  | - | 0.0630 | 5.0 |
| 5 | 1.079 |  | - | 0.0616 | 4.7 |
| 6 | 1.199 |  | - | 0.0620 | 4.8 |
| 7 | Purified water |  | + | 0.5920 | 100 |
| 8 | 0 |  | - | 0.035 | 0 |