Fabrication of New Hyper-Cross-linked polymer for Efficient Heavy metal Adsorption from Industrial Wastewater

Supportive data file

Table S1 Effect of adsorbent dose of R-HCP

| Initial concentration | Solution volume | Adsorbent Dose | Ce | Adsorption quantity | Removal Efficiency |
| --- | --- | --- | --- | --- | --- |
| mg/L | L | G | mg/g | mg/g | % |
| 10 | 0.05 | 0.1 | 2.91 | 3.55 | 70.9% |
| 10 | 0.05 | 0.2 | 1.58 | 2.11 | 84.2% |
| 10 | 0.05 | 0.3 | 1.16 | 1.47 | 88.4% |
| 10 | 0.05 | 0.4 | 0.79 | 1.15 | 92.1% |
| 10 | 0.05 | 0.5 | 0.73 | 0.92 | 92.7% |
| 10 | 0.05 | 0.6 | 0.73 | 0.92 | 92.7% |
| 10 Real Water sample 5 | 0.05 0.05 | 0.7 0.5 | 0.73 1.61 | 0.92 2.16 | 92.7% 83.9 % |

Table S2 Effect of different pH on adsorption

| Initial Concentration | Solution volume | Adsorbent Dose | Solution pH | Ce | Removal Efficiency |
| --- | --- | --- | --- | --- | --- |
| mg/L | L | G |  | mg/g | % |
| 10 | 0.05 | 0.5 | 2 | 5.37 | 40.9 |
| 10 | 0.05 | 0.5 | 4 | 3.78 | 62.2 |
| 10 | 0.05 | 0.5 | 6 | 2.54 | 78.6 |
| 10 | 0.05 | 0.5 | 8 | 1.23 | 88.5 |
| 10 | 0.05 | 0.5 | 10 | 0.85 | 93.5 |
| 10 | 0.05 | 0.5 | 12 | 1.89 | 84.2 |

Table S3: effect of contact time on adsorption.

| Initial Concentration | Solution volume | Adsorbent Dose | Contact Time | Ce | Adsorption Quantity | Removal Efficiency |
| --- | --- | --- | --- | --- | --- | --- |
| mg/L | L | G | Min | mg/L | mg/g | % |
| 10 | 0.05 | 0.5 | 1 | 4.71 | 0.54 | 54.9 |
| 10 | 0.05 | 0.5 | 3 | 2.39 | 0.72 | 72.3 |
| 10 | 0.05 | 0.5 | 6 | 1.68 | 0.86 | 86.4 |
| 10 | 0.05 | 0.5 | 9 | 0.88 | 0.93 | 93.1 |
| 10 | 0.05 | 0.5 | 12 | 0.88 | 0.93 | 93.1 |
| 10 | 0.05 | 0.5 | 15 | 1.02 | 0.89 | 89.3 |
|  |  |  | 18 | 1.97 | 0.82 | 82.1 |

Table S4 effect of acid, base modifications and interfering ions on adsorption.

| Initial Concentration | Solution volume | Adsorbent Dose | Ionic effect | Ce | Percentage removal |
| --- | --- | --- | --- | --- | --- |
| mg/L | L | G |  | mg/L | % |
| 10 | 0.05 | 0.5 | HCl | 9.13 | 8.7 |
| 10 | 0.05 | 0.5 | NaOH | 0.85 | 91.5 |
| 10 | 0.05 | 0.5 | NaCl | 3.81 | 61.9 |
| 10 | 0.05 | 0.5 | KCl | 6.02 | 39.8 |
| 10 | 0.05 | 0.5 | MgCl2 | 2.71 | 72.9 |
| 10 | 0.05 | 0.5 | CaCl2 | 4.96 | 50.4 |

Table S5 effect of temperature.

| Initial concentration | Solution volume | Adsorbent dose | T (oC) | Ce | Removal Efficiency |
| --- | --- | --- | --- | --- | --- |
| mg/l | Ml | G |  | mg/l | % |
| 10 | 50 | 0.5 | 10 | 0.92 | 90.8% |
| 10 | 50 | 0.5 | 20 | 1.58 | 84.2% |
| 10 | 50 | 0.5 | 30 | 2.14 | 78.6% |
| 10 | 50 | 0.5 | 40 | 2.91 | 70.9% |
| 10 | 50 | 0.5 | 50 | 3.41 | 65.9% |
| 10 | 50 | 0.5) | 60 | 4.19 | 58.1% |

Table S6 results for Langmuir adsorption isotherm

| Initial concentration | Equilibrium concentration | Adsorbent Dose | Adsorption quantity | 1/Ce | 1/qe |
| --- | --- | --- | --- | --- | --- |
| mg/L | L | G |  |  |  |
| 10 | 3.17 | 0.5 | 0.68 | 0.315 | 1.464 |
| 20 | 8.49 | 0.5 | 1.15 | 0.12 | 0.87 |
| 30 | 16.02 | 0.5 | 1.398 | 0.062 | 0.72 |
| 60 | 37.78 | 0.5 | 2.22 | 0.026 | 0.45 |
| 100 | 71.64 | 0.5 | 2.84 | 0.0139 | 0.352 |
| 150 | 118.20 | 0.5 | 3.18 | 0.008 | 0.314 |

Table S7 Results for Freundlich adsorption isotherm

| Initial concentration | Equilibrium concentration | Adsorbent Dose | Adsorption quantity | ln Ce | ln qe |
| --- | --- | --- | --- | --- | --- |
| mg/L | L | G |  |  |  |
| 10 | 3.17 | 0.5 | 0.68 | 1.15 | -0.381 |
| 20 | 8.49 | 0.5 | 1.15 | 2.14 | 0.13 |
| 30 | 16.02 | 0.5 | 1.398 | 2.77 | 0.33 |
| 60 | 37.78 | 0.5 | 2.22 | 3.63 | 0.79 |
| 100 | 71.64 | 0.5 | 2.84 | 4.27 | 1.04 |
| 150 | 118.20 | 0.5 | 3.18 | 4.77 | 1.16 |

Table S8 Results for Temkin adsorption isotherm

| Initial Concentration | Equilibrium Concentration | Adsorbent Dose | Adsorption quantity | ln Ce |
| --- | --- | --- | --- | --- |
| mg/L | L | G |  |  |
| 10 | 3.17 | 0.5 | 0.68 | 1.15 |
| 20 | 8.49 | 0.5 | 1.15 | 2.14 |
| 30 | 16.02 | 0.5 | 1.398 | 2.77 |
| 60 | 37.78 | 0.5 | 2.22 | 3.63 |
| 100 | 71.64 | 0.5 | 2.84 | 4.27 |
| 150 | 118.20 | 0.5 | 3.18 | 4.77 |

Table S9 results for Pseudo 1st order kinetic data.

| Equilibrium concentration | Adsorption time | Adsorption quantity | Qt | (qe-qt) | ln(qe-qt) |
| --- | --- | --- | --- | --- | --- |
| Mg/l | Min | Qe |  |  |  |
|  | 1 | 0.54 | 0.28 | 0.26 | -1.34 |
| 2.71 | 3 | 0.73 | 0.54 | 0.19 | -1.66 |
| 1.39 | 6 | 0.861 | 0.73 | 0.13 | -2.03 |
| 0.68 | 9 | 0.93 | 0.86 | 0.069 | -2.67 |

| Equilibrium Concentration | Adsorption time | Adsorption quantity | Qt | t/qt |
| --- | --- | --- | --- | --- |
| Mg/l | Min | Qe |  |  |
|  | 1 | 0.54 | 0.28 | 17.87 |
| 2.71 | 3 | 0.73 | 0.54 | 18.51 |
| 1.39 | 6 | 0.861 | 0.73 | 27.39 |
| 0.68 | 9 | 0.93 | 0.86 | 34.84 |

Table S10 results for Pseudo 2nd order kinetic data

Table S11 Results of regeneration study

| Adsorbent | R-HCP |
| --- | --- |
| Adsorbate | Cadmium ion |
| Chemical Used | 1M HNO3 |
| Contact Time | 1 Hour |
| Desorption Efficiency | 82% |