Preparation of NiFeCoMnCr Hydroxide on Nickel Foam by Corrosion Method and its Enhanced Electrochemical Performance in Oxygen Evolution Reaction

Hyein Lee, Han Minho, Noh Heejin, Taekyung Yu*

Department of Chemical Engineering, College of Engineering, Integrated Engineering Major, Kyung Hee University, Yongin 17140, Korea.

* Corresponding Author: tkyu@khu.ac.kr (T. Y.)

Figure S1. a) Typical and b) high-resolution SEM images of bare Ni foam.

Figure S3. XRD patterns of the synthesized samples.

Figure S4. TEM and EDX elemental mapping images of the a) NiFe(OH)x/NF, b) NiFeCo(OH)x/NF, and c) NiFeCoMn(OH)x/NF.

Figure S5. Cyclic voltammetry curves of the a) NiFe(OH)x/NF, b) NiFeCo(OH)x/NF, C) NiFeCoMn(OH)x/NF, and d) NiFeCoMnCr(OH)x/NF in non-faradaic regions.

Figure S6. Chronopotentiometric response of the NiFeCoMnCr(OH)x/NF at current density of 100 mA/cm2 for 30 h.

Table S1. Redox potential table

| Electrode pair | Potential [V] |
| --- | --- |
| Fe3+/Fe2+ | 0.771 |
| Ni2+/Ni | -0.257 |
| Co2+/Co | -0.280 |
| Mn2+/Mn | -1.18 |
| Cr3+/Cr | -0.744 |
| O2/OH- | 0.401 |

Table S2. Molar ratio of synthesized samples

|  | Fe | Co | Mn | Cr |
| --- | --- | --- | --- | --- |
| NiFe(OH)x /NF | 1 |  |  |  |
| NiFeCo(OH)x/NF | 1 | 0.8 |  |  |
| NiFeCoMn(OH)x/NF | 1 | 0.83 | 0.5 |  |
| NiFeCoMnCr(OH)x /NF | 1 | 0.88 | 0.75 | 1 |