Supplementary Information for

P123-CoMgAl nanocomposite for sustainable and high-conversion epoxide ring-opening polymerization

Xiao Xua,b , Xiaoyan Caoa,b , Yipeng Yanga,b , Fangyi Chena,b , Zhenggui Gu a,b*

a School of Chemistry and Materials Science, Nanjing Normal University, Nanjing 210023, China

b Jiangsu Provincial Key Laboratory of Materials Cycling and Pollution Control, Nanjing Normal University, Nanjing 210023, China

*Corresponding Author

Email: 07160@njnu.edu.cn

Phone: +86 13801581773

Submission: January 6 2024

Supplementary Tables

Table S1 Textural properties of synthesized LDOs

| Catalyst | SBET (m2/g) | Pore volume (cm3/g) | DBJH（nm） |
| --- | --- | --- | --- |
| CoMgAl-LDO | 67.6 | 0.4 | 29.0 |
| CoMgAl-LDO (0.25wtP123) | 183.6 | 0.9 | 23.1 |
| CoMgAl-LDO (0.5wtP123) | 190.0 | 1.0 | 24.5 |
| CoMgAl-LDO (1wtP123) | 185.5 | 0.9 | 21.7 |

Table S2 Cystal structures of CoMgAl-LDH and CoMgAlLDH (P123)

| Catalyst | d(003) () | c() | d(110)() |  | a() |  |
| --- | --- | --- | --- | --- | --- | --- |
| CoMgAl-LDH | 7.754 | 23.26 |  | 1.529 |  | 3.059 |  |
| CoMgAlLDH(P123) | 7.684 | 23.05 |  | 1.528 |  | 3.056 |  |

Table S3 The number of basic sites of LDOs

| Samples | Maximum temperature (℃) | Quantity (mmol/g STP) |
| --- | --- | --- |
| MgAl-LDO | 101.6 | 0.451 |
|  | 308.0 | 3.601 |
|  | 645.0 | 0. 541 |
| MgAl-LDO(0.5wtP123) | 105.3 | 0.441 |
|  | 340.0 | 5.522 |
|  | 464.3 | 0.317 |
| CoMgAl-LDO | 101.1 | 0.322 |
|  | 387.3 | 9.035 |
|  | 553.4 | 0.354 |
| CoMgAl-LDO (0.5wtP123) | 104.8 | 0.281 |
|  | 385.4 | 9.242 |
|  | 543.2 | 0. 322 |

Table S4 Catalytic synthesis of MPPG using different catalysts

| Catalyst | PO/ glycerol （mol mol-1） | Xpo (%) | Mn | PDI | OHV (mgKOH/g) |
| --- | --- | --- | --- | --- | --- |
| Al2O3 | 7 | 25.04 | 194 | 1.12 | 869.0 |
| MgO | 7 | 42.82 | 266 | 1.11 | 633.1 |
| MgAl-LDH | 7 | 51.11 | 300 | 1.10 | 561.9 |
| MgAl-LDO | 7 | 65.02 | 356 | 1.08 | 472.8 |
| MgAl-LDO (P123) | 7 | 74.30 | 394 | 1.08 | 427.5 |
| CeO2/MgAl-LDO (P123) | 7 | 92.04 | 466 | 1.04 | 361.4 |
| MCM-41@DMC | 7 | 90.60 | 460 | 1.12 | 366.0 |
| CoMgAl-LDH | 7 | 84.30 | 434 | 1.08 | 387.6 |
| CoMgAl-LDO | 7 | 95.10 | 478 | 1.06 | 352.0 |
| CoMgAl-LDO (P123) | 7 | 96.30 | 483 | 1.05 | 348.5 |

Supplementary Figures

Scheme. S1 Mechanism of anionic ring-opening polymerization of propylene oxide

Fig. S1 TEM of CoMgAl-LDO (P123)

Fig. S2 SEM images of synthesized catalysts. (a,b) CoMgAl-LDH(P123), (c,d) CoMgAl-LDO(P123)

Fig. S3 Elemental distributions of CoMgAl-LDO (P123)

Fig. S4 (a) XPS survey of the CoMgAl-LOD (P123) before and after catalysis. (b,c) TG-DTG profiles of MgAl-LDH (b) and CoMgAl-LDH (c)

Fig. S5 FT-IR spectra of standard and homemade PPG samples: (a) standard PPG and (b) homemade PPG

Fig. S6 Single-factor optimization of the polymerization reaction: (a) catalyst amount, (b) reaction temperature, (c) reaction time, and (d) reaction pressure

Fig. S7 Recycle tests of CoMgAl(P123). Error bars are determined by the standard deviation of 3 measurements