Topological transformation of synthetic ferromagnetic skyrmions: thermal assisted switching of helicity by spin-orbit torque

Kai Wu1,#, Yuelei Zhao1,#, Hongyuan Hao2,#,Sheng Yang1, Shuang Li1, Qingfang Liu2, Senfu Zhang2,3*, Xixiang Zhang3, Johan Åkerman4,5,6 and Yan Zhou1,*

1School of Science and Engineering, The Chinese University of Hong Kong, Shenzhen, Shenzhen, 518172, China

2Key Laboratory for Magnetism and Magnetic Materials of the Ministry of Education, Lanzhou University, Lanzhou, 730000, China

3Physical Science and Engineering Division, King Abdullah University of Science and Technology, Thuwal 23955-6900, Saudi Arabia.

4Department of Physics, University of Gothenburg, Gothenburg 41296, Sweden.

5Center for Science and Innovation in Spintronics, Tohoku University,2-1-1 Katahira, Aoba-ku, Sendai 980-8577, Japan.

6Research Institute of Electrical Communication, Tohoku University, 2-1-1 Katahira, Aoba-ku, Sendai 980-8577, Japan.

#These authors contributed equally.

*Corresponding Authors:

E-mail: zhangsenfu@lzu.edu.cn

E-mail: zhouyan@cuhk.edu.cn

(Dated: Dec. 11, 2023)

Fig.S1

Fig. S1 Waveform captured on the oscillometer, displaying the voltage response of the sample over time. In (a), a single current pulse of 500 μs duration at a current density of ~2.10×1011 A/m2 is applied to create the skyrmion bubbles. The resistance of the sample is approximately 780 Ω. In (b)-(f), a series of repeating square-wave current pulses are applied to drive the motion of the skyrmion bubble. The current spacing varies across the panels: 980 μs in (b), (c); 180 μs in (d); 80 μs in (e); and 30 μs in (f). Panel (c) provides an enlargement of the black box in panel (b), highlighting a specific section of the waveform.