Supporting Information

Ligand-functionalized Anderson-type Polyoxometalate for Efficient Selective Cationic Dye Adsorption

Hongji Kang,aǂ Lili Yang,bǂ Yuqi Liu,a Ke Su,b Hao Zhang,a Xiaoxue Huang,a Lu Yanga*

[a] Shandong University of Technology, School of Chemistry and Chemical Engineering, Zibo, 255000, P. R. China.

[b] Shangqiu Product Quality Inspection and Research Center, Shangqiu, 476000, P. R. China.

(a)

(b)

(c)

Figure S1. Front, side, and top views of the POM-1 structure.

Figure S2. FT-IR spectrum of POM-1.

Figure S3. (a) XPS survey spectrum of POM-1; (b) C 1s XPS spectrum of POM-1.

Table S1. The structural formulas of used organic dyes.

|  | Structure | Size | Charge |
| --- | --- | --- | --- |
| MB |  | 7.3339 Å | +1 |
| Rh6G |  | 8.5652 Å | +1 |
| MO |  | 8.6609 Å | -1 |