High-performance and economic biodegradable composites based on polybutylene adipate terephthalate and modified lignin

Van-Dung Mai a,1, Gihyun Kwon b,1, Yewon Jang a, Jiho Min a, Jee-hoon Han b*, and Sung-Kon Kim, a *

a School of Chemical Engineering, School of Semiconductor and Chemical Engineering, and Clean Energy Research Center, Jeonbuk National University, Jeonju 54896, Republic of Korea

b Department of Chemical Engineering, Pohang University of Science and Technology, Pohang, 37673, Republic of Korea

1 These authors contributed equally to this work.

*Corresponding authors.

E-mail addresses: jhhan@postech.ac.kr (J.-h. Han), skkim@jbnu.ac.kr (S.-K. Kim)

Table S1 Input data for PBAT-mLigA and weight percentage of each material after modification

| Sample codes | PBAT |  | LigA |  | MDI |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | g | wt.% | g | wt.% | g | wt.% |
| PBAT | 1000 | 0 | 0 | 0 | 0 | 0 |
| PBAT-24mLigA1 | 989.11 | 98.91 | 10.00 | 1.00 | 0.89 | 0.09 |
| PBAT-48mLigA1 | 987.78 | 98.78 | 10.00 | 1.00 | 2.22 | 0.22 |
| PBAT-72mLigA1 | 987.43 | 98.74 | 10.28 | 1.03 | 2.29 | 0.23 |
| PBAT-24mLigA3 | 967.33 | 96.73 | 30.00 | 3.00 | 2.67 | 0.27 |
| PBAT-48mLigA3 | 963.33 | 96.33 | 30.00 | 3.00 | 6.67 | 0.67 |
| PBAT-72mLigA3 | 962.28 | 96.23 | 30.00 | 3.00 | 7.72 | 0.77 |
| PBAT-24mLigA5 | 945.56 | 94.56 | 50.00 | 5.00 | 4.44 | 0.44 |
| PBAT-48mLigA5 | 938.7 | 93.87 | 50.16 | 5.02 | 11.14 | 1.11 |
| PBAT-72mLigA5 | 937.14 | 93.71 | 50.00 | 5.00 | 12.86 | 1.29 |
| PBAT-24mLigA7 | 923.78 | 92.38 | 70.00 | 7.00 | 6.22 | 0.62 |
| PBAT-48mLigA7 | 914.45 | 91.45 | 70.00 | 7.00 | 15.55 | 1.56 |
| PBAT-72mLigA7 | 911.99 | 91.20 | 70.00 | 7.00 | 18.01 | 1.80 |

Table S2 Life cycle inventory sources of each material and energy for PBAT-mLigA composites

| ReCiPe 2016 Midpoint (H) V1.03 / World (2010) H |  |  |  |  |
| --- | --- | --- | --- | --- |
| Material |  |  | Type |  |
| Lignin | Sulfuric Acid |  | GLO | Production |
|  | Corn stover |  | US | Production |
| PBAT (Efficiency: 90%) | 1,4-butanediol |  | RoW | Production |
|  | Adipic acid |  | RoW | Production |
|  | Terephthalate | Para-xylene (Xylene) | RoW | Market |
|  |  | Industry water | RER | Industry |
|  |  | Electricity | RoW | Production |
| Methyl Diisocyanate |  |  | RoW | Market |
| Electricity (For Twin screw extruder) |  |  | RoW | Production |

| Table S3 Mass fraction of LigA, and MDI before and after surface modification |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Sample codes | Before modification |  |  | Modification condition |  | After modification |  |
|  | LigA (wt.%) | MDI (wt.%) | Et3N (wt.%) | Temp. | Time (h) | LigA (wt.%) | MDI (wt.%) |
| 24mLigAA | 48.44 | 49.08 | 2.48 | r.t. | 24 | 91.84 | 8.16 |
| 48mLigA | 48.68 | 48.82 | 2.49 | r.t. | 48 | 81.81 | 18.19 |
| 72mLigA | 48.73 | 48.65 | 2.62 | r.t. | 72 | 79.55 | 20.45 |

Table S4 Mechanical properties of PBAT, PBAT-LigA, and PBAT-mLigA composite

| Sample codes | Tensile strength (MPa) | Elongation at break (%) |
| --- | --- | --- |
| PBAT | 41.0±2.8 | 1074.9±10.0 |
| PBAT-LigA1 | 40.9±0.9 | 801.3±14.0 |
| PBAT-24mLigA1 | 43.7±0.9 | 871.8±11.2 |
| PBAT-48mLigA1 | 46.0±1.0 | 880.4±20.3 |
| PBAT-72mLigA1 | 44.4±1.7 | 872.8±17.1 |
| PBAT-LigA3 | 38.9±1.3 | 791.2±15.2 |
| PBAT-24mLigA3 | 43.1±1.6 | 844.7±16.1 |
| PBAT-48mLigA3 | 45.3±1.0 | 858.3±12.7 |
| PBAT-72mLigA3 | 43.6±1.4 | 859.0±15.5 |
| PBAT-LigA5 | 34.9±1.7 | 759.9±18.3 |
| PBAT-24mLigA5 | 42.4±1.2 | 818.3±26.9 |
| PBAT-48mLigA5 | 44.7±2.1 | 838.3±23.9 |
| PBAT-72mLigA5 | 42.5±2.1 | 831.1±18.7 |
| PBAT-LigA7 | 29.9±0.9 | 705.1±25.5 |
| PBAT-24mLigA7 | 30.9±1.5 | 770.4±30.5 |
| PBAT-48mLigA7 | 33.2±1.3 | 785.2±23.0 |
| PBAT-72mLigA7 | 30.8±1.6 | 785.3±25.4 |

Fig. S1 Torque of twin-screw extruder during blending process at various lignin contents: (a) 1 wt.%, (b) 3 wt.%, (c) 5 wt.%, and (d) 7 wt.%

Fig. S2 TGA and DTG curves of PBAT, PBAT-LigA, and PBAT-mLigA at various lignin contents: (a) 1 wt.%, (b) 3 wt.%, (c) 5 wt.%, and (d) 7 wt.%

Fig. S3 DSC curves of PBAT, PBAT-LigA and PBAT-mLigA at various lignin contents: (a) 1 wt.%, (b) 3 wt.%, (c) 5 wt.%, and (d) 7 wt.%

Table S5 Thermal properties of PBAT, PBAT-LigA, and PBAT-mLigA

| Sample codes | DSC |  |  | TGA |  |
| --- | --- | --- | --- | --- | --- |
|  | Tg (℃) | Tm (℃) | ΔHm (J/g) | Tonset (oC) | Tmax (oC) |
| PBAT | -33.2 | 129.5 | 8.2 | 387.7 | 412.7 |
| PBAT-LigA1 | -31.0 | 129.5 | 8.5 | 389.9 | 415.2 |
| PBAT-24mLigA1 | -31.5 | 129.4 | 8.4 | 389.6 | 412.9 |
| PBAT-48mLigA1 | -31.6 | 129.6 | 8.1 | 390.1 | 415.3 |
| PBAT-72mLigA1 | -31.3 | 129.6 | 8.1 | 390.0 | 414.7 |
| PBAT-LigA3 | -32.4 | 128.5 | 7.9 | 390.6 | 415.8 |
| PBAT-24mLigA3 | -32.8 | 128.4 | 7.8 | 391.2 | 415.6 |
| PBAT-48mLigA3 | -32.5 | 128.4 | 7.3 | 391.8 | 415.9 |
| PBAT-72mLigA3 | -32.6 | 128.2 | 7.1 | 391.3 | 415.1 |
| PBAT-LigA5 | -32.3 | 129.5 | 7.9 | 386.6 | 412.1 |
| PBAT-24mLigA5 | -32.7 | 128.6 | 7.7 | 388.5 | 413.2 |
| PBAT-48mLigA5 | -32.6 | 128.2 | 7.7 | 388.5 | 414.1 |
| PBAT-72mLigA5 | -32.9 | 127.4 | 7.3 | 388.0 | 412.8 |
| PBAT-LigA7 | -32.9 | 127.5 | 6.7 | 389.1 | 412.9 |
| PBAT-24mLigA7 | -32.8 | 128.5 | 6.5 | 388.8 | 412.2 |
| PBAT-48mLigA7 | -31.3 | 128.6 | 6.6 | 389.1 | 412.7 |
| PBAT-72mLigA7 | -32.3 | 128.2 | 5.9 | 389.1 | 414.1 |