Supplementary Information:

Lignite-based hard carbon high-performance potassium-ion batteries anode

Hui Yang1, Long Lei1, Yue Zhao, Dawei Lan, Shengli An, Yunying Liu*, Jinlong Cui*

School of Silicon Industry, Inner Mongolia University of Science & Technology, Baotou 014010, China

1These authors contributed equally to this work.

*Corresponding author at: Aerding Road 7#, Kundulun District, Inner Mongolia University of Science and Technology, Baotou 014010, China.

E-mail: jinlong_cuiyuan@foxmail.com (J. Cui),

yunying_liu@126.com (Y. Liu);

Characterization

The moisture and ash content of lignite is analyzed by the industrial analysis method of GB/T 212--2008; the content of humic acid is determined by the volumetric method of GB/T 11957--2001; the content of water-soluble humic acid and water-insoluble matter in lignite is characterized according to the test standard of sodium humate for agriculture in HGT 3278--2011.

Table S1. Chemical composition of lignite

| Component analysis, wt% (as received) |  |
| --- | --- |
| Ash | 10.15 |
| Moisture | 8.07 |
| Organic components | 81.78 |
| Main constituents, wt.% (on dry basis after pretreatment) |  |
| Total humic acid | 32.62 |
| Free humic acid | 24.93 |
| Alkali insoluble organic matter | 57.34 |
| SiO2 | 3.63 |
| Al2O3 | 1.13 |
| Fe2O3 | 1.65 |
| CaO | 1.11 |
| MgO | 0.33 |
| K2O | 0.12 |
| Na2O | 0.08 |
| Other compositions | 1.89 |

Table S2. Pore structure parameters of LC and LCN samples

| Sample | Specific surface area (m2 g-1) | Pore volume (cm3 g-1) | Average pore diameter (nm) |
| --- | --- | --- | --- |
| LC | 30.49 | 0.13 | 17.03 |
| LCN6/1 | 32.45 | 0.15 | 18.29 |
| LCN5/1 | 199.09 | 0.26 | 5.91 |
| LCN4/1 | 205.64 | 0.29 | 5.02 |

Table S3. Atomic percentage of different elements calculated from XPS spectra.

| Samples | Element content (wt.%) |  |  | Other compositions (wt.%) |
| --- | --- | --- | --- | --- |
|  | C (at.%) | O (at.%) | N (at.%) |  |
| LC | 79.55 | 19.83 | 0 | 0 |
| LCN6/1 | 73.4 | 21.76 | 4.72 | 0.12 |
| LCN5/1 | 68.01 | 22.23 | 9.62 | 0.14 |
| LC N4/1 | 64.06 | 23.03 | 12.80 | 0.11 |

Table S4. The content of different N in the total mass of LCN samples

| Samples | N-O (at.%) | Graphitic N (at.%) | Pyrrole N (at.%) | Pyridine N (at.%) |
| --- | --- | --- | --- | --- |
| LCN6/1 | 0.81 | 0.50 | 2.09 | 1.32 |
| LCN5/1 | 1.87 | 1.08 | 4.45 | 2.22 |
| LCN4/1 | 3.01 | 3.04 | 4.33 | 2.41 |

Table S5. Parameters of equivalent circuit components of LC and all LCN electrodes.

| Samples | Rs (ohm) | Rct (ohm) |
| --- | --- | --- |
| LC | 9.9 | 1750 |
| LCN6/1 | 7.4 | 908.8 |
| LCN5/1 | 6.9 | 506.7 |
| LCN4/1 | 5.7 | 489.5 |

Table S6. Comparison of electrochemical performance with hard carbon materials electrodes

| Samples | Current density (mA/g) | Cycles | Capacity (mAh/g) | Ref. |
| --- | --- | --- | --- | --- |
| Nitrogen-Doping Hard-Carbon | 200 | 100 | 224 | [1] |
| N-doped carbon | 100 | 200 | 242.5 | [2] |
| Nitrogen-doped Porous Carbon | 200 | 200 | 297 | [3] |
| Nitrogen Doped Porous Carbon | 100 | 100 | 289.1 | [4] |
| N-doped carbon fibers decorated with N-doped carbon clusters | 100 | 100 | 310 | [5] |
| S-doped flowerlike porous carbon | 100 | 700 | 206.3 | [6] |
| S-doped hard carbon | 100 | 1000 | 298.1 | [7] |
| N/S co-doped porous carbon | 50 | 70 | 289.7 | [8] |
| N/S co-doped porous carbon | 100 | 100 | 278 | [9] |
| S/N-co-doped graphite nanosheets | 200 | 100 | 159.5 | [10] |
| S, Se and N co-doped hard carbon | 100 | 450 | 207 | [11] |
| N/S co-doped porous carbon | 50 | 50 | 285.3 | [12] |
| N-doped hierarchical porous carbon | 100 | 100 | 314 | This work |
|  | 1000 | 1500 | 124.3 |  |

Figure S1. C 1s spectra of (a) LCN6/1 and (b) LCN4/1.

Figure S2. N 1s spectra of (a) LCN6/1 and (b) LCN4/1.

Figure S3. (a) initial charge/discharge profiles of LC and all LCN electrodes at 0.1 A g-1 and (b) charge/discharge profiles of LCN5/1 electrode at under different cycles at 0.1 A g-1

Figure S4. The equivalent circuit of LC and all LCN electrodes.

Figure S5. (a) CV curves at 0.05 mV s-1, (b) CV curves at diverse sweep rates from 0.1 to 5 mV s-1, (c) log(i) versus log(ν) plots of anodic and cathodic current response in (a), respectively, (d) capacity contribution ratios at diverse scan rates of LC.

Figure S6. (a) Cycling performance at 0.1 A/g of C3N4

References

[1] C.D. Chen, K. Zhao, M. La, C.H. Yang, Insight into a nitrogen-doping mechanism in a hard-carbon-microsphere anode material for the long-term cycling of potassium-ion batteries, Materials 15(12) (2022) 4249.

[2] C.L. Gao, Q. Wang, S.H. Luo, Z.Y. Wang, Y.H. Zhang, Y.G. Liu, A.M. Hao, R. Guo, J.-Y. Hwang, S.-T. Myung, Y.-K. Sun, High performance potassium-ion battery anode based on biomorphic N-doped carbon derived from walnut septum. J. Power Sources. 415 (2019) 165-171.

[3] Y.S. Zhou, Y.C. Zhu, B.S. Xu, X.J. Zhang, Nitrogen-doped porous carbon with complicated architecture and superior K+ storage performance, Sustain. Energy Fuels 5(2) (2021) 396-400.

[4] D.M. Zhang, Z.W. Chen, J. Bai, C.C. Yang, Q. Jiang, Highly nitrogen doped porous carbon nanosheets as high-performance anode for potassium-ion batteries, Batteries Supercaps. 3(2)(2019) 185-193.

[5] S.H. Chen, Y.H. Feng, J. Wang, E.J. Zhang, X.Z. Yu, B.A. Lu, Free-standing N-doped hollow carbon fibers as high-performance anode for potassium ion batteries, Sci. China Mater. 64(3) (2021) 547-556.

[6] Y.Q. Zuo, P. Li, R. Zang, S.J. Wang, Z.M. Man, P.X. Li, S.Y.Wang, W. Zhou, Sulfur-doped flowerlike porous carbon derived from metal-organic frameworks as a high-performance potassium-ion battery anode, ACS Appl. Energy Mater. 4(3) (2021) 2282-2291.

[7] X.Y. Chen, X.B. Cheng, Z.G. Liu, High sulfur-doped hard carbon anode from polystyrene with enhanced capacity and stability for potassium-ion storage, J. Energy Chem. 68 (2022) 688-698.

[8] H.L. Ma, X.J. Qi, D.Q. Peng, Y.X. Chen, D.C. Wei, Z.C. Ju, Q.C. Zhuang, Novel fabrication of N/S Co-doped hierarchically porous carbon for potassium-ion batteries, ChemistrySelect 4(39) (2019) 11488-11495.

[9] W.F. Liu, Y.T. Yang, P.G. Liu, Y.P. Huang, P.L. Li, T. Chen, Y. Zhuo, J. Yan, K.Y. Liu, Construction of nitrogen-sulfur co-doped porous carbon to boost, integrate Li/Na/K ion storage, Solid State Ion. 356 (2020).

[10] X. Wang, Z.C. Luo, J.T. Huang, Z. Chen, T. Xiang, Z.J. Feng, J. Wang, S.N. Wang, Y.C. Ma, H.Y. Yang, X.B. Li, S/N-co-doped graphite nanosheets exfoliated via three-roll milling for high-performance sodium/potassium ion batteries, J. Mater. Sci. Technol. 147 (2023) 47-55.

[11] Y. Liu, H.D Dai, Y.K. An, L.J. Fu Q.Y. An, Y.P. Wu, A facile and scalable synthesis of sulfur, selenium and nitrogen co-doped hard carbon anode for high performance Na- and K-ion batteries, J. Mater. Chem. A. 8(30) (2020) 14993-15001.

[12] L.F. Wang, S.J. Li, J.L. Li, S. Yan, X.Y. Zhang, D.H. Wei, Z. Xing, Q.C. Zhuang, Z.C. Ju, Nitrogen/sulphur co-doped porous carbon derived from wasted wet wipes as promising anode material for high performance capacitive potassium-ion storage, Mater. Today Energy 13 (2019) 195-204.