Highlights

on the research paper titled:

Synthesis of sodium silicate from the Acid leached calcined kaolinitic clay residue of aluminum sulfate industry

Nabil A. ABDULLAH*, Gamal H. Aboulfotouh*

*Research & Development Dept. of , Aluminum Sulphate Co. of Egypt, nabilxp9@gmail.com

- Acid leached calcined kaolinitic clay (the residue of alum industry) which is environmentally harmful acid solid waste can be utilized for synthesis of high-modulus sodium silicate.

- The leachate solution resulted from digestion of the acid leached kaolin was reused to prepare high basicity PAC.

- The silica extraction rate from ALCKC reached 88% and the SiO2:nNa2O of the prepared sodium silicate was 1.1 with NaOH–ALCKC ratio of 5:1 at the 20% NaOH at 75°C for 2 h.

- The recovery rate of amorphous silica from alkaline leachate reached 98.62% using sulfuric acid at pH of 7. Then liquid sodium silicate in combination with amorphous silica is used to prepare liquid sodium silicate with a modulus of 3 at 80°C for 3h.