Integrated Insulin-Iron Nanoparticles: A Multi-Modal Approach for Receptor-Specific Bioimaging, Reactive Oxygen Species Scavenging, and Wound Healing

Komal Attri1,4, Bhupendra Chudasama2,4*, Roop L. Mahajan3,4*, Diptiman Choudhury1,4*

1School of Chemistry and Biochemistry, Thapar Institute of Engineering and Technology, Patiala-147004, Punjab, India.

2School of Physics and Material Sciences, Thapar Institute of Engineering and Technology, Patiala-147004, Punjab, India

3Department of Mechanical Engineering, Virginia Tech, Blacksburg, VA 24061, United States; Institute for Critical Technology and Applied Science, Virginia Tech, Blacksburg, VA 24061, United States.

4TIET-VT Centre of Excellence for Emerging Materials, Thapar Institute of Engineering and Technology, Patiala-147004 Punjab, India.

*Corresponding E-mail: diptiman@thapar.edu, mahajanr@vt.edu, bnchudasama@thapar.edu

*Corresponding Phone:  +91-8196949843 / +1-5402312597 / +91-9781966136

Figure S1: Median plots of (a) FeSO4 salt (b) Insulin for finding the y-intercept and m values to calculate Dm to determine the combination index of iron and insulin.

Table S1 The table shows the % variation in mitochondrial reductase activity in MTT assay for determining cellular metabolism rate using HEKa cells. The cells were treated with varying concentrations; 1.5 µM, 7.5 µM, 15 µM, 30 µM of Insulin, FeSO4, Insulin + FeSO4 and IFe(II)NPs for a duration of 24 hours. The data was plotted as mean value ± SD of three independent experiments.

| % change in mitochondrial reductase activity |  |  |  |  |
| --- | --- | --- | --- | --- |
| Dose | Insulin | FeSO4 | FeSO4 + Insulin | IFe(II)NPs |
| 1.5 µM | 105.19 ± 6.25 % | 103.12 ± 8.00% | 104.42 ± 7.49 % | 114.60 ± 17.55 % |
| 7.5 µM | 109.67 ± 5.05 % | 104.36 ± 2.31 % | 112.12 ± 2.33 % | 129.79 ± 4.16 % |
| 15 µM | 113.86 ± 4.02 % | 108.14 ± 2.96 % | 116.72 ± 2.61 % | 136.28 ± 8.20 % |
| 30 µM | 129.88 ± 2.89 % | 109.91 ±2.88 % | 123.77 ± 7.93 % | 145.13 ± 2.96 % |

Table S2 It shows the p values calculated for % variation in wound diameter after treatment with 15 µM of Insulin, FeSO4, Insulin + FeSO4 and IFe(II)NPs. The data is considered to be statistically significant when p < 0.05.

| P value for checking the statistical significance of data |  |  |  |  |
| --- | --- | --- | --- | --- |
| Time | Insulin | FeSO4 | Insulin +FeSO4 | IFe(II)NPs |
| 8h | 0.000766 | 0.00844 | 0.000944 | 5.1E-05 |
| 16h | 0.001854 | 0.020972 | 8.07E-05 | 1.18E-05 |
| 32h | 0.000385 | 0.007966 | 0.001317 | 6.66E-05 |