## Table Caption

Table S1 Model and calculation equations of all equations, kinetic models, and isotherm models.

Table S2 Constants of pseudo-first-order and pseudo-second-order models for adsorbing hydroquinone on BC, BCNP-Fe, BCHNP-Fe, and BCP-Fe.

Table S3 Constants of intra-particle diffusion models for adsorbing hydroquinone on BC, BCNP-Fe, BCHNP-Fe, and BCP-Fe.

Table S4 Constants of film diffusion models for adsorbing hydroquinone on BC, BCNP-Fe, BCHNP-Fe, and BCP-Fe.

Table S5 Constants of isotherms for adsorbing hydroquinone on BC, BCNP-Fe, BCHNP-Fe, and BCP-Fe.

Table S6 Constants of thermodynamic for adsorbing hydroquinone on BC, BCNP-Fe, BCHNP-Fe, and BCP-Fe.

Table. S1

| Classification |  | Equation |  |  |  | Parameters |
| --- | --- | --- | --- | --- | --- | --- |
| - |  | Adsorption capacity |  | qe=(Co-Ce)Vm |  | Co (mg/L) and Ce (mg/L) are initial concentration and equilibrium concentration of adsorbent, V (L) is hydroquinone solution volume, and m (g) is biochar samples mass. |
|  |  | Adsorption efficiency |  | Removal (%)=Co-Ce×100Co |  |  |
| Kinetic models |  | Pseudo-first order model |  | ln(qe-qt) = lnqe–k1t |  | qt (mg/g) is adsorption capacity at t time, qe (mg/g) is adsorption capacity at equilibrium time, k1 (min-1) is pseudo-first order constant, k2 (min-1) is pseudo-second order constant, kid (mg/( g min12)) is intra-particle diffusion model rate constant, I (mg/g) is intra-particle diffusion model constant, k3 (mg/(g min)) is film-pore diffusion model rate constant, and A (mg/g) is film-pore diffusion model constant. |
|  |  | Pseudo-second order model |  | tqt=1k2qe2+tqe |  |  |
|  |  | Intra-particle diffusion model |  | qt=kidt12+I |  |  |
|  |  | Film diffusion diffusion model |  | ln(1-qtqe)=-k3t+A |  |  |
| Isotherm models |  | Langmuir isotherm model |  | Ceqe=1qmKL+Ceqm |  | Ce (mg/L) is equilibrium hydroquinone concentration, qe (mg/g) is equilibrium adsorption capacity, qm(mg/g) is the maximum adsorption capacity, KL(L/mg) is Langmuir adsorption equilibrium constant, KF ((mg/g)·(L/mg)1/n) is Freundlich adsorption equilibrium constant, n is Freundlich constant, R (=8.314J/(mol·K)) is gas constant, T (K) is absolute temperature, βT is Temkin constant, KT (L/g) is Temkin adsorption equilibrium constant, qD (mg/g) is D-R equilibrium adsorption capacity, E (KJ/mol) is average free energy of adsorption. |
|  |  | Freundlich isotherm model |  | lnqe=lnKF+1nlnCe |  |  |
|  |  | Temkin isotherm model |  | qe=RTβTln⁡(KTCe) |  |  |
|  |  | D-R isotherm model |  | lnqe=lnqD-RT2E2(ln⁡(1+1Ce))2 |  |  |
| Thermodynamic |  | Gibbs-Helmholtz equation |  | KC=qeCe ∆G°=∆H°-T∆S° ∆G°=-RTlnKC lnKC=∆S°R-∆H°RT |  | KC (L/g) is thermodynamic equilibrium constant, qe (mg/g) is adsorption capacity at equilibrium time, Ce (mg/L) is equilibrium hydroquinone concentration, ∆G° (KJ/mol) is Gibbs free energy, ∆H° (KJ/mol) is enthalpy, T (K) is absolute temperature, ∆S° (J/mol·K) is entropy, R (=8.314J/(mol·K)) is gas constant. |

Table. S2

| Adsorbate |  | qe,exp (mg/g) |  | Pseudo-first order model |  |  |  | Pseudo-second order model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | k1 | R2 | qe,cal(mg/g) |  | k2 | R2 | qe,cal(mg/g) |
| BC |  | 83.640 |  | 0.0339 | 0.953 | 71.389 |  | 0.00002 | 0.986 | 91.491 |
| BCNP-Fe |  | 94.872 |  | 0.0251 | 0.990 | 86.936 |  | 0.00002 | 0.976 | 103.093 |
| BCHNP-Fe |  | 92.928 |  | 0.0339 | 0.983 | 76.563 |  | 0.00001 | 0.984 | 96.993 |
| BCP-Fe |  | 96.984 |  | 0.0217 | 0.991 | 80.331 |  | 0.00002 | 0.989 | 104.603 |

Table. S3

| Adsorbate |  | Intra-particle diffusion |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | ks1 | C1 | R2 |  | ks1 | C2 | R2 |  | ks1 | C3 | R2 |
| BC |  | 12.595 | -0.879 | 0.892 |  | 6.980 | 14.981 | 0.993 |  | 0.281 | 79.482 | 0.627 |
| BCNP-Fe |  | 7.804 | 3.278 | 0.916 |  | 7.123 | 14.443 | 0.978 |  | 3.432 | 51.822 | 0.957 |
| BCHNP-Fe |  | 2.843 | -0.383 | 0.905 |  | 10.566 | -38.616 | 0.980 |  | 0.712 | 25.802 | 0.982 |
| BCP-Fe |  | 10.291 | 0.035 | 0.980 |  | 9.630 | 2.618 | 0.986 |  | 1.793 | 71.235 | 0.961 |

Table. S4

| Adsorbate |  | Film diffusion model |  |  |
| --- | --- | --- | --- | --- |
|  |  | kF | A | R2 |
| BC |  | -0.0334 | -0.158 | 0.953 |
| BCNP-Fe |  | -0.0251 | -0.087 | 0.990 |
| BCHNP-Fe |  | -0.0339 | -0.194 | 0.983 |
| BCP-Fe |  | -0.0215 | -0.188 | 0.991 |

Table. S5

| Adsorbate |  | Langmuir isotherms |  |  |  | Freundlich isotherms |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | kL(L/mg) | qL(mg/g) | R2 |  | kF | 1/n | R2 |
| BC |  | 0.288 | 141.443 | 0.963 |  | 50.727 | 0.259 | 0.925 |
| BCNP-Fe |  | 0.316 | 154.321 | 0.974 |  | 54.593 | 0.268 | 0.910 |
| BCHNP-Fe |  | 0.121 | 203.666 | 0.951 |  | 26.201 | 0.601 | 0.960 |
| BCP-Fe |  | 0.592 | 142.045 | 0.983 |  | 55.691 | 0.292 | 0.962 |
| Adsorbate |  | Temkin isotherms |  |  |  | D-R isotherms |  |  |
|  |  | kT(L/g) | βT(kJ/mol) | R2 |  | qD(mg/g) | E(kJ/mol) | R2 |
| BC |  | 65.994 | 0.149 | 0.784 |  | 87.845 | 5.616 | 0.586 |
| BCNP-Fe |  | 65.732 | 0.139 | 0.759 |  | 91.131 | 5.854 | 0.572 |
| BCHNP-Fe |  | 1.625 | 0.057 | 0.919 |  | 98.766 | 1.147 | 0.682 |
| BCP-Fe |  | 40.881 | 0.122 | 0.882 |  | 94.091 | 4.747 | 0.633 |

Table. S6

| Adsorbent |  | ∆G°(kJ/mol) |  |  |  |  |  | ∆H°(kJ/mol) |  | ∆S°(J/mol) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 283K | 293K | 303K | 313K | 323K |  |  |  |  |
| BC |  | -0.152 | -2.845 | -4.884 | -5.295 | -5.617 |  | 38.085 |  | 138.034 |
| BCNP-Fe |  | -6.386 | -6.787 | -7.571 | -7.867 | -8.182 |  | 6.933 |  | 47.145 |
| BCHNP-Fe |  | -6.715 | -7.413 | -7.683 | -7.957 | -8.226 |  | 3.389 |  | 36.247 |
| BCP-Fe |  | -5.860 | -6.372 | -7.697 | -8.455 | -8.910 |  | 17.469 |  | 82.230 |