Name of Journal: Environmental Science and Pollution Research

Enhancing Biofuel Pellet Quality using Combined Torrefaction and Co-pelletization Processes of Palm Kernel Shell and Empty Fruit Bunch

Chang Siaw Sang, Noor Asma Fazli Abdul Samad, Suriyati Binti Saleh*

Faculty of Chemical & Process Engineering Technology, Universiti Malaysia Pahang, Lebuh Persiaran Tun Khalil Yaakob, 26300, Kuantan, Pahang, Malaysia

*Corresponding author: suriyati@umpsa.edu.my

Tel.: +609-4315731; fax: +609-5492689.

Supplementary Material

Table S1. UANOVA results of all samples.

| Pellet properties | Sources of variation | Df | Mean square | p | η2 |
| --- | --- | --- | --- | --- | --- |
|  | Temperature | 3 | 9.17 | <0.0001 | 0.94 |
| Higher heating value | Sample | 2 | 3.78 | <0.0001 | 0.82 |
|  | Temperature x Sample | 6 | 0.80 | <0.0001 | 0.74 |
|  | Error | 24 | 0.07 |  |  |
|  | Temperature | 3 | 26367.56 | <0.0001 | 0.85 |
| Initial density | Sample | 2 | 57899.80 | <0.0001 | 0.89 |
|  | Temperature x Sample | 6 | 6660.82 | <0.0001 | 0.74 |
|  | Error | 24 | 583.76 |  |  |
|  | Temperature | 3 | 1916.67 | 0.0197 | 0.33 |
| Final density | Sample | 2 | 50801.87 | <0.0001 | 0.90 |
|  | Temperature x Sample | 6 | 5114.39 | <0.0001 | 0.73 |
|  | Error | 24 | 482.16 |  |  |
|  | Temperature | 3 | 219869.66 | <0.0001 | 0.98 |
| Compression force | Sample | 2 | 1242306.88 | <0.0001 | 1.00 |
|  | Temperature x Sample | 6 | 59164.51 | <0.0001 | 0.97 |
|  | Error | 24 | 450.78 |  |  |
|  | Temperature | 3 | 2.75 | <0.0001 | 0.99 |
| Compression strength | Sample | 2 | 15.49 | <0.0001 | 1.00 |
|  | Temperature x Sample | 6 | 0.73 | <0.0001 | 0.98 |
|  | Error | 24 | 0.00 |  |  |
|  | Temperature | 3 | 2.27 | <0.0001 | 0.98 |
| Ash content | Sample | 2 | 3.92 | <0.0001 | 0.98 |
|  | Temperature x Sample | 6 | 0.73 | <0.0001 | 0.97 |
|  | Error | 24 | 0.01 |  |  |