Supporting Information

Low-cost pyrolysis of biomass-derived nitrogen-doped porous carbon: chlorella vulgaris replaces melamine as a nitrogen source

Changxing Lu a, b, Jing Yang c, Zhaosheng Yu a, b, *, Xikui Zhang a, b, Xiaoqian Ma a, b

a School of Electric Power, South China University of Technology, 510640 Guangzhou, China

b Guangdong Province Key Laboratory of Efficient and Clean Energy Utilization, 510640 Guangzhou, China

c China CEC Engineering Corporation,410000 Changsha, China

∗ Corresponding author at: School of Electric Power, South China University of Technology, 510640 Guangzhou, China

E-mail addresses: zsyu@scut.edu.cn (Z. Yu)

2. Material and methods

2.1 Preparation of porous carbon materials

In order to ensure the doping of equal amounts of nitrogen, the nitrogen content of 5 g of Chlorella was first calculated based on the results of elemental analysis.

N Content: 5 g∙9.14%=0.457 (g)

Suppose the mass of melamine to be doped is x:

C3H6N6~ 6N

126.12~ 84.0402

χ ~ 0.457

The value of x was calculated to be 0.686, so the mass of the doped melamine was 0.686 g.

2.2 Characterization

The content of C, H, N, and S in bagasse and chlorella was determined by an Elementar UNICUBE. The XRD spectrum was analyzed with the scan from 10 to 80° with a scanning rate of 10°/min. The surface area was calculated according to the Brunauer-Emmett-Teller (BET) method during N2 adsorption-desorption experiment.

2.3 Electrode preparation and electrochemical measurements

For the GCD graphs, the specific capacitance of the electrode materials were counter by Eq. (1):

C=I∆tm∆V#1

Where C represents the specific capacitance (F/g), I represents the charge-discharge current (A), Δt represents discharge time (s), m represents the loading mass (g) of the active material in the working electrode, and ΔV represents the potential window (V) of the charge–discharge excluding voltage drop.

The working electrodes were prepared as follows: The obtained carbon, PTFE (polytetrafluoroethylene), and commercial carbon black (mass ratio 8:1:1) were mixed in anhydrous ethanol and ground uniformly to form a slurry. The slurry was transferred to nickel foam and dried at 105°C for 12 hours. The dried working electrodes were pressed at 5 MPa for 30 s and the weight of the active material was calculated by weighing the nickel foam sheet before and after loading. The electrochemical properties of porous carbon were tested using a three-electrode system with a Pt electrode and Hg/HgO as the counter and reference electrode, respectively, and 6 mol/L aqueous KOH solution as the electrolyte. Cyclic voltammetry (CV), Galvanostatic charge and discharge (GCD), and electrochemical impedance spectroscopy (EIS) were performed using electrochemical equipment (CHI660E, Shanghai Chenhua, China). CV and GCD tests were performed at various spot scan rates and current densities from -1.0 to 0 V. EIS data were collected in the frequency range of 0.01HZ-100 kHZ with an amplitude of 5 mV.

In two-electrode system, the specific capacitance, energy density and power density were calculated by the following.

C=2I∆tm∆V#2

E=C8×∆V2×13.6#3

P=E∆t×3600#4

Where I represents the charge-discharge current (A), Δt represents discharge time (s), m represents the loading mass (g) of the active material in the working electrode, and ΔV represents the potential window (V) of the charge–discharge excluding voltage drop.

3 Results and discussion

Fig. S1 SEM images of (a, b) ZBC, and (c, d) ZCC.