CuO/PANI nanocomposites: An efficient catalyst for degradation and reduction of pollutants

Ammara 1, Sadia Noreen 1, Sarmed Ali2, Saba Jamil1, Shamsa Bibi1, Muhammad Jamshed Latif1,Touseef Jafar1, , Arslan Bashir1, Shanza Rauf Khan1

(SUPPLEMENTARY INFORMATION)

- Synthesis of copper oxide nanoparticles

Fig S1. Schematic diagram of CuO nanoparticle

- Synthesis of copper oxide/polyaniline nanocomposites

Fig S2. Schematic diagram of CuO/PANI nanocomposite

- XRD

(a)

O-atom

Cu-atom

(102)

(210)

(121)

(002)

(111)

(202)

Fig 3. Monoclinic crystal system of CuO (a). Unit cell with different bonding arrangements of atoms with miller indices.

Table 1. Summary of structural parameters of CuO nanoparticles

| Parameters | Details |
| --- | --- |
| Name of compound | Copper oxide NPs |
| Crystal system | Monoclinic |
| Space group | C 2/c (1 5) |
| Type | Primitive |
| Cell parameters: a, b and c (Å) β (o) | 4.6530, 3.4100, 5.1080 99.480 |
| x, y and z coordinates for Cu atom | 0.2500, 0.2500 and 0.2500 |
| x, y and z coordinates for O atom | 0.000, 0.000 and 0.000 |
| d-spacing, 2 theta (o) and miller indices (hkl) | 7.5747, 16.76 and (101) 5.3922, 24.00 and (210) 4.3709, 32.51 and (110) 4.1917, 34.06 and (121) 3.3680, 35.64 and (002) 3.3316, 38.69 and (111) 2.8621, 52.02 and (112) 2.096, 53.44 and (020) 2.074, 57.87 and (021) 2.024, 61.59 and (202) |
| I/Ic | 4.92 |
| Density (g/cm3) | 6.608 |

(b)

O-atom

Cu-atom

N-atom

C-atom

H-atom

(004)

(102)

(014)

(111)

(210)

(120)

Fig 4. Orthorhombic crystal system of CuO/PANI nanocomposite (b). Unit cells with miller indices.

Table 2: Summary of structural parameters of CuO/PANI nanocomposites

| Parameters | Details |
| --- | --- |
| Name of compound | CuO/PANI NCs |
| Crystal system | Orthorhombic |
| Space group | P c m n (6 2) |
| Type | Primitive |
| Cell parameters: a, b and c (Å) α, β and γ (o) | 5.8300, 6.7750 and 21.7110 111.9790, 96.8790 and 106.6780 |
| x, y and z coordinates for Cu atom | 0.16819, 0.39624 and 0.29210 |
| x, y and z coordinates for O atom | 0.24510, 0.50330 and 0.49580 |
| x, y and z coordinates for N atom | 0.14420, 0.72260 and 0.30980 |
| x, y and z coordinates for Nʹ atom | 0.11890, 0.59480 and 0.29720 |
| x, y and z coordinates for C atom | 0.11890, 0.59480 and 0.29720 |
| d-spacing, 2 theta (o) and miller indices (hkl) | 3.6387, 10.56 and (002) 2.6930, 16.27 and (004) 2.5211, 17.25 and (102) 2.2075, 21.19 and (014) 1.8692, 25.38 and (105) 1.6960, 39.79 and (206) 1.4868, 56.51 and (229) 1.4530, 65.23 and (404) |
| I/Ic | 3.64 |
| Density (g/cm3) | 2.895 |

- SEM

Fig 5. Histogram size distribution graph of the synthesized needle-like CuO nanoparticles

Fig 6. Histogram size distribution graph of the synthesized CuO/PANI nanocomposites

- EDX

Table 3. Showing the atomic and weight percentage of the elements present in (a) CuO nanoparticles (b) CuO/PANI nanocomposite.

| Spectrum (a) |  |  |
| --- | --- | --- |
| Element | Weight % | Atomic % |
| C K |  |  |
| O K | 62.92 | 24.94 |
| Cu K | 37.08 | 70.06 |
| Total | 100.00 |  |

| Spectrum (b) |  |  |
| --- | --- | --- |
| Element | Weight% | Atomic% |
| C K | 70.79 | 78.11 |
| O K | 23.94 | 19.83 |
| S K | 3.38 | 1.40 |
| Cl K | 1.58 | 0.59 |
| Cu K | 0.31 | 0.07 |
| Totals | 100.00 |  |

- FTIR

Table 4 Summary of all the characteristic bands observed along with their functional groups, vibrations and wavenumber

| Functional Group | Vibrations | Wavenumber (cm-1) |
| --- | --- | --- |
| Carbonyl group (C=O) | Stretching | 1735, 1638 |
| Carboxylic acid (C-O) | Stretching | 1319, 849 |
| Hydroxyl compounds (O-H) | Stretching | 3349 |
| Ketone (C-H) | Stretching | 765 |
| Allenes (C=C=C) | Stretching | 1994 |
| Primary Amines (N-H) | Stretching | 3317 |
| Aliphatic amines (C-N) | Stretching | 1209 |
| Alkenes (C=C) | Stretching | 1388, 1528 |
| Cu-O | Bending | 652 |
| PANI matrix | Stretching | 700, 765 |

Corresponding author: shanzaraufkhan@gmail.com