Supporting Information

Positive effect of deactivated ion Tb3+ and non-optical active ion Al3+ co-doping on the Dy3+: CaLaGa3O7 crystal as a promising 574 nm yellow laser crystal

Yunyun Liu1, Meimeng Jiang1, Lu Wang1, Chuanxin Huang1, Ju Gao1, Yijian Sun2,3*, Yan Wang4*

1School of Opto-Electronic Engineering, Zaozhuang University, Zaozhuang, Shandong, 277160, China

2School of Chemistry and Chemical Engineering, Jiangxi Provincial Key Laboratory of Functional Molecular Materials Chemistry, Jiangxi University of Science and Technology, Ganzhou, 341000, Jiangxi, China

3National Rare Earth Functional Material Innovation Center, Ganzhou, 341000, Jiangxi, China
4Key Laboratory of Optoelectronic Materials Chemistry and Physics, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou, Fujian, 350002, China

*E-mail: sunyijian@jxust.edu.cn

**E-mail: wy@fjirsm.ac.cn

Contents

Figure S1. Calculated band structure of CLAGO (Al ions occupy the sites of Ga-Ⅰ).

Figure S2. Density of states of CLAGO (Al ions occupy the sites of Ga-Ⅰ).

Figure S3. (a) XRD patterns of Dy/Tb: CLAGO samples and (b) their XRD peaks in the range of 30.0–31.0◦.

Table S1. Calculated lattice parameters of Dy/Tb: CLAGO polycrystals.

Figure S1. Calculated band structure of CLAGO (Al ions occupy the sites of Ga-Ⅰ).

Figure S2. Density of states of CLAGO (Al ions occupy the sites of Ga-Ⅰ).

Figure S3. (a) XRD patterns of Dy/Tb: CLAGO samples and (b) their XRD peaks in the range of 30.0–31.0◦.

Table S1. Calculated lattice parameters of CaDy0.02TbxLa0.98-xAl0.1Ga2.9O7 polycrystals.

| Sample | a (Å) | c (Å) | α (°) | β (°) | γ (°) |
| --- | --- | --- | --- | --- | --- |
| x=0 | 11.2266 | 5.2625 | 90 | 90 | 90 |
| x=0.001 | 11.2258 | 5.2633 |  |  |  |
| x=0.002 | 11.2170 | 5.2574 |  |  |  |
| x=0.003 | 11.2182 | 5.2512 |  |  |  |
| x=0.005 | 11.2113 | 5.2570 |  |  |  |