Supporting Information

Low-cost conversion of Mo industrial waste powder into MoO3 nanobelts catalysts for Oxygen Evolution Reaction

F. Ursino1,2, G. Mineo1, A. Scandurra1,2, Angelo Forestan3, Catya Alba3, R. Reitano1, A. Terrasi1,2 and S. Mirabella1,2*

1 Dipartimento di Fisica e Astronomia “Ettore Majorana”, Università degli Studi di Catania, via S. Sofia 64, 95123 Catania, Italy.

2 CNR-IMM, Università di Catania, via S. Sofia 64, 95123 Catania, Italy.

3R&D Spirit Srl-Soc. Unipersonale, Via dei Laghi 67, 36072 Vicenza, Italy.

*E-mail corresponding: salvo.mirabella@dfa.unict.it

## RBS analysis

The Mo and O atomic doses were estimated thanks to Rutherford Backscattering Spectrometry (RBS). For stoichiometric MoO3 the expected O/Mo atomic dose ratio is equal to 3. The doses were calculated for the signal starting at 0.7 and 2.1 MeV (Figure S 1a-b), which stand, respectively, for He+ backscattered by oxygen (O) and by molybdenum (Mo). The area under the peak is proportional to the atomic dose multiplied by the back-scatering atomic cross section. The O/Mo ratio for Mo-based powder is equal to 2.0, while for pH 1.26 sample the ratio is close to 3.4. From these results we assign pH 1.26 sample to MoO3, while the Mo-based starting powder are substoichimetric molybdenum oxide.

Figure S 1 RBS analysis of: a) Mo-based powder with a Mo/O ratio of about 11 b) pH 1.26 synthesis with a Mo/O ratio equal to 6.

## SEM images

Figure S 2 SEM images of pH1.26 synthesis a) cross-section of the nanobelts; b) low-magnification to highlight the absence of spheres within the sample.

## EIS measurements

Figure S 3 EIS measurements for pH 1.26 sample (lilac curve), pH 1.35 sample (blue curve), pH 1.60 sample (yellow curve), pH 2.35 sample (burgundy curve).

## Mass Activity

Table S 1 Summary of the values reported in Figure 4c.

| Overpotential [V] | Mass Activity [A mg-1] | Catalyst loading [mg] | Catalyst | Reference |
| --- | --- | --- | --- | --- |
| 0.318 | 0.00667 | 1.5 | Zr-baed MOF-Mo2C/NF | [1] |
| 0.310 | 0.01471 | 0.68 | NiMo HNRs/TiM | [2] |
| 0.340 | 0.01 | 1 | MoO3-x | This work |
| 0.324 | 0.0125 | 0.8 | MoO3-nanobelts | This work |

## Mott-Schottky measurements

Figure S 4 a-d) Mott-Schottky measurements for pH 1.26 sample (lilac curve), pH 1.35 sample (blue curve), pH 1.60 sample (yellow curve), pH 2.35 sample (burgundy curve.

# References

| [1] | M. Ali et al. «Enhancing the Overall Electrocatalytic Water-Splitting Efficiency of Mo2C Nanoparticles by Forming Hybrids with UiO-66 MOF,» ACS Omega, vol. 6, pp. 34193-35144, 2021. |
| --- | --- |
| [2] | J. Tian et al. «Self-supported NiMo hollow nanorod array: an efficient 3D bifunctional catalytic electrode for overall water splitting,» Journal of Materials Chemistry A, vol. 3, pp. 20056-20059, 2015. |