Supplementary Information

A dynamically gated triangular DNA nanopore for molecular sensing and cross-membrane transport

Xiaoming Liu1,2,6,*, Fengyu Liu1,2,6, Hemani Chhabra3, Christopher Maffeo3,4, Qiang Huang1,2, Aleksei Aksimentiev3,4,* & Tatsuo Arai1,2,5

1School of Mechatronical Engineering, Beijing Institute of Technology, Beijing, China.

2Beijing Advanced Innovation Center for Intelligent Robots and Systems, Beijing Institute of Technology, Beijing, China.

3Department of Physics, University of Illinois at Urbana Champaign, Urbana, IL, USA.

4Beckman Institute for Advanced Science and Technology, University of Illinois at Urbana Champaign, Urbana, IL, USA.

5Center for Neuroscience and Biomedical Engineering, The University of Electro-Communications, Tokyo, Japan.

6These authors contributed equally: Xiaoming Liu, Fengyu Liu.

*Correspondence should be addressed to Xiaoming Liu (liuxiaoming555@bit.edu.cn) or Aleksei Aksimentiev (aksiment@illinois.edu).

Supplementary Fig. 1 The route designs of DNP-E and DNP-C. The novel design enables the bidirectional mechanical transition of the DNA nanopore between DNP-E (a) and DNP-C (b) by pinching and releasing the three corners of the triangular frame. The blue line represents the scaffold DNA of designed DNA nanopores. Some nucleotides in the scaffold DNA are not complementary to any of the staple strands and serve as single-stranded hinges at each corner to minimize bending stress. The 67nt nucleotides of the scaffold DNA form a bottom ring that can be used to define the bottom subunit of DNA nanopores. Staple strands with different functions are marked in gray, purple, and green, respectively. The staple strands utilized to assemble the main structures are gray. The staple strands utilized to capture Cy3 strands are green. The staple strands applied to hybridize cholesterol strands are purple. All oligonucleotide sequences of staple strands are included in Supplementary Data 1.

Supplementary Fig. 2 Toehold-mediated strand displacement reactions dominate the dynamic switching of the triangular DNA nanopore. a, Triggers are introduced to pinch the three corners of the triangular DNA nanopore, enabling the mechanical transition from the expanded state to the contracted state. The green rectangles represent the toehold domains for sensing triggers. b, With the participation of reverse triggers, the three pinched corners of the triangular DNA nanopore can be released, resulting in the mechanical transition from the contracted state to the expanded state. The toehold domains used to recognize reverse triggers are indicated by green rectangles. All oligonucleotide sequences of triggers and reverse triggers are included in Supplementary Data 1.

Supplementary Fig. 3 Gel electrophoresis characterization of synthetic DNA nanopores. a, Various DNA nanopore samples were subjected to 1.0% agarose gel electrophoresis before and after filtration. The dashed rectangle referred to the excess staple strands. b, Comparative analysis of the mobility and signal intensity of the different bands measured from Supplementary Fig. 3a.

Supplementary Fig. 4 Gel electrophoresis analysis of DNA nanopores before (lane 1, lane 2) and after (lane 4, lane 5) cholesterol strands treatment. Upshifted bands can be observed in lanes 4 and 5, indicating that DNP-E and DNP-C have been successfully tagged with cholesterol moieties.

Supplementary Fig. 5 Interaction between cholesterol-tagged DNA nanopores and lipid vesicles. a, Size distribution of small unilamellar vesicles (SUVs) was measured by a Malvern analyzer. b, Interaction between DNP-C and SUVs was analyzed by 1.5% agarose gel electrophoresis at different lipid concentrations. The lipid concentrations of SUV in lanes 1-5 were 0 nM, 5 nM, 10 nM, 20 nM, and 40 nM, respectively. c, Statistical analysis of the gel electrophoresis results of DNP-C bound to SUVs with different lipid concentrations. All gray values measured from other lanes were normalized to Lane 1. Error bars point to the standard deviation of the mean grayscale counted from three independent experiments. The shaded bands around the Gaussian fit curves represented the respective 95% confidence regions.

Supplementary Fig. 6 Synthetic DNA nanopores in different states were unable to puncture lipid membranes without cholesterol modifications. Schematics illustrated the inability of unmodified DNP-C (a) and DNP-E (c) to insert into planar lipid bilayers. Typical current traces were recorded after the addition of unmodified DNP-C (b) and DNP-E (d) at a constant voltage of +80 mV.

Supplementary Fig. 7 Electrical conductivity of cholesterol-tagged DNA nanopores with different lumens. Schematic diagrams illustrated the varying lumen sizes of DNP-C (a) and DNP-E (b), which enable electrolyte ions with different intensities to pass through the lipid bilayer. Current traces for DNP-C (c) and DNP-E (d) were recorded from -100 mV to +100 mV in 20 mV voltage steps. The data of the current-voltage plots were expressed as mean ± SD.

Supplementary Fig. 8 The addition of random strands does not activate DNP-C and DNP-E. a, Schematic depicted that the random strands were incapable of actuating the bidirectional mechanical transition of the triangular DNA nanopore. Single-channel current analysis of the membrane-spanning DNP-C (b) and DNP-E (c) after the addition of random strands. Electrophysiological experiments were performed at a constant potential of +80 mV.

Supplementary Fig. 9 Statistical analyses of current signal changes of triangular DNA nanopores. a, Comparative analysis of current signals recorded by the embedded DNP-C before and after the addition of reverse triggers. b, Mean current signal changes of inserted DNP-E before and after the incubation of triggers. Each dot (circle or triangle) represented the average of the current signals recorded from each independent electrophysiological experiment.

Supplementary Fig. 10 Details of the method employed to calculate the ionic current through the DNA nanopore systems. a, Density map of the DNP-C and DNP-E embedded in the DPhPC lipid bilayer at a resolution of 1 Å. The Inset showed an all-atom representation of the DPhPC lipid bilayer used for accommodating triangular DNA nanopores. Scale bars: 10 nm. b, Local electrolyte conductivity as a function of distance from atoms of DNA or lipids. Voxels positioned further than 1 nm from lipids or 1.5 nm from DNA exhibit bulk conductivity.

Supplementary Fig. 11 Power spectrum analysis of membrane-spanning DNP-C (a) and DNP-E (b) with and without trypsin treatment. All Trypsin treatments were performed at a concentration of 10 μM. The pH of the electrophysiological buffer consisting of 1 M KCl and 10 mM HEPES was 7.4.

Supplementary Fig. 12 Fluorescence influx studies of cholesterol-free DNA nanopores. Representative confocal images showed almost no influx of FITC-dextran (40 kDa) and TRITC-dextran (500 kDa) into the GUVs incubated with DNP-C (a) and DNP-E (c). Scale bars: 10μm. Fluorescent traces (b, d) showed no apparent increase in fluorescent intensity in the interior of the GUVs incubated with DNP-C and DNP-E, respectively. In control experiments, relevant DNA nanopores in question were not modified by cholesterol strands. All fluorescent traces were recorded from the GUVs marked with white circles. Corresponding GUVs were scanned every 15 min for 3 h with a confocal microscope.