Gold Nanostructure-Enhanced Immunosensing: Ultra-Sensitive Detection of VEGF Tumor Marker for Early Disease Diagnosis

Sadaf Yarjoo1, Hossein Siampour1,2, Mehrsa Khalilipour1, Reza .H Sajedi4, Hassan Bagheri5, Ahmad Moshaii1,3*

1 Department of Physics, Tarbiat Modares University, Tehran, P.O Box 14115-175, Iran

2 Biosensor Research Center (BRC), Isfahan University of Medical Sciences, P.O.Box: 81746-73461, Isfahan, Iran

3 Department of Sensor and Biosensor, Faculty of Interdisciplinary Sciences and Technologies, Tarbiat Modares University, P.O.Box: 14115-336, Tehran, Iran

4 Department of Biochemistry, Faculty of Biological Sciences, Tarbiat Modares University, Jalal Ale Ahmad Highway, Tehran 14115-154, Iran

5Chemical Injuries Research Center, Systems Biology and Poisonings Institute, Baqiyatallah University of Medical Sciences, Tehran, Iran

*Email: moshaii@modares.ac.ir

Figure.S1: FESEM images and histogram of different sizes of the formed nanostructures after the thermal annealing for the temperatures of a) 450℃, b) 550℃,c) 600℃. The thicknesses of gold and silver layers in all cases are fixed at 5nm gold and 25nm silver, respectively.

Figure.S2: The impact of the thermal annealing of the electrode on the CV (a), and EIS characterization results (b).

Figure.S3: CVs of the modified gold electrode at different scanning rates ranging from 10 to 100 mV/s.