| Basu-HDI | Basu | Parameter |
| --- | --- | --- |
| 256.2 | 1107.1 | as (m2/g) |
| 58.8 | 254.3 | Vm (cm3/g) |
| 0.1 | 0.8 | Total pore volume (cm3/g) |
| 2.7 | 2.9 | Mean pore diameter (nm) |

Table 1. Results from the BET analysis of the Basu and Basu-HDI

| Entry | Condition | Catal. Amount (mg) | Time (h) | Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | EtOH, reflux | 20 | 2 | 90 |
| 2 | EtOH:H2O (1:1), 80 °C | 20 | 2 | 64 |
| 3 | CH3CN, reflux | 20 | 2 | 68 |
| 4 | CO(CH3)2, reflux | 20 | 2 | 68 |
| 5 | Solvent-free, 110 °C | 20 | 2 | 30 |
| 6 | EtOH, reflux | 40 | 2 | 82 |
| 7 | EtOH, reflux | 60 | 2 | 79 |
| 8 | EtOH, reflux | - | 2 | 43 |

Table 2. Optimization of the reaction conditions for the synthesis of compound 4a

| Entry | Catalyst | Catal. Amount (mg) | Time (h) | Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | Basu-DPU32 | 20 | 2 | 75 |
| 2 | MIL(Cr)/NHEtN(CH2PO3H2)237 | 20 | 2 | 68 |
| 3 | MIL-125(Ti)-N(CH2PO3H2)238 | 20 | 2 | 75 |
| 4 | p-TSA | 20 | 2 | 65 |
| 5 | L-Proline | 20 | 2 | 60 |
| 6 | SSA | 20 | 2 | 75 |
| 7 | FSiPSS | 20 | 2 | 68 |
| 8 | ATSPTC-Mn39 | 20 | 2 | 70 |

Table 3. Screening the model reaction in the presence of several catalysts

Table 4. Synthesis of new 4(a-m) using Basu-HDI. Reaction conditions: 2,6-diaminopyridine (1.0 mmol), malononitrile/ethyl cyanoacetate (1.0 mmol), aromatic aldehyde (1.0 mmol), Basu-HDI (20.0 mg) and ethanol (5.0 mL) under reflux.