Supporting Information

Bias-stress-stable Sub-1.5 V Oxide Thin-film-transistors via Synergistic Composition of Sol-gel Quaternary High-k Metal Oxide Dielectrics

Seokhyeon Baek1†, Jun-Gyu Choi2†, Won-June Lee3†, Taehyun Kwak1†, Yong-Ryun Jo4, Myung-Han Yoon2, and Sungjun Park1*

1Department of Electrical and Computer Engineering, Ajou University, Suwon 16499, Republic of Korea

2School of Materials Science and Engineering, Gwangju Institute of Science and Technology, Gwangju 61005, Republic of Korea

3Department of Chemistry, Purdue University, West Lafayette, Indiana, 47907, United States

4Gwangju Institute of Science and Technology Central Research Facilities, Gwangju Institute of Science and Technology, Gwangju 61005, Republic of Korea

† These authors contributed equally to this work.

*Authors to whom correspondence should be addressed: sj0223park@ajou.ac.kr (S. Park)

This “Supporting Information” includes:

Figure S1 to S6

Table S1 to S3

Figure S1. Leakage current densities (Jleak) of MIM capacitors based on (a) AlOx, (b) HfOx, and (c) ZrOx as function of electric fields (E). 5 devices were measured for each capacitor to ensure reliable comparison.

Figure S2. Areal capacitance (Ci) of MIM capacitors based on (a) AlOx, (b) HfOx, and (c) ZrOx as function of AC frequency (f). 5 devices were measured for each capacitor to ensure reliable comparison.

Figure S3. Triangular phase diagrams for leakage current density (Jleak) of Al–Hf–Zr–O (AHZO) MIM capacitors, extracted from the J–E curves at different electric field; (a) 1 MV cm-1, (b) 2 MV cm-1, and (c) 3 MV cm-1.

Figure S4. Triangular phase diagrams for dielectric constant (k) of Al–Hf–Zr–O (AHZO) MIM capacitors, extracted from the Ci–f curves at different frequency; (a) 1 kHz, (b) 10 kHz, and (c) 100 kHz.

Figure S5. Surface roughness evaluation of AHZO films with different stoichiometry using atomic force microscopy (AFM). AFM images (scale bars indicate 0.5m) of (a) AlOx, (b) HfOx, (c) ZrOx, (d) AHZO (1:2:2), (e) AHZO (2:2:1), and (f) AHZO (3:1:1), respectively.

Figure S6. Transfer curves of In–Ga–Zn–O thin-film transistors (TFTs) based on AHZO with different stoichiometry; Al:Hf:Zr ratio was (a) 1:2:2, (e) 2:2:1, and (f) 3:1:1, respectively.

| Parameters | HfOx |  | ZrOx |  |
| --- | --- | --- | --- | --- |
|  | m(111) | m(-111) | t(112) | m(111) |
| 2θ [degree] | 31.650 | 28.347 | 50.699 | 31.482 |
| FWHM | 0.5101 | 0.5166 | 0.9390 | 0.7170 |
| D [nm] | 13.91 | 16.57 | 9.78 | 12.03 |

Table S1. Summarized full width half maximum (FWHM) and average grain sizes (D) for each crystalline phase of HfOx and ZrOx, calculated from Scherrer equation.

Table S2. Summarized figure-of-merit parameters of IGZO/AHZO TFTs with different conditions, including saturation mobility, threshold voltage, subthreshold swing, and on/off current ratio.

Table S3. Calculated interface trap densities (Dit) of TFTs with different conditions.