Supplementary Information

Nanoscale chemical heterogeneities control magma viscosity and failure

## S.1 Preliminary characterization of the glasses

In Table S1, we present microprobe chemical analysis results of our samples, alongside chemistry data from relevant literature 1–5, calculated NBO/T for each sample after Prata et al. (2019), Brillouin and Mössbauer spectroscopy results. Our chemical analysis results affirm that the composition of AND100 (SiO2 = 60.38 wt%; NBO/T=0.34) closely aligns, considering experimental uncertainties, with previous andesites reported in the literature 1,2,5. We also confirm that samples AND100ox (retrieved after concentric-cylinder viscometry) and AND100red (melted under reductive conditions) are virtually identical to that of AND100. Moreover, we achieved the synthesis of a transition-metal-free analog (AND0, SiO2 = 65.91 wt%; NBO/T=0.16), which is meant to represent the complete removal of iron (FeOtot), titanium (TiO2), and manganese (MnO) from sample AND100. Lastly, we successfully produced an intermediate glass AND65 (SiO2 = 62.65 wt%; NBO/T=0.27), designed to contain 65% of the total transition metal contained in AND100.

Mössbauer results reveal Fe3+/∑Fetot ratios of 0.27, 0.64 and 0.70 for as-synthesized AND100red, AND100 and AND65 glasses, respectively (Table S1). The Fe3+/∑Fetot ratio of AND100ox (Fe3+/∑Fetot = 0.71) was slightly higher than AND100, revealing that concentric cylinder (CC) viscometry measurements induced a non-negligible iron oxidation.

| Table S1. Electron microprobe chemistry and K/G factor of starting materials. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SiO2 | TiO2 | Al2O3 | FeOtot | MnO | MgO | CaO | Na2O | K2O | P2O5 | Fe3+/∑Fetota | NBO/Tb | K/Gc |
| AND100d | 60.38 (0.36) | 0.79 (0.04) | 16.69 (0.18) | 6.77 (0.12) | 0.17 (0.03) | 3.00 (0.07) | 6.62 (0.09) | 3.50 (0.15) | 1.58 (0.07) | 0.18 (0.05) | 0.64 | 0.34 | 1.56 (0.02) |
| AND100redd | 60.47 (0.40) | 0.80 (0.07) | 16.83 (0.22) | 6.87 (0.12) | 0.18 (0.04) | 2.94 (0.06) | 6.51 (0.11) | 3.46 (0.10) | 1.65 (0.07) | 0.18 (0.05) | 0.27 | 0.34 | 1.57 (0.02) |
| AND100oxd | 60.56 (0.35) | 0.81 (0.06) | 16.79 (0.19) | 6.76 (0.15) | 0.18 (0.03) | 2.95 (0.06) | 6.49 (0.11) | 3.40 (0.10) | 1.66 (0.06) | 0.18 (0.05) | 0.71 | 0.34 | 1.58 (0.02) |
| AND65d | 62.52 (0.19) | 0.56 (0.04) | 17.28 (0.22) | 4.40 (0.11) | 0.11 (0.03) | 3.02 (0.07) | 6.76 (0.13) | 3.49 (0.11) | 1.70 (0.05) | 0.16 (0.05) | 0.70 | 0.27 | 1.53 (0.02) |
| AND0d | 65.91 (0.34) | 0.04 (0.03) | 18.01 (0.11) | 0.04 (0.03) | 0.01 (0.01) | 3.21 (0.06) | 7.26 (0.11) | 3.82 (0.14) | 1.75 (0.06) | 0.04 (0.03) | - | 0.16 | 1.48 (0.02) |
| Ande | 61.47 (0.26) | 0.81 (0.14) | 16.25 (0.15) | 6.76 (0.19) | 0.14 (0.13) | 2.78 (0.09) | 6.53 (0.09) | 3.54 (0.08) | 1.61 (0.05) | 0.11 (0.08) | - | 0.34 | - |
| MSTf | 60.71 | 0.58 | 18.29 | 6.38 | 0.19 | 2.58 | 7.1 | 3.57 | 0.85 | - | - | 0.29 | - |
| AndUg | 56.65 (0.41) | 1.01 (0.04) | 17.41 (0.15) | 8.16 (0.21) | 0.13 (0.04) | 4.30 (0.07) | 7.38 (0.11) | 3.23 (0.15) | 1.56 (0.07) | - | 0.33-0.57 | 0.44 | - |
| iron-free AndUg | 58.69 (0.33) | 0.01 (0.01) | 21.57 (0.33) | 0.02 (0.03) | 0.02 (0.02) | 5.38 (0.10) | 9.49 (0.18) | 3.30 (0.10) | 1.57 (0.12) | - | - | 0.23 | - |
| ME13lleh | 59.70 | 0.52 | 18.30 | 7.58 | 0.20 | 2.59 | 7.21 | 3.44 | 0.90 | 0.17 | - | 0.33 | - |
| Andesiteh | 62.40 (0.69) | 0.55 (0.02) | 20.01 (0.11) | 0.03 (0.03) | 0.02 (0.03) | 3.22 (0.05) | 9.08 (0.14) | 3.52 (0.07) | 0.93 (0.05) | 0.12 (0.03) | - | 0.16 | - |
| Andesitei | 61.17 (0.15) | 0.84 (0.02) | 17.29 (0.05) | 5.39 (0.19) | - | 3.35 (0.05) | 5.83 (0.05) | 3.85 (0.06) | 1.39 (0.02) | - | - | 0.30 | - |
| aRatios derived using Mossa software 7. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| bNBO/T values were calculated using a supporting spreadsheet reported by Prata et al. (2019). |  |  |  |  |  |  |  |  |  |  |  |  |  |
| cValues derived using Brillouin spectroscopy data and Eq. 4. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| dThis study. eOkumura et al. (2022). fGiordano et al. (2006). gLiebske et al. (2003). hRichet et al. (1996). iNeuville et al. (1993). |  |  |  |  |  |  |  |  |  |  |  |  |  |

To verify the pristine glassy nature of all these specimens, we combined scanning electron microscopy (SEM) imaging, in backscattered electron (BSE) mode, with Raman spectroscopy analysis. While SEM imaging verified the absence of bubbles and micro-sized crystals, our Raman results (Fig. S1) showed that all our starting glasses are amorphous and are in good agreement with previously reported Raman spectra for similar compositions 8,9. This conclusion is drown from the absence of characteristic features in the 650–690 cm−1 range, which were previously linked to the presence of Fe-Ti-oxide nanolites 10–13.

Figure S1. Raman spectra of glassy samples before C-DSC and viscosity measurements. The shaded area in grey (660-690 cm-1) corresponds to the most prominent area commonly affected by the presence of Fe-Ti-oxides 11,14.

Additionally, using sound velocities (vp and vs) from BLS measurements and Eq. 4, we calculated the K/G ratios for all five starting materials (Table S1). The K/G ratios inversely correlate with the SiO2 wt% of the glasses, in agreement with Cassetta et al., (2021). Notably, the measured K/G value of AND65 corresponds to an ideal mixing between its two compositional endmembers (AND100 and AND0).

## S2.1 Conventional Differential Scanning Calorimetry (C-DSC)

Table S2 lists the measured characteristic Tonset and Tpeak at various matching heating-cooling rates (qh=qc) via C-DSC (10-20 ℃ min-1) and F-DSC (1,000-10,000 ℃ s-1). We observed that both Tonset and Tpeak increase with increasing qh=qc values (Table S2). AND0 displays the highest Tonset (737 ℃) and Tpeak (782 ℃) at a heating rate of 10 ℃ min-1, while sample AND100red exhibits the lowest Tonset (645 ℃) and Tpeak (694 ℃) under the same heating conditions. At the same heating rate, the Tonset and Tpeak of AND100, AND100ox, and AND65 fall between AND0 and AND100red.

| Table S2. C-DSC, F-DSC, MP, and CC result as a function of temperature and post-experimental Mössbauer results. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Sample | Typea | T (℃) |  | log η (η in Pa s) |  | ΔFe3+/∑Fetotb |  |
| AND100 | C-DSC10_on | 654 | 11.98 |  | 0.12 |  |  |
|  | C-DSC10_pk | 715 | 10.62 |  | 0.12 |  |  |
|  | C-DSC10bis_on | 654 | 11.98 |  | 0.16 |  |  |
|  | C-DSC10bis_pk | 695 | 10.62 |  | 0.16 |  |  |
|  | C-DSC20_on | 675 | 11.68 |  | 0.05 |  |  |
|  | C-DSC20_pk | 724 | 10.32 |  | 0.05 |  |  |
|  | F-DSC1000_on | 796 | 8.40 |  | - |  |  |
|  | F-DSC1000_pk | 867 | 6.85 |  | - |  |  |
|  | F-DSC10000_on_#1 | 851 | 7.40 |  | - |  |  |
|  | F-DSC10000_on_#2 | 858 | 7.40 |  | - |  |  |
|  | F-DSC10000_on_#3 | 864 | 7.40 |  | - |  |  |
|  | F-DSC10000_on_#4 | 886 | 7.40 |  | - |  |  |
|  | F-DSC10000_on_#5 | 890 | 7.40 |  | - |  |  |
|  | MP660_0 | 657 | 12.00 |  | - |  |  |
|  | MP660_90 | 660 | 12.70 |  | 0.06 |  |  |
|  | MP723_0 | 720 | 11.04 |  | - |  |  |
|  | MP723_60 | 723 | 11.90 |  | 0.15 |  |  |
|  | MP808_0 | 807 | 9.74 |  | - |  |  |
|  | MP808_60 | 808 | 10.17 |  | 0.19 |  |  |
|  | CC | 1435 | 2.03 |  |  |  |  |
|  | CC | 1405 | 2.19 |  |  |  |  |
|  | CC | 1355 | 2.45 |  | - |  |  |
|  | CC | 1306 | 2.75 |  | - |  |  |
|  | CC | 1255 | 3.09 |  | - |  |  |
|  | CC | 1226 | 3.29 |  | - |  |  |
|  | CC | 1206 | 3.44 |  | - |  |  |
|  | CC | 1182 | 3.62 |  | - |  |  |
|  | CC | 1152 | 3.87 |  | - |  |  |
| AND100ox | C-DSC10_on | 662 | 11.98 |  | 0.02 |  |  |
|  | C-DSC10_pk | 702 | 10.62 |  | 0.02 |  |  |
| AND100red | C-DSC10_on | 645 | 11.98 |  | 0.02 |  |  |
|  | C-DSC10_pk | 694 | 10.62 |  | 0.02 |  |  |
|  | C-DSC20_pk | 652 | 11.68 |  | 0.02 |  |  |
| AND65 | C-DSC10_on | 696 | 11.98 |  | 0.02 |  |  |
|  | F-DSC1000_on | 847 | 8.20 |  | - |  |  |
|  | F-DSC1000_pk | 929 | 6.84 |  | - |  |  |
|  | MP695 | 695 | 12.13 |  | 0.03 |  |  |
|  | MP711 | 711 | 11.66 |  | 0.01 |  |  |
|  | MP761 | 761 | 10.23 |  | 0.01 |  |  |
| AND0 | C-DSC10_on | 737 | 11.98 |  | - |  |  |
|  | C-DSC10_pk | 782 | 10.62 |  | - |  |  |
|  | C-DSC20_on | 747 | 11.68 |  | - |  |  |
|  | C-DSC20_pk | 792 | 10.32 |  | - |  |  |
|  | MP792 | 792 | 10.43 |  | - |  |  |
|  | CC | 1404 | 2.82 |  | - |  |  |
|  | CC | 1355 | 3.11 |  | - |  |  |
|  | CC | 1307 | 3.43 |  | - |  |  |
|  | CC | 1256 | 3.79 |  | - |  |  |
|  | CC | 1205 | 4.20 |  | - |  |  |
|  | CC | 1179 | 4.42 |  | - |  |  |
|  | CC | 1154 | 4.65 |  | - |  |  |
|  | CC | 1130 | 4.91 |  | - |  |  |
| aC- and F-DSC-type experiments are reported as DSCheating-rate_thermal-event , with heating rates expressed in °C min-1 and °C s-1, respectively. Thermal events are identified as on = Tonset and pk = Tpeak. F-DSC experiments at 10000 K s-1 are numbered to show their relative positions in the series of measurements. MP data is reported as MPtemperature_duration, with temperature expressed in °C and the duration in minutes. (if time is not reported, the measurement remained constant within the experimental time). |  |  |  |  |  |  |  |
| bDifference between Fe3+/∑Fetot after measurements and initial conditions from Table 1. Ratios derived using Mossa software (Prescher et al. 2012). |  |  |  |  |  |  |  |

Our C-DSC data suggest that Tonset increases with increasing SiO2 content and decreasing FeOtot content (Table S1 and S2). Moreover, at a heating rate of 10 ℃ min-1, we observe that Tonset of isochemical samples (i.e., AND100red, AND100, and AND100ox) increased with increasing initial Fe3+/∑Fetot, (Table S1). Nevertheless, we did not observe the same trend when comparing the Tpeak values of these three samples, as we obtained Tpeak values of 694, 715 and 702 ℃ for AND100red, AND100, and AND100ox, respectively.

To assess potential sample crystallization and/or iron oxidation during the C-DSC heat treatments 10–12,15–17 we conducted Mössbauer and Raman spectroscopy analyses on the recovered samples. For sample AND100, we observed an increase in ΔFe3+/∑Fetot by 0.12 and 0.16 following C-DSC measurements at 10 (AND100_C-DSC10) and 20 ℃ min-1 (AND100_C-DSC20), respectively (Table S2). On the other hand, Raman spectra of AND100_C-DSC10 and AND100_C-DSC20 displayed the development of noticeable peaks associated with titanomagnetite crystallization (Fig. S2a; (Shebanova and Lazor 2003; Jubb and Allen 2010)), suggesting that nanocrystallization of Fe-Ti-oxide occurred during measurements. In addition, we noticed the total disappearance of their respective Boson peaks (Fig. S2a). The Boson peak 18–20, which is located below 100 cm-1, serves as a distinctive marker for the intrinsic disorder within the system and is associated with the collective atomic motions, especially acoustic phonons, arising from the short-to-medium range order of glasses.

Figure S2. Raman spectra of samples after DSC measurements. a) After C-DSC measurements. b) Raman spectra of the same AND100 sample after a series of F-DSC measurements. The shaded area in grey corresponds to Raman peaks for titanomagnetite 21,22. The shaded area in red corresponds to hematite 22.

Consistently with recent literature 10,15,17, our findings indicate that C-DSC experiments have the potential to induce structural modifications (including nanocrystallization) and alter the iron oxidation state within the sample, particularly when the temperature exceeds Tonset at the end of the heating segments. To mitigate temperature overshoot after reaching their respective Tonset, and to explore the possible changes during heating, we conducted a conservative C-DSC experiment on sample AND100 (AND100_C-DSC10bis) dividing it into two steps: (1) the first upscan was performed as usual but halted after the matching cooling segment with qc = -10 ℃ min-1 and (2) using the same sample, we completed the matching C-DSC measurement with qh = 10 ℃ min-1. Mössbauer and Raman spectroscopy were carried out after steps 1 and 2 to detect potential modifications in each segment. Mössbauer results show that sample AND100 did not experience iron oxidation after step 1 (C-DSC10bis_1) but showed a slight increase in Fe3+/∑Fetot after step 2 (C-DSC10bis_2), from 0.64 to 0.69 (Table 2). Similarly, Raman spectroscopy results (Fig. S2a) suggest no changes after step 1, while the Raman spectrum collected after step 2 shows a new and weak contribution around 660–690 cm−1, and a Boson peak shift from 70 to 63 cm-1 (Fig. S2a). After this run, we obtained Tonset and Tpeak values of 654 and 694 ℃, respectively (Table S2). We notice a significant decrease in the Tpeak, from 715 (AND100_C-DSC10_pk) to 695 ℃ (AND100_C-DSC10bis_pk). After this run, we observe only a slight oxidation of iron, in addition to a weak contribution in the 660-690 cm−1 Raman range. Furthermore, we infer that the most accurate C-DSC results for the AND100 composition are those obtained after AND100_DSC10bis which was the sample that displayed the least changes after the measurement.

For both samples AND100red and AND100ox, Mössbauer results indicated a minor alteration in the iron oxidation following C-DSC experiments at 10 ℃ min-1, with ΔFe3+/∑Fetot equal to 0.02 (Table S2). In contrast, Raman spectroscopy results suggest that both samples developed prominent peaks within the 660–690 cm−1 range after C-DSC measurements, accompanied by the complete shift of the Boson peak under the Rayleigh line (Fig. S2a). On the other hand, samples AND65 and AND0 did not display significant changes following C-DSC experiments, as indicated by both Mössbauer and Raman results (Table S2 and Fig. S2a).

Using our Tonset measurements at 10 ℃ min-1 and Eq. 2 (main text, Materials and Methods section), we derived C-DSC-based glass transition temperature Tg (η ⁓ 1012 Pa s) values of 645, 654, 662, 696 and 737 ℃ (±0.5 ℃) for samples AND100red, AND100, AND100ox, AND65, and AND0, respectively. All in all, we argue that C-DSC measurements performed at Tg remained virtually unaffected by potential nanocrystallization and/or iron oxidation, especially when employing a conservative temperature treatment during the first upscan, as evidenced by the congruent Tonset values of AND100_C-DSC10 and AND100_C-DSC10bis, in contrast to the considerable different Tpeak values of 715 vs 695 ℃, respectively. By applying Eq. 2 (main text, Materials and Methods section), we associated our characteristic Tonset and Tpeak from our C-DSC measurements, which are dependent on qh=qc, to viscosity values (Table S2).

## S2.2 Flash Differential Scanning Calorimetry (F-DSC)

F-DSC measurements of AND100 and AND65 using a heating rate of 1,000 ℃ s-1 resulted in Tonset values of 796 and 847 ℃, and Tpeak values of 867 and 929 ℃, respectively (Fig. S3; Table S2). We observe that F-DSC Tonset and Tpeak increased with increasing SiO2 content and decreasing FeOtot content, in good agreement with our previous C-DSC results. Furthermore, we performed a subsequent series of measurements on the same sample AND100 used before but increasing the heating rate from 1,000 to 10,000 ℃ s-1. Our results evidenced a sustained increase in Tonset, from 851 (F-DSC10000_on_#1) to 890 ℃ (F-DSC10000_on_#5) (Table S2).

Figure S3. F-DSC results for: a) AND100 and b) AND65 using qh=qc= 1000 ℃ s-1.

The collected Raman spectra after F-DSC measurement suggested that sample AND100 underwent minimal changes after the first measurement at 1000 ℃ s-1, manifesting a subtle contribution within the 660–690 cm−1 range and a shift in the boson peak from 70 to 64 cm-1 (Fig 4b). In contrast, sample AND65 did not show any changes after the F-DSC measurement using the same conditions. Noticeably, the collected Raman spectra of AND100 at 10,000 ℃ s-1 showed a progressive increase in the 660–690 cm−1 range, alongside a continuous shift of the boson peak towards lower wavenumbers until the complete disappearance after the last run (F-DSC1000_#5; Fig 3Sb). Moreover, we noted the appearance and gradual strengthening of a new Raman contribution within the 250-305 cm-1 range (highlighted in red in Fig. 3Sb) following the measurement of F-DSC10000_on_#1. This peak is likely associated with the formation of hematite (Jubb and Allen 2010), possibly arising from the oxidation of previously crystallized titanomagnetite nanolites during the F-DSC experiments. Finally, by applying Eq. 2 (main text, Materials and Methods section), we associated viscosity values to our characteristic Tonset and Tpeak from our F-DSC measurements (Table S2).

## S3 Micropenetration and in situ Raman analyses

Micropenetration viscometry results are reported in Table S2 as a function of temperature and experimental duration. We explored samples AND0, AND65 and AND100 targeting temperatures relative to our previous C-DSC measurements. For AND0, we explored the highest characteristic temperature derived via C-DSC (792 ℃), which corresponds to the C-DSC20-pk temperature. For AND65, we employed the Tg (C-DSC10-on, 696 ℃) and two additional temperatures:  Tg + 15 ℃ (711 ℃) and Tg  + 65 ℃ (761 ℃). For AND100, we selected the retrieved Tg (C-DSC10_on, 654 ℃) and C-DSC20_pk (724 ℃) temperatures. In addition, we measured the viscosity at 808 ℃ which corresponds to the maximum temperature employed by Okumura et al. (2022) for a similar andesitic melt (Ande, Table S1).

Micropenetration results (Table S2) showed that viscosity decreases with increasing temperature and that sample AND0 is the most viscous composition, followed by AND65 and then AND100, respectively. For AND0, we measured a viscosity of 1010.43 Pa s at 792 ℃. For AND65, we recorded viscosities of 1012.13, 1010.23 and 1011.66 Pa s at 696, 711 and 761 ℃, respectively. Notably, for sample AND100, we observed a time-dependent increase in viscosity at fixed temperatures. For instance, the viscosity of AND100 at 658.5 ± 1.5 ℃ increased from 1012 to 1012.7 Pa s in 60 minutes. At 723 ± 1.5 ℃, we observed an increase from 1011.04 to 1011.90 Pa over 90 minutes. Finally, at 807 ± 0.5 ℃, we recorded an increase from 109.74 to 1010.17 Pa s in 60 minutes, exhibiting a similar viscosity increase as the one reported by Okumura et al. (2022) at the same temperature (namely, ⁓0.5 log10 units).

Following Eq. 2, we expected to measure a viscosity of ⁓1012 Pa s for measurements performed at the calorimetric Tg (C-DSC10-on) and ⁓1010.3 Pa s for measurements close to the C-DSC20-peak temperature. This was found to be the case for samples AND0 and AND65 where viscosity did not increase over time within the experimental timescale. Nonetheless, in the case of AND100, our observations indicate that the initially recorded viscosity in proximity to the calorimetric Tg corresponds to the anticipated C-DSC-derived viscosity (AND100_MP660_0).

Following the micropenetration measurements, all of our samples underwent subsequent Mössbauer and Raman analyses. Mössbauer and Raman analyses of samples AND65 and AND0 post-micropenetration experiments show no evidence of relevant modifications during measurements (Table S2, Fig. S4). In contrast, Mössbauer results evidence that samples AND100_MP660, AND100_MP723 and AND100_MP808 underwent a significant change in Fe3+/∑Fetot, namely from Fe3+/∑Fetot of 0.64 to 0.70, 0.79 and 0.83 respectively (Table S2). Likewise, these samples exhibited notable development of Raman peaks within the 660–690 cm−1 range (Fig. S4a), suggesting Fe-Ti-oxide nanocrystallization 10,11. Moreover, samples AND100_MP723 and AND100_MP808 developed two additional Raman peaks in the 305-335 and 530-550 cm-1 ranges (Fig. S4a). Additionally, sample AND100_MP808 developed a fourth peak in the 190-200 cm-1 range (Fig. S4a). We notice that these four peaks perfectly match with four of the five theoretically predicted phonon bands of titanomagnetite 21,22. In addition, we noted that the boson peak position of sample AND100_MP660 shifted from 70 to 57 cm-1, while for samples AND100_MP723 and AND100_MP808, the boson peaks completely disappeared after micropenetration experiments. Importantly, we observed a direct correlation between the degree of iron oxidation and nanocrystallization and the experimental temperature. Specifically, samples that deviated further from Tg exhibited more pronounced changes during the measurements. To further explore this phenomenon, we conducted in situ Raman measurements while heating AND100 to 655, 723 and 808 ℃, following a similar heat treatment we implemented for our micropenetration experiments. A comparison between room-temperature Raman spectra after micropenetration measurements and after in situ Raman experiments at a given temperature (Fig. S4b) displayed similar spectroscopic features. In addition, we explored the applicability of Raman spectroscopy to identify presence of Fe-Ti-oxides and to investigate glass structures at high temperatures. Investigating nano-bearing glass, we observed that the intensity of the peak at 660–690 cm−1 range gradually decreases with increasing temperature from the room temperature until it completely disappears at about 500 ℃. While cooling, the mentioned peak reemerges in a similar fashion. However, since the concentration of nanolites remains constant below the glass transition, this effect is purely spectroscopic.

Figure S4. a Raman spectra of samples after micropenetration measurements. The numeric suffixes correspond to the experimental temperature. b Raman spectra of AND100 after in situ Raman experiments. The shaded area in grey corresponds to Raman peaks for titanomagnetite 21,22.

## S4 In-situ TEM analyses

Energy-dispersive X-ray spectra (EDS) before and after experiments are shown in Table S3. These results are affected by systematic errors due to the contribution of the sample holder to EDS spectra (visible as an increase in SiO2, P2O5 and Na2O contents).

| Table S3. High-temperature EDS (TEM) results. |  |  |  |
| --- | --- | --- | --- |
|  | Bulkbefore | Bulkafter, e-beama | Bulkafter, no-beamb |
| SiO2 | 61.0 | 65.9 | 61.3 |
| TiO2 | 1.0 | 0.9 | 0.8 |
| Al2O3 | 14.1 | 18 | 15.7 |
| FeOtot | 7.0 | 6.7 | 6.7 |
| MgO | 2.2 | 2.1 | 2.7 |
| CaO | 6.2 | 5 | 7.2 |
| Na2O | 3.1 | 0 | 2.7 |
| K2O | 1.6 | 0 | 1.3 |
| P2O5 | 3.8 | 1.4 | 1.6 |
| aEDS result of the post in-situ area affected by the electron beam. |  |  |  |
| bEDS result of an adjacent region that was not directly affected by the electron beam. |  |  |  |

Figure S5. HAADF and EDS elemental map of sample AND100 after in-situ high-temperature experiments. Maps show the distribution of Fe, Si, Al, and Fe+Si+Al.

Figure S6. Temperature profile for High-temperature TEM experiment

## S5 Concentric cylinder (CC) measurements

The viscosity of AND100ox and AND0 melts were determined using a concentric cylinder setup. High-temperature melt viscosity results are reported as a function of temperature in Table S2 and shown in Fig. S7. AND100 melt viscosity increases from 102.0 to 103.8 Pa s when decreasing the temperature from 1435 to 1150 ℃. The AND0 viscosity grew from 102.8 to 104.9 Pa s when decreasing the temperature from 1404 to 1130 ℃. At constant temperature, the viscosity of AND100 is at least ~100.8 Pa s lower than AND0 in this temperature range, showing a direct relationship with SiO2 content and thereby NBO/T (Table S1).

Figure S7. Concentric cylinder results and literature viscosity data 2,4,5.

## S6 Viscosity models of andesitic melts free of nanocrystals

Considering our comprehensive experimental investigations, we introduce novel viscosity parameterizations for various andesitic melts (Fig. S8). These curves are obtained by fitting viscosity data from samples free of nanolites (further details in S2.1, S2.2 and S3), classified by consistent iron oxidation states. We utilized the MYEGA parametrization (Eq. 5), with log10η∞ fixed at -2.93 15,17,23,24 to fit the melt fragility index (m). Together with our C-DSC-derived Tg  (Table 2), this approach enables us to characterize melt viscosity over a broad range of temperatures.

For our AND100, we combined our high-temperature concentric cylinder viscosity data along with C- and F-DSC-derived viscosity data (Table S2). By fitting Tg_AND100 =  654 ± 0.5 ℃ (from AND100_DSC10-matching),  and using Eq. 5, we derived a fragility (mAND100) of 30.5 ± 0.5. For the iron-free analog sample (AND0), by utilizing our C-DSC-derived viscosity data (Table S2) along with micropenetration and concentric cylinder data, we determined mAND0 = 31.8 ± 0.2 by fitting Tg_AND0 = 737 ± 0.5 ℃. For AND65, it was observed that its K/G ratio exhibited ideal mixing relative to its two end members in terms of transition metal content, namely AND0 and AND100. Therefore, by assuming that the fragility of AND65 can be obtained as the simple linear combination of the fragility values of AND100 and AND0 (i.e., mAND65 = 0.65 ⨉ mAND100 + 0.35 ⨉ mAND0  = 31.3 ± 0.2) and using the C-DSC derived Tg_AND65 = 696 ± 0.5 ℃, we derive a viscosity parametrization for AND65. Notably, our micropenetration and F-DSC-derived viscosity values, which were not used in this parametrization, closely align with our predictions (Fig. 2a). These results confirm that the shift factor approach (Eq. 2) is also valid for this composition. It is noteworthy to mention that when using all our viscosity results for AND65, we obtain the same fragility results.

Regarding AND100red and AND100ox, the absence of viscosity data in the high-temperature range via concentric cylinder measurements prevents direct determination of the melt fragility index (m). Nevertheless, we can estimate their fragility values by leveraging our prior fragility estimations (i.e., AND100) along with our Brillouin data. Brillouin results show that the K/G ratios of AND100red, AND100ox and AND100 are identical within experimental uncertainty (Table S1). Therefore, assuming a linear correlation between K/G and m 20,25,  we infer that the fragility of AND100red and AND100ox are comparable to that of AND100 (mAND100red = mAND100ox = mAND100 = 30.5 ± 0.5). By using Tg_AND100red = 645 ℃ and Tg_AND1000ox = 662 ℃ (Table 1), and Eq. 5, we derive the viscosity parametrization for AND100red and AND100ox (Fig S8). Overall, our viscosity parametrization for AND100red aligns slightly lower than that of AND100, while AND100ox sits slightly above AND100, consistent with their respective lower and higher Fe3+/∑Fetot content and Tg values.

Figure S8. Viscosity result and MYEGA parametrizations. Each colour represents a  distinct chemical composition (Table 1). The proposed viscosity models, based on Mauro et al., 2009, are represented by straight lines. Red crosses depict viscosity from Okumura et al, 2022, showing a composition similar to our AND100. Red and black dashed line corresponds to the predicted viscosity of Giordano et al., 2008, for AND100 and AND0 composition, respectively.

## S6 TEM analysis of post-micropenetration samples

Diffraction patterns of AND100 samples after micropenetration experiments are shown in Fig. S9.   AND100_MP660 displays one diffraction ring (d = 2.532(5) Å) and assigned to the most intense reflection of titanomagnetite (311) (Fig. S9a). For AND100_MP723, we observe the appearance of two extra low-intensity rings with associated d-spacings of 1.484(8) and 2.099(9) Å, assignable to 440 and 400 respectively (Fig. S9b). These three diffraction rings were even more evident in AND100_MP808 and accompanied by other less intense ones, assigned to 220, 511, 620, and 642 orientations 26 (Fig. S9c). Notably, pseudobrookite (Fe2TiO5) was exclusively identified in sample AND100_MP808 (Fig S9c) as an individual diffraction spot.

Figure S9. TEM diffraction patterns of AND100 samples after micropenetration experiments. a MP660. b MP723. c MP807. Yellow values correspond to d-spacings associated with titanomagnetite. In red, the identification of a d-spacings associated with pseudobrookite (Fe2TiO5).

Figure S10 shows the pixel segmentation methodology using the ilastik software 27. STEM-HAADF images were segmented and separated based on hand-picked contrast thresholds software training. Further, we extracted the geometrical properties of every single nanolite providing radius, minimum nanolite content (in vol%) and minimum nanolite number density (NND) for the three AND100 samples subjected to micropenetration (Table S4). It is important to mention that these results represent a conservative minimum estimation.

Figure S10. a HAADF image of sample AND100_ MP723. b pixel segmentation of HAADF image c. phase separation of nanolites. Pixel segmentation and separation using the ilastik software, version 1.4.0 27.

Figure S11. HAADF and EDS elemental map of sample AND100_MP660 showing Fe, Ti, Si, Al, and Fe+Ti+Al distribution.

Figure S12. HAADF and EDS elemental map of sample AND100_MP723 showing Fe, Ti, Si, Al, and Fe+Ti+Al distribution.

| Table S4. Post-micropenetration EDS (STEM) results for AND100 samples. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample label | Region | SiO2 | TiO2 | Al2O3 | FeOtot | MgO | CaO | Na2O | K2O | P2O5 | min. crystal radiusavg. (nm) | lamella thickness (nm) | min. crystal vol% | min. NND* (nm-3) ⨉ 10-4 |
| MP660 | Bulk | 61.8 | 0.7 | 17.5 | 7.1 | 3.0 | 5.7 | 1.3 | 2.3 | 0.60 | 1.39 ± 0.55 | 50 | 0.12 | 0.43 |
|  | Matrix | 70 (9) | 0.5 (1) | 16 (7) | 6.9 (2) | 3.1 (5) | 3.6 (2) | 0.5 (1) | 0.9 (1) | 1.2 (2) |  |  |  |  |
|  | Nanolite | 55 (9) | 0.8 (1) | 21 (7) | 10.6 (6) | 4.3 (6) | 6.1 (3) | 0.7 (1) | 0.8 (1) | 1.3 (2) |  |  |  |  |
|  | Nanolite+Halo | 60 (3) | 1 (1) | 20 (4) | 8 (2) | 2.8 (2) | 6.3 (2) | 0.5 (0.5) | 0.6 (0.6) | 0.8 (1) |  |  |  |  |
| MP723 | Bulk | 62.7 | 0.8 | 17.4 | 7.1 | 2.8 | 6.1 | 0.8 | 2.0 | 0.20 | 2.44 ± 0.71 | 50 | 1.70 | 2.09 |
|  | Matrix | 71 (5) | 0.8 (0.9) | 16 (4.8) | 2.8 (1.6) | 2 (1) | 4.7 (2) | 0.4 (0.6) | 0.8 (0.9) | 1 (0.6) |  |  |  |  |
|  | Nanolite | 53 (9) | 1.6 (1) | 18.6 (6) | 13 (5) | 2.5 (2) | 7.3 (4) | 0.8 (1) | 1.3 (2) | 0.7 (2) |  |  |  |  |
|  | Nanolite+Halo | 60 (3) | 1.1 (0.5) | 18 (1.4) | 8.4 (2) | 3.1 (1) | 6.8 (4) | 0.5 (0.4) | 0.9 (0.6) | 0.4 (0.6) |  |  |  |  |
| MP808 | Bulk | 60.4 | 1.1 | 16.7 | 7.2 | 2.8 | 7.0 | 2.5 | 2.3 | 2.29 | 2.60 ± 0.82 | 24 | 1.01 | 1.35 |
|  | Matrix | 70 (3) | 0.6 (0.9) | 14 (3.4) | 1.7 (1) | 2.2 (1.9) | 6.3 (2) | 2 (1.6) | 1.7 (1.1) | 0.9 (1) |  |  |  |  |
|  | Nanolite | 44 (10) | 2.9 (2) | 16.1 (7) | 22 (5) | 4 (3) | 8 (4) | 1 (1) | 0.8 (1) | 1 (0.9) |  |  |  |  |
|  | Nanolite+Halo | 58 (4) | 1.4 (0.5) | 18.5 (1.4) | 11 (2) | 3.4 (1) | 7.8 (1) | 0.9 (0.8) | 1 (1) | 1 (1) |  |  |  |  |
| *Nanolite number density (NND): amount of nanolites per volume |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

# References

1.	Okumura, S. et al. Rheology of nanocrystal-bearing andesite magma and its roles in explosive volcanism. Commun. Earth Environ. 3, 241 (2022).

2.	Giordano, D. et al. An expanded non-Arrhenian model for silicate melt viscosity: A treatment for metaluminous, peraluminous and peralkaline liquids. Chem. Geol. 229, 42–56 (2006).

3.	Liebske, C., Behrens, H., Holtz, F. & Lange, R. A. The influence of pressure and composition on the viscosity of andesitic melts. Geochim. Cosmochim. Acta 67, 473–485 (2003).

4.	Richet, P., Lejeune, A. M. M., Holtz, F. & Roux, J. Water and the viscosity of andesite melts. Chem. Geol. 128, 185–197 (1996).

5.	Neuville, D. R., Courtial, P., Dingwell, D. B. & Richet, P. Thermodynamic and rheological properties of rhyolite and andesite melts. Contrib. to Mineral. Petrol. 113, 572–581 (1993).

6.	Prata, G. S. et al. A New Parameterization of Volcanic Ash Complex Refractive Index Based on NBO/T and SiO 2 Content. J. Geophys. Res. Atmos. 124, 1779–1797 (2019).

7.	Prescher, C., McCammon, C. & Dubrovinsky, L. MossA : a program for analyzing energy-domain Mössbauer spectra from conventional and synchrotron sources. J. Appl. Crystallogr. 45, 329–331 (2012).

8.	Le Losq, C., Neuville, D. R., Moretti, R. & Roux, J. Determination of water content in silicate glasses using Raman spectrometry: Implications for the study of explosive volcanism. Am. Mineral. 97, 779–790 (2012).

9.	Giordano, D. et al. A calibrated database of Raman spectra for natural silicate glasses: implications for modelling melt physical properties. J. Raman Spectrosc. 51, 1822–1838 (2020).

10.	Di Genova, D. et al. In situ observation of nanolite growth in volcanic melt: A driving force for explosive eruptions. Sci. Adv. 6, (2020).

11.	Di Genova, D., Zandona, A. & Deubener, J. Unravelling the effect of nano-heterogeneity on the viscosity of silicate melts: Implications for glass manufacturing and volcanic eruptions. J. Non. Cryst. Solids 545, 120248 (2020).

12.	Di Genova, D. et al. Effect of iron and nanolites on Raman spectra of volcanic glasses: A reassessment of existing strategies to estimate the water content. Chem. Geol. 475, 76–86 (2017).

13.	Schiavi, F. et al. Water quantification in silicate glasses by Raman spectroscopy: Correcting for the effects of confocality, density and ferric iron. Chem. Geol. 483, 312–331 (2018).

14.	Stabile, P. et al. The effect of iron and alkali on the nanocrystal-free viscosity of volcanic melts: A combined Raman spectroscopy and DSC study. Chem. Geol. 559, 119991 (2021).

15.	Scarani, A. et al. A chemical threshold controls nanocrystallization and degassing behaviour in basalt magmas. Commun. Earth Environ. 3, 284 (2022).

16.	Di Genova, D. et al. A compositional tipping point governing the mobilization and eruption style of rhyolitic magma. Nature 552, 235–238 (2017).

17.	Valdivia, P. et al. Are volcanic melts less viscous than we thought? The case of Stromboli basalt. Contrib. to Mineral. Petrol. 178, 45 (2023).

18.	Schroeder, J. et al. Raman scattering and Boson peaks in glasses: temperature and pressure effects. J. Non. Cryst. Solids 349, 88–97 (2004).

19.	Zanatta, M. et al. Debye to non-Debye scaling of the Boson peak dynamics: Critical behavior and local disorder in vitreous germania. J. Chem. Phys. 135, (2011).

20.	Cassetta, M. et al. Estimating the viscosity of volcanic melts from the vibrational properties of their parental glasses. Sci. Rep. 11, 1–14 (2021).

21.	Shebanova, O. N. & Lazor, P. Raman spectroscopic study of magnetite (FeFe2O4): a new assignment for the vibrational spectrum. J. Solid State Chem. 174, 424–430 (2003).

22.	Jubb, A. M. & Allen, H. C. Vibrational Spectroscopic Characterization of Hematite, Maghemite, and Magnetite Thin Films Produced by Vapor Deposition. ACS Appl. Mater. Interfaces 2, 2804–2812 (2010).

23.	Langhammer, D., Di Genova, D. & Steinle-Neumann, G. Modeling the Viscosity of Anhydrous and Hydrous Volcanic Melts. Geochemistry, Geophys. Geosystems 22, 1–26 (2021).

24.	Mauro, J. C., Yue, Y., Ellison, A. J., Gupta, P. K. & Allan, D. C. Viscosity of glass-forming liquids. Proc. Natl. Acad. Sci. U. S. A. 106, 19780–4 (2009).

25.	Novikov, V. N., Ding, Y. & Sokolov, A. P. Correlation of fragility of supercooled liquids with elastic properties of glasses. Phys. Rev. E - Stat. Nonlinear, Soft Matter Phys. 71, 1–12 (2005).

26.	Wechsler, B. A., Lindsley, D. H. & Prewitt, C. T. Crystal structure and cation distribution in titanomagnetites (Fe3-xTixO4). Am. Mineral. 69, 754–770 (1984).

27.	Berg, S. et al. Ilastik: Interactive Machine Learning for (Bio)Image Analysis. Nat. Methods 16, 1226–1232 (2019).