Electronic Supporting Information (ESI)

for

Solid-state NMR spectroscopic studies of 13C,15N,29Si-enriched biosilica from the marine diatom Cyclotella cryptica

Felicitas Kolbe,1 Helena L. Ehren,2 Simon Kohrs,1 Daniel Butscher,1 Lukas Reiß,1# 
Marc Baldus,2 Eike Brunner1

1 Chair Bioanalytical Chemistry, Faculty of Chemistry and Food Chemistry, TU Dresden, 01062 Dresden, Germany

2 NMR Spectroscopy, Bijvoet Center for Biomolecular Research Utrecht University, 3584 CH Utrecht, The Netherlands

# present address: Hochschule für Bildende Künste (HfBK) Dresden, Güntzstraße 34, 01307 Dresden, Germany

1. Additional solid-state NMR spectra of C. cryptica

Additional 1- and 2-dimensional NMR spectra

Figure S1. 29Si MAS NMR spectrum (direct excitation) of 13C,15N,29Si-enriched biosilica of C. cryptica.

Figure S2. 15N CP/MAS NMR spectrum of 13C,15N,29Si-enriched biosilica of C. cryptica. CP contact time: 4 ms.

Figure S3. 13C MAS NMR spectrum (direct excitation) of the NaOH-treated insoluble organic matrix of C. cryptica. The main signals can be assigned to different chitin conformations (cf. Table 1, main article).

Figure S4. Zoom into the C-1 Signal at the 13C MAS NMR spectrum (direct excitation) of the NaOH-treated insoluble organic matrix of C. cryptica. Right: Resulting fit of the C-1 signal.

A zoom into the characteristic C-1 signal confirms the presence of two different chitin conformations. The signal splits into two doublets due to the 13C-13C spin-spin coupling. The observed coupling constant is around 44 Hz for both C-1 signals. This signal with its two overlapping doublets can be fitted using Dmfit.1 As result the contribution of both chitin signals to the total signal intensity can be estimated. For the C-1 signal which is used exemplary here, a α-like chitin : β-chitin ratio of 1:2 was determined. Thus, the amount of the β-chitin fibers is approximately twice as high as the amount of chitin in the α-like conformation.

Figure S5. PDSD (Proton-Driven Spin-Diffusion) experiment of 13C,15N,29Si-enriched C. cryptica and T. pseudonana biosilica. Top: The chitin correlation signals are highlighted. The correlation signals at 78 ppm and 83 ppm which are an indication for cross-linking occur in both samples (marked with green crosses). Bottom: A zoom into the carbohydrate region shows the presence of two different chitin forms. The amorphous chitin is marked in pink.

A comparison of the NMR spectra of C. cryptica and T. pseudonana reveals similar correlation signals especially in the carbohydrate region. Both species have two different forms of chitin, a crystalline β-chitin and an amorphous chitin, which was found to build a chitin-based meshwork in T. pseudonana, previously. Interestingly, the correlation signals at 78 ppm and 83 ppm which were discussed for C. cryptica in the main article also occur in the spectrum of T. pseudonana. Since cross-linking between proteins and carbohydrates was already shown for T. pseudonana,2,3 the occurrence of this correlation signals in both spectra is a very strong indication for cross-linking.

Additional 13C{29Si} REDOR data

Figure S6. Pulse sequence of the 13C{29Si} REDOR experiment. A signal intensity Sr is measured when the π-pulses on the 29Si channel cause partial echo dephasing. The echo intensity S0 is measured without 29Si irradiation. The scheme is drawn for N = 2.

Figure S7. 13C{29Si} REDOR curves and the fitted first order approximation of the 13C,15N,29Si-enriched C. cryptica biosilia for the signals at 43 ppm and 56 ppm.

2. Scanning Electron Microscopy (SEM) images

Figure S8. SEM image of the 13C,15N,29Si-enriched C. cryptica biosilica prepared for the NMR experiments, originally. The fibers shown in this image are supposed to consist of β-chitin. Fibers like this were found in ca. 1 of 10 image sections only.

Figure S9. SEM images of the insoluble organic matrix of C. cryptica. Even after desilification the valve shape remains nearly unchanged. Various valve-shaped organic matrices were found. Additionally, some chitin fibers were also observed.

3. Monosaccharide analysis of C. cryptica biosilica and its insoluble organic matrix

Figure S10. Presence of N-acetyl-glucosamine (NAG) in the isolated insoluble organic matrix of C. cryptica after chitinase treatment with chitinase from Trichoderma viride detected with GC-MS in comparison to a chitin reference sample.

Figure S11. Exemplary mass spectrum of a non-assigned pyranose from the C. cryptica biosilica sample (normalized retention time tR, norm. = 1.240).

4. Amino acid analysis of C. cryptica biosilica

Experimental setup

The amino acid analysis was performed using a slightly modified protocol for LC-MS (liquid chromatography coupled with mass spectrometry) measurements.4

1. Hydrolysis

For the amino acid analysis, biosilica samples were hydrolyzed. 5 mg of a sample were sealed under vacuum in a glass ampoule after adding 0.5 mL 6 N HCl. The glass ampoules were put into a thermomixer and hydrolysis was performed at 110°C and shaking of 250 rpm for 24 h. Afterwards, the ampoules were opened and the hydrolysates were dried under vacuum at room temperature.

2. Sample preparation

The dried hydrolysates were extracted with 0.5 mL of ultrapure water six times (20800g, 5 min). The supernatants of the first three extraction steps were collected in one vial as main fraction. The supernatants of the three later extraction steps were used for a second extraction of the residue from the main fraction. The enriched rest fraction was collected in another vial as rest fraction. 100 µL of an internal standard solution (300 mg/L L-3,4-Dihydroxyphenylalanine (L-DOPA, Alfa Aesar) in ultrapure water) were added to the main fraction. All main and rest fractions were dried under vacuum at room temperature. The residue of the rest fraction was dissolved in 1 mL ultrapure water and transferred to the vial of the main fraction. The sample was diluted 1:10 for the measurements.

Calibration was performed using a standard solution that contains all 21 proteinogenic amino acids and the internal Standard L-DOPA.

3. LC-MS analysis

For liquid chromatography, a Polaris 3 C18 ether column (150x3 mm, Agilent Technologies) was used in a HPLC system Agilent 1260 Infinity (Agilent Technologies). For detection, an Agilent 6538 UHD Accurate-Mass Q-TOF-mass spectrometer with electron spray ionization (ESI) ion source was used. 5 µL of each sample were injected. The flow rate was set to 0.3 mL/min. The temperature of the column oven was 25°C. For the elution a mixture of 0.1% HCOOH in H2O and acetonitrile is used. The solvent gradient is described in Table S1. The carrier gas in the coupled mass spectrometer was set to a temperature of 250°C and a flow rate of 12 L/min. Ionization occurs using ESI (positive) with an ionization voltage of 2500 V. The fragmentor voltage was set to 80 V, the voltage of the skimmer was set to 45 V and the voltage of the octopole was set to 250 V.

Two samples of C. cryptica biosilica were prepared and measured parallel for validation of the results.

Table S1. Solvent gradient during LC-MS measurements used for amino acid analysis.

| t / min | 0.1% HCOOH in H2O / % | acetonitrile / % |
| --- | --- | --- |
| 0 | 99 | 1 |
| 10 | 99 | 1 |
| 15 | 0 | 100 |
| 25 | 0 | 100 |
| 27 | 99 | 1 |
| 40 | 99 | 1 |

Results

The two parallel measurements of the hydrolysates of C. cryptica biosilica show similar results. The averaged results are shown in Figure S12. Note, that asparagine and glutamine react under the chosen hydrolysis conditions (24 h, 110°C, 6 N HCl) to aspartic acid and glutamic acid and cannot be determined separately. The disulfide bridges in cystine were not broken during hydrolysis. Thus, cysteine can only be detected as cystine. Tryptophan is destroyed completely during hydrolysis.

The amino acid analysis shows that the silica-associated proteins are built up mainly of a minor number of the proteinogenic amino acids. Especially the amino acids serine, glycine, aspartic and glutamic acid as well as alanine and leucine should be mentioned. This observation is in good agreement to former amino acid analysis of diatom biosilica and its insoluble organic matrices.4,5

Figure S12. Results of the amino acid analysis of C. cryptica biosilica (mole fraction χi in mol%) using LC-MS. The amino acids asparagine and glutamine as well as cysteine and tryptophan are not listed due to the described influence of the chosen hydrolysis conditions (see above).

5. References

(1) 	Massiot, D.; Fayon, F.; Capron, M.; King, I.; Le Calvé, S.; Alonso, B.; Durand, J. O.; Bujoli, B.; Gan, Z.; Hoatson, G. Modelling One- and Two-Dimensional Solid-State NMR Spectra. Magn. Reson. Chem. 2002, 40 (1), 70–76.

(2) 	Poulsen, N.; Sumper, M.; Kröger, N. Biosilica Formation in Diatoms: Characterization of Native Silaffin-2 and Its Role in Silica Morphogenesis. Proc. Natl. Acad. Sci. U. S. A. 2003, 100 (21), 12075–12080.

(3) 	Poulsen, N.; Kröger, N. Silica Morphogenesis by Alternative Processing of Silaffins in the Diatom Thalassiosira Pseudonana. J. Biol. Chem. 2004, 279 (41), 42993–42999.

(4) 	Jantschke, A.; Koers, E.; Mance, D.; Weingarth, M.; Brunner, E.; Baldus, M. Insight into the Supramolecular Architecture of Intact Diatom Biosilica from DNP-Supported Solid-State NMR Spectroscopy. Angew. Chem. Int. Ed. 2015, 54 (50), 15069–15073.

(5) 	Pawolski, D.; Heintze, C.; Mey, I.; Steinem, C.; Kröger, N. Reconstituting the Formation of Hierarchically Porous Silica Patterns Using Diatom Biomolecules. J. Struct. Biol. 2018, 204 (1), 64–74.