Basic magnesium sulfate@TiO2 composite for efficient adsorption and photocatalytic degradation of 4-dodecylmorpholine in brine

Zhongmei Song a,d, Huifang Zhang a,, Liang Maa,d, Miao Lua,d, Chengyou Wub,, Qingqing Liu c, Xuefeng Yu c, Haining Liu a,, Xiushen Ye a, Zhen Ma c, Zhijian Wua

a Key Laboratory of Green and High-end Utilization of Salt Lake Resources, Qinghai Institute of Salt Lakes, Chinese Academy of Sciences, Xining 810008, China

b Qinghai University, Xining 810016, China

c Qinghai Salt Lake Industry Co., Ltd., Golmud 816000, China

d University of Chinese Academy of Sciences, Beijing 100049, China

Contents:

Text sections:

S1. Adsorption isotherms

S2. Adsorption kinetics

S3. Adsorption thermodynamics

S4. Density functional theory (DFT) calculation methods

Tables: 8

Figures: 4

S1. Adsorption isotherms

The adsorption isotherm of the prepared BMS@TiO2 was analyzed using the Langmuir, and Freundlich models. The mathematical expressions are shown in Eq. (S1) ~ (S2), respectively [1].

(S1)

(S2)

Where qe, qmax, and Ce represent the equilibrium adsorption (mg·g-1), the maximum adsorption (mg·g-1), and the equilibrium concentration of DMP (mg·L-1), respectively. KL, KF, and n represent Langmuir, and Freundlich’s constants, respectively.

S2. Adsorption kinetics

As the prediction of the adsorption speed is essential in the surface adsorption process, several kinetics models such as the pseudo-first-order, and pseudo-second-order are applied to evaluate the kinetics behavior of BMS@TiO2. Eq. (S3) ~ (S4) show the mathematical expression of the pseudo-first-order, and pseud-second-order [2].

(S3)

(S4)

Where qt and qe represent the DMP adsorption capacity at a certain time (mg·g-1) and its equilibrium adsorption capacity (mg·g-1), K1 (h-1) and K2 (g·mg-1·h-1) are the kinetics constants of pseudo-first order and pseudo-second order, respectively, and t is the adsorption time (h).

S3. Adsorption thermodynamics

The thermodynamics parameters, such as the thermodynamic equilibrium constant (Keq), Gibbs free energy (ΔG), standard enthalpy of adsorption (ΔH°), and standard entropy of adsorption (ΔS°) for the removal of DMP using BMS@TiO2 are determined by applying the Van’t Hoff equations as expressed by Eq. (S5) ~ (S7) [3, 4].

(S5)

(S6)

(S7)

Here KL, and Keq represent the Langmuir constant and the standard thermodynamic equilibrium constant of adsorption, respectively. The KL constant is simply recalculated as dimensionless by multiplying it by 55.5 (the number of moles of water per liter of solution). Madsorbate represents the molar mass of DMP. ΔG (kJ mol-1), ΔH° (kJ mol-1), and ΔS° (J mol-1·K-1) represent the standard Gibbs free energy, enthalpy, and entropy of adsorption. R (8.314 J·mol-1·K-1) is the universal gas constant, and T represent the absolute temperature (K).

S4. Density functional theory (DFT) calculation methods

The theoretical calculations were performed via the Gaussian 16 suite of programs [5]. The structure of the studied molecules was fully optimized at the B3LYP-D3BJ/def2-SVP level of theory. The solvent effect was included in the calculations using the solvation model based on the density (SMD) model. The vibrational frequencies of the optimized structures were carried out at the same level. The structures were characterized as a local energy minimum on the potential energy surface by verifying that all the vibrational frequencies were real. The Visual Molecular Dynamics (VMD) program [6] was used to plot the color-filled iso-surface graphs to visualize the molecular orbitals and the molecular electrostatic potential (MESP).

Tables

Table S1. Key physicochemical properties of dodecylmorpholine [7].

| Molecular formula | C16H33NO | 2-D structure |  |
| --- | --- | --- | --- |
| Molecular weight (g·mol-1) | 255.44 | 3-D structure |  |
| Density (25℃) (g·cm-3) | 0.859 | Octanol-water partition coefficient log Kow | 5.05 |
| Water solubility (25℃) (mg·L-1) | insoluble | Boiling point (℃) | 321 |

Table S2. Elemental composition in BMS and BMS@TiO2.

| Elementals | Elemental measurement |  |  |  |
| --- | --- | --- | --- | --- |
|  | BMS |  | BMS@TiO2 |  |
|  | Mass fraction/% | Atom fraction | Mass fraction/% | Atom fraction |
| Oxygen (O) | 59.3 | 0.2 | 55.3 | 0.2 |
| Magnesium (Mg) | 27.9 | 0.2 | 31.8 | 0.2 |
| Sulfur (S) | 6.9 | 0.1 | 8.3 | 0.1 |
| Carbon (C) | 5.9 | 0.3 | 3.2 | 0.3 |
| Titanium (Ti) | 0.0 | 0.0 | 1.4 | 0.1 |

Table S3. Pore features of BMS and BMS@TiO2.

| Sample | BET surface area (m2·g-1) | Pore volume (cm3·g-1) | Average pore diameter (nm) |
| --- | --- | --- | --- |
| BMS | 35.30 | 0.084 | 9.53 |
| BMS@TiO2 | 37.24 | 0.083 | 8.95 |

Table S4. Kinetic model parameters of adsorption for DMP onto BMS@TiO2.

| Model | Parameter | Values |
| --- | --- | --- |
| Pseudo-first-order | K1 (h-1) | 0.2128 |
|  | qe (mg·g-1) | 5.5131 |
|  | R2 | 0.9349 |
| Pseudo-second-order | K2 (g·mg-1·h-1) | 0.1635 |
|  | qe (mg·g-1) | 5.4905 |
|  | R2 | 0.9907 |

Table S5. Isotherm model parameters of adsorption for DMP onto BMS@TiO2.

| Model | Temperature | Parameter | Values |
| --- | --- | --- | --- |
| Langmuir | 25℃ | qmax (mg·g-1) | 12.8927 |
|  |  | KL (L·mg-1) | 0.0279 |
|  |  | R2 | 0.9995 |
|  | 35℃ | qmax (mg·g-1) | 8.5984 |
|  |  | KL (L·mg-1) | 0.0784 |
|  |  | R2 | 0.9977 |
|  | 45℃ | qmax (mg·g-1) | 7.5442 |
|  |  | KL (L·mg-1) | 0.1657 |
|  |  | R2 | 0.9947 |
| Freundlich | 25℃ | KF (L·g-1) | 0.5798 |
|  |  | n-1 | 0.6697 |
|  |  | R2 | 0.9949 |
|  | 35℃ | KF (L·g-1) | 1.2853 |
|  |  | n-1 | 0.4673 |
|  |  | R2 | 0.9706 |
|  | 45℃ | KF (L·g-1) | 2.2493 |
|  |  | n-1 | 0.3146 |
|  |  | R2 | 0.9072 |

Table S6. The thermodynamic parameters of adsorption for DMP onto BMS@TiO2.

| T (℃) | ΔH° (kJ·mol-1) | ΔS° (J·mol-1·K-1) | ΔG (kJ·mol-1) |
| --- | --- | --- | --- |
| 25 | 70.40 | 343.58 | -31.94 |
| 35 |  |  | -35.67 |
| 45 |  |  | -38.80 |

Table S7. Binding energy of elements on BMS@TiO2 surface before and after adsorption

| Atomic orbital | Binding energy before adsorption (eV) | Binding energy after adsorption(eV) | Binding energy offset(eV) |
| --- | --- | --- | --- |
| Mg1s | 1303.68 | 1303.16 | -0.52 |
| O1s | 531.10 | 530.90 | -0.20 |
| Ti2p | 457.81 | 457.80 | -0.01 |
| S2p | 168.60 | 168.75 | +0.15 |

Table S8. Kinetic model parameters of photodegradation for DMP by BMS@TiO2.

|  | Pseudo-first order |  | Pseudo-second order |  |
| --- | --- | --- | --- | --- |
| Parameter | k1 (h-1) | R2 | k2 (h·mg-1) | R2 |
| Values | 0.2281 | 0.9813 | 0.6081 | 0.9187 |

Figures

Fig. S1. (a) Schematic diagram of the formation and decomposition process of methyl orange and DMP complexes, and (b) DMP concentration standard curve.

Fig. S2. XRD patterns of effect of co-existing salt: (a) KCl, (b) NaCl, and (c) MgCl2, (d) XRD patterns of 1 mol·L-1 ionic strength with different salts.

Fig. S3. (a) SEM images, (b) XRD patterns, (c) FTIR spectra, and (d) XPS full-scan spectra for BMS@TiO2 before and after adsorption.

Fig. S4. (a) TOC removal efficiency of DMP adsorbed on BMS@TiO2 by photocatalytic degradation, (b) Total gas chromatogram of DMP at 0, 12, and 16 hours of photocatalytic degradation by BMS@TiO2, and (c) Mass spectra of main substances appeared in the gas chromatogram.

References

- Gao, M.W., Li, B., Liu, J., Hu, Y.N., Cheng, H.F. Adsorption behavior and mechanism of p-arsanilic acid on a Fe-based metal-organic framework. J. Colloid Interface Sci. 629, 616-627 (2023).

- Tseng, R.L., Wu, P.H., Wu, F.C., Juang, R.S. A convenient method to determine kinetic parameters of adsorption processes by nonlinear regression of pseudo-nth-order equation. Chem. Eng. J. 237, 153-161 (2014).

- Hasanzadeh, M., Simchi, A., Shahriyari Far, H. Nanoporous composites of activated carbon-metal organic frameworks for organic dye adsorption: Synthesis, adsorption mechanism and kinetics studies. J. Ind. Eng. Chem. 81, 405-414 (2020).

- Zhou, X.Y., Zhou, X. The unit problem in the thermodynamic calculation of adsorption using the Langmuir equation. Chem. Eng. Commun. 201, 1459-1467 (2014).

- Frisch, M.J. et al. Gaussian 16 Revision A 03 (Gaussian, 2016).

- Humphrey, W., Dalke, A., Schulten, K. VMD: Visual molecular dynamics. J. Mol. Graphics 14, 33-38(1996).

- U.S. Environmental Protection Agency. Comptox Chemicals Dashboard. https://comptox.epa.gov/dashboard/chemical/details/DTXSID4042171 (accessed January 23, 2024).

Corresponding authors. E-mail addresses: zhanghf@isl.ac.cn (H.F. Zhang); wuchengyou86@163.com; liuhn@isl.ac.cn (H.N. Liu).