Supporting Information

Supracluster Rotaxanes with Adaptive Al8 Macrocycle for Tunable Optical Limiting

Ya-Jie Liu, Chan Zheng, Di Wang, Han Xiao, Zirui Wang, Cheng-Yang Zhang, Xue-Zhen Zhang, San-Tai Wang, Ran-Qi Chen, Wei-Hui Fang* and Jian Zhang*

Table of Content

Experimental Section	S2

1.	A summary of reported macrocycles used for constructing rotaxane	S4

2.	Crystallographic data and structure refinement parameters	S5

3.	Structure description for Al8 macrocycle	S9

4.	BVS analysis for AlOC-137 to AlOC-149	S10

5.	PXRD analyses	S15

6.	FT-IR analyses	S19

7.	EDS analyses	S23

8.	Reaction equations	S28

9.	UV-vis analyses	S29

10.	Structure description for AlOC-137 to AlOC-149	S33

11.	NLO analyses	S51

References	S58

Experimental Section

Chemicals and Materials All the reagents and solvents employed are purchased commercially and used as received without further purification. Al(OiPr)3 was acquired from Aladdin Chemical Reagent Shaihai. Acetonitrile (99%), 1-naphthoic acid (NA), AgNO3, silver acetate (AgAc) and 1,3-propylenediamine were bought from Sinopharm Chemical Reagent Beijing. Ti(OiPr)4, 4,4’-bipyridine (bpy), silver benzoate (AgBC), AgI, CuBr, tetrabutylammonium chloride (TBACl), tetrabutylammonium bromide (TBAB) and sodium anthraquinone-1-sulfonate (NaAQS) were purchased from Adamas-beta.

Materials and Instrumentation.

The energy dispersive spectroscopy (EDS) analyses of single crystals were performed on a JEOL JSM6700F field-emission scanning electron microscope equipped with an Oxford INCA system.

IR spectra (KBr pellets) were recorded on an ABB Bomem MB102 spectrometer over a range 600-3800 cm-1.

Powder X-ray diffraction (PXRD) data were collected on a Rigaku Mini Flex II diffractometer using CuK radiation (λ = 1.54056 Å) under ambient conditions.

The UV-vis diffuse reflection data were recorded at room temperature using a powder sample with BaSO4 as a standard (100% reflectance) on a PerkinElmer Lamda-950 UV spectrophotometer and scanned at 190–1000 nm. The absorption data were calculated from the Kubelka-Munk function, (F(R) = (1-R)2/2R), where R represents the reflectance.1

General methods for X-ray Crystallography. Crystallographic data for compounds (AlOC-137 to AlOC-144, AlOC-146, AlOC-147 and AlOC-149) were collected on Hybrid Pixel Array detector equipped with graphite-monochromated Ga Kα radiation (λ = 1.3405 Å). While the crystallographic data for AlOC-145 and AlOC-148 were collected on a Supernova single crystal diffractometer equipped with graphite-monochromatic Cu Kα radiation (λ = 1.5418 Å). The structures were solved with direct methods using OLEX2 and refined by full-matrix least-squares on F2 using SHELXTL.2 Contributions to scattering due to disordered solvent molecules were removed using the SQUEEZE routine of PLATON. All hydrogen atoms were theoretical hydrogenation, riding on the concerned atoms and refined with fixed thermal factors. Non-hydrogen atoms were refined anisotropically.

Solvothermal synthesis of AlOC-137. Al(OiPr)3 (0.251 g, 1.23 mmol), 1-NA (0.432 g, 2.5 mmol) were mixed and dissolved in acetonitrile (10 mL) at room temperature. The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, colorless block crystals of AlOC-137 were obtained (maximum yield: ~20% for AlOC-137 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-138. Al(OiPr)3 (0.245 g, 1.20 mmol), 1-NA (0.518 g, 3.0 mmol), AgI (0.202 g, 0.86 mmol) were mixed and dissolved in acetonitrile (10 mL), then three drops 1,3-propylenediamine were added. The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, faint yellow block crystals of AlOC-138 were obtained (maximum yield: ~40% for AlOC-138 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-139. Al(OiPr)3 (0.199 g, 0.97 mmol), 1-NA (1.013 g, 5.89 mmol), AgBC (0.235 g, 1.03 mmol) were mixed and dissolved in acetonitrile (10 mL). The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, colorless square crystals of AlOC-139 were obtained (maximum yield: ~60% for AlOC-139 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-140. Al(OiPr)3 (0.256 g, 1.25 mmol), 1-NA (0.625 g, 3.63 mmol), TBACl (0.277 g, 1.00 mmol), AgBC (0.224 g, 0.98 mmol) were mixed and dissolved in acetonitrile (10 mL). The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, faint yellow square crystals of AlOC-140 were obtained (maximum yield: ~55% for AlOC-140 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-141. Al(OiPr)3 (0.257 g, 1.26 mmol), 1-NA (0.371 g, 2.16 mmol), 4,4’-bpy (0.158 g, 1.01 mmol), CuSCN (0.123 g, 1.02 mmol) were mixed and dissolved in acetonitrile (10 mL), then one drop Ti(OiPr)4 were added. The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, yellow octahedral crystals of AlOC-141 were obtained (maximum yield: ~16% for AlOC-141 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-142. Al(OiPr)3 (0.260 g, 1.27 mmol), 1-NA (0.395 g, 2.30 mmol), AgNO3 (0.152 g, 0.90 mmol), 4,4’-bpy (0.152 g, 0.97 mmol) were mixed and dissolved in acetonitrile (10 mL), then one drop Ti(OiPr)4 were added. The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, yellow block crystals of AlOC-142 were obtained (maximum yield: ~20% for AlOC-142 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-143. Al(OiPr)3 (0.245 g, 1.20 mmol), 1-NA (1.002 g, 5.83 mmol), silver acetate (0.162 g, 0.97 mmol) were mixed and dissolved in acetonitrile (10 mL). The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, colorless square crystals of AlOC-143 were obtained (maximum yield: ~80% for AlOC-143 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-144. Al(OiPr)3 (0.251 g, 1.23 mmol), 1-NA (0.623 g, 3.62 mmol), AgBC (0.222 g, 0.97 mmol) were mixed and dissolved in acetonitrile (10 mL). The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, colorless square crystals of AlOC-144 were obtained (maximum yield: ~80% for AlOC-144 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-145. Al(OiPr)3 (0.257 g, 1.26 mmol), 1-NA (0.395 g, 2.30 mmol), AgNO3 (0.186 g, 1.10 mmol), 4,4’-bpy (0.173 g, 1.11 mmol), NaAQS (0.02 g, 0.065 mmol) were mixed and dissolved in acetonitrile (10 mL), then one drop Ti(OiPr)4 was added. The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, colorless parallelogram crystals of AlOC-145 were obtained (maximum yield: ˂1% for AlOC-145 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-146. Al(OiPr)3 (0.263 g, 1.29 mmol), 1-NA (0.362 g, 2.10 mmol), AgNO3 (0.183 g, 1.08 mmol) and 4,4-bpy (0.160 g, 1.03 mmol) were mixed and dissolved in acetonitrile (10 mL), then 20 μL ethyl amine alcohol solution was added. The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, colorless block crystals of AlOC-146 were obtained (maximum yield: ~20% for AlOC-146 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-147. Al(OiPr)3 (0.258 g, 1.26 mmol), 1-NA (0.406 g, 2.36 mmol), AgNO3 (0.160 g, 0.94 mmol), 4,4’-bpy (0.170 g, 1.09 mmol) were mixed and dissolved in acetonitrile (10 mL). The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, colorless square crystals of AlOC-147 were obtained (maximum yield: ~65% for AlOC-147 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-148. Al(OiPr)3 (0.257 g, 1.26 mmol), 1-NA (0.372 g, 2.16 mmol), AgNO3 (0.418 g, 2.47 mmol), 4,4’-bpy (0.184 g, 1.18 mmol) were mixed and dissolved in acetonitrile (10 mL), then one drop Ti(OiPr)4 were added. The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, yellow strip crystals of AlOC-148 were obtained (maximum yield: ~10% for AlOC-148 based on Al(OiPr)3).

Solvothermal synthesis of AlOC-149. Al(OiPr)3 (0.248 g, 1.22 mmol), 1-NA (0.367 g, 2.13 mmol), CuBr (0.163 g, 1.14 mmol), 4,4’-bpy (0.152 g, 0.97 mmol), TBAB (0.252 g, 0.78 mmol) were mixed and dissolved in acetonitrile (10 mL), then one drop Ti(OiPr)4 were added. The resultant solution was heated at 80 oC for seven days. After cooling to room temperature, green parallelogram crystals of AlOC-149 were obtained (maximum yield: ~15% for AlOC-149 based on Al(OiPr)3).

Interaction energy decomposition analysis (EDA). The interaction energy between Ag(bpy)2+ thread and Al8 macrocycle was calculated on Xiamen Atomistic Computing Suite (XACS).3, 4

- A summary of reported macrocycles used for constructing rotaxanes

Table S1. A summary of reported macrocycles used for constructing rotaxanes.

| Macrocycle types | Early representative structure | Early Reporting year | Reported group | Reference |
| --- | --- | --- | --- | --- |
| alkyl macrocycle |  | 1967 | Zollenkopf | 5 |
| poly(ethylene glycol) /crown ether macrocycle |  | 1976 | Zilkha | 6 |
| cyclodextrin |  | 1981 | Ogino | 7 |
| cyclobis(paraquat-p-phenylene) |  | 1991 | Stoddart | 8 |
| metal-binding macrocycle |  | 1991 | Gibson | 9 |
| amide based macrocycle |  | 1995 | Lindoy | 10 |
| cucurbituril |  | 1996 | Kim | 11 |
| calixarene |  | 2000 | Pochini | 12 |
| coordination bonds constructed macrocycles |  | 2001 | Jeong | 13 |
| heterometallic Cr7MF8 macrocycle |  | 2003 | Winpenny | 14 |
| porphyrin-macrocycle |  | 2003 | Nolte | 15 |
| 1,4,8,11-tetraazacyclotetradecane |  | 2004 | Suh | 16 |
| azacalix[8]pyridine |  | 2011 | Wang | 17 |
| cyanostar |  | 2013 | Flood | 18 |
| Inorganic Ti8 macrocycle |  | 2021 | Wang | 19 |

- Crystallographic data and structure refinement parameters

Table S2. Crystallographic data and structure refinement parameters for AlOC-137 to AlOC-140.

|  | AlOC-137 | AlOC-138 | AlOC-139 | AlOC-140 |
| --- | --- | --- | --- | --- |
| Empirical formula | C182H129Al8N3O40 | C195H140Al8N4O42 | C202H142Al8N2O44 | C190H132Al8O44 |
| Formula weight | 3213.71 | 3426.94 | 3517.01 | 3334.79 |
| Temperature / K | 100.0(4) K | 144.97(12) K | 99.97(17) K | 99.98(14) K |
| Crystal system | monoclinic | orthorhombic | monoclinic | monoclinic |
| Space group | P2/c | Pccn | P2/c | P2/n |
| a [Å] | 31.0683(4) | 17.5033(4) | 17.6007(2) | 19.7430(12) |
| b [Å] | 18.4306(2) | 32.2577(9) | 16.1038(2) | 17.0738(7) |
| c [Å] | 29.0563(4) | 32.0754(7) | 71.1974(7) | 28.1234(15) |
| α [o] | 90 | 90 | 90 | 90 |
| β [o] | 109.842(2) | 90 | 95.1650(10) | 97.872(5) |
| γ [o] | 90 | 90 | 90 | 90 |
| V [Å3] | 15650.1(6) | 18110.3(8) | 20098.1(4) | 9390.7(9) |
| Z | 4 | 4 | 4 | 2 |
| ρcalcd [g cm-3] | 1.364 | 1.257 | 1.162 | 1.179 |
| μ [mm–1] | 0.769 | 0.692 | 0.635 | 0.66 |
| F (000) | 6664.0 | 7112 | 7296.0 | 3456 |
| Index ranges | ‒36 ≤ h ≤ 36 ‒21 ≤ k ≤ 14 ‒33 ≤ l ≤ 34 | ‒18 ≤ h ≤ 20 ‒36 ≤ k ≤ 37 ‒36 ≤ l ≤ 23 | ‒17 ≤ h ≤ 18 ‒17 ≤ k ≤ 17 ‒76 ≤ l ≤ 74 | ‒22 ≤ h ≤ 23 ‒20 ≤ k ≤ 19 ‒33 ≤ l ≤ 31 |
| Reflns collected | 71815 | 41721 | 94601 | 55202 |
| unique reflns [Rint] | 23220[0.0473] | 12882 [0.0585] | 26036 [0.0299] | 16204 [0.0317] |
| data/restraints/parameters | 23220/618/2269 | 12882/165/1112 | 26036/128/2278 | 16204/3094/888 |
| GOF on F2 | 1.793 | 1.288 | 1.019 | 1.360 |
| R1, wR2 [I > 2σ(I)] | 0.1315, 0.3821 | 0.1265, 0.3235 | 0.1012, 0.2780 | 0.1600, 0.3892 |
| R1, wR2 [all data] | 0.1522, 0.4113 | 0.1864, 0.3725 | 0.1120, 0.2881 | 0.2161, 0.4380 |
| Δρmin/Δρmax(e∙Å-3) | 1.29/‒0.67 | 0.73/-0.40 | 1.69/‒1.56 | 0.93/‒0.41 |
| CCDC number | 2322760 | 2322761 | 2322762 | 2322763 |

Table S3. Crystallographic data and structure refinement parameters for AlOC-141 to AlOC-144.

|  | AlOC-141 | AlOC-142 | AlOC-143 | AlOC-144 |
| --- | --- | --- | --- | --- |
| Empirical formula | C196H136Al8N4O40 | C196H136AgAl8N5O43 | C202H140Ag2Al8N2O44 | C190H131AgAl8O44 |
| Formula weight | 3402.92 | 3572.80 | 3730.73 | 3441.65 |
| Temperature / K | 149.99(10) K | 293(2) K | 293(2) K | 293(2) K |
| Crystal system | monoclinic | monoclinic | tetragonal | monoclinic |
| Space group | P2/n | C2/c | I-42d | I2/a |
| a [Å] | 17.3233(3) | 17.0671(3) | 24.65680(10) | 33.7018(13) |
| b [Å] | 18.6619(4) | 43.9438(7) | 24.65680(10) | 17.0426(3) |
| c [Å] | 24.7441(3) | 23.5220(4) | 57.5237(4) | 33.1000(9) |
| α [o] | 90 | 90 | 90 | 90 |
| Β [o] | 94.4820(10) | 105.350(2) | 90 | 116.568(4) |
| γ [o] | 90 | 90 | 90 | 90 |
| V [Å3] | 7975.0(2) | 17012.0(5) | 34972.0(4) | 17004.0(10) |
| Z | 2 | 4 | 8 | 4 |
| ρcalcd [g cm-3] | 1.417 | 1.395 | 1.417 | 1.344 |
| μ [mm–1] | 0.777 | 1.346 | 1.923 | 1.330 |
| F (000) | 3528.0 | 7368.0 | 15328.0 | 7096.0 |
| Index ranges | ‒17 ≤ h ≤ 17 ‒19 ≤ k ≤ 16 ‒25 ≤ l ≤ 25 | ‒18 ≤ h ≤ 18 ‒47 ≤ k ≤ 46 ‒25 ≤ l ≤ 25 | ‒19 ≤ h ≤ 30 ‒29 ≤ k ≤ 30 ‒67 ≤ l ≤ 71 | ‒38 ≤ h ≤ 39 ‒19 ≤ k ≤ 10 ‒38 ≤ l ≤ 38 |
| Reflections collected | 31454 | 53194 | 57197 | 51406 |
| Independent reflections [Rint] | 8867 [0.0225] | 10126 [0.0343] | 17416 [0.0206] | 13605 [0.0341] |
| data/restraints/parameters | 8867/414/1252 | 10126/87/1126 | 17416/126/1145 | 13605/424/1079 |
| GOF on F2 | 1.835 | 1.189 | 1.025 | 1.404 |
| R1, wR2 [I > 2σ(I)] | 0.1397, 0.3996 | 0.0898, 0.2524 | 0.0686, 0.2000 | 0.1065, 0.3223 |
| R1, wR2 [all data] | 0.1621, 0.4209 | 0.1006, 0.2675 | 0.0722, 0.2059 | 0.1230, 0.3434 |
| Δρmin/Δρmax (e∙Å-3) | 1.84/‒0.63 | 0.86/‒1.46 | 0.59/‒1.51 | 0.90/‒0.61 |
| CCDC number | 2322764 | 2322765 | 2322766 | 2322767 |

Table S4. Crystallographic data and structure refinement parameters for AlOC-145 to AlOC-147.

|  | AlOC-145 | AlOC-146 | AlOC-147 |
| --- | --- | --- | --- |
| Empirical formula | C211H141AgAl8N2NaO50S2 | C190H134AgAl8N5O43 | C197H135AgAl8N2O42 |
| Formula weight | 3915.07 | 3498.72 | 3525.77 |
| Temperature / K | 293(2) K | 293(2) | 293(2) K |
| Crystal system | triclinic | triclinic | monoclinic |
| Space group | P-1 | P-1 | Cc |
| a [Å] | 19.3196(8) | 20.20900(10) | 33.4626(18) |
| b [Å] | 19.7123(8) | 21.16690(10) | 26.0205(15) |
| c [Å] | 27.1042(5) | 22.5720(2) | 22.4279(8) |
| α [o] | 85.287(2) | 90.8290(10) | 90 |
| Β [o] | 87.002(2) | 115.3670(10) | 101.795(5) |
| γ [o] | 64.714(4) | 96.9510(10) | 90 |
| V [Å3] | 9299.9(6) | 8636.65(12) | 19115.9(17) |
| Z | 2 | 2 | 4 |
| ρcalcd [g cm-3] | 1.398 | 1.345 | 1.225 |
| μ [mm–1] | 2.186 | 1.318 | 1.202 |
| F (000) | 4030.0 | 3608.0 | 7272.0 |
| Index ranges | ‒22 ≤ h ≤ 16 ‒21 ≤ k ≤ 23 ‒33 ≤ l ≤ 33 | ‒23 ≤ h ≤ 23 ‒24 ≤ k ≤ 21 ‒26 ≤ l ≤ 26 | ‒36 ≤ h ≤ 40 ‒28 ≤ k ≤ 30 ‒26 ≤ l ≤ 24 |
| Reflections collected | 52510 | 100811 | 24054 |
| Independent reflections [Rint] | 24882 [0.0641] | 28417 [0.0222] | 13599 [0.2452] |
| data/restraints/parameters | 24882/275/2660 | 28417/0/2225 | 13599/1973/1830 |
| GOF on F2 | 1.441 | 1.058 | 1.665 |
| R1, wR2 [I > 2σ(I)] | 0.1036, 0.3208 | 0.0460, 0.1411 | 0.1739, 0.3878 |
| R1, wR2 [all data] | 0.1157, 0.3482 | 0.0543, 0.1480 | 0.3389, 0.4852 |
| Δρmin/Δρmax (e∙Å-3) | 0.82/‒1.61 | 1.59/-1.07 | 1.67/‒1.89 |
| CCDC number | 2322768 | 2322769 | 2322770 |

Table S5. Crystallographic data and structure refinement parameters for AlOC-148 and AlOC-149.

|  | AlOC-148 | AlOC-149 | AlOC-142-H |
| --- | --- | --- | --- |
| Empirical formula | C196H136Ag2Al8N6O46 | C244H170Al8BrCu3N6O48 | C196H136AgAl8N5O43 |
| Formula weight | 3742.68 | 4440.22 | 3572.80 |
| Temperature / K | 293(2) | 293(2) | 293(2) |
| Crystal system | tetragonal | monoclinic | monoclinic |
| Space group | P-4n2 | C2/c | C2/c |
| a [Å] | 31.4705(4) | 22.7481(9) | 16.9017(3) |
| b [Å] | 31.4705(4) | 20.8568(6) | 43.9044(5) |
| c [Å] | 17.6581(6) | 46.1178(12) | 23.5810(4) |
| α [o] | 90 | 90 | 90 |
| Β [o] | 90 | 102.434(3) | 104.847(2) |
| γ [o] | 90 | 90 | 90 |
| V [Å3] | 17488.5(7) | 21367.5(12) | 16914.3(5) |
| Z | 4 | 4 | 4 |
| ρcalcd [g cm-3] | 1.421 | 1.380 | 1.403 |
| μ [mm–1] | 2.902 | 2.388 | 2.072 |
| F (000) | 7680.0 | 9144 | 7368.0 |
| Index ranges | ‒33 ≤ h ≤ 25 ‒32 ≤ k ≤ 33 ‒18 ≤ l ≤ 18 | ‒23 ≤ h ≤ 23 ‒19 ≤ k ≤ 21 ‒46 ≤ l ≤ 48 | ‒20 ≤ h ≤ 20 ‒52 ≤ k ≤ 52 ‒23 ≤ l ≤ 28 |
| Reflections collected | 43486 | 37772 | 46664 |
| Independent reflections [Rint] | 10440 [0.0358] | 12656 [0.0489] | 13945 [0.0614] |
| data/restraints/parameters | 10440/1187/1051 | 12656/81/1374 | 13945/27/1105 |
| GOF on F2 | 1.548 | 1.065 | 1.646 |
| R1, wR2 [I > 2σ(I)] | 0.1394, 0.3514 | 0.0654, 0.1847 | 0.1262, 0.3691 |
| R1, wR2 [all data] | 0.1627, 0.3767 | 0.0862, 0.1972 | 0.1397, 0.3900 |
| Δρmin/Δρmax (e∙Å-3) | 1.26/-0.56 | 0.72/‒0.52 | 1.34/-1.12 |
| CCDC number | 2322771 | 2322772 | 2326287 |

- Structure description for Al8 macrocycle

Figure S1. The side and top view of Al8 macrocycle. Color code: Al, green; O, red; C, grey; H, white.

Figure S2. The distribution of –OH groups on Al8 macrocycle. Color code: Al, green; O, red; H, white.

Figure S3. The distribution of two kinds of NA ligands. (a) Sixteen of them are located on the equator of Al8 macrocycle. Color code: Al, green; O, red; C, grey; H, white; (b) Eight of them are almost perpendicular to Al8 macrocycle. Color code: Al, green; O, red; C, turquoise; H, white.

Figure S4. The tubular cavity in Al8 macrocycle. Color code: Al, green; O, red; C, turquoise; H, white.

- BVS analysis for AlOC-137 to AlOC-149

Table S6. BVS analysis for AlOC-137.

| Al1 3.247 Al1―O1 1.853(3) Al1―O3 1.847(3) Al1―O4 1.894(3) Al1―O5 1.900(4) Al1―O7 1.877(3) Al1―O8 1.900(4) | Al2 3.218 Al2―O2 1.897(4) Al2―O6 1.854(3) Al2―O9 1.892(4) Al2―O11 1.852(4) Al2―O13 1.907(4) Al2―O25 1.888(4) | Al3 3.220 Al3―O3 1.867(4) Al3―O6 1.838(4) Al3―O12 1.908(4) Al3―O16 1.892(4) Al3―O18 1.902(4) Al3―O24 1.883(4) | Al4 3.227 Al4―O1 1.853(4) Al4―O19 1.848(4) Al4―O20 1.892(4) Al4―O23 1.890(4) Al4―O26 1.886(4) Al4―O33 1.916(5) |
| --- | --- | --- | --- |
| Al5 3.196 Al5―O14 1.853(4) Al5―O15 1.899(4) Al5―O17 1.851(5) Al5―O29 1.894(6) Al5―O34 1.891(5) Al5―O36 1.918(5) | Al6 3.239 Al6―O10 1.832(5) Al6―O17 1.844(5) Al6―O21 1.902(4) Al6―O31 1.897(7) Al6―O35 1.918(5) Al6―O37 1.866(7) | Al7 3.283 Al7―O10 1.832(5) Al7―O11 1.844(5) Al7―O27 1.902(4) Al7―O28 1.897(7) Al7―O30 1.918(5) Al7―O32 1.886(7) | Al8 3.159 Al8―O14 1.851(4) Al8―O19 1.847(4) Al8―O22 1.897(6) Al8―O38 1.921(6) Al8―O39 1.907(5) Al8―O40 1.911(7) |
| O1 1.157 Al1―O1 1.853(3) Al4―O1 1.853(4) | O3 1.145 Al1―O3 1.847(3) Al3―O3 1.867(4) | O6 1.180 Al2―O6 1.854(3) Al3―O6 1.838(4) | O10 1.180 Al6―O10 1.832(5) Al7―O10 1.832(5) |
| O11 1.180 Al2―O11 1.852(4) Al7―O11 1.844(5) | O14 1.160 Al5―O14 1.853(4) Al8―O14 1.851(4) | O17 1.174 Al5―O17 1.851(5) Al6―O17 1.844(5) | O19 1.175 Al4―O19 1.848(4) Al8―O19 1.847(4) |

Table S7. BVS analysis for AlOC-138.

| Al1 3.210 Al1―O1 1.831(4) Al1―O3 1.851(5) Al1―O5 1.880(5) Al1―O6 1.894(5) Al1―O9 1.925(5) Al1―O12 1.920(5) | Al2 3.157 Al2―O1 1.844(5) Al2―O2 1.843(5) Al2―O13 1.919(5) Al2―O14 1.913(5) Al2―O15 1.910(6) Al2―O16 1.908(5) | Al3 3.157 Al3―O3 1.834(5) Al3―O4 1.922(5) Al3―O7 1.826(4) Al3―O8 1.910(5) Al3―O10 1.926(5) Al3―O11 1.926(5) | Al4 3.213 Al4―O2 1.839(5) Al4―O7 1.833(4) Al4―O17 1.891(6) Al4―O18 1.904(6) Al4―O19 1.898(5) Al4―O20 1.935(6) |
| --- | --- | --- | --- |
| O1 1.207 Al1―O1 1.945(4) Al2―O1 1.844(5) | O2 1.195 Al2―O2 1.843(5) Al4―O2 1.839(5) | O3 1.191 Al1―O3 1.851(5) Al3―O3 1.834(5) | O7 1.233 Al3―O7 1.826(4) Al4―O7 1.833(4) |

Table S8. BVS analysis for AlOC-139.

| Al1 3.180 Al1―O1 1.842(3) Al1―O6 1.893(4) Al1―O11 1.839(3) Al1―O13 1.917(4) Al1―O15 1.905(4) Al1―O19 1.927(4) | Al2 3.183 Al2―O4 1.915(4) Al2―O7 1.832(4) Al2―O9 1.844(4) Al2―O17 1.907(4) Al2―O24 1.903(4) Al2―O25 1.920(4) | Al3 3.213 Al3―O5 1.835(3) Al3―O8 1.907(4) Al3―O12 1.846(3) Al3―O36 1.911(4) Al3―O41 1.901(4) Al3―O42 1.898(4) | Al4 3.202 Al4―O5 1.836(3) Al4―O11 1.853(3) Al4―O20 1.895(4) Al4―O27 1.896(4) Al4―O31 1.918(4) Al4―O38 1.907(4) |
| --- | --- | --- | --- |
| Al5 3.244 Al5―O2 1.836(4) Al5―O9 1.820(4) Al5―O29 1.917(4) Al5―O30 1.914(4) Al5―O33 1.906(4) Al5―O37 1.888(4) | Al6 3.152 Al6―O2 1.847(4) Al6―O14 1.910(4) Al6―O22 1.826(4) Al6―O23 1.919(4) Al6―O32 1.913(4) Al6―O35 1.931(4) | Al7 3.183 Al7―O1 1.852(3) Al7―O3 1.896(4) Al7―O7 1.834(3) Al7―O10 1.907(4) Al7―O18 1.911(4) Al7―O34 1.920(4) | Al8 3.140 Al8―O12 1.832(4) Al8―O16 1.914(4) Al8―O21 1.930(4) Al8―O22 1.849(4) Al8―O26 1.923(4) Al8―O39 1.905(4) |
| O1 1.177 Al1―O1 1.842(3) Al7―O1 1.852(3) | O2 1.194 Al5―O2 1.836(4) Al6―O2 1.847(4) | O5 1.214 Al2―O5 1.832(4) Al3―O5 1.835(3) | O7 1.222 Al2―O7 1.832(4) Al7―O7 1.834(3) |
| O9 1.226 Al2―O9 1.844(4) Al5―O9 1.820(4) | O11 1.180 Al1―O11 1.839(3) Al4―O11 1.853(3) | O12 1.202 Al3―O12 1.846(3) Al8―O12 1.832(4) | O22 1.207 Al6―O22 1.826(4) Al8―O22 1.849(4) |

Table S9. BVS analysis for AlOC-140.

| Al1 3.262 Al1―O1 1.827(4) Al1―O1 1.827(4) Al1―O4 1.920(5) Al1―O4 1.920(5) Al1―O7 1.887(5) Al1―O7 1.887(5) | Al2 3.191 Al2―O2 1.822(4) Al2―O3 1.834(4) Al2―O6 1.920(5) Al2―O8 1.886(4) Al2―O13 1.920(5) Al2―O16 1.939(6) | Al3 3.188 Al3―O1 1.834(4) Al3―O2 1.844(4) Al3―O5 1.925(5) Al3―O9 1.910(6) Al3―O12 1.906(4) Al3―O14 1.898(5) | Al4 3.277 Al4―O3 1.841(4) Al4―O10 1.832(5) Al4―O11 1.890(4) Al4―O15 1.867(5) Al4―O18 1.915(6) Al4―O19 1.909(6) | Al5 3.327 Al5―O10 1.839(4) Al5―O10 1.839(4) Al5―O17 1.876(8) Al5―O17 1.876(8) Al5―O20 1.893(5) Al5―O20 1.893(5) |
| --- | --- | --- | --- | --- |
| O1 1.230 Al1―O1 1.827(4) Al3―O1 1.834(4) | O2 1.222 Al2―O2 1.822(4) Al3―O2 1.844(4) | O3 1.207 Al2―O3 1.834(4) Al4―O3 1.841(4) | O10 1.213 Al4―O10 1.832(5) Al5―O10 1.839(4) |  |

Table S10. BVS analysis for AlOC-141.

| Al1 3.092 Al1―O1 1.819(5) Al1―O2 1.835(6) Al1―O8 1.926(8) Al1―O9 1.939(6) Al1―O10 1.940(7) Al1―O12 1.937(6) | Al2 3.097 Al2―O2 1.828(5) Al2―O5 1.958(8) Al2―O6 1.843(7) Al2―O7 1.913(6) Al2―O11 1.928(6) Al2―O14 1.918(7) | Al3 2.993 Al3―O6 1.806(6) Al3―O13 2.083(1) Al3―O15 1.817(8) Al3―O16 1.918(8) Al3―O17 1.961(7) Al3―O19 1.929(1) | Al4 2.877 Al4―O15 1.808(8) Al4―O15 1.808(8) Al4―O18 1.961(9) Al4―O18 1.961(9) Al4―O20 2.035(14) Al4―O20 2.035(14) | Al5 3.058 Al5―O1 1.843(5) Al5―O1 1.843(5) Al5―O3 1.922(5) Al5―O3 1.922(5) Al5―O4 1.942(6) Al5―O4 1.942(6) |
| --- | --- | --- | --- | --- |
| O1 1.229 Al1―O1 1.819(5) Al5―O1 1.843(5) | O2 1.226 Al1―O2 1.835(6) Al2―O2 1.828(5) | O6 1.251 Al2―O6 1.843(7) Al3―O6 1.806(6) | O15 1.290 Al3―O15 1.817(8) Al4―O15 1.808(8) |  |

Table S11. BVS analysis for AlOC-142.

| Al1 2.931 Al1―O2 1.813(3) Al1―O4 1.798(3) Al1―O7 1.981(3) Al1―O11 1.988(3) Al1―O12 2.001(3) Al1―O13 1.976(4) | Al2 2.945 Al2―O3 1.805(3) Al2―O4 1.835(3) Al2―O5 1.960(3) Al2―O9 1.955(3) Al2―O10 1.974(3) Al2―O15 2.001(4) | Al3 2.894 Al3―O1 1.799(3) Al3―O2 1.834(3) Al3―O6 1.943(4) Al3―O16 2.016(3) Al3―O18 1.947(4) Al3―O20 2.050(4) | Al4 2.888 Al4―O1 1.825(3) Al4―O3 1.794(3) Al4―O8 1.977(4) Al4―O14 1.986(5) Al4―O17 2.023(4) Al4―O19 1.988(4) | Ag1 0.851 Ag1―N1 1.958(5) Ag1―N2 2.064(3) |
| --- | --- | --- | --- | --- |
| O1 1.294 Al3―O1 1.799(3) Al4―O1 1.825(3) | O2 1.254 Al1―O2 1.813(3) Al3―O2 1.834(3) | O3 1.338 Al2―O3 1.805(3) Al4―O3 1.794(3) | O4 1.279 Al1―O4 1.798(3) Al2―O4 1.835(3) |  |

Table S12. BVS analysis for AlOC-143.

| Al1 3.242 Al1―O2 1.818(4) Al1―O10 1.885(4) Al1―O16 1.864(3) Al1―O30 1.894(5) Al1―O36 1.900(4) Al1―O38 1.918(4) | Al2 3.145 Al2―O6 1.906(4) Al2―O14 1.854(3) Al2―O16 1.847(4) Al2―O24 1.916(4) Al2―O26 1.924(4) Al2―O28 1.898(4) | Al3 3.230 Al3―O4 1.920(4) Al3―O14 1.846(3) Al3―O18 1.899(4) Al3―O20 1.830(4) Al3―O22 1.895(4) Al3―O32 1.897(4) | Al4 3.185 Al4―O2 1.843(3) Al4―O2 1.843(3) Al4―O8 1.900(4) Al4―O8 1.900(4) Al4―O40 1.916(4) Al4―O40 1.916(4) | Al5 3.256 Al5―O12 1.878(4) Al5―O12 1.878(4) Al5―O20 1.837(3) Al5―O20 1.838(3) Al5―O34 1.920(4) Al5―O34 1.920(4) | Ag1 0.662 Ag1―N2 2.259(11) Ag1―N2 2.259(11) |
| --- | --- | --- | --- | --- | --- |
| Ag2 1.070 Ag2―O42 2.419(6) Ag2―O42 2.419(6) Ag2―O44 2.257(9) Ag2―O44 2.257(9) | O2 1.230 Al1―O2 1.818(4) Al4―O2 1.843(3) | O14 1.167 Al2―O14 1.854(3) Al3―O14 1.846(3) | O16 1.150 Al1―O16 1.864(3) Al2―O16 1.847(4) | O20 1.220 Al3―O20 1.830(4) Al5―O20 1.837(3) |  |

Table S13. BVS analysis for AlOC-144.

| Al1 3.232 Al1―O4 1.896(2) Al1―O4 1.896(2) Al1―O6 1.896(2) Al1―O6 1.886(3) Al1―O7 1.886(3) Al1―O7 1.886(3) | Al2 3.139 Al2―O1 1.896(2) Al2―O3 1.896(2) Al2―O8 1.896(2) Al2―O15 1.886(3) Al2―O16 1.886(3) Al2―O18 1.886(3) | Al3 3.181 Al3―O1 1.895(3) Al3―O2 1.895(3) Al3―O7 1.895(3) Al3―O10 1.892(3) Al3―O12 1.892(3) Al3―O14 1.892(3) | Al4 3.191 Al4―O3 1.896(2) Al4―O5 1.896(2) Al4―O9 1.896(2) Al4―O17 1.886(3) Al4―O19 1.886(3) Al4―O20 1.886(3) | Al5 3.201 Al5―O5 1.896(2) Al5―O5 1.896(2) Al5―O11 1.896(2) Al5―O11 1.886(3) Al5―O13 1.886(3) Al5―O13 1.886(3) |
| --- | --- | --- | --- | --- |
| Ag1 0.955 Ag1―O21 2.342(6) Ag1―O21 2.342(6) Ag1―O22 2.403(5) Ag1―O22 2.403(5) | O1 1.183 Al2―O1 1.896(2) Al3―O1 1.895(3) | O3 1.189 Al2―O3 1.896(2) Al4―O3 1.896(2) | O5 1.189 Al4―O5 1.896(2) Al5―O5 1.896(2) | O7 1.172 Al1―O7 1.886(3) Al3―O7 1.895(3) |

Table S14. BVS analysis for AlOC-145.

| Al1 3.150 Al1―O2 1.873(3) Al1―O4 1.888(4) Al1―O5 1.866(4) Al1―O10 1.909(4) Al1―O13 1.875(4) Al1―O20 1.927(5) | Al2 3.125 Al2―O3 1.898(4) Al2―O5 1.852(4) Al2―O6 1.848(3) Al2―O14 1.951(4) Al2―O24 1.925(4) Al2―O32 1.889(4) | Al3 3.145 Al3―O1 1.831(4) Al3―O7 1.837(3) Al3―O8 1.912(4) Al3―O21 1.915(5) Al3―O22 1.925(5) Al3―O27 1.932(3) | Al4 3.120 Al4―O1 1.832(4) Al4―O12 1.839(4) Al4―O19 1.898(4) Al4―O29 1.927(4) Al4―O34 1.952(4) Al4―O41 1.924(5) | Al5 3.169 Al5―O6 1.823(4) Al5―O9 1.828(3) Al5―O30 1.930(4) Al5―O33 1.916(5) Al5―O35 1.914(4) Al5―O37 1.927(4) |
| --- | --- | --- | --- | --- |
| Al6 3.120 Al6―O7 1.838(4) Al6―O9 1.838(3) Al6―O11 1.907(4) Al6―O15 1.924(4) Al6―O18 1.943(4) Al6―O23 1.920(4) | Al7 3.127 Al7―O12 1.835(4) Al7―O16 1.867(3) Al7―O25 1.888(4) Al7―O26 1.908(4) Al7―O39 1.935(5) Al7―O40 1.927(4) | Al8 3.155 Al8―O2 1.854(4) Al8―O16 1.871(3) Al8―O17 1.895(4) Al8―O28 1.908(4) Al8―O31 1.904(4) Al8―O36 1.902(4) | Ag1 0.962 Ag1―N1 2.176(9) Ag1―N2 2.072(1) | Na1 0.902 Na1―O42 2.419(6) Na1―O44 2.687(6) Na1―O45 2.358(7) Na1―O16 2.603 Na1―O2 2.375 Na1―O5 2.784 |
| O1 1.227 Al3―O1 1.831(4) Al4―O1 1.832(4) | O2 1.339 Al1―O2 1.873(3) Al8―O2 1.854(4) Na1―O2 2.375 | O5 1.209 Al1―O5 1.866(4) Al2―O5 1.852(4) Na1―O5 2.784 | O6 1.214 Al2―O6 1.848(3) Al5―O6 1.823(4) | O7 1.207 Al3―O7 1.837(3) Al6―O7 1.838(4) |
| O9 1.222 Al5―O9 1.828(3) Al6―O9 1.838(3) | O12 1.215 Al4―O12 1.839(4) Al7―O12 1.835(4) | O16 1.224 Al7―O16 1.867(3) Al8―O16 1.871(3) Na1―O16 2.603 |  |  |

Table S15. BVS analysis for AlOC-146.

| Al1 3.200 Al1―O3 1.8987(16) Al1―O4 1.9092(16) Al1―O8 1.9059(15) Al1―O10 1.8449(15) Al1―O13 1.8315(15) Al1―O17 1.9215(16) | Al2 3.135 Al2―O2 1.8489(16) Al2―O6 1.8447(15) Al2―O11 1.9230(16) Al2―O16 1.8956(16) Al2―O18 1.9200(15) Al2―O24 1.9242(15) | Al3 3.164 Al3―O6 1.8411(15) Al3―O12 1.9099(16) Al3―O13 1.8470(15) Al3―O14 1.9068(16) Al3―O21 1.9104(16) Al3―O38 1.9197(16) | Al4 3.184 Al4―O2 1.8483(15) Al4―O9 1.8429(16) Al4―O15 1.8948(16) Al4―O20 1.9243(17) Al4―O29 1.9053(17) Al4―O32 1.9045(16) | Al5 3.214 Al5―O1 1.8484(16) Al5―O10 1.8407(15) Al5―O22 1.9113(17) Al5―O23 1.8993(17) Al5―O28 1.9059(16) Al5―O35 1.8928(17) |
| --- | --- | --- | --- | --- |
| Al6 3.159 Al6―O5 1.8400(16) Al6―O9 1.8480(15) Al6―O27 1.9063(17) Al6―O30 1.9205(17) Al6―O34 1.9003(17) Al6―O40 1.9238(17) | Al7 3.143 Al7―O5 1.8439(16) Al7―O7 1.8605(16) Al7―O19 1.9123(17) Al7―O25 1.9096(16) Al7―O26 1.9131(17) Al7―O37 1.9084(17) | Al8 3.161 Al8―O1 1.8379(15) Al8―O7 1.8450(16) Al8―O31 1.9321(17) Al8―O33 1.9094(18) Al8―O36 1.8845(17) Al8―O39 1.9316(18) | Ag1 0.990 Ag1―N2 2.133(3) Ag1―N4 2.088(3) | O1 1.190 Al5―O1 1.8484(16) Al8―O1 1.8379(15) |
| O2 1.172 Al2―O2 1.8489(16) Al4―O2 1.8483(15) | O5 1.194 Al6―O5 1.8400(16) Al7―O5 1.8439(16) | O6 1.191 Al2―O6 1.8447(15) Al3―O6 1.8411(15) | O7 1.160 Al7―O7 1.8605(16) Al8―O7 1.8450(16) | O9 1.182 Al6―O9 1.8480(15) Al4―O9 1.8429(16) |
| O10 1.191 Al1―O10 1.8449(15) Al5―O10 1.8407(15) | O13 1.203 Al1―O13 1.8315(15) Al3―O13 1.8470(15) |  |  |  |

Table S16. BVS analysis for AlOC-147.

| Al1 2.646 Al1―O3 1.95(3) Al1―O10 2.00(3) Al1―O11 1.90(3) Al1―O17 1.99(4) Al1―O31 1.85(3) Al1―O36 2.05(4) | Al2 2.912 Al2―O7 1.80(3) Al2―O16 1.91(3) Al2―O20 1.87(2) Al2―O28 2.02(3) Al2―O32 1.95(2) Al2―O39 1.99(3) | Al3 3.215 Al3―O10 1.71(3) Al3―O12 1.92(3) Al3―O15 1.82(3) Al3―O27 2.00(3) Al3―O29 1.93(3) Al3―O33 1.98(2) | Al4 3.498 Al4―O6 1.822(19) Al4―O8 1.89(3) Al4―O14 1.77(3) Al4―O16 1.82(3) Al4―O18 1.89(3) Al4―O38 1.92(2) | Al5 3.107 Al5―O5 2.03(3) Al5―O7 1.86(3) Al5―O9 1.86(2) Al5―O13 1.964(19) Al5―O21 1.78(3) Al5―O37 1.91(3) |
| --- | --- | --- | --- | --- |
| Al6 3.535 Al6―O4 1.68(3) Al6―O19 1.92(2) Al6―O23 1.89(2) Al6―O26 1.90(4) Al6―O31 1.86(3) Al6―O34 1.87(4) | Al7 3.493 Al7―O2 1.79(3) Al7―O4 1.97(3) Al7―O18 1.79(3) Al7―O22 1.84(2) Al7―O30 1.84(4) Al7―O35 1.89(2) | Al8 3.218 Al8―O1 1.92(4) Al8―O15 1.76(3) Al8―O21 1.99(3) Al8―O24 1.94(2) Al8―O25 1.93(2) Al8―O42 1.79(3) | Ag1 0.814 Ag1―N1 2.14(9) Ag1―N2 2.219(17) | O4 1.336 Al6―O4 1.68(3) Al7―O4 1.97(3) |
| O7 1.227 Al2―O7 1.80(3) Al5―O7 1.86(3) | O10 1.232 Al1―O10 2.00(3) Al3―O10 1.71(3) | O15 1.367 Al3―O15 1.82(3) Al8―O15 1.76(3) | O16 1.121 Al2―O16 1.91(3) Al4―O16 1.82(3) | O18 1.201 Al4―O18 1.89(3) Al7―O18 1.79(3) |
| O21 1.097 Al5―O21 1.78(3) Al8―O21 1.99(3) | O31 1.143 Al1―O31 1.85(3) Al6―O31 1.86(3) |  |  |  |

Table S17. BVS analysis for AlOC-148.

| Al1 2.895 Al1―O2 1.786(13) Al1―O3 1.958(14) Al1―O7 2.026(13) Al1―O9 2.008(14) Al1―O11 1.833(10) Al1―O17 1.981(15) | Al2 3.020 Al2―O1 1.937(13) Al2―O2 1.825(11) Al2―O4 1.822(13) Al2―O16 1.899(17) Al2―O18 2.012(16) Al2―O19 1.975(12) | Al3 2.824 Al3―O5 2.051(14) Al3―O6 1.990(12) Al3―O10 1.808(12) Al3―O11 1.782(11) Al3―O12 1.999(11) Al3―O14 2.051(14) | Al4 3.008 Al4―O4 1.793(15) Al4―O8 1.993(14) Al4―O10 1.756(11) Al4―O13 1.984(15) Al4―O15 2.028(19) Al4―O20 1.980(13) | Ag1 0.920 Ag1―N1 2.093 Ag1―N2 2.187 | Ag2 0.918 Ag1―N4 2.138 Ag1―N4 2.138 |
| --- | --- | --- | --- | --- | --- |
| Ag3 0.783 Ag1―N3 2.197 Ag1―N3 2.197 | O2 1.319 Al1―O2 1.786(13) Al2―O2 1.825(11) | O4 1.311 Al2―O4 1.822(13) Al4―O4 1.793(15) | O10 1.407 Al3―O10 1.808(12) Al4―O10 1.756(11) | O11 1.313 Al1―O11 1.833(10) Al3―O11 1.782(11) |  |

Table S18. BVS analysis for AlOC-149.

| Al1 3.220 Al1―O1 1.846(4) Al1―O5 1.890(4) Al1―O6 1.838(3) Al1―O7 1.906(4) Al1―O11 1.906(4) Al1―O14 1.906(4) | Al2 3.139 Al2―O4 1.857(4) Al2―O6 1.838(3) Al2―O9 1.918(4) Al2―O10 1.908(4) Al2―O12 1.926(4) Al2―O17 1.904(4) | Al3 3.201 Al3―O2 1.846(4) Al3―O3 1.903(4) Al3―O4 1.830(3) Al3―O16 1.912(4) Al3―O18 1.922(4) Al3―O19 1.895(4) | Al4 3.149 Al4―O1 1.834(3) Al4―O2 1.852(4) Al4―O8 1.910(4) Al4―O13 1.920(5) Al4―O15 1.924(4) Al4―O21 1.905(4) | Cu1 1.866 Cu1―O20 1.974(4) Cu1―O22 1.969(4) Cu1―O23 1.964(4) Cu1―O24 1.964(5) Cu1―N1 2.159(4) |
| --- | --- | --- | --- | --- |
| Cu2 0.918 Cu2―Br1 2.4903(15) Cu2―N2 1.947(4) Cu2―N2 1.947(4) | O1 1.199 Al1―O1 1.846(4) Al4―O1 1.834(3) | O2 1.170 Al3―O2 1.846(4) Al4―O2 1.852(4) | O4 1.188 Al2―O4 1.857(4) Al3―O4 1.830(3) | O6 1.206 Al1―O6 1.838(3) Al2―O6 1.838(3) |

- PXRD analyses

Figure S5. The PXRD patterns of AlOC-137 (simulated, black; experimental, red).

Figure S6. The PXRD patterns of AlOC-138 (simulated, black; experimental, red).

Figure S7. The PXRD patterns of AlOC-139 (simulated, black; experimental, red).

Figure S8. The PXRD patterns of AlOC-140 (simulated, black; experimental, red).

Figure S9. The PXRD patterns of AlOC-141 (simulated, black; experimental, red).

Figure S10. The PXRD patterns of AlOC-142 (simulated, black; experimental, red).

Figure S11. The PXRD patterns of AlOC-143 (simulated, black; experimental, red).

Figure S12. The PXRD patterns of AlOC-144 (simulated, black; experimental, red).

Figure S13. The PXRD patterns of AlOC-146 (simulated, black; experimental, red).

Figure S14. The PXRD patterns of AlOC-147 (simulated, black; experimental, red).

Figure S15. The PXRD patterns of AlOC-148 (simulated, black; experimental, red).

Figure S16. The PXRD patterns of AlOC-149 (simulated, black; experimental, red).

Discussion for PXRD patterns:

The experimental PXRD patterns for above compounds are consistent well with the simulated ones from single-crytsal X-ray diffraction, which indicates that the samples are pure (Figure S5–S16). The differences in indendity between the experimental and simulated patterns might be due to the variation in crystal orientation for power samples.

- FT-IR analyses

Figure S17. The IR spectrum of AlOC-137.

Figure S18. The IR spectrum of AlOC-138.

Figure S19. The IR spectrum of AlOC-139.

Figure S20. The IR spectrum of AlOC-140.

Figure S21. The IR spectrum of AlOC-141.

Figure S22. The IR spectrum of AlOC-142.

Figure S23. The IR spectrum of AlOC-143.

Figure S24. The IR spectrum of AlOC-144.

Figure S25. The IR spectrum of AlOC-146.

Figure S26. The IR spectrum of AlOC-147.

Figure S27. The IR spectrum of AlOC-148.

Figure S28. The IR spectrum of AlOC-149.

- EDS analyses

Figure S29. The EDS analysis profile of AlOC-137.

Figure S30. The EDS analysis profile of AlOC-138.

Figure S31. The EDS analysis profile of AlOC-139.

Figure S32. The EDS analysis profile of AlOC-140.

Figure S33. The EDS analysis profile of AlOC-141.

Figure S34. The EDS analysis profile of AlOC-142.

Figure S35. The EDS analysis profile of AlOC-143.

Figure S36. The EDS analysis profile of AlOC-144.

Figure S37. The EDS analysis profile of AlOC-146.

Figure S38. The EDS analysis profile of AlOC-147.

Figure S39. The EDS analysis profile of AlOC-148.

Figure S40. The EDS analysis profile of AlOC-149.

- Reaction equations

Table S19. Reaction equation for AlOC-137–AlOC-148.

| Complex | Formula | Equation |
| --- | --- | --- |
| 8Al(OiPr)3 + 16HNA + 8H2O + molecules → Al8(OH)8(NA)16molecules + 24HOiPr |  |  |
| AlOC-137 | Al8(OH)8(NA)163MeCN | 8Al(OiPr)3 + 16HNA + 8H2O + 3MeCN → Al8(OH)8(NA)163MeCN + 24HOiPr |
| AlOC-138 | Al8(OH)8(NA)16HNA4MeCN | 8Al(OiPr)3 + 17HNA + 8H2O + 4MeCN → Al8(OH)8(NA)16HNA4MeCN + 24HOiPr |
| AlOC-139 | Al8(OH)8(NA)162HNA2MeCN | 8Al(OiPr)3 + 18HNA + 8H2O + 2MeCN → Al8(OH)8(NA)162HNA2MeCN + 24HOiPr |
| AlOC-140 | Al8(OH)8(NA)162HBA | 8Al(OiPr)3 + 18HNA + 8H2O + 2AgBA + 2TBACl → Al8(OH)8(NA)162HBA + 24HOiPr + 2AgCl↓ + 2TBANA |
| AlOC-141 | Al8(OH)8(NA)162bpy | 8Al(OiPr)3 + 16HNA + 8H2O + 2bpy → Al8(OH)8(NA)162bpy + 24HOiPr |
| 8Al(OiPr)3 + 16HNA + 8H2O + metals + ligands → Al8(OH)8(NA)16complex + 24HOiPr |  |  |
| AlOC-142 | Al8(OH)8(NA)16Ag(bpy)2NO3 | 8Al(OiPr)3 + 16HNA + 8H2O + AgNO3 + 2bpy → Al8(OH)8(NA)16Ag(bpy)2NO3 + 24HOiPr |
| AlOC-143 | Al8(OH)8(NA)16Ag(NA)2Ag(MeCN)2 | 8Al(OiPr)3 + 18HNA + 8H2O + 2AgAc + 2MeCN →Al8(OH)8(NA)16Ag(NA)2Ag(MeCN)2 + 2HAc + 24HOiPr |
| AlOC-144 | Al8(OH)8(NA)16HAg(BA)2 | 8Al(OiPr)3 + 16HNA + 8H2O + 2AgBA → Al8(OH)8(NA)16HAg(BA)2 + 23HOiPr + AgOiPr |
| AlOC-145 | Al8(OH)8(NA)16Na(AQS)2Ag(MeCN)(bpy)0.5 | 8Al(OiPr)3 + 16HNA + 8H2O + 2NaAQS + AgNO3 + 0.5bpy + MeCN → Al8(OH)8(NA)16Na(AQS)2Ag(MeCN)(bpy)0.5 + 24HOiPr + NaNO3 |
| AlOC-146 | Al8(OH)8(NA)16NO3Ag(MeCN)(bpy)MeCN | 8Al(OiPr)3 + 16HNA + 8H2O + AgNO3 + 2MeCN + bpy →Al8(OH)8(NA)16NO3Ag(MeCN)(bpy)MeCN + 24HOiPr |
| 8nAl(OiPr)3 + 16nHNA + 8nH2O + metals + ligands → [Al8(OH)8(NA)16]npolymer + 24nHOiPr |  |  |
| AlOC-147 | [Al8(OH)8(NA)16NA]nAgn(bpy)n | 8nAl(OiPr)3 + 17nHNA + 8nH2O + nAgNO3 + nbpy → [Al8(OH)8 (NA)16NA]nAgn(bpy)n + 24nHOiPr + nHNO3 |
| AlOC-148 | [Al8(OH)8(NA)16]nAg2n(bpy)2n2nNO3 | 8nAl(OiPr)3 + 16nHNA + 8nH2O + 2nAgNO3 + 2nbpy → [Al8(OH)8(NA)16]nAg2n(bpy)2n2nNO3 + 24nHOiPr |
| AlOC-149 | [Al8(OH)8(NA)162MeCN]nn[CuBr(bpy)2]n[Cu2(NA)4] | 8nAl(OiPr)3 + 20nHNA + 8nH2O + 3nCuBr + 2nbpy + n/2O2 + 2nMeCN → [Al8(OH)8(NA)162MeCN]nn[CuBr(bpy)2]n[Cu2(NA)4] + 24nHOiPr + nH2O + 2nHBr |

- UV-vis analyses

Figure S41.  UV-vis absorption spectrum of AlOC-137. Inset: the diffuse reflectance UV-vis spectrum of AlOC-137.

Figure S42. UV-vis absorption spectrum of AlOC-138. Inset: the diffuse reflectance UV-vis spectrum of AlOC-138.

Figure S43. UV-vis absorption spectrum of AlOC-139. Inset: the diffuse reflectance UV-vis spectrum of AlOC-139.

Figure S44. UV-vis absorption spectrum of AlOC-140. Inset: the diffuse reflectance UV-vis spectrum of AlOC-140.

Figure S45. UV-vis absorption spectrum of AlOC-141. Inset: the diffuse reflectance UV-vis spectrum of AlOC-141.

Figure S46. UV-vis absorption spectrum of AlOC-142. Inset: the diffuse reflectance UV-vis spectrum of AlOC-142.

Figure S47. UV-vis absorption spectrum of AlOC-143. Inset: the diffuse reflectance UV-vis spectrum of AlOC-143.

Figure S48. UV-vis absorption spectrum of AlOC-144. Inset: the diffuse reflectance UV-vis spectrum of AlOC-144.

Figure S49. UV-vis absorption spectrum of AlOC-146. Inset: the diffuse reflectance UV-vis spectrum of AlOC-146.

Figure S50. UV-vis absorption spectrum of AlOC-147. Inset: the diffuse reflectance UV-vis spectrum of AlOC-147.

Figure S51. UV-vis absorption spectrum of AlOC-148. Inset: the diffuse reflectance UV-vis spectrum of AlOC-148.

Figure S52. UV-vis absorption spectrum of AlOC-149. Inset: the diffuse reflectance UV-vis spectrum of AlOC-149.

- Structure description for AlOC-137 to AlOC-149

Figure S53. The structure and packing views of AlOC-137. (a) The side view of AlOC-137. (b) The top view of AlOC-137. (c) the distribution of three MeCN guests in AlOC-137. (d) The interactions between MeCN guests and Al8 macrocycle. The strong hydrogen-bond interactions (O-H···N), C-H···π interactions are respectively highlighted by wathet dotted bonds and yellow dotted bonds. (e) The simulated residual cavity and pore surface structure of AlOC-137 through Mercury analysis. (f) The distribution of residual cavities in AlOC-137. (g) The packing view of AlOC-137 along the crystallographic a-axis. (h) The packing view of AlOC-137 along the crystallographic b-axis. (i) The packing view of AlOC-137 along the crystallographic c-axis. Color code: Al, green; O, red; C, grey; H, white; N, blue.

AlOC-137 crystallizes in the P2/c space group (no. 13), contains one Al8 macrocycle and three MeCN guests (Fig. S53a and S53b). As shown in Fig. S53c, two orientations were identified for three MeCN guests. MeCN (A) and MeCN (B) are perpendicular to Al8 macrocycle in head-to-head fashion. Each N atom of MeCN (A) and MeCN (B) was located below or above Al8 macrocycle with the O-H…N distances of 3.021–3.922 Å and C-H···π distances of 3.541–3.673 Å (Fig. S53d). MeCN (C) is disordered in two position, and approximately parallel to Al8(OH)8 plane. It is fixed to the upper cavity of Al8 macrocycle through two O-H…N interactions (3.541 Å and 3.673 Å) and two C-H···π interactions (2.892 Å and 4.093 Å). Thus, a small residual intramolecular cavity can be found below Al8 plane through the comparison of two hydrophilic cavities (Fig. S53e and S53f). Besides, due to the dense accumulation of Al8 macrocycle (Fig. S53g–S53i), there is no intermolecular cavity or pore stuctures in AlOC-137. Thus, the calculated porosity is only 1.1% for AlOC-137 according to PLATON.

Figure S54. The structure and packing views of AlOC-138. (a) The side view of AlOC-138. (b) The top view of AlOC-138. (c) The distribution of HNA and two inner MeCN guests in AlOC-138. (d) The interactions between HNA guests, inner MeCN guests and Al8 macrocycle. The strong hydrogen-bond interactions (O-H···O), C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (e) The remaining cavity in AlOC-138. (f) The interactions between two external MeCN guests and Al8 macrocycle. (g) The packing view of AlOC-138 along the crystallographic a-axis. (h) The packing view of AlOC-138 along the crystallographic b-axis. (i) The packing view of AlOC-138 along the crystallographic c-axis. (j) The simulated pore surface structure of AlOC-138 along the crystallographic a-axis through Mercury analysis. (k) The simulated pore surface strcuture of AlOC-138 along the crystallographic b-axis through Mercury analysis. (l) The simulated pore surface strcuture of AlOC-138 along the crystallographic c-axis through Mercury analysis. Color code: Al, green; O, red; C, grey; H, white; N, blue.

AlOC-138 crystallizes in Pccn space group, contains one Al8 macrocycle, one HNA guests and four MeCN guests (Fig. S54a and S54b). The HNA and two MeCN guests are located on the one side of Al8(OH)8 plane and confined in the hydrophobic cavity (Fig. S54c). The HNA interact with Al8 macrocycle through 12 O-H…O hydrogen bonds (bond lengths: 2.886–3.060 Å), and the two inner MeCN guests further bonded with HNA guest through C-H…π interactions (bond length: 3.583 Å) (Fig. S54d). The other side of Al8(OH)8 plane is not occupied by any guest, thus, a residual cavity can be observed on Fig. S54e. For the outside MeCN guests, they interact with Al8 macrocycles through C-H…π interaction (bond length: 3.540 Å) and C-H…N interaction (bond length: 2.580 Å). The Al8 macrocycles in AlOC-201 were stacked in parallel with -ABAB- alternations (Fig. S54g–S54i), and form obvious intramolecular channel with minimum diameter of 7.088 Å (Fig. S54j–S54l). The calculated total solvent accessible volume for AlOC-201 is 597.3 Å3, and porosity is 13.6%.

Figure S55. The structure and packing views of AlOC-139. (a) The side view of AlOC-139; (b) The top view of AlOC-139; (c) the distribution of two HNA guests in AlOC-139; (d) the interactions between HNA guests and Al8 macrocycle. The strong hydrogen-bond interactions (O-H···O), C-H···π interactions, π…π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds; (e) The C-H···π and C-H···N interactions between MeCN (A) and two neighboring Al8 macrocycles; (f) The C-H···π and C-H···N interactions between MeCN (B) and two neighboring Al8 macrocycles; (g) the packing view of AlOC-139 along the crystallographic a-axis; (h) the packing view of AlOC-139 along the crystallographic b-axis; (i) the packing view of AlOC-139 along the crystallographic c-axis; (j) the simulated pore surface structure of AlOC-139 along the crystallographic a-axis through Mercury analysis; (k) the simulated pore surface strcuture of AlOC-139 along the crystallographic b-axis through Mercury analysis; (l) the simulated pore surface strcuture of AlOC-139 along the crystallographic c-axis through Mercury analysis. Color code: Al, green; O, red; C, grey; H, white; N, blue.

AlOC-139 crystallizes in monoclinic P2/c space group, contains one Al8 macrocycle, two HNA guests and two MeCN guests (Fig. S55a and S55b). The two HNA guests are located on the upper and lower sides of Al8(OH)8 plane (Fig. S55c), and interact with Al8 macrocycle through 17 hydrogen bonds (O-H…O bond lengths: 2.859–3.966 Å), 4 C-H···π interactions (bond lengths: 3.532–3.906 Å) and 2 π···π interactions (bond lengths: 3.755–3.992 Å) (Fig. S55d). The MeCN (A) is located on the top of hydrophobic cavity, and interact with two Al8 macrocycle through two C-H···π interactions (bond lengths: 3.811–3.943 Å) and C-H···N interaction (bond length: 3.613 Å) (Fig. S55e). The other MeCN (B) is located on the outside of Al8 macrocycle, and fixed by two NA ligands through C-H···N (3.797 Å) and C-H···C interactions (3.760 Å) (Fig. S55f). Besides, the Al8 macrocycles in AlOC-139 were stacked in -ABCD- alternations (Fig. S55g–S55i), and form 2D channel when viewed from b direction (Fig. S55j–S55l). The calculated total solvent accessible volume for AlOC-139 is 2233.9 Å3, and porosity is 25.5%.

Figure S56. The structure and packing views of AlOC-140. (a) The side view of AlOC-140. (b) The top view of AlOC-140. (c) the distribution of two HBA guests in AlOC-140. (d) The interactions between HBA guests and Al8 macrocycle. The strong hydrogen-bond interactions (O-H···O), C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (e) The packing view of AlOC-140 along the crystallographic a-axis. (f) The packing view of AlOC-140 along the crystallographic b-axis. (g) The packing view of AlOC-140 along the crystallographic c-axis. (h) The simulated pore surface strcuture of AlOC-140 along the crystallographic a-axis through Mercury analysis. (i) The simulated pore surface strcuture of AlOC-140 along the crystallographic b-axis through Mercury analysis. (j) The simulated pore surface strcuture of AlOC-140 along the crystallographic c-axis through Mercury analysis. Color code: Al, green; O, red; C, grey; H, white; N, blue.

AlOC-140 crystallizes in P2/n space group, contains one Al8 macrocycle and two HBA guests (Fig. S56a and S56b). The two HBA guests are located on the upper and lower sides of Al8(OH)8 plane (Fig. S56c), and interact with Al8 macrocycle through 16 hydrogen bonds (O-H…O bond lengths: 2.761–3.800 Å), 6 C-H···π interactions (bond lengths: 3.534–3.977 Å) and 4 π···π interactions (bond lengths: 3.791–3.955 Å) (Fig. S56d). The Al8 macrocycles in AlOC-140 were stacked in parallel with -ABAB- alternations (Fig. S56e–S56g), and form obvious intramolecular channel with minimum diameter of 13.42 Å (Fig. S56h–S56j). The calculated total solvent accessible volume for AlOC-140 is 2233.9 Å3, and porosity is 23.8%.

Figure S57. The structure and packing views of AlOC-141. (a) The side view of AlOC-141. (b) The top view of AlOC-141. (c) The distribution of two bpy guests in AlOC-141. (d) The interactions between bpy guests and Al8 macrocycle. The strong hydrogen-bond interactions (O-H···O), C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (e) The packing view of AlOC-141 along the crystallographic a-axis. (f) The packing view of AlOC-201 along the crystallographic b-axis. (g) The packing view of AlOC-141 along the crystallographic c-axis. Color code: Al, green; O, red; C, grey; H, white; N, blue.

AlOC-141 crystallizes in P2/n space group, contains one Al8 macrocycle and two bpy guests (Fig. S57a and S57b). The two slant bpy guests are located on the upper and lower sides of Al8(OH)8 plane (Fig. S57c), and interact with Al8 macrocycle through 16 hydrogen bonds (O-H…N bond lengths: 2.934–3.975 Å), 6 C-H···π interactions (bond lengths: 3.846–3.901 Å) and 2 π···π interactions (bond lengths: 3.238 Å) (Fig. S57d). The Al8 macrocycles in AlOC-141 were stacked compactly in -ABAB- alternations (Fig. S57e–S57g), thus, there is no solvent accessible volume for AlOC-141.

Figure S58. The angle of guest tilt in AlOC-139 (a), AlOC-140 (b) and AlOC-141 (c). Color code: Al, green; O, red; C, grey; H, white; N, blue.

Figure S59. The embedded molecule guests in Al8 macrocycle. (a, d, g, j and m) The distribution of molecule guests in Al8 macrocycle in AlOC-137–AlOC-141. The coordinated equatorial NA ligand have been omitted for clarify. (b, e, h, k and n) The dominating interactions between molecule guests and Al8 macrocycle. The strong hydrogen-bond interactions (O-H···O), C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (c, f, i, l and o) The top view of Al8 macrocycle with confined molecule guests. Color code: Al, green; O, red; C, grey; H, white; N, blue.

Figure S60. The structure and packing views of AlOC-142. (a) The side view of AlOC-142. (b) The top view of AlOC-142. (c) The distribution of Ag(bpy)2 guests in AlOC-142. (d) The interactions between Ag(bpy)2 guests and Al8 macrocycle. The strong hydrogen-bond interactions (O-H···N), C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (e) The packing view of AlOC-142 along the crystallographic a-axis. (f) The packing view of AlOC-142 along the crystallographic b-axis. (g) The packing view of AlOC-142 along the crystallographic c-axis. (h) The interactions between Ag(bpy)2 thread with two outside Al8 macrocycles. (i) The simulated pore surface strcuture of AlOC-142 along the crystallographic c-axis through Mercury analysis. (j) The side view of channel in AlOC-142 along the crystallographic a-axis through Mercury analysis. Color code: Al, green; O, red; C, grey; H, white; N, blue; Ag, pink.

AlOC-142 crystallizes in C2/c space group, contains one Al8 macrocycle and one Ag(bpy)2 thread (Fig. S60a and S60b). The Ag(bpy)2 thread is perpendicular to Al8(OH)8 plane (Fig. S60c), and interact with Al8 macrocycle through 8 O-H…N hydrogen bonds (bond lengths: 3.688–3.771 Å) and 8 C-H···π interactions (bond lengths: 3.865–3.871 Å) (Fig. S60d). The Al8 macrocycles in AlOC-142 were stacked parallelly in -AABB- mode when viewed from c axis (Fig. S60e–S60g). Besides, there are strong C-H···N interactions (bond length: 3.5119 Å) between uncoordinated N sites on Ag(bpy)2 threads and two neighboring Al8 macrocycle, thus, the further extension of thread was prevented. A perforative intermolecular channel can be found in AlOC-142 with the maximum diameter of 6.189 Å. The calculated total solvent accessible volume is 1227.9 Å3 for AlOC-142, and porosity is 7.2%.

Figure S61. EDA data between Al8 macrocycle and Ag(bpy)2. ΔEelec is the electrostatic energy with the value of -131.04 kcal/mol, ΔEexrep is the exchenge/repulsion energy with the value of 254.53 kcal/mol, ΔEpol represents the polarization energy with the value of -55.10 kcal/mol, ΔEcorr/disp is the electron correlation energy with the value of -80.92 kcal/mol, ΔEtot is the total interaction energy with the value of -12.52 kcal/mol.

Figure S62. The IGMH graph when ginter= 0.01. The electrostatic interaction between Ag(bpy)2 thread and Al8 macrocycle is mainly concentrated between the Ag+ and μ2-OH groups. Color code: Al, green; O, red; C, black; H, white; N, blue; Ag, grey.

Figure S63. The IGMH graph when ginter= 0.004. There is weak van der Waals interactions between Ag(bpy)2 thread and Al8 macrocycle. Color code: Al, green; O, red; C, black; H, white; N, blue; Ag, grey.

Figure S64. The structure and packing views of AlOC-143. (a) The side view of AlOC-143. (b) The top view of AlOC-143. (c) The distribution of [Ag(NC)2]– guest in AlOC-143. (d) The interactions between [Ag(NC)2]– guest and Al8 macrocycle. The strong O-H···O hydrogen-bond interactions, C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (e) The coordination environment of Ag2 in AlOC-143. (f) The packing view of AlOC-143 along the crystallographic a-axis. (g) The packing view of AlOC-143 along the crystallographic b-axis. (h) The packing view of AlOC-143 along the crystallographic c-axis. Color code: Al, green; O, red; C, grey; H, white; N, blue; Ag, pink.

AlOC-143 crystallizes in I-42d space group, contains one Al8 macrocycle, one [Ag(NC)2]– thread and one [Ag(MeCN)2]+ (Fig. S64a and S64b). The [Ag(NC)2]– thread is perpendicular to Al8(OH)8 plane (Fig. S64c), and interact with Al8 macrocycle through 12 O-H…O hydrogen bonds (bond lengths: 2.970–3.463 Å), 8 C-H···π interactions (bond lengths: 3.483–3.987 Å) (Fig. S64d) and 6 π···π interactions (bond lengths: 3.669–4.085 Å). The [Ag(MeCN)2]+ is located between two equatorial coordinated NA ligands and fixed through weak Ag–C bonds (Fig. S64e). The Al8 macrocycles in AlOC-143 were stacked campactly (Fig. S64f–S64h), and the calculated total solvent accessible porosity is 4.2%.

Figure S65. The structure and packing views of AlOC-144. (a) The side view of AlOC-144. (b) The top view of AlOC-144. (c) The distribution of AgH(BC)2 guest in AlOC-144. (d) The interactions between AgH(BC)2 guest and Al8 macrocycle. The strong O-H···O hydrogen-bond interactions, C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (e) The packing view of AlOC-144 along the crystallographic a-axis. (f) The packing view of AlOC-144 along the crystallographic b-axis. (g) The packing view of AlOC-144 along the crystallographic c-axis. (h) The simulated pore surface strcuture of AlOC-144 along the crystallographic a-axis through Mercury analysis. (i) The simulated pore surface strcuture of AlOC-142 along the crystallographic b-axis through Mercury analysis. (j) The simulated pore surface strcuture of AlOC-142 along the crystallographic c-axis through Mercury analysis. Color code: Al, green; O, red; C, grey; H, white; N, blue; Ag, pink.

AlOC-144 crystallizes in monoclinic I2/a space group, contains one Al8 macrocycle and one AgH(BC)2 thread (Fig. S65a and S65b). The AgH(BC)2 thread is perpendicular to Al8(OH)8 plane and one H atom is disordered on four carboxylic acid oxygen atoms with 0.25 occupancy for each position (Fig. S65c). It interacts with Al8 macrocycle through 12 O-H…O hydrogen bonds (bond lengths: 2.943–3.483 Å), 4 C-H···π interactions (bond lengths: 3.764–3.844 Å) (Fig. S65d) and 2 π···π interactions (bond length: 3.847 Å). The Al8 macrocycles in AlOC-144 were stacked parrallelly (Fig. S65e–S65g), and the calculated total solvent accessible porosity is 10.5% (Fig. S65h–S65j).

Figure S66. The structure and packing views of AlOC-145. (a) The side view of AlOC-145. (b) The top view of AlOC-145. (c) The distribution of Na(AQS)2– guest in AlOC-145. (d) The interactions between Na(AQS)2– guest and Al8 macrocycle. The strong O-H···O hydrogen-bond interactions, C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (e) The C-H···π and π···π interactions between [Ag2(bpy)(MeCN)2]+ and Al8 macrocycles. (f) The packing view of AlOC-145 along the crystallographic a-axis. (g) The packing view of AlOC-145 along the crystallographic b-axis. (h) The packing view of AlOC-145 along the crystallographic c-axis. Color code: Al, green; O, red; C, grey; H, white; N, blue; Na, turquoise.

AlOC-145 crystallizes in triclinic P-1 space group, contains one Al8 macrocycle, one inner Na(AQS)2– thread and one outside [Ag2(bpy)(MeCN)2]+ chain (Fig. S66a and S66b). The Na(AQS)2– thread is perpendicular to Al8(OH)8 plane (Fig. S66c), and interacts with Al8 macrocycle through 18 O-H…O hydrogen bonds (bond lengths: 2.752–3.969 Å), 6 C-H···π interactions (bond lengths: 3.440–3.786 Å) and 6 π···π interactions (bond length: 3.601–3.766 Å) (Fig. S66d). The [Ag2(bpy)(MeCN)2]+ chain is located between two Al8 macrocycles and fixed by strong C-H···π (bond length: 3.954 Å) and π···π interactions (bond length: 3.556 Å) (Fig. S66e). The Al8 macrocycles in AlOC-145 were stacked parrallelly (Fig. S66f–S66h), and the calculated total solvent accessible porosity is 5.8%.

Figure S67. The distribution of metal ion in AlOC-142 (a), AlOC-143 (b), AlOC-144 (c) and AlOC-145 (d). Color code: Al, green; Ag, pink; Na, turquoise; O, red; C, grey; N, blue.

Figure S68. The embedded complex guests in Al8 macrocycle. (a, d, g and j) The distribution of guests in Al8 macrocycle in AlOC-142–AlOC-145. The coordinated equatorial NA ligand have been omitted for clarify. (b, e, h and k) The dominating interactions between complex guests and Al8 macrocycle. The strong hydrogen-bond interactions (O-H···O/N), C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (c, f, i and l) The top view of Al8 macrocycle with confined complex guests. Color code: Al, green; Ag, pink; Na, turquoise; O, red; C, grey; N, blue; H, white.

Figure S69. The structure and packing views of AlOC-146. (a) The side view of AlOC-146. (b) The top view of AlOC-146. (c) The distribution of NO3– and Ag(MeCN)(bpy)+ ion pair in AlOC-146. (d) The interactions between guests and Al8 macrocycle. The strong O-H···O hydrogen-bond interactions, C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (e) The packing view of AlOC-146 along the crystallographic a-axis. (f) The packing view of AlOC-146 along the crystallographic b-axis. (g) The packing view of AlOC-146 along the crystallographic c-axis. Color code: Al, green; Ag, pink; O, red; C, grey; N, blue; H, white.

AlOC-146 crystallizes in triclinic P-1 space group, contains one Al8 macrocycle, one inner NO3– ion, one Ag(MeCN)(bpy)+ complex and one outside MeCN guest (Fig. S69a and S69b). The upper hydrophobic cavity of Al8 macrocycle is occupied by NO3– and Ag(MeCN)(bpy)+ ion pair, both of which are parallel to Al8(OH)8 plane (Fig. S69c). The NO3– interacts with Al8 macrocycle through ten O-H…O hydrogen bonds (bond lengths: 2.751–3.957 Å). The Ag(MeCN)(bpy)+ is located above NO3–and fixed by three C-H···π (bond lengths: 3.660–3.871 Å) and two π···π interactions (bond length: 3.773–3.857 Å) (Fig. S69d). The outside MeCN molecule also bonded with Al8 macrocycle through equatorial NA ligand with C-H···π bond lengths ranging from 3.939–3.996 Å. The Al8 macrocycles in AlOC-146 were stacked alternatively in -ABAB- manner(Fig. S69e–S69g), and the calculated total solvent accessible porosity is 10.6%.

Figure S70. The structure and packing views of AlOC-147. (a) The side view of AlOC-147. (b) The top view of AlOC-147. (c) The distribution of NA– and Ag(bpy)+ guests in AlOC-147. (d) The interactions between NA– and Al8 macrocycle. (e, f and g) The interactions between Agn(bpy)nn+ and Al8 macrocycle. (h and i) The packing view of AlOC-147 along the crystallographic a-axis. (j and k) The packing view of AlOC-147 along the crystallographic b-axis. (l and m) The packing view of AlOC-147 along the crystallographic c-axis. The strong O-H···O hydrogen-bond interactions, C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. Color code: Al, green; Ag, pink; O, red; C, grey; N, blue; H, white.

AlOC-147 crystallizes in mnoclinic Cc space group, its unit cell contains one Al8 macrocycle, one inner NA– guest and one outside Ag(bpy)+ complex (Fig. S70a–S70c). The inner NA– guest interacts with Al8 macrocycle through seven O-H…O hydrogen bonds (bond lengths: 2.726–3.478 Å), three C-H···π (bond lengths: 3.656–3.987 Å) and three π···π interactions (bond lengths: 3.688–3.925 Å) (Fig. S70d). The outside [Agn(bpy)n]n+ chain also bonded with Al8 macrocycle through C-H···π interactions (bond lengths: 3.655–3.761 Å) and π···π interactions (bond lengths: 3.601–3.741 Å) (Fig. S70e–S70g). The Al8 macrocycles and polymer chains in AlOC-147 were stacked alternatively when viewed along c axis (Fig. S70h–S70m), and the calculated total solvent accessible porosity is 22.6%.

Figure S71. The structure and packing views of AlOC-148. (a) The side view of AlOC-148. (b) The top view of AlOC-148. (c) The distribution of Ag2(bpy)22+ guests in AlOC-148. (d) The interactions between Ag2(bpy)2+ guests and Al8 macrocycle. (e) The 1D penetrative polyrotaxane in AlOC-148. (f) The C-H···π interactions between two vertical polyrotaxanes in ab plane. (g) The π···π interactions between two parallel polyrotaxanes along the c axis. (h and i) The packing view of AlOC-148 along the crystallographic a-axis. (j and k) The packing view of AlOC-148 along the crystallographic b-axis. (l and m) The packing view of AlOC-148 along the crystallographic c-axis. The strong O-H···N hydrogen-bond interactions, C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. Color code: Al, green; Ag, pink; O, red; C, grey; N, blue; H, white.

AlOC-148 crystallizes in tetragonal P-4n2 space group, its unit cell contains one Al8 macrocycle, one inner Ag2(bpy)22+ guest and two unresolved NO3– counterion (Fig. S71a and S71b). The inner Ag2(bpy)22+ guest is perpendicular to Al8(OH)8 plane and interacts with Al8 macrocycle through eight O-H…N hydrogen bonds (bond lengths: 3.609–3.852 Å), seven C-H···π (bond length: 3.531–4.014 Å) and two π···π interactions (bond lengths: 4.168 Å) (Fig. S71c and S71d). The neighboring two Ag2(bpy)22+ threads can combined together through Ag–N bonds generating main-chain penetrative polyrotaxane (Fig. S71e). The polyrotaxane chains are arranged vertically in ab plane (Fig. S71f) and stacked parallelly along c axis (Fig. S71g). Such dense packing mode leads to lower solvent accessible porosity with calculated value of 6.6% (Fig. S71h–S71m).

Figure S72. Dihedral angles of two pyridine rings for confined bpy. Color code: Al, green; Ag, pink; O, red; C, grey; N, blue; H, white.

Figure S73. The structure and packing views of AlOC-149. (a) The side view of AlOC-149. (b) The top view of AlOC-149. (c) The distribution of CuBr(bpy)2Cu2(NA)4 and two MeCN guests in AlOC-149. (d) The interactions between guests and Al8 macrocycle. (e and f) The packing view of AlOC-149 along the crystallographic a-axis. (g and h) The packing view of AlOC-149 along the crystallographic b-axis. (i and j) The packing view of AlOC-149 along the crystallographic c-axis. The strong O-H…O hydrogen-bond interactions, C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. Color code: Al, green; O, red; C, grey; N, blue; H, white; Br, dark yellow; Cu, turquoise.

AlOC-149 crystallizes in tetragonal C2/c space group, its unit cell contains one Al8 macrocycle, one CuBr(bpy)2Cu2(NA)4 guest and two MeCN molecules (Fig. S73a and S73b). The CuBr(bpy)2Cu2(NA)4 guest is located in the above hydrophobic cavity and interacts with Al8 macrocycle through eight O-H···Br hydrogen bonds (bond lengths: 3.464–3.914 Å) and eight π···π interactions (bond lengths: 3.662–4.014 Å) (Fig. S73c and S73d). While two MeCN guests are confined in the lower hydrophobic cavity and bonded to Al8 macrocycle through C-H···π interactions (bond lengths: 3.889–4.033 Å). The CuBr(bpy)2Cu2(NA)4 guests are extended infinitely along c axis through Cu–N bonds generating zigzag side-chain polyrotaxane (Fig. S70e–S70j). The polyrotaxane chains are further arranged parallelly in 3D space with calculated total solvent accessible porosity of 6.7%.

Figure S74. The embedded complex guests in Al8 macrocycle. (a, d, g and j) The distribution of guests in Al8 macrocycle in AlOC-142–AlOC-145. The coordinated equatorial NA ligand have been omitted for clarify. (b, e, h and k) The dominating interactions between complex guests and Al8 macrocycles. The strong hydrogen-bond interactions (O-H···O/Br/N), C-H···π interactions, π···π interactions are respectively highlighted by wathet dotted bonds, yellow dotted bonds and lilac dotted bonds. (c, f, i and l) The top view of Al8 macrocycle with confined complex guests. Color code: Al, green; Ag, pink; O, red; C, grey; N, blue; H, white; Br, dark yellow; Cu, turquoise.

Figure S75. The comparison of polyrotaxane types and non-covalent interactions in macrocycle centre. Type 1) is reported by Zang et al.20 Color code for structure in Type 1): O, red; C, grey; N, blue. Type 2) is reported by Winpenny et al.21 Color code for structure in Type 2): Cr/M heterometallic sites, sea green; C, grey; N, blue; F, green. Type 3) are found in our work. Color code for structure in Type 3): Al, green; O, red; N, blue; H, white; Br, dark yellow; Cu, turquoise; Ag, pink.

Figure S76. The torsion angle (θ) diagram in NA– ligand. Color code: O, red; C, grey; H, white.

Table S20. The Ө value of eight non-equatorial NA– ligands in AlOC-137–AlOC-149.

|  | Guest in upper cavity | Ө1 | Ө2 | Ө3 | Ө4 | Guest in upper cavity | Ө5 | Ө6 | Ө7 | Ө8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AlOC-137 | MeCN | 32.9 | 33.3 | 18.4 | 24.0 | 2MeCN | 12.1 | 8.6 | 19.2 | 23.5 |
| AlOC-138 | 2MeCN+NA | 27.6 | 27.6 | 24.1 | 24.1 | ― | 25.6 | 25.6 | 42.4 | 42.4 |
| AlOC-139 | MeCN+NA | 59.4 | 38.0 | 27.3 | 17.9 | NA | 63.4 | 31.7 | 25.9 | 27.5 |
| AlOC-140 | HBA | 20.4 | 13.0 | 21.3 | 12.6 | HBA | 20.4 | 13.0 | 21.3 | 12.6 |
| AlOC-141 | bpy | 21.7 | 6.7 | 10.9 | 12.2 | bpy | 21.7 | 6.7 | 10.9 | 12.2 |
| AlOC-142 | 1/2Ag(bpy)2 | 27.4 | 27.4 | 13.3 | 13.3 | 1/2Ag(bpy)2 | 22.0 | 22.0 | 2.5 | 2.5 |
| AlOC-142 after heating | 1/2Ag(bpy)2 | 27.9 | 27.9 | 16.0 | 16.0 | 1/2Ag(bpy)2 | 22.3 | 22.3 | 0.8 | 0.8 |
| AlOC-143 | 1/2Ag(NA)2 | 2.3 | 25.6 | 11.6 | 39.6 | 1/2Ag(NA)2 | 2.3 | 25.6 | 11.6 | 39.6 |
| AlOC-144 | 1/2Ag(BA)2H | 9.9 | 11.9 | 16.6 | 16.3 | 1/2Ag(BA)2H | 9.9 | 11.9 | 16.6 | 16.3 |
| AlOC-145 | 1/2Na(AQS)2 | 37.6 | 47.3 | 10.2 | 5.8 | 1/2Na(AQS)2 | 9.3 | 49.9 | 50.7 | 8.2 |
| AlOC-146 | NO3– + Ag(MeCN)(bpy) | 32.2 | 47.5 | 30.7 | 38.3 | ― | 38.6 | 17.3 | 5.9 | 52.8 |
| AlOC-147 | NA | 53.1 | 28.7 | 20.8 | 17.1 | ― | 16.9 | 29.1 | 24.7 | 61.2 |
| AlOC-148 | 1/2Agn(bpy)n | 35.5 | 35.5 | 11.7 | 11.7 | 1/2Agn(bpy)n | 14.5 | 14.5 | 16.6 | 16.6 |
| AlOC-149 | CuBr(bpy)2 | 47.8 | 47.8 | 39.5 | 39.5 | 2MeCN | 22.4 | 22.4 | 22.8 | 22.8 |

Figure S77. The conformation variation for hydrophobic cavities on Al8 macrocycle. Color code: Al, green; Ag, pink; Na, teal; Cu, turquoise; O, red; C, grey; S, yellow; N, blue; H, white.

Figure S78. The dihedral angle (δ) diagram in bpy. Color code: N, blue; C, grey; H, white.

Figure S79. The C-H···π interactions between Ag(bpy)2+ and Al8 macrocycle in AlOC-142 before and after heating. Color code: Al, green; Ag, pink; O, red; C, grey; N, blue; H, white.

- NLO analyses

Figure S80. The open-aperture Z-scan results at 532 nm for AlOC-137 under different energy.

Figure S81. The open-aperture Z-scan results at 532 nm for AlOC-139 under different energy.

Figure S82. The open-aperture Z-scan results at 532 nm for AlOC-140 under different energy.

Figure S83. The open-aperture Z-scan results at 532 nm for AlOC-142 under different energy.

Figure S84. The open-aperture Z-scan results at 532 nm for AlOC-143 under different energy.

Figure S85. The open-aperture Z-scan results at 532 nm for AlOC-144 under different energy.

Figure S86. The open-aperture Z-scan results at 532 nm for AlOC-148 under different energy.

Table S21. The list of nonlinear parameters for AlOC-137, AlOC-139, AlOC-140, AlOC-142, AlOC-143, AlOC-144, AlOC-148 and AlOC-142 after heating.

|  | T (%) | α(cm-1) | β(cm/GW) | Imχ(3) (×10-13 esu) | FOM (×10-14 esu) | FOL (J/cm2) |
| --- | --- | --- | --- | --- | --- | --- |
| AlOC-137 | 0.64 | 0.45 | 0.42 | 0.54 | 0.12 | 14.873 |
| AlOC-139 | 0.63 | 0.46 | 4.56 | 5.89 | 1.27 | 0.079 |
| AlOC-140 | 0.65 | 0.43 | 3.11 | 4.01 | 0.93 | 0.068 |
| AlOC-142 | 0.74 | 0.30 | 0.86 | 1.11 | 0.37 | 1.194 |
| AlOC-143 | 0.61 | 0.49 | 16.05 | 20.71 | 4.19 | 0.042 |
| AlOC-144 | 0.70 | 0.36 | 4.82 | 6.22 | 1.74 | 0.066 |
| AlOC-148 | 0.75 | 0.29 | 1.95 | 2.52 | 0.87 | 0.139 |
| AlOC-142 after heating | 0.76 | 2.74 | 17.5 | 20.7 | 0.75 | 2.363 |

Table S22. The nonlinear parameters of some reported materials measured in solution.

| No. | Compounds | Measurement conditions | β(cm/GW) | Imχ(3) (×10-13 esu) | FOM (×10-14 esu) | FOL (J/cm2) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Cu50(PhCOO)10(4-F-PhS)20(PPh3)6H2 | in DMF | 12.5 | 27.3 | 43 | ˃10 | 22 |
| 2 | Pt-Ni NP/rGO | in water | 1.64 | – | – | – | 23 |
| 3 | Pt-Ni cluster/rGO | in water | 1.98 | – | – | – | 23 |
| 4 | [Ni(1,2-BIB)(CEDA)]∙1.5H2O | in DMSO | 10.1 | 35.4 | – | – | 24 |
| 5 | [Zn(1,2-BIB)(CADA)] | in DMSO | 4.2 | 14.7 | – | – | 24 |
| 6 | [Zn2(1,4-BIB)2(CADA)2]∙2H2O | in DMSO | 4.6 | 16.1 | – | – | 24 |
| 7 | {[ET4N][Ag2I3]}n | in CH2Cl2 | 3.04 | – | – | – | 25 |
| 8 | [(HgI2(4,4-azpy)]n | in CH2Cl2 | 1.3 | – | – | – | 25 |
| 9 | AlOC-76 | in solution | 0.61 | 2.38 | 2.87 | 0.009 | 26 |
| 10 | 4Br4MSP | in DMF | 5.5×10-5 | 4.6×10-12 | – | – | 27 |
| 11 | P3HT-MoS2 | in chloroform | 5.5 | – | – | – | 28 |
| 12 | MoS2 | in ethanol/water | 1.5 | – | – | – | 28 |
| 13 | [Ni6(Py)6(H2O)5(μ3−OH)3(PW9O34)]2·10H2O | in DMSO | 0.003384 | – | – | – | 29 |
| 14 | [H2N(CH3)2]12.5(H3N(CH2)2NH3)(H3O)1.5(VIIIμ2-OH)8(SO4)16·2H2O | in water | 0.008377 | – | – | – | 30 |
| 15 | [(C4O6H2)2V4O8]·2C6N2H18 | in water | 0.003167 | – | – | – | 31 |

Figure S87. The OL curve for AlOC-137.

Figure S88. The OL curve for AlOC-139.

Figure S89. The OL curve for AlOC-140.

Figure S90. The OL curve for AlOC-142.

Figure S91. The OL curve for AlOC-143.

Figure S92. The OL curve for AlOC-144.

Figure S93. The OL curve for AlOC-148.

Figure S94. The OA Z-scan curve for AlOC-142 after heating at 160oC for 12h.

Figure S95. The curve of output fluence versus input fluence for AlOC-142 after heating at 160oC for 12h.

Figure S96. The OL curve for AlOC-142 after heating at 160oC for 12h.

References

1. Wendlandt, W. W. & Hecht, H. G. Reflectance spectroscopy; interscience. New York (1966).

2. Sheldrick, G. M. SHELXL-2014 Program for Crystal Structure Solution and Refinement, (Univerity of Göttingen, Göttingen, Germany, 2014).

3. Tang, Z. et al. XEDA, a fast and multipurpose energy decomposition analysis program. J. Comput. Chem. 42, 2341–2351 (2021).

4. Su, P., Tang, Z. & Wu, W. Generalized kohn-sham energy decomposition analysis and its applications. WIREs Comput. Mol. Sci. 10, e1460 (2020).

5. Schill, G. & Zollenkopf, H. Rotaxane. Nachr. Chem. Techn. 15, 149–150 (1967).

6. Agam, G., Graiver, D. & Zilkha, A. Studies on the formation of topological isomers by statistical methods. J. Am. Chem. Soc. 98, 5206–5214 (1976).

7. Ogino, H. Relatively high-yield syntheses of rotaxanes. Syntheses and properties of compounds consisting of cyclodextrins threaded by α,ω-diaminoalkanes coordinated to cobalt(III) complexes. J. Am. Chem. Soc. 103, 1303–1304 (1981).

8. Anelli, P. L., Spencer, N. & Stoddart, J. F. A molecular shuttle. J. Am. Chem. Soc. 113, 5131–5133 (1991).

9. Wu, C., Lecavalier, P. R., Shen, Y. X. & Gibson, H. W. Synthesis of a rotaxane via the template method. Chem. Mater. 3, 569-572 (1991).

10. Lindoy, L. F. New ribbons and threads. Nature 376, 293–294 (1995).

11. Jeon, Y.-M., Whang, D., Kim, J. & Kim, K. A simple construction of a rotaxane and pseudorotaxane: Syntheses and X-ray crystal structures of cururbituril threaded on substituted spermine. Chem. Lett. 25, 503–504 (1996).

12. Arduini, A., Ferdani, R., Pochini, A., Secchi, A. & Ugozzoli, F. Calix[6]arene as a wheel for rotaxane synthesis. Angew. Chem. 112, 3595–3598 (2000).

13. Chang, S.-Y., Choi, J. S. & Jeong, K.-S. Self-assembly and dynamics of [2]- and [3]rotaxanes with a dinuclear macrocycle containing reversible Os−N coordinate bonds. Chem. Eur. J. 7, 2687–2697 (2001).

14. Larsen, F. K. et al. Synthesis and characterization of heterometallic {Cr7M} wheels. Angew. Chem. Int. Ed. 42, 101–105 (2003).

15. Thordarson, P., Bijsterveld, E. J. A., Rowan, A. E. & Nolte, R. J. M. Epoxidation of polybutadiene by a topologically linked catalyst. Nature 424, 915–918 (2003).

16. Lee, E. Y. & Suh, M. P. A robust porous material constructed of linear coordination polymer chains: Reversible single-crystal to single-crystal transformations upon dehydration and rehydration. Angew. Chem. Int. Ed. 43, 2798–2801 (2004).

17. Gao, C.-Y., Zhao, L. & Wang, M.-X. Designed synthesis of metal cluster-centered pseudo-rotaxane supramolecular architectures. J. Am. Chem. Soc. 133, 8448–8451 (2011).

18. Lee, S., Chen, C.-H. & Flood, A. H. A pentagonal cyanostar macrocycle with cyanostilbene CH donors binds anions and forms dialkylphosphate [3]rotaxanes. Nat. Chem. 5, 704–710 (2013).

19. Liu, C. et al. Assembly of interlocked superstructures with a titanium oxide molecular ring in water. Inorg. Chem. 60, 14520–14524 (2021).

20. Li, N.-N. et al. Ensembles from silver clusters and cucurbit[6]uril-containing linkers. Dalton Trans. 50, 15267-15273 (2021).

21. Whitehead, G. F. S. et al. Rings and threads as linkers in metal-organic frameworks and poly-rotaxanes. Chem. Commun. 49, 7195–7197 (2013).

22. Sun, J. et al. Labile ligands protected Cu50 nanoclusters with tailorable optical limiting effect. ACS Materials Lett. 6, 281–289 (2024).

23. Zheng, C. et al. Facile control of metal nanoparticles from isolated nanoparticles to aggregated clusters on two-dimensional graphene to form optical limiters. J. Mater. Chem. C 5, 11579–11589 (2017).

24. Liu, R.-Q. et al. Enhanced third-order nonlinear optical properties of three 2D coordination polymers based on bis(imidazole) ligands and dicarboxylic ligands. Polyhedron 111, 16–25 (2016).

25. Zhou, J.-L., Chen, Q.-Y., Gu, Y.-Y., Mei, G.-Q. & Yang, H.-W. Syntheses, crystal structures and third-order nonlinear optical properties of coordination polymers {[Et4N][Ag2I3]}n and [CuBr(C10H8N2S2)]n. Transition Met. Chem. 30, 1036–1041 (2005).

26. Li, Y. et al. Record aluminum molecular rings for optical limiting and nonlinear optics. Angew. Chem. Int. Ed. 61, e202116563 (2022).

27. D'silva, E. D., Podagatlapalli, G. K., Venugopal Rao, S. & Dharmaprakash, S. M. Study on third-order nonlinear optical properties of 4-methylsulfanyl chalcone derivatives using picosecond pulses. Mater. Res. Bull. 47, 3552-3557 (2012).

28. Zhao, M. et al. Unexpected optical limiting properties from MoS2 nanosheets modified by a semiconductive polymer. Chem. Commun. 51, 12262–12265 (2015).

29. Wang, J.-L. et al. Two Ni-substituted trilacunary keggin-type polyoxometalates: Syntheses, crystal structures, NLO studies, and magnetic properties. Inorg. Chem. 60, 13748–13755 (2021).

30. Cao, J. P. et al. Exploring the magnetic interaction of asymmetric structures based on chiral VIII8 clusters. Inorg. Chem. 58, 2645–2651 (2019).

31. Cao, J. et al. A pair of new chiral polyoxovanadates with decent NLO properties. Dalton Trans. 47, 6054–6058 (2018).