Supplementary Information

Unraveling the atomic structure evolution of titanium nitride upon oxidation

Ronghui Hao1,7, Wenkang Miao1,7, Wanyin Xu1, Yicheng Lin1, Qiling Xiao1, Zihan Wang1, Qianqian Li1,*, Peng Wang2,*, Tianzhong Wang3,*, Anmin Nie4,*, Jinsong Wu5 and Hongtao Wang6

1Materials Genome Institute, Shanghai University, Shanghai 200444, China

2Shanghai Key Laboratory of Mechanics in Energy Engineering, Shanghai Institute of Applied Mathematics and Mechanics, School of Mechanics and Engineering Science, Shanghai University, Shanghai, 200444, China

3School of Materials Science and Engineering, Xi’an University of Technology, Xi’an 710048, China

4Center for High Pressure Science, State Key Laboratory of Metastable Materials Science and Technology, Yanshan University, Qinhuangdao 066004, China

5Nanostructure Research Center, Wuhan University of Technology, Wuhan 430070, China

6Center for X-mechanics, Zhejiang University, Hangzhou, 310027, China

Institute of Applied Mechanics, Zhejiang University, Hangzhou, 310027, China

7These authors contributed equally to this work.

*Corresponding author. E-mail: qianqianli@shu.edu.cn (Q.Q.L); wangp@shu.edu.cn (P.W); wangtzh07@163.com (T.Z.W.); anmin@ysu.edu.cn (A.M.N)

This file includes：

Figure S1 to S13

.

Fig. S1 | a, TEM sample holder schematic diagram. b, Schematic diagram of MEMS chip and its sample loading area. c, HAADF-STEM image of TiN particles in the [110] zone axis, providing atomic resolution and revealing lattice spacings of 0.24 nm and 0.21 nm corresponding to the (111) and (002) planes of TiN, respectively. Blue spheres representing titanium atoms and yellow spheres representing nitrogen atoms. d, The SAED of the sample region in (c). the inward-outward blue semicircles in the patterns corresponded to the (111), (200), and (220) diffraction planes of TiN.

Fig. S2 | ETEM gas flow control and pressure display. a, The various valves that control the gas flow in the electron microscope, among them, the PP/O and BC/O valves monitor the pressure of the gas entering the microscope chamber. b, Pressure curve of the gas entering the microscope chamber during the heating process.

Fig. S3 | The gases detected by the mass spectrometer during the heating process and released from the electron microscope. a-c, (a), (b), and (c) represent the mass spectrometry curves before ventilation, during ventilation, and after gas stabilization, respectively.  Among them, mass numbers 14, 16, 28, and 32 represent nitrogen (N), oxygen (O), nitrogen gas molecule (N2), and oxygen gas molecule (O2), respectively.

Fig. S4 | HAADF-STEM images reveal the oxidation of TiN in O2 with p = 50 Pa and T = 450 °C. a, The oxidation process of titanium nitride begins with the initial phase along the [001] axis of TiN (a), as oxidation progresses, a large number of titanium vacancies are formed along the (200) crystal plane (b).

Fig. S5 | HAADF-STEM images reveal the oxidation of TiN in O2 with p = 50 Pa and T = 450 °C. a,b, The oxidation process of titanium nitride begins with the initial phase along the [001] axis of TiN (a), as oxidation progresses, a large number of titanium vacancies are formed along the (200) crystal plane, as a large number of titanium atoms migrate, z-shaped structural units form in the oxide structure (b). c, After the formation of the z-shaped structure, the structure of sharp titanium oxide (anatase) with misaligned atomic pairs occurs along the [001] axis.

Fig. S6 | HAADF-STEM images reveal the oxidation of TiN in O2 with p = 50 Pa and T = 450 °C. In the annotated area of the image, although a large number of vacancies are generated, they do not exhibit a distribution pattern along the (200) or (020) crystal planes like in Fig. 1. In this region, the vacancies are randomly dispersed rather than showing a clear arrangement along the crystal planes.

Fig. S7 | HAADF-STEM images reveal the oxidation of TiN in O2 with p = 20 Pa and T = 400 °C. The image shown is an enlarged view of the grain boundary region in Fig. 4a. In this area, the grain boundary is clearly visible, and on both sides of the grain boundary, the crystallographic axes of the grains are close to [001].

Fig. S8 | HAADF-STEM images reveal the oxidation of TiN in O2 with p = 20 Pa and T = 400 °C. a, The image shown is an enlarged view of the grain boundary region in Fig. 3c. b-e , The intermediate structures within the dashed boxes labeled as 1 and 2 are manifested in the first oxidation pathway, while the structures within the dashed boxes labeled as 3 and 4 do not appear in the first oxidation pathway; therefore, these two structures are categorized as the second oxidation pathway.

Fig. S9 | HAADF-STEM images reveal the oxidation of TiN in O2 with p = 20 Pa and T = 400 °C. The image shown is an enlarged view of the region in Fig. 3e. At this stage, the oxide structure completely matches the structure of anatase along the [001] axis. This indicates that TiN has been oxidized to anatase.

Fig. S10 | The results of first-principles calculations regarding the energy variation in the system caused by different numbers of atomic steps. a, The results indicate that the fewer atomic steps in the oxide structure, the more stable the system. (b), (c), and (d), the structural models contain four, two, and zero atomic steps, respectively.

Fig. S11 | The oxide structure after simulating the formation of titanium vacancies using first-principles calculations for the second oxidation pathway was studied. The simulation results reveal that after the creation of the titanium vacancy, oxygen atoms occupy the vacant sites and form titanium-oxygen bonds with the titanium atoms on both sides of the vacancy, thereby shortening the distance between the two columns of titanium atoms. In the representation, blue spheres represent titanium atoms, yellow spheres represent nitrogen atoms, and red spheres represent oxygen atoms. The arrows represent the direction of atomic motion.

Fig. S12 | The method of measuring the curvature radius in the text. The curvature radius of the current region is defined by the radius of the circumscribed circle of the region.

Fig. S13 | The XRD characterization of oxidation products of TiN with different preferred orientations. a, d, The XRD data of randomly oriented and (200)-preferred oriented TiN before oxidation, respectively. b, e, The XRD data of randomly oriented and (200)-preferred oriented TiN after heat treatment in air at 500 °C for 40 minutes, respectively. c, f, The XRD data of randomly oriented and (200)-preferred oriented TiN after heat treatment in air at 600 °C for 40 minutes, respectively.